3.1 Thermal decomposition process

In order to understand the synthesis process of SmAlO3, the thermal analysis including TG-DTA for the dried gel was examined, and the results are shown in Fig. 2. The endothermic peak in the DTA curve at 110 ℃ is due to the volatilization of residual water and the melting of gel, accompanied by a weight loss of about 13.3% between room temperature and 230 ℃ in the TG curve. When the temperature is over 230 ℃, all other peaks are exothermal, which indicates that a series of oxidation and combustion reactions are involved in the thermal decomposition process. In the second step, a huge weight loss (43.9%) at the temperature range of 230-600 ℃ can be attributed to the combustion of organic substances in the gel, and the formation and decomposition of samarium and aluminum complexes. It can be observed from the DTA curve that there are four relatively strong exothermal peaks at 318, 388, 465, and 585 ℃. Especially, the strongest peak at 585 ℃ may indicate the decomposition of samarium and aluminum complexes, and the formation of some amorphous phases. When the temperature exceeds 585 ℃, no apparent weight loss is found. However, a weak exothermal peak at 683 ℃ appears in the DTA curve, indicating that a phase transition from an amorphous phase to a crystalline phase occurs. This means that the minimum crystalline temperature to synthesize SmAlO3 powders by stearic acid method is approximately 683 ℃.

3.2 X-ray diffraction patterns and FT-IR spectra analysis

Fig. 3 displays the XRD patterns of SmAlO3 powders after calcination from 750 to 900 ℃ for 2 h. After calcination at 750 ℃ for 2 h, the product exhibits favorable crystallinity, which can be characterized by some sharp diffraction peaks. These XRD peaks, corresponding to the reflections from the orthorhombic phase, are in strong agreement with the database in JCPDS # 71-1597 for SmAlO3 with a perovskite structure. Further increasing the calcination temperature makes the XRD peaks of the powders stronger and stronger. Additionally, no impurity or other intermediate phase is observed in the investigated calcination temperatures. The XRD patterns of SmAlO3 in our present work are similar to those of the nanopowders synthesized by the polymeric precursor method [19], and the sol–gel route using malic acid as a complexing agent [22]. However, the synthesis temperature of the stearic acid method is about 750 ℃, which lowers those of other wet-chemistry routes (800 ℃ for the polymeric precursor method and 950 ℃ for the sol–gel technique route). This synthesis temperature for the solid-state reaction to obtain pure phase SmAlO3 is as high as 1400 ℃ [5]. This evidence indicates that the stearic acid approach is a speedy and energy-saving route for the synthesis of ultrafine SmAlO3 powders with high sintering activity.

In addition, the refined lattice parameters, cell volume, and crystallite size for the products derived from different synthesis approaches are calculated using the FULLPROF software package, and the Debye-Scherrer formula [23, 24]. Table 1 summarizes these calculated results.

D=0.89λβcosθ                                (2)

Where D, λ, β and θ are the average crystallite size, X-ray wavelength, full width at half maximum (FWHM) of the diffraction peak, and Bragg's angle, respectively. The calculated crystallite size is 29 nm for the SmAlO3 powder calcined at 750 ℃, while taking the diffraction angle 2θ = 33.9 °. It is seen that the cell volume of SmAlO3 phase obtained by wet-chemistry methods, is relatively smaller than that of the conventional solid state reaction method.

In order to confirm the structural changes between the precursor and the powders that underwent calcination processes, FT-IR analysis was done and the results are shown in Fig. 4. Small absorption bands at about 2920 cm−1, 1630 cm−1, and 1067 cm−1 in the precursor after heat treatment at 230 ℃ reveal that a small amount of organic substance still exists. When increasing the temperature to 750 ℃, no obvious absorption bands of organic substances are observed, as shown in Fig. 4(b). Meanwhile, the absorption bands in the range of 400-700 cm−1 get stronger, which is attributed to the formation of MO6 octahedra (M = Sm/Al). In addition, a broad band centered at 3427 cm−1 is assigned to the adsorbed water of these powders.

3.3 Morphology observation

Fig. 5 shows the scanning electron image of SmAlO3 powder calcined at 750 ℃ for 2 h without grinding. As displayed in Fig. 5, a large-size sheet structure is composed of a number of micro/nano-scale crystallites. To draw a reliable conclusion based on the above result, the transmission electron analysis was carried out and the corresponding TEM image is present in Fig. 6. The particle size estimated from the TEM image is about 70 nm, which is significantly larger than that calculated from the Debye-Scherrer formula. It is observed that nearly all crystallites are mostly irregular in shape due to the mutual growth and overlapped shapes of adjacent grains. This may be due to the variety of solution concentration and pH values. In a recent study, Zhang et al. have found that the pH value has remarkable effects on the crystal structure, surface morphology, and microwave dielectric properties of Bi12TiO20 ceramics fabricated by the sol–gel method [25]. Therefore, it is of great necessity to synthesize fine particles with high reactive activity and favorable sintering activity in our future research.

3.4 Sintering of SmAlO3

The powder synthesized by the stearic acid method is used as starting material to prepare SmAlO3 ceramics for the purpose of application as microwave dielectric materials. The synthesized powders were uniformly mixed with 5 wt% PVA solution, pressed into some bulk specimens, and sintered at 1350–1550 ℃ for 4 h.

Fig. 7 illustrates the bulk densities of SmAlO3 ceramics sintered at different temperatures. At 1350-1425 ℃, the bulk density drastically increases. But the low bulk densities indicate that the current SmAlO3 ceramics are not dense. When the sintering temperature is over 1425 ℃, the bulk density gradually increases until 1500 ℃, and then it decreases. The maximum bulk density of 6.92 g·cm-3, which is about 96.5% of the theoretical density, was obtained at 1500 ℃ for 4 h. Compared with the densification temperature of 1650 ℃ required by the conventional solid state reaction route, the best sintering temperature of SmAlO3 ceramics prepared using the powders syntheiszed by the stearic acid method as raw materials can be reduced about 150 ℃. In fact, the theoretical density values all exceed 95%, at which the influence of pores can be ignored for the microwave dielectric properties. A recent study suggested that a reasonable calcination temperature is critical for obtaining dense ceramics with favorable microwave dielectric properties [26]. Low or high calcination temperature is disadvantageous to achieving high-density ceramics in the sintering process. A systematic investigation is worthy to explore for greater optimization of density and microwave dielectric properties.

The SEM image of SmAlO3 ceramics at 1500 ℃ for 4 h is shown in Fig. 8. A dense, uniform microstructure with an average grain size of about 1.8 μm can be observed, which is advantageous to enhancing microwave dielectric properties. In addition, a layered growth step morphology can be found based on the SEM image. Similar results have been reported in the ceramic systems of 0.75CaTiO3-0.35SmAlO3 and 0.95(Ca0.88Sr0.12)TiO3-0.05(Bi0.5Na0.5)TiO3 [26, 27]. These phenomena have a close relationship with the grain growth and mass transfer in the sintering process.

3.5 Microwave dielectric properties of as-prepared SmAlO3ceramics

The microwave dielectric properties of SmAlO3 ceramics are demonstrated in Fig. 9. As can be seen, the relationship between the εr value and sintering temperature is in firm agreement with that between the density and sintering temperature. The εr firstly increases to the saturated value at 1500 ℃ and then decreases slightly in the investigated sintering temperature. Also, the Q·f value exhibits a similar behavior. The dielectric constant and Q·f are strongly affected by the pores in the structure before the ceramics are well sintered. Therefore, the εr and Q·f values are obviously reduced when the sintering temperature is below 1525 ℃. However, when the sintering temperature is in the range of 1450-1550 ℃, the variations in the εr and Q·f values are relatively smaller, which are attributed to high density and uniform microstructure with reduced porosity. The maximum values of 20.22 and 74110 GHz for the SmAlO3 ceramics at 1500 ℃ are obtained, respectively. Compared to the conventional solid-state reaction method, the Q·f value can be improved by the stearic acid method. As is well known, the Q·f of ceramics is closely related to the two factors of intrinsic defects and extrinsic defects. Intrinsic defects are related with lattice vibrational modes, while extrinsic defects depend on density and secondary phase, as well as grain size. The fine microstructure with homogeneous grain morphology and grain size, obtained using fine nanopowders as starting materials, should be responsible for the increase of the Q·f value for the present ceramics, though the microstructure of the ceramics was not provided in the reference [5].

Fig. 9(b) shows the τf of SmAlO3 ceramics obtained from the stearic acid method. At 1350-1550 ℃, the τf varies between -74.04 ppm/℃ to -75.94 ppm/℃. It is generally known that the τf is closely related to the εr of a given composition, which depends on the distortion of the oxygen octahedral in the crystal structure [28]. Therefore, no significant rule can be found for the relationship between τf and sintering temperature.

The sintering properties and microwave dielectric characteristics of SmAlO3 ceramics, derived from various methods, are summarized in Table 2. Compared to the conventional solid-state reaction method, the stearic acid approach significantly reduces the calcination temperature and sintering temperature of SmAlO3 ceramics. Moreover, the microwave dielectric properties, especially the Q·f value, are greatly improved. As a result, the stearic acid method is one of the most facile, energy-saving and promising approaches to preparing SmAlO3 ceramics with favorable microwave dielectric properties. However, the εr and Q·f values obtained by the stearic acid method are slightly lower than those achieved by polymeric precursor method, as shown in Table 2. It is essential to study the process optimization of the current synthesis method such as the adjustment of solution concentration, pH, and calcination temperature, for further improvement of the microwave dielectric properties.