Sorption of long-lived 94Nb on magnetite: Spectroscopic and electrochemical investigation of the associated mechanism

M. Ghosha, A. K. Yadavb, A. K. Debnathc, M. K. Deya, K. K. Swaina,d*

aAnalytical Chemistry Division, Bhabha Atomic Research Centre, Mumbai-400085, India

bAtomic & Molecular Physics Division, Bhabha Atomic Research Centre, Mumbai-400085, India

cTechnical Physics Division, Bhabha Atomic Research Centre, Mumbai-400085, India

dHomi Bhabha National Institute, Mumbai-400094, India

Phone No.: 91-22-25590320; Fax: 91-22-25505331

* E-mail of the corresponding author: kallola@barc.gov.in

Supplementary Information

Table S1

Results of solvent extraction study of Nb sorbed magnetite at different pH conditions

| System | Condition | Nb(IV) fraction (%) | Nb(V) fraction (%) |
| --- | --- | --- | --- |
| Nb tracer | N2 atmosphere | 0.84 | 99.16 |
| Nb(V)-Fe3O4 at pH 1.4 | N2 atmosphere | 0.90 | 99.10 |
| Nb(V)-Fe3O4 at pH 6.6 | N2 atmosphere | 0.97 | 99.03 |
| Nb(V)-Fe3O4 at pH 10.4 | N2 atmosphere | 1.20 | 98.80 |

Fig. S1: XRD pattern of synthesized iron oxide

Fig. S2: Surface charge of magnetite as a function of solution pH (Magnetite conc. 2 mg mL-1, Ionic strength: 0.05 M NaClO4, Nitrogen gas purged to avoid CO2 interference during the sample preparation)

Fig. S 3: Dissolution of magnetite with variation of pH of the medium (Initial amount of magnetite: 50 mg and volume of the solution: 25 mL)

Fig. S4: (a) Nb 3d peaks and (b) Fe 2p peaks in XPS measurement of Nb sorbed magnetite at pH 6.6 medium

Fig. S5: (a) Nb 3d peaks and (b) Fe 2p peaks in XPS measurement of Nb sorbed magnetite at pH 10.4 medium

Fig. S6: Fe K weight test (weighted factor: 1,2,3) for Nb sorbed magnetite at pH 1

Fig. S7: Fe K weight test (weighted factor: 1,2,3) for Nb sorbed magnetite at pH 6

Fig. S8: Fe K weight test (weighted factor: 1,2,3) for Nb sorbed magnetite at pH 10