Synthesis, Structure, and Properties of a Dinuclear Cu(II) Coordination Polymer based on Quinoxaline and 3,3-thiodipropionic acid Ligands

Adedibu C. Tellaa*, Samson O. Owaludea, Vincent O. Adimulaa,b*, Adetola C. Oladipoa, Victoria T. Olayemia, Bushra Ismailb, Amara Mumtazb, Attiq Ur Rehmanb, Asad M. Khanb, Hadley S. Claytonc, Nawaz M. Tahird

aDepartment of Chemistry, P.M.B.1515, University of Ilorin, Ilorin, Kwara State, Nigeria

bDepartment of Chemistry, COMSATS University, Islamabad, Abbottabad Campus, 22060, Pakistan

cDepartment of Chemistry, University of South Africa, South Africa

dUniversity of Sargodha: Sargodha, Punjab, PK

*Corresponding author. ac_tella@yahoo.co.uk; vincentadimula@gmail.com

[Cu2(TDPH)4(QNX)].DMF 1 Cambridge Crystallography Database Centre (CCDC) Deposition No.: 2015762

Volume adsorbed (cm3g-1)

0.04

0.08

0.12

0.16

0.20

0.24

0.28

0.32

8000

16000

24000

32000

40000

48000

56000

64000

72000

80000

Relative Pressure (P/Po)

Figure S1. BET Nitrogen isotherm of compound 1

a

b

Figure S2. 1H NMR Spectra of (a) 4-aminophenol; (b) 4-nitrophenol

Table S1: Rate constants (kapp) and thermodynamic parameters for the reduction reduction of 4-NP at different temperatures using 1 as catalyst.

| Parameters | [Cu2(TDPH)4(QNX)].DMF 1 |
| --- | --- |
| 30 °C | 8.0 x 10-4 s-1 |
| 40 °C | 4.0 x 10-4 s-1 |
| 50 °C | 3.0 x 10-4 s-1 |
| 60 °C | 8.0 x 10-4 s-1 |
| Ea (kJ mol-1) | -3.290 |
| ΔH (kJ mol-1) | -5.929 |
| Δs (J mol-1 K-1) | 326.872 |