Supplementary Information

Structure-Aromaticity-Spectroscopy Relationship in Conjugated Polymers

Masiyappan Karuppusamya,b,#, Shyam Vinod Kumar Panneerc,#, Abigail Jennifer Gd, Elumalai Varathand, Ravva Mahesh Kumare and Venkatesan Subramaniana,c,f*

aCentre for High Computing, CSIR-Central Leather Research Institute, Adyar, Chennai - 600 020, India.

bAcademy of Scientific and Innovative Research (AcSIR), Ghaziabad - 201 002, India.

cInorganic and Physical Chemistry, CSIR-Central Leather Research Institute, Adyar, Chennai - 600 020, India.

dDepartment of Chemistry, SRM Institute of Science and Technology, Kattankulathur, Chennai - 603 203, Tamil Nadu, India.

eDepartment of Chemistry, SRM University - AP, Amaravati - 522 502, India.

fDepartment of Chemistry, Indian Institute of Technology-Madras, Chennai - 600 036, India.

#equally contributed.

Table S1. Calculated NICS(0) and NICS(1) values (in ppm) along with the vertical excitation energy of benzene and benzene-based oligomers at B3LYP/6-311G(d,p) level of theory.

| Molecule | Nucleus Independent Chemical Shift (NICS) |  | Vertical Excitation Energy (eV) |
| --- | --- | --- | --- |
|  | NICS(0) | NICS(1) |  |
| Benzene oligomer (BZn; n=1-5) |  |  |  |
| BZ1 | -8.89 | -11.13 | 7.45 |
| BZ2 Ring 1 Ring 2 | -16.44 -8.22 -8.22 | -20.93 -10.42 -10.51 | 6.84 |
| BZ3 Ring 1 Ring 2 Ring 3 | -23.71 -8.13 -7.45 -8.13 | -30.53 -10.42 -9.68 -10.43 | 6.74 |
| BZ4 Ring 1 Ring 2 Ring 3 Ring 4 | -30.96 -8.11 -7.38 -7.38 -8.10 | -40.27 -10.50 -9.69 -9.73 -10.34 | 6.68 |
| BZ5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -38.15 -8.09 -7.36 -7.26 -7.36 -8.09 | -49.56 -10.33 -9.64 -9.54 -9.73 -10.32 | 6.65 |
| Benzene oligomer with vinyl linkers (BZVn; n=1-5) |  |  |  |
| BZV1 Ring 1 Ring 2 | -15.40 -7.70 -7.70 | -20.27 -10.12 -10.15 | 4.31 |
| BZV2 Ring 1 Ring 2 Ring 3 | -21.82 -7.64 -6.54 -7.64 | -29.19 -10.04 -9.11 -10.04 | 3.65 |
| BZV3 Ring 1 Ring 2 Ring 3 Ring 4 | -28.21 -7.64 -6.47 -6.47 -7.64 | -38.98 -10.18 -9.29 -9.28 -10.22 | 3.35 |
| BZV4 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -34.59 -7.64 -6.46 -6.40 -6.46 -7.64 | -47.41 -10.09 -9.08 -9.05 -9.11 -10.07 | 3.19 |
| BZV5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 | -40.97 -7.64 -6.46 -6.39 -6.39 -6.46 -7.64 | -56.37 -10.10 -9.07 -9.00 -9.03 -9.11 -10.06 | 3.09 |
| Benzene oligomer with ethynyl linkers (BZEn; n=1-5) |  |  |  |
| BZE1 Ring 1 Ring 2 | -16.82 -8.41 -8.41 | -20.72 -10.36 -10.36 | 7.32 |
| BZE2 Ring 1 Ring 2 Ring 3 | -24.58 -8.37 -7.85 -8.37 | -30.29 -10.33 -9.63 -10.33 | 3.88 |
| BZE3 Ring 1 Ring 2 Ring 3 Ring 4 | -32.32 -8.36 -7.80 -7.80 -8.36 | -39.85 -10.33 -9.60 -9.60 -10.33 | 3.60 |
| BZE4 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -40.05 -8.36 -7.79 -7.75 -7.79 -8.36 | -49.40 -10.33 -9.59 -9.56 -9.59 -10.33 | 3.45 |
| BZE5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 | -47.78 -8.35 -7.79 -7.74 7.74 7.79 8.35 | -58.94 -10.33 -9.59 -9.55 -9.55 -9.59 -10.32 | 3.36 |
| Benzene oligomer with thiophene linkers (BZTn; n=1-5) |  |  |  |
| BZT1 Ring 1 Ring 2 Ring 3 | -25.55 -7.87 -9.81 -7.87 | -28.30 -10.14 -8.10 -10.05 | 4.15 |
| BZT2 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -41.57 -7.84 -9.59 -6.71 -9.59 -7.84 | -45.32 -10.17 -7.98 -8.95 -8.23 -9.99 | 3.65 |
| BZT3 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 Ring 7 | -57.94 -7.84 -9.64 -6.70 -9.52 -6.72 -9.67 -7.84 | -62.14 -9.95 -8.19 -8.82 -8.19 -8.85 -8.05 -10.08 | 3.43 |
| BZT4 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 Ring 7 Ring 8 Ring 9 | -74.12 -7.85 -9.66 -6.70 -9.46 -6.67 -9.55 -6.72 -9.66 -7.85 | -79.05 -9.95 -8.23 -8.95 -7.95 -8.76 -8.00 -8.82 -8.38 -10.00 | 3.33 |
| BZT5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 Ring 7 Ring 8 Ring 9 Ring 10 Ring 11 | -90.08 -7.83 -9.60 -6.68 -9.44 -6.64 -9.44 -6.67 -9.54 -6.72 -9.67 -7.85 | -96.09 -9.98 -8.35 -8.86 -7.99 -8.80 -7.97 -8.93 -8.22 -8.82 -8.14 -10.06 | 3.27 |

Table S2. Calculated NICS(0) and NICS(1) values (in ppm) along with the vertical excitation energy of thiophene and thiophene-based oligomers at B3LYP/6-311G(d,p) level of theory.

| Molecule | Nucleus Independent Chemical Shift (NICS) |  | Vertical Excitation Energy (eV) |
| --- | --- | --- | --- |
|  | NICS(0) | NICS(1) |  |
| Thiophene oligomer (THn; n=1-5) |  |  |  |
| TH1 | -13.88 | -11.33 | 9.89 |
| TH2 Ring 1 Ring 2 | -23.67 -11.83 -11.83 | -19.08 -9.58 -9.50 | 4.36 |
| TH3 Ring 1 Ring 2 Ring 3 | -33.23 -11.72 -9.79 -11.72 | -26.86 -9.43 -7.98 -9.45 | 3.68 |
| TH4 Ring 1 Ring 2 Ring 3 Ring 4 | -42.71 -11.68 -9.67 -9.67 -11.68 | -34.26 -9.43 -7.73 -7.67 -9.43 | 3.30 |
| TH5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -52.17 -11.67 -9.63 -9.56 -9.63 -11.67 | -42.12 -9.42 -7.83 -7.65 -7.82 -9.40 | 3.07 |
| Thiophene oligomer with vinyl linkers (THVn; n=1-5) |  |  |  |
| THV1 Ring 1 Ring 2 | -22.79 -11.39 -11.39 | -18.75 -9.40 -9.35 | 3.84 |
| THV2 Ring 1 Ring 2 Ring 3 | -31.81 -11.32 -9.17 -11.32 | -26.17 -9.27 -7.62 -9.28 | 3.11 |
| THV3 Ring 1 Ring 2 Ring 3 Ring 4 | -40.76 -11.29 -9.09 -9.09 -11.29 | -34.43 -9.46 -7.68 -7.85 -9.44 | 2.76 |
| THV4 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -49.74 -11.29 -9.07 -9.00 -9.07 -11.29 | -41.26 -9.30 -7.57 -7.54 -7.57 -9.28 | 2.56 |
| THV5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 | -58.67 -11.28 -9.08 -8.98 -8.98 -9.08 -11.28 | -48.76 -9.29 -7.57 -7.52 -7.50 -7.61 -9.28 | 2.44 |
| Thiophene oligomer with ethynyl linkers (THEn; n=1-5) |  |  |  |
| THE1 Ring 1 Ring 2 | -25.88 -12.94 -12.94 | -20.83 -10.27 -10.56 | 3.97 |
| THE2 Ring 1 Ring 2 Ring 3 | -37.74 -12.88 -11.97 -12.88 | -29.59 -10.17 -10.18 -9.24 | 3.34 |
| THE3 Ring 1 Ring 2 Ring 3 Ring 4 | -49.57 -12.86 -11.92 -11.92 -12.86 | -40.10 -10.58 -9.68 -9.44 -10.40 | 3.04 |
| THE4 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -61.41 -12.87 -11.91 -11.86 -11.91 -12.87 | -48.24 -9.26 -9.30 -10.26 -9.20 -10.23 | 2.87 |
| THE5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 | -73.23 -12.85 -11.91 -11.85 -11.85 -11.91 -12.85 | -57.06 -10.18 -9.17 -9.19 -9.19 -9.15 -10.17 | 2.76 |
| Thiophene oligomer with phenyl linkers (THPn; n=1-5) |  |  |  |
| THP1 Ring 1 Ring 2 Ring 3 | -30.39 -11.70 -6.99 -11.70 | -28.58 -9.88 -8.99 -9.71 | 4.19 |
| THP2 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 | -46.73 -11.70 -6.87 -9.61 -6.86 -11.69 | -45.89 -9.57 -9.05 -8.71 -9.02 -9.55 | 3.64 |
| THP3 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 Ring 7 | -62.69 -11.67 -6.83 -9.45 -6.66 -9.54 -6.85 -11.69 | -62.54 -9.61 -9.10 -8.20 -8.89 -7.82 -8.99 -9.93 | 3.43 |
| THP4 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 Ring 7 Ring 8 Ring 9 | -78.93 -11.69 -6.85 -9.54 -6.68 -9.51 -6.68 -9.48 -6.83 -11.69 | -79.94 -9.68 -9.28 -8.47 -9.13 -7.96 -8.80 -7.90 -9.04 -9.69 | 3.33 |
| THP5 Ring 1 Ring 2 Ring 3 Ring 4 Ring 5 Ring 6 Ring 7 Ring 8 Ring 9 Ring 10 Ring 11 | -95.34 -11.67 -6.85 -9.58 -6.69 -9.53 -6.69 -9.53 -6.69 -9.58 -6.85 -11.67 | -95.99 -9.71 -8.98 -8.05 -9.04 -8.18 -8.80 -7.81 -8.81 -8.12 -8.92 -9.55 | 3.27 |

Figure S3: Correlation between the calculated ΣNICS0 and the number of repeating units in the studied oligomers at B3LYP/6-31G(d,p) level of theory.

Figure S4: Correlation between the calculated ΣNICS1 and the number of repeating units in the studied oligomers at B3LYP/6-31G(d,p) level of theory.

Figure S5. The variation of First Transition Energy (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS0 at B3LYP/6-311G(d,p) level of theory) for benzene based oligomers

Figure S6. The variation of First Transition Energy (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS0 at B3LYP/6-311G(d,p) level of theory) for thiophene based oligomers

Figure S7. The variation of First Transition Energy (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS1 at B3LYP/6-311G(d,p) level of theory) for benzene based oligomers

Figure S8. The variation of First Transition Energy (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS1 at B3LYP/6-311G(d,p) level of theory) for thiophene based oligomers

Figure S9. The variation of λmax (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS0 at B3LYP/6-311G(d,p) level of theory) for benzene based oligomers

Figure S10. The variation of λmax (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS0 at B3LYP/6-311G(d,p) level of theory) for thiophene based oligomers

Figure S1. The variation of λmax (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS1 at B3LYP/6-311G(d,p) level of theory) for benzene based oligomers

Figure S12. The variation of λmax (calculated at ωB97X-D/6-31G(d,p) level of theory) with aromaticity (as predicted by 1/NICS1 at B3LYP/6-311G(d,p) level of theory) for thiophene based oligomers

Figure S13. The variation of reorganization energies (λe and λh, calculated at B3LYP/6-31G(d) level of theory) with aromaticity (as predicted by 1/NICS0 at B3LYP/6-311G(d,p) level of theory) for benzene based oligomers

Figure S14. The variation of reorganization energies (λe and λh, calculated at B3LYP/6-31G(d) level of theory) with aromaticity (as predicted by 1/NICS0 at B3LYP/6-311G(d,p) level of theory) for thiophene based oligomers

Figure S15. The variation of reorganization energies (λe and λh, calculated at B3LYP/6-31G(d) level of theory) with aromaticity (as predicted by 1/NICS1 at B3LYP/6-311G(d,p) level of theory) for benzene based oligomers

Figure S16. The variation of reorganization energies (λe and λh, calculated at B3LYP/6-31G(d) level of theory) with aromaticity (as predicted by 1/NICS1 at B3LYP/6-311G(d,p) level of theory) for thiophene based oligomers