Supplementary Information

Title: Migration and interaction of tetracycline and heavy metals on goethite-coated sand under dynamic flow conditions

Si-Jia Liu a, De-Hua Zeng a, Chen Yang a, b, c, *, Zhi Dang a, b, Xiao-Yan Ma a

a School of Environment and Energy, South China University of Technology, Guangzhou 510006, China

b The Key Laboratory of Pollution Control and Ecosystem Restoration in Industry Clusters, Ministry of Education, South China University of Technology, Guangzhou 510006, China

c Guangdong Provincial Key Laboratory of Atmospheric Environment and Pollution Control, South China University of Technology, Guangzhou 510006, China

*Corresponding author:

School of Environment and Energy, South China University of Technology, Guangzhou 510006, China (E-mail addresses: cyanggz@scut.edu.cn)

Supporting Information Including:

- 4 tables

Table S1 Each stage of the column experiment

| Influent stage 1 | Influent stage 2 | Research Purpose |
| --- | --- | --- |
| TC | NaCl | Migration of TC |
|  | Heavy metal | Effect of heavy metals on desorption of TC; Adsorption of heavy metals on GCS column saturated with TC |
| Heavy metal | NaCl | Migration of heavy metals |
|  | TC | Effect of TC on desorption of heavy metals; Adsorption of TC on GCS column saturated with heavy metals |
| TC+ Heavy metal | NaCl | Migration of heavy metals and antibiotics under combined pollution |

Table S2 The parameters of Thomas model for migration of TC on the GCS columns under different conditions

| Experimental condition |  | PVb | Kt L/(min·mg) | Q μg/g | R2 |
| --- | --- | --- | --- | --- | --- |
| pH 3.0 | TC | 15.3 | 1.37E-3 | 733.86 | 0.989 |
|  | Cu-TC | 16.3 | 7.22E-4 | 807.68 | 0.966 |
|  | Cu+TC | 15.6 | 1.07E-3 | 783.90 | 0.999 |
|  | Cd-TC | 15.3 | 1.36E-3 | 706.93 | 0.987 |
|  | Cd+TC | 15.6 | 1.61E-3 | 704.04 | 0.991 |
| pH 5.5 | TC | 7.6 | 4.87E-3 | 452.48 | 0.887 |
|  | Cu-TC | 9.0 | 5.70E-4 | 519.84 | 0.941 |
|  | Cu+TC | 63.3 | 1.56E-5 | 7699.72 | 0.860 |
|  | Cd-TC | 8.0 | 7.64E-4 | 447.68 | 0.905 |
|  | Cd+TC | 8.0 | 4.92E-4 | 474.68 | 0.887 |
| pH 8.0 | TC | 5.0 | 4.87E-4 | 334.57 | 0.893 |
|  | Cd-TC | 12.6 | 2.62E-4 | 833.91 | 0.911 |
|  | Cd+TC | 5.6 | 5.42E-4 | 327.11 | 0.853 |

Table S3 The parameters of Thomas model for migration of Cu on the GCS columns under different conditions

| Experimental condition |  | PVb | Kt L/(min·mg) | Q μg/g | R2 |
| --- | --- | --- | --- | --- | --- |
| pH 3.0 | Cu | 1.0 | 0.172 | 6.16 | 0.997 |
|  | TC-Cu | 1.8 | 0.034 | 15.35 | 0.995 |
|  | TC+Cu | 1.2 | 0.099 | 6.88 | 0.917 |
| pH 5.5 | Cu | 4.1 | 0.030 | 25.89 | 0.992 |
|  | TC-Cu | 9.5 | 0.015 | 52.34 | 0.977 |
|  | TC+Cu | 6.7 | 1.21E-4 | 740.21 | 0.836 |

Table S4 The parameters of Thomas model for migration of Cd on the GCS columns under different conditions

| Experimental condition |  | PVb | Kt L/(min·mg) | Q μg/g | R2 |
| --- | --- | --- | --- | --- | --- |
| pH 3.0 | Cd | 1.0 | 0.100 | 11.47 | 0.997 |
|  | TC-Cd | 1.0 | 0.044 | 9.96 | 0.990 |
|  | TC+Cd | 1.0 | 0.122 | 10.25 | 0.989 |
| pH 5.5 | Cd | 2.0 | 0.036 | 21.34 | 0.996 |
|  | TC-Cd | 1.8 | 0.035 | 21.30 | 0.996 |
|  | TC+Cd | 2.0 | 0.026 | 21.94 | 0.980 |
| pH 8.0 | Cd | 260 | 2.526E-4 | 2798.82 | 0.968 |
|  | TC-Cd | 193* | 5.305E-4 | 1909.15 | 0.977 |
|  | TC+Cd | 155* | 3.831E-4 | 1721.17 | 0.985 |

* Due to the lack of experimental data, this was the estimated value.