Supplementary Information

Mechanistic Analysis of Nanocellulose Formation Tuned by Deep Eutectic Solvents

Xuerong Bia , Jiansheng Guoa,b, Jin Wenc*, Chongwen Yua,b*

aCollege of Textiles, Donghua University, Shanghai, 201620, China

bKey Laboratory of Textile Science & Technology, Ministry of Education, Donghua University, Shanghai, 201620, China

cState Key Laboratory for Modification of Chemical Fibers and Polymer Materials, College of Materials Science and Engineering, Donghua University, Shanghai 201620, China

*Corresponding author:

Chongwen Yu: yucw@dhu.edu.cn

Jin Wen: jinwen@dhu.edu.cn

Fig. S1 The flow chart of CNCs preparation.

Electrostatic potential (ESP) analysis. Electrostatic potential (ESP) is defined as a positive charge that moves from infinity to the surface of the molecule to measure everywhere properties. It has profound theoretical and practical significance in investigating the intermolecular electrostatic interaction, predicting the reaction site and molecular properties. The ESP plot distinguishes the strength of the electrostatic potential on the surface of the molecules by colors (Lu & Chen, 2012).

Fig. S2 The ESP of different molecules(kcal/mol).

(a)Cl-; (b)Ch+; (c)oxalic acid (OA); (d)H2O; (e)citric acid (CA); (f)cellobiose. Blue region represents the negative electrostatic potential (high electron density), red region represents the positive electrostatic potential (low electron density), white region represents the intermediate level of the electrostatic potential. The yellow and blue points depict the configuration corresponding local maximum and local minimum of ESP, respectively.

Fig. S3 Snapshot and RDF of the specific atom of four cellulose-DESs systems. (a)-(b) DES1-cellulose chains; (c)-(d) DES3-cellulose chains. (ChCl, blue; OA, pink; CA, yellow; cellulose, green).

Fig. S4 The structure of (C6H10O5)10-DESs. (a)DES1-cellulose chains; (b)DES2-cellulose chains; (c)DES3-cellulose chains; (d)DES4-cellulose chains

Fig. S5 RDG of two kinds of cellobiose dimer

(a)-(c) cellobiose dimer of (100) lattice plane; (d)-(f) cellobiose dimer of (010) lattice plane.

Fig. S6 AIM analysis of DESs-cellobiose. (a)DES1-cellobiose; (b)DES2-cellobiose; (c)DES3-cellobiose; (d)DES4-cellobiose; (e)cellobiose dimer of (100) lattice plane; (f) cellobiose dimer of (010) lattice plane. The orange points present the BCPs and the yellow lines present the bond path.

Fig. S7 Optimized structures of reactants, TSs, and products. (a-c) OA-cellobiose esterify; (d-f) CA-cellobiose esterify; (g-i) hydrolysis(non-catalysis); (j-l) hydrolysis(H+ catalysis)

Table S1 Binding energy of cellulose chains-DESs

| Binding Energy(kcal/mol) | DES1 | DES2 | DES3 | DES4 |
| --- | --- | --- | --- | --- |
| (C6H10O5)2 | -9.6 | -30.9 | -22.8 | -25.4 |
| (C6H10O5)10 | -77.2 | -129.3 | -76.3 | -63.5 |

Table S2 AIM analysis of DESs-cellobiose.

| Complexes | HB | ρBCP(a.u.) | ∇2ρBCP(a.u.) | VCP(a.u.) | EHB(kcal/mol) |
| --- | --- | --- | --- | --- | --- |
| DES1-cellobiose | 1:O31…H75-O74 | 0.03460 | 0.12148 | -0.03025 | -9.49 |
|  | 2:O73…H36-O35 | 0.02345 | 0.10267 | -0.01852 | -5.81 |
| DES2-cellobiose | 3:O31…H75-O74 | 0.04757 | 0.13602 | -0.04595 | -14.42 |
|  | 4:O79…H32-O31 | 0.03505 | 0.13511 | -0.03221 | -10.11 |
|  | 5:O79…H36-O35 | 0.03029 | 0.11787 | -0.02583 | -8.10 |
| DES3-cellobiose | 6:O84…H36-O35 | 0.02961 | 0.12201 | -0.02542 | -7.98 |
|  | 7:O37…H86-O85 | 0.02791 | 0.10327 | -0.02266 | -7.11 |
| DES4-cellobiose | 8:O89…H40-O39 | 0.04119 | 0.13894 | -0.03860 | -12.11 |
|  | 9:O37…H86-O85 | 0.03494 | 0.12379 | -0.03075 | -9.65 |
|  | 10:O84…H36-O35 | 0.03345 | 0.13551 | -0.03040 | -9.54 |
| Cellobiose dimer100 | 11:O35…H90-O89 | 0.02074 | 0.07263 | -0.01421 | -4.46 |
|  | 12:O80…H45-O44 | 0.02077 | 0.07272 | -0.01424 | -4.47 |
| Cellobiose dimer 010 | 13:O76…H38-O37 | 0.03025 | 0.11445 | -0.02577 | -8.09 |
|  | 14:O31…H83-O82 | 0.03026 | 0.11446 | -0.02578 | -8.09 |

Table S3 The optimized coordinates of complex.

| Element | x | y | z |
| --- | --- | --- | --- |
| DES1-Cellobiose |  |  |  |
| C | 0.768654 | 4.001008 | 0.863268 |
| C | 1.99429 | 3.237418 | 1.348433 |
| C | 1.577339 | 1.9861 | 2.131203 |
| C | -0.56015 | 1.920986 | 0.972834 |
| C | -0.13821 | 3.075352 | 0.061721 |
| H | 2.577788 | 2.931085 | 0.469935 |
| H | 0.215756 | 4.374499 | 1.740822 |
| H | -1.10604 | 2.297584 | 1.853398 |
| H | 0.422485 | 2.659438 | -0.77917 |
| H | 1.135815 | 2.306696 | 3.088643 |
| O | 0.60955 | 1.214882 | 1.397913 |
| O | -1.35708 | 1.031913 | 0.255956 |
| C | -2.27429 | 0.189483 | 0.966372 |
| C | -1.59087 | -1.13447 | 1.3627 |
| H | -2.63746 | 0.704039 | 1.865011 |
| C | -2.59408 | -2.22213 | 1.735487 |
| H | -1.05222 | -1.46494 | 0.463534 |
| C | -3.76898 | -2.2721 | 0.761651 |
| H | -2.99712 | -2.0028 | 2.731795 |
| H | -3.41988 | -2.62541 | -0.22372 |
| O | -4.35368 | -0.98954 | 0.607838 |
| O | -0.70857 | -0.99057 | 2.45657 |
| H | -0.01767 | -0.34798 | 2.212653 |
| O | -1.90938 | -3.47601 | 1.733414 |
| H | -2.55595 | -4.13948 | 2.000422 |
| C | -3.43376 | -0.08512 | -0.00575 |
| H | -3.00487 | -0.5551 | -0.89891 |
| C | -4.17481 | 1.166612 | -0.44421 |
| H | -5.02887 | 1.323618 | 0.221749 |
| H | -3.50202 | 2.025654 | -0.39883 |
| O | -4.63417 | 0.969491 | -1.80026 |
| H | -5.11914 | 1.756526 | -2.06902 |
| O | -4.71119 | -3.14613 | 1.305085 |
| H | -5.43111 | -3.24588 | 0.672634 |
| O | -1.25107 | 3.825038 | -0.40733 |
| H | -1.47251 | 3.462195 | -1.27848 |
| O | 1.225851 | 5.094648 | 0.084733 |
| H | 0.451003 | 5.442431 | -0.37371 |
| O | 2.78144 | 4.032846 | 2.227195 |
| H | 2.990077 | 4.842481 | 1.747058 |
| C | 2.767511 | 1.068202 | 2.376852 |
| H | 3.176212 | 0.763785 | 1.411326 |
| H | 3.532994 | 1.628044 | 2.922616 |
| O | 2.403053 | -0.13642 | 3.055627 |
| H | 2.157513 | 0.082212 | 3.960352 |
| N | 1.925806 | -3.39924 | -0.16942 |
| C | 2.360282 | -4.62385 | 0.573068 |
| H | 1.603402 | -4.86398 | 1.318692 |
| H | 2.4673 | -5.44791 | -0.13162 |
| H | 3.310652 | -4.43042 | 1.065049 |
| C | 1.800456 | -2.24517 | 0.798353 |
| H | 1.611739 | -1.33833 | 0.227763 |
| H | 0.982831 | -2.44945 | 1.486509 |
| H | 2.724834 | -2.13048 | 1.355626 |
| C | 0.578191 | -3.65481 | -0.79342 |
| H | 0.293914 | -2.77422 | -1.36736 |
| H | 0.664131 | -4.5175 | -1.45384 |
| H | -0.14639 | -3.8472 | -0.00195 |
| C | 2.902076 | -3.05492 | -1.29007 |
| H | 2.508685 | -2.15248 | -1.75705 |
| H | 2.861405 | -3.87845 | -2.00547 |
| C | 4.357532 | -2.79396 | -0.87443 |
| H | 4.856689 | -3.72032 | -0.57525 |
| H | 4.400597 | -2.08621 | -0.04041 |
| O | 5.039607 | -2.29948 | -2.00011 |
| H | 4.76223 | -1.36598 | -2.09051 |
| Cl | 3.487276 | 0.416482 | -1.48616 |
| C | -0.01744 | 0.348402 | -2.64057 |
| O | 0.083367 | -0.83558 | -2.39851 |
| O | 0.937208 | 1.235196 | -2.70697 |
| H | 1.835021 | 0.867531 | -2.38483 |
| C | -1.40682 | 1.007505 | -2.84304 |
| O | -1.61394 | 2.193589 | -2.72847 |
| O | -2.3497 | 0.103931 | -3.08057 |
| H | -3.22811 | 0.521417 | -2.91435 |
| DES2-Cellobiose |  |  |  |
| C | -2.95461 | -3.17206 | -1.09313 |
| C | -1.51764 | -3.56645 | -1.40279 |
| C | -0.80204 | -2.37788 | -2.04823 |
| C | -2.25384 | -0.78814 | -0.93388 |
| C | -3.01984 | -1.91358 | -0.23264 |
| H | -1.00844 | -3.82977 | -0.4657 |
| H | -3.4642 | -2.96645 | -2.04799 |
| H | -2.75032 | -0.52022 | -1.8793 |
| H | -2.53477 | -2.10723 | 0.729257 |
| H | -1.29279 | -2.16876 | -3.01322 |
| O | -0.9132 | -1.22136 | -1.20038 |
| O | -2.17572 | 0.325491 | -0.09561 |
| C | -2.10711 | 1.622626 | -0.70235 |
| C | -0.69259 | 1.968461 | -1.21072 |
| H | -2.81538 | 1.668112 | -1.53965 |
| C | -0.60561 | 3.441632 | -1.60872 |
| H | -0.00374 | 1.782921 | -0.37494 |
| C | -1.26708 | 4.366674 | -0.58876 |
| H | -1.13549 | 3.568313 | -2.56076 |
| H | -0.66471 | 4.386564 | 0.335864 |
| O | -2.57833 | 3.92879 | -0.26811 |
| O | -0.31631 | 1.222822 | -2.35221 |
| H | -0.20077 | 0.294647 | -2.08457 |
| O | 0.771848 | 3.794909 | -1.75411 |
| H | 0.785515 | 4.708215 | -2.06307 |
| C | -2.5306 | 2.645102 | 0.363232 |
| H | -1.76688 | 2.668383 | 1.149493 |
| C | -3.87626 | 2.366243 | 1.038419 |
| H | -4.40619 | 3.318443 | 1.127009 |
| H | -4.47678 | 1.677336 | 0.439993 |
| O | -3.66874 | 1.818092 | 2.350582 |
| H | -4.22567 | 1.02586 | 2.46363 |
| O | -1.33236 | 5.631577 | -1.17386 |
| H | -1.67642 | 6.251023 | -0.52116 |
| O | -4.39295 | -1.59 | -0.06174 |
| H | -4.52038 | -1.263 | 0.845145 |
| O | -3.57852 | -4.27281 | -0.44755 |
| H | -4.45818 | -3.96796 | -0.19423 |
| O | -1.47441 | -4.64715 | -2.32431 |
| H | -2.03518 | -5.34081 | -1.95802 |
| C | 0.680728 | -2.62354 | -2.28159 |
| H | 1.201532 | -2.71802 | -1.32645 |
| H | 0.798595 | -3.55917 | -2.83546 |
| O | 1.292707 | -1.52386 | -2.9658 |
| H | 0.970732 | -1.51443 | -3.87303 |
| N | 3.767938 | 1.31063 | -0.46933 |
| C | 4.735275 | 1.973815 | -1.39947 |
| H | 4.20439 | 2.743531 | -1.958 |
| H | 5.541238 | 2.417085 | -0.81568 |
| H | 5.138954 | 1.236192 | -2.08903 |
| C | 2.688833 | 0.618857 | -1.26579 |
| H | 2.028729 | 0.11768 | -0.56271 |
| H | 2.140208 | 1.362422 | -1.8404 |
| H | 3.130926 | -0.11753 | -1.929 |
| C | 3.125658 | 2.362493 | 0.397604 |
| H | 2.460373 | 1.862515 | 1.098288 |
| H | 3.912539 | 2.894153 | 0.931613 |
| H | 2.558502 | 3.039617 | -0.24093 |
| C | 4.471918 | 0.316858 | 0.445623 |
| H | 3.683601 | -0.1504 | 1.035755 |
| H | 5.133929 | 0.884669 | 1.10131 |
| C | 5.286842 | -0.78212 | -0.25108 |
| H | 6.155641 | -0.36858 | -0.76915 |
| H | 4.676209 | -1.34048 | -0.96572 |
| O | 5.782049 | -1.6513 | 0.75048 |
| H | 5.024843 | -2.22361 | 1.012342 |
| Cl | 2.994829 | -2.9439 | 0.987368 |
| C | 0.427164 | -0.64344 | 2.249707 |
| O | 1.203613 | 0.188918 | 1.824345 |
| O | 0.604204 | -1.9267 | 2.347838 |
| H | 1.489736 | -2.22981 | 1.931487 |
| C | -0.99469 | -0.23685 | 2.711964 |
| O | -1.86721 | -1.05981 | 2.912129 |
| O | -1.13404 | 1.066881 | 2.815244 |
| H | -2.09984 | 1.317812 | 2.829232 |
| O | 7.014485 | 0.296582 | 2.386477 |
| H | 6.74681 | -0.52877 | 1.942945 |
| H | 6.704078 | 0.182708 | 3.289904 |
| O | -4.52559 | -0.74862 | 2.619393 |
| H | -3.59639 | -0.95081 | 2.87606 |
| H | -5.10185 | -1.20221 | 3.241919 |
| DES3-Cellobiose |  |  |  |
| C | -0.6982 | -1.46585 | 2.833144 |
| C | -0.26308 | -0.16172 | 3.4857 |
| C | 1.252068 | 0.037799 | 3.312511 |
| C | 1.315181 | -1.44196 | 1.402365 |
| C | -0.2007 | -1.59523 | 1.39462 |
| H | -0.78235 | 0.674486 | 3.00154 |
| H | -0.29955 | -2.30049 | 3.425283 |
| H | 1.78879 | -2.22135 | 2.024331 |
| H | -0.60199 | -0.7742 | 0.793667 |
| H | 1.778579 | -0.70268 | 3.937886 |
| O | 1.63497 | -0.15733 | 1.941929 |
| O | 1.800738 | -1.48964 | 0.103205 |
| C | 3.220312 | -1.63549 | -0.05415 |
| C | 3.76738 | -0.32196 | -0.63026 |
| H | 3.690472 | -1.83925 | 0.91548 |
| C | 5.180623 | -0.46259 | -1.1834 |
| H | 3.11409 | -0.08909 | -1.48611 |
| C | 5.306913 | -1.72789 | -2.0282 |
| H | 5.887489 | -0.54602 | -0.34855 |
| H | 4.687106 | -1.63041 | -2.93688 |
| O | 4.881336 | -2.86219 | -1.2972 |
| O | 3.757828 | 0.743027 | 0.300489 |
| H | 3.070873 | 0.590875 | 0.975061 |
| O | 5.453378 | 0.692476 | -1.97309 |
| H | 6.345669 | 0.582263 | -2.32056 |
| C | 3.483149 | -2.80968 | -1.01126 |
| H | 2.916597 | -2.64137 | -1.93901 |
| C | 3.047219 | -4.14543 | -0.44502 |
| H | 3.728911 | -4.42391 | 0.371325 |
| H | 2.032244 | -4.02809 | -0.04904 |
| O | 3.084881 | -5.10182 | -1.49883 |
| H | 2.675626 | -5.90988 | -1.1777 |
| O | 6.656727 | -1.87174 | -2.35376 |
| H | 6.747992 | -2.6553 | -2.90724 |
| O | -0.61008 | -2.84554 | 0.870038 |
| H | -1.28312 | -2.63716 | 0.201108 |
| O | -2.13614 | -1.53964 | 2.868918 |
| H | -2.36578 | -2.44908 | 2.637953 |
| O | -0.51348 | -0.18044 | 4.889012 |
| H | -1.4694 | -0.15913 | 5.00268 |
| C | 1.669782 | 1.450814 | 3.70889 |
| H | 1.074208 | 2.165911 | 3.139845 |
| H | 1.443426 | 1.586338 | 4.771418 |
| O | 3.034614 | 1.733109 | 3.40916 |
| H | 3.591709 | 1.174025 | 3.959944 |
| N | 1.638373 | 3.649899 | -1.27105 |
| C | 2.27573 | 4.822764 | -1.94813 |
| H | 3.356131 | 4.748457 | -1.83157 |
| H | 2.013489 | 4.809073 | -3.00564 |
| H | 1.918811 | 5.7421 | -1.48881 |
| C | 2.018105 | 3.630663 | 0.197274 |
| H | 1.335183 | 2.960313 | 0.718169 |
| H | 3.045861 | 3.284084 | 0.281471 |
| H | 1.908348 | 4.632908 | 0.603704 |
| C | 2.139966 | 2.382564 | -1.90855 |
| H | 1.666914 | 1.54498 | -1.40264 |
| H | 1.864975 | 2.392283 | -2.96254 |
| H | 3.219048 | 2.313728 | -1.78692 |
| C | 0.123441 | 3.667942 | -1.44377 |
| H | -0.24375 | 2.800143 | -0.89743 |
| H | -0.06672 | 3.536564 | -2.51053 |
| C | -0.6169 | 4.901841 | -0.90159 |
| H | -0.58194 | 5.73437 | -1.60849 |
| H | -0.18584 | 5.22537 | 0.049635 |
| O | -1.97874 | 4.561078 | -0.71335 |
| H | -1.99953 | 4.038927 | 0.13451 |
| Cl | -1.14421 | 2.775369 | 1.56259 |
| C | -5.12142 | -1.85499 | -2.06023 |
| H | -5.84549 | -1.59523 | -2.83211 |
| H | -4.23112 | -2.27336 | -2.53701 |
| C | -4.74124 | -0.58869 | -1.27783 |
| C | -4.13452 | 0.451508 | -2.25922 |
| H | -4.84779 | 0.602675 | -3.07645 |
| H | -3.20286 | 0.082612 | -2.68856 |
| C | -3.89578 | 1.810214 | -1.62092 |
| O | -4.52923 | 2.24082 | -0.6829 |
| O | -2.92253 | 2.493802 | -2.23003 |
| H | -2.75086 | 3.334686 | -1.73128 |
| C | -5.7025 | -2.92978 | -1.16562 |
| O | -5.30555 | -3.22017 | -0.0663 |
| O | -6.71987 | -3.58393 | -1.7697 |
| H | -7.01595 | -4.26538 | -1.14718 |
| C | -3.64484 | -0.95368 | -0.24501 |
| O | -2.63088 | -1.538 | -0.59486 |
| O | -3.89936 | -0.52063 | 0.968965 |
| H | -3.17123 | -0.7517 | 1.594513 |
| O | -5.92626 | -0.11605 | -0.69154 |
| H | -5.71708 | 0.740588 | -0.28351 |
| DES4-Cellobiose |  |  |  |
| C | -1.52244 | 0.638385 | 3.028069 |
| C | -0.68012 | 1.843067 | 2.62555 |
| C | 0.799638 | 1.398594 | 2.666954 |
| C | 0.266687 | -0.89822 | 2.097212 |
| C | -1.22115 | -0.56111 | 2.124981 |
| H | -0.92182 | 2.121013 | 1.59213 |
| H | -1.29747 | 0.387589 | 4.072688 |
| H | 0.614253 | -1.2989 | 3.06366 |
| H | -1.47249 | -0.28809 | 1.096367 |
| H | 1.043746 | 1.088359 | 3.697185 |
| O | 1.01158 | 0.287598 | 1.779881 |
| O | 0.46379 | -1.81535 | 1.075489 |
| C | 1.674369 | -2.5791 | 1.028421 |
| C | 2.740189 | -1.82556 | 0.202533 |
| H | 2.061483 | -2.73917 | 2.043332 |
| C | 3.837398 | -2.74078 | -0.32358 |
| H | 2.207674 | -1.40238 | -0.6625 |
| C | 3.242916 | -4.01945 | -0.89999 |
| H | 4.492692 | -3.03133 | 0.506859 |
| H | 2.6105 | -3.78397 | -1.77365 |
| O | 2.463772 | -4.66959 | 0.080534 |
| O | 3.372832 | -0.80735 | 0.95465 |
| H | 2.682668 | -0.20405 | 1.288875 |
| O | 4.578258 | -2.03566 | -1.32592 |
| H | 5.176772 | -2.68514 | -1.71509 |
| C | 1.284704 | -3.92497 | 0.392044 |
| H | 0.719037 | -3.72079 | -0.5282 |
| C | 0.407742 | -4.76103 | 1.301852 |
| H | 1.025333 | -5.14745 | 2.125249 |
| H | -0.37153 | -4.10801 | 1.709606 |
| O | -0.1464 | -5.8206 | 0.529339 |
| H | -0.79771 | -6.27195 | 1.073093 |
| O | 4.314883 | -4.8396 | -1.26269 |
| H | 3.957016 | -5.64903 | -1.64411 |
| O | -1.99185 | -1.67558 | 2.539474 |
| H | -2.67147 | -1.78993 | 1.853931 |
| O | -2.92573 | 0.941295 | 2.936646 |
| H | -3.38147 | 0.20351 | 3.36155 |
| O | -0.88213 | 2.934612 | 3.488551 |
| H | -1.0137 | 3.714195 | 2.908828 |
| C | 1.734797 | 2.518558 | 2.238951 |
| H | 1.47911 | 2.869489 | 1.238179 |
| H | 1.610708 | 3.355357 | 2.929882 |
| O | 3.108876 | 2.099667 | 2.173315 |
| H | 3.416927 | 1.921963 | 3.068198 |
| N | 4.594134 | 2.068207 | -1.32879 |
| C | 5.326483 | 2.127529 | -2.63426 |
| H | 6.344242 | 2.468217 | -2.44893 |
| H | 5.344459 | 1.129793 | -3.07084 |
| H | 4.825064 | 2.822815 | -3.30331 |
| C | 4.48177 | 3.447491 | -0.72407 |
| H | 4.112324 | 3.33467 | 0.293243 |
| H | 5.473387 | 3.900131 | -0.725 |
| H | 3.772022 | 4.049773 | -1.28687 |
| C | 5.368595 | 1.192257 | -0.37551 |
| H | 4.81421 | 1.133749 | 0.556344 |
| H | 5.452415 | 0.191903 | -0.79686 |
| H | 6.348222 | 1.646159 | -0.2236 |
| C | 3.204466 | 1.461295 | -1.5255 |
| H | 2.667438 | 1.629355 | -0.59561 |
| H | 3.362535 | 0.391026 | -1.65254 |
| C | 2.388503 | 2.052408 | -2.69205 |
| H | 2.620655 | 1.536047 | -3.62685 |
| H | 2.593262 | 3.118576 | -2.82158 |
| O | 1.01337 | 1.875653 | -2.4309 |
| H | 0.724728 | 2.657538 | -1.89086 |
| Cl | 1.048378 | 4.431565 | -0.82041 |
| C | -5.55504 | -1.07452 | -1.94154 |
| H | -5.76131 | -1.07426 | -3.01169 |
| H | -5.2512 | -2.08122 | -1.64213 |
| C | -4.41579 | -0.08833 | -1.64665 |
| C | -3.159 | -0.51274 | -2.45088 |
| H | -3.42549 | -0.56644 | -3.51104 |
| H | -2.8133 | -1.50239 | -2.14695 |
| C | -2.00832 | 0.469071 | -2.31644 |
| O | -2.11299 | 1.567165 | -1.80714 |
| O | -0.87382 | -0.00344 | -2.82336 |
| H | -0.16601 | 0.685414 | -2.71453 |
| C | -6.81965 | -0.73695 | -1.18063 |
| O | -6.87142 | -0.39962 | -0.02641 |
| O | -7.92282 | -0.90392 | -1.94439 |
| H | -8.6818 | -0.69328 | -1.3794 |
| C | -4.04718 | -0.15455 | -0.14495 |
| O | -3.69491 | -1.20948 | 0.360408 |
| O | -4.06936 | 1.012154 | 0.460744 |
| H | -3.69137 | 0.953365 | 1.376628 |
| O | -4.87113 | 1.181289 | -2.04708 |
| H | -4.16646 | 1.807636 | -1.82217 |
| O | -1.12495 | 4.780153 | 1.478607 |
| H | -0.41283 | 4.778469 | 0.804328 |
| H | -1.93307 | 4.704257 | 0.961517 |
| Cellobiose dimer (100) |  |  |  |
| C | 3.555713 | 2.281322 | 0.135431 |
| C | 3.839989 | 1.894009 | -1.31428 |
| C | 2.66439 | 1.063545 | -1.81588 |
| C | 1.091943 | 2.049194 | -0.40136 |
| C | 2.156914 | 2.861242 | 0.333673 |
| H | 3.927339 | 2.804829 | -1.92154 |
| H | 3.643181 | 1.362025 | 0.726391 |
| H | 0.962719 | 1.070041 | 0.076211 |
| H | 2.133301 | 3.884492 | -0.05605 |
| H | 2.542847 | 0.213983 | -1.13235 |
| O | 1.496975 | 1.873957 | -1.75119 |
| O | -0.1048 | 2.748346 | -0.37621 |
| C | -1.29746 | 1.936932 | -0.42994 |
| C | -1.50832 | 1.247838 | -1.79024 |
| H | -1.2066 | 1.165968 | 0.334391 |
| C | -2.9492 | 0.756111 | -1.9302 |
| H | -1.30127 | 1.961918 | -2.5936 |
| C | -3.94605 | 1.827544 | -1.51535 |
| H | -3.10966 | -0.0912 | -1.25205 |
| H | -3.8595 | 2.711923 | -2.1685 |
| O | -3.69145 | 2.218725 | -0.17322 |
| O | -0.6603 | 0.110647 | -1.90048 |
| H | 0.042055 | 0.247086 | -2.55631 |
| O | -3.14938 | 0.369245 | -3.2788 |
| H | -4.05807 | 0.054767 | -3.34017 |
| C | -2.43146 | 2.885495 | -0.04328 |
| H | -2.41966 | 3.769857 | -0.69612 |
| C | -2.34873 | 3.326117 | 1.41185 |
| H | -2.28906 | 2.434548 | 2.050777 |
| H | -1.44595 | 3.920247 | 1.555761 |
| O | -3.44741 | 4.150002 | 1.761144 |
| H | -4.23499 | 3.654813 | 1.508774 |
| O | -5.21621 | 1.260472 | -1.59113 |
| H | -5.86881 | 1.945425 | -1.41338 |
| O | 1.910361 | 2.863594 | 1.749398 |
| H | 1.055927 | 3.287871 | 1.891922 |
| O | 4.574781 | 3.191201 | 0.535522 |
| H | 4.457576 | 3.362718 | 1.47601 |
| O | 5.021764 | 1.11143 | -1.39737 |
| H | 5.682152 | 1.544949 | -0.84402 |
| C | 2.771553 | 0.489321 | -3.21414 |
| H | 2.687675 | 1.289769 | -3.95155 |
| H | 3.744018 | 0.002688 | -3.33314 |
| O | 1.693704 | -0.4117 | -3.4576 |
| H | 1.838138 | -1.21454 | -2.92941 |
| C | 3.556419 | -2.28069 | -0.13558 |
| C | 3.8404 | -1.89374 | 1.314315 |
| C | 2.664684 | -1.06343 | 1.815912 |
| C | 1.092648 | -2.04897 | 0.40097 |
| C | 2.157764 | -2.86086 | -0.33404 |
| H | 3.927617 | -2.80472 | 1.921355 |
| H | 3.643842 | -1.3612 | -0.72624 |
| H | 0.96348 | -1.06974 | -0.07648 |
| H | 2.134347 | -3.88412 | 0.05568 |
| H | 2.543205 | -0.21376 | 1.132503 |
| O | 1.497338 | -1.87395 | 1.750864 |
| O | -0.10409 | -2.74817 | 0.375342 |
| C | -1.29681 | -1.93688 | 0.429432 |
| C | -1.50736 | -1.24785 | 1.789833 |
| H | -1.20619 | -1.1658 | -0.33481 |
| C | -2.94829 | -0.75654 | 1.930504 |
| H | -1.2997 | -1.96189 | 2.593071 |
| C | -3.94497 | -1.82829 | 1.516074 |
| H | -3.10935 | 0.090754 | 1.252468 |
| H | -3.8577 | -2.71276 | 2.169006 |
| O | -3.69089 | -2.21911 | 0.173734 |
| O | -0.65948 | -0.11048 | 1.899607 |
| H | 0.042372 | -0.24632 | 2.556103 |
| O | -3.14787 | -0.36977 | 3.279223 |
| H | -4.05675 | -0.05592 | 3.341162 |
| C | -2.43082 | -2.88555 | 0.043067 |
| H | -2.41849 | -3.77004 | 0.695736 |
| C | -2.34869 | -3.32589 | -1.41217 |
| H | -2.28966 | -2.43421 | -2.05099 |
| H | -1.44578 | -3.91968 | -1.55669 |
| O | -3.44726 | -4.15012 | -1.76102 |
| H | -4.23489 | -3.65519 | -1.5083 |
| O | -5.21532 | -1.26176 | 1.59266 |
| H | -5.86775 | -1.94699 | 1.415324 |
| O | 1.911138 | -2.86325 | -1.74972 |
| H | 1.056275 | -3.28679 | -1.89197 |
| O | 4.575767 | -3.19027 | -0.53568 |
| H | 4.458798 | -3.36167 | -1.47621 |
| O | 5.022163 | -1.11121 | 1.397799 |
| H | 5.682692 | -1.54479 | 0.844664 |
| C | 2.771553 | -0.48942 | 3.214282 |
| H | 2.687484 | -1.28998 | 3.951555 |
| H | 3.744019 | -0.00286 | 3.33356 |
| O | 1.693711 | 0.411612 | 3.457691 |
| H | 1.838049 | 1.214406 | 2.929414 |
| Cellobiose dimer (010) |  |  |  |
| C | 0.100205 | -3.36225 | 0.457117 |
| C | -0.32957 | -3.89296 | -0.91591 |
| C | -1.81678 | -3.65042 | -1.14502 |
| C | -1.85885 | -1.84601 | 0.337443 |
| C | -0.36635 | -1.91999 | 0.656656 |
| H | 0.234368 | -3.33688 | -1.67887 |
| H | -0.3765 | -3.98271 | 1.228987 |
| H | -2.43108 | -2.50244 | 1.010946 |
| H | 0.170594 | -1.25914 | -0.03319 |
| H | -2.38707 | -4.20844 | -0.38542 |
| O | -2.06171 | -2.25483 | -0.99987 |
| O | -2.26959 | -0.52754 | 0.492483 |
| C | -3.67011 | -0.2933 | 0.726796 |
| C | -4.54569 | -0.67646 | -0.47952 |
| H | -3.99813 | -0.8997 | 1.580946 |
| C | -5.897 | 0.035078 | -0.44633 |
| H | -4.02064 | -0.36523 | -1.38833 |
| C | -5.74524 | 1.511995 | -0.11107 |
| H | -6.50934 | -0.41519 | 0.346629 |
| H | -5.15409 | 2.018922 | -0.89124 |
| O | -5.08485 | 1.656257 | 1.139156 |
| O | -4.77111 | -2.0763 | -0.47885 |
| H | -4.3802 | -2.45754 | -1.27929 |
| O | -6.49579 | -0.12396 | -1.72012 |
| H | -7.35095 | 0.317531 | -1.678 |
| C | -3.73249 | 1.195774 | 1.073117 |
| H | -3.18896 | 1.75466 | 0.30131 |
| C | -3.12337 | 1.509767 | 2.427083 |
| H | -3.699 | 1.00122 | 3.209528 |
| H | -2.08577 | 1.18939 | 2.459893 |
| O | -3.10733 | 2.92187 | 2.66236 |
| H | -4.00284 | 3.234252 | 2.481948 |
| O | -7.02766 | 2.051099 | -0.01361 |
| H | -6.95514 | 3.009379 | 0.038849 |
| O | -0.14211 | -1.51964 | 2.007716 |
| H | -0.68227 | -0.72824 | 2.133789 |
| O | 1.507612 | -3.535 | 0.488337 |
| H | 1.866951 | -3.44863 | 1.390884 |
| O | -0.06681 | -5.28222 | -1.011 |
| H | 0.835201 | -5.39694 | -0.68669 |
| C | -2.32432 | -4.04401 | -2.51776 |
| H | -1.88321 | -3.38392 | -3.26649 |
| H | -2.03199 | -5.07416 | -2.73666 |
| O | -3.7413 | -3.86126 | -2.61011 |
| H | -4.17083 | -4.61373 | -2.19042 |
| C | -0.10027 | 3.362188 | 0.457196 |
| C | 0.329657 | 3.893289 | -0.91562 |
| C | 1.816897 | 3.650918 | -1.14466 |
| C | 1.858874 | 1.846036 | 0.337314 |
| C | 0.366323 | 1.9199 | 0.656367 |
| H | -0.23417 | 3.337383 | -1.6788 |
| H | 0.376286 | 3.982458 | 1.229307 |
| H | 2.430994 | 2.502224 | 1.011159 |
| H | -0.17051 | 1.259246 | -0.03376 |
| H | 2.387073 | 4.208825 | -0.38488 |
| O | 2.061976 | 2.255324 | -0.99983 |
| O | 2.26959 | 0.52751 | 0.491948 |
| C | 3.670061 | 0.2932 | 0.72649 |
| C | 4.545829 | 0.676147 | -0.47978 |
| H | 3.998009 | 0.899717 | 1.580583 |
| C | 5.89708 | -0.03548 | -0.44635 |
| H | 4.020886 | 0.364835 | -1.38863 |
| C | 5.745192 | -1.51233 | -0.11086 |
| H | 6.509379 | 0.414887 | 0.3466 |
| H | 5.15408 | -2.01934 | -0.89101 |
| O | 5.084672 | -1.65634 | 1.139324 |
| O | 4.77148 | 2.075948 | -0.47932 |
| H | 4.379703 | 2.457286 | -1.27929 |
| O | 6.496015 | 0.123284 | -1.7201 |
| H | 7.351117 | -0.31831 | -1.67781 |
| C | 3.732332 | -1.19583 | 1.073071 |
| H | 3.188863 | -1.75484 | 0.301316 |
| C | 3.123126 | -1.50959 | 2.427051 |
| H | 3.698716 | -1.0009 | 3.209437 |
| H | 2.085528 | -1.18921 | 2.459799 |
| O | 3.107076 | -2.92165 | 2.662559 |
| H | 4.002647 | -3.23402 | 2.48243 |
| O | 7.027567 | -2.05151 | -0.01318 |
| H | 6.954974 | -3.00978 | 0.039362 |
| O | 0.141956 | 1.519144 | 2.007263 |
| H | 0.681646 | 0.727354 | 2.132958 |
| O | -1.5077 | 3.534837 | 0.488276 |
| H | -1.86709 | 3.448565 | 1.390814 |
| O | 0.066832 | 5.28257 | -1.01038 |
| H | -0.83524 | 5.397143 | -0.68619 |
| C | 2.324442 | 4.044861 | -2.51731 |
| H | 1.883217 | 3.385031 | -3.2662 |
| H | 2.032184 | 5.075105 | -2.7359 |
| O | 3.741365 | 3.861984 | -2.6098 |
| H | 4.171023 | 4.613982 | -2.18938 |

Table S4 The optimized coordinates of reactants, TS and products.

| Element | x | y | z | x | y | z | x | y | z |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OA esterify | reactants |  |  | TS |  |  | products |  |  |
| C | 3.608 | -2.336 | 0.504 | 3.251 | -2.538 | 0.181 | 3.982 | -2.339 | -0.123 |
| C | 4.347 | -1.398 | -0.450 | 4.297 | -1.445 | -0.080 | 4.938 | -1.239 | 0.321 |
| C | 3.328 | -0.472 | -1.122 | 3.612 | -0.283 | -0.817 | 4.421 | 0.115 | -0.181 |
| C | 1.819 | -0.648 | 0.735 | 1.490 | -0.747 | 0.185 | 2.129 | -0.681 | -0.140 |
| C | 2.725 | -1.593 | 1.506 | 2.022 | -1.985 | 0.917 | 2.557 | -2.062 | 0.336 |
| H | 5.064 | -0.789 | 0.133 | 4.678 | -1.077 | 0.886 | 4.977 | -1.229 | 1.427 |
| H | 2.948 | -2.977 | -0.116 | 2.928 | -2.935 | -0.796 | 3.990 | -2.361 | -1.233 |
| H | 1.139 | -1.225 | 0.076 | 1.074 | -1.061 | -0.792 | 2.071 | -0.657 | -1.248 |
| H | 3.362 | -0.984 | 2.176 | 2.318 | -1.682 | 1.932 | 2.526 | -2.055 | 1.443 |
| H | 2.613 | -1.074 | -1.715 | 3.237 | -0.642 | -1.789 | 4.425 | 0.121 | -1.288 |
| O | 2.630 | 0.207 | -0.071 | 2.535 | 0.184 | -0.027 | 3.082 | 0.296 | 0.307 |
| O | 1.105 | 0.167 | 1.599 | 0.532 | -0.145 | 0.973 | 0.913 | -0.373 | 0.435 |
| C | -0.005 | 0.831 | 0.975 | -0.342 | 0.783 | 0.338 | 0.070 | 0.577 | -0.236 |
| C | 0.273 | 2.334 | 0.863 | 0.075 | 2.236 | 0.671 | 0.397 | 2.021 | 0.186 |
| H | -0.168 | 0.428 | -0.035 | -0.308 | 0.655 | -0.752 | 0.205 | 0.490 | -1.330 |
| C | -0.973 | 3.040 | 0.343 | -1.018 | 3.225 | 0.253 | -0.727 | 2.971 | -0.211 |
| H | 0.495 | 2.726 | 1.877 | 0.219 | 2.316 | 1.759 | 0.485 | 2.031 | 1.292 |
| C | -2.197 | 2.650 | 1.173 | -2.398 | 2.762 | 0.765 | -2.098 | 2.420 | 0.180 |
| H | -1.152 | 2.708 | -0.699 | -1.040 | 3.269 | -0.848 | -0.727 | 3.065 | -1.316 |
| H | -2.075 | 3.013 | 2.214 | -2.411 | 2.849 | 1.865 | -2.163 | 2.322 | 1.289 |
| O | -2.374 | 1.225 | 1.221 | -2.679 | 1.449 | 0.361 | -2.279 | 1.113 | -0.384 |
| O | 1.349 | 2.614 | -0.014 | 1.252 | 2.585 | -0.002 | 1.594 | 2.468 | -0.427 |
| H | 2.049 | 1.970 | 0.200 | 1.900 | 1.887 | 0.189 | 2.264 | 1.786 | -0.229 |
| O | -0.778 | 4.437 | 0.428 | -0.721 | 4.482 | 0.796 | -0.508 | 4.218 | 0.420 |
| H | -1.580 | 4.845 | 0.065 | -1.481 | 5.059 | 0.642 | -1.290 | 4.752 | 0.207 |
| C | -1.244 | 0.545 | 1.820 | -1.766 | 0.486 | 0.836 | -1.357 | 0.185 | 0.149 |
| H | -1.112 | 0.939 | 2.845 | -1.752 | 0.500 | 1.937 | -1.414 | 0.170 | 1.258 |
| C | -1.595 | -0.933 | 1.902 | -2.262 | -0.880 | 0.324 | -1.741 | -1.194 | -0.356 |
| H | -1.695 | -1.341 | 0.877 | -2.035 | -0.973 | -0.748 | -1.935 | -1.173 | -1.437 |
| H | -0.763 | -1.462 | 2.388 | -1.776 | -1.684 | 0.879 | -0.973 | -1.933 | -0.101 |
| O | -2.758 | -1.152 | 2.679 | -3.647 | -1.008 | 0.437 | -2.947 | -1.609 | 0.346 |
| O | -3.312 | 3.200 | 0.550 | -3.409 | 3.579 | 0.284 | -3.051 | 3.270 | -0.333 |
| H | -4.064 | 3.151 | 1.158 | -3.643 | 3.266 | -0.601 | -3.943 | 2.858 | -0.196 |
| O | 1.916 | -2.498 | 2.233 | 1.001 | -2.940 | 0.957 | 1.653 | -3.009 | -0.202 |
| H | 2.510 | -3.200 | 2.543 | 1.387 | -3.750 | 1.316 | 2.051 | -3.879 | -0.038 |
| O | 4.502 | -3.140 | 1.258 | 3.778 | -3.577 | 0.967 | 4.348 | -3.607 | 0.396 |
| H | 5.062 | -3.596 | 0.610 | 4.612 | -3.848 | 0.563 | 5.271 | -3.749 | 0.130 |
| O | 5.026 | -2.251 | -1.372 | 5.325 | -2.056 | -0.823 | 6.208 | -1.580 | -0.234 |
| H | 5.726 | -1.742 | -1.803 | 6.027 | -1.420 | -0.995 | 6.899 | -1.130 | 0.271 |
| C | 3.887 | 0.627 | -2.012 | 4.526 | 0.932 | -1.048 | 5.215 | 1.314 | 0.321 |
| H | 4.582 | 1.251 | -1.410 | 4.775 | 1.369 | -0.071 | 5.166 | 1.330 | 1.428 |
| H | 4.466 | 0.170 | -2.831 | 5.446 | 0.614 | -1.546 | 6.270 | 1.181 | 0.027 |
| O | 2.863 | 1.387 | -2.610 | 3.949 | 1.876 | -1.899 | 4.794 | 2.531 | -0.255 |
| H | 2.293 | 1.740 | -1.903 | 3.140 | 2.225 | -1.500 | 3.938 | 2.784 | 0.127 |
| C | -3.403 | -1.206 | -2.872 | -5.543 | -2.000 | -0.660 | -5.238 | -1.428 | 0.841 |
| O | -2.772 | -1.891 | -3.634 | -6.595 | -1.632 | -0.195 | -6.013 | -0.536 | 1.107 |
| O | -4.737 | -1.034 | -2.915 | -5.213 | -3.245 | -0.899 | -5.266 | -2.645 | 1.390 |
| H | -5.050 | -1.564 | -3.672 | -5.917 | -3.861 | -0.634 | -6.015 | -2.655 | 2.018 |
| C | -2.742 | -0.421 | -1.725 | -4.389 | -1.048 | -0.993 | -4.117 | -1.260 | -0.189 |
| O | -1.535 | -0.333 | -1.656 | -3.705 | -1.056 | -1.972 | -4.328 | -0.825 | -1.295 |
| O | -3.618 | 0.094 | -0.872 | -5.046 | 0.431 | -0.609 | -5.340 | 1.872 | -0.413 |
| H | -3.117 | 0.573 | -0.153 | -5.954 | 0.204 | -0.323 | -5.679 | 1.235 | 0.242 |
| H | -3.466 | -0.635 | 2.264 | -4.338 | 0.300 | 0.206 | -4.989 | 1.281 | -1.102 |
| CA esterify | reactants |  |  | TS |  |  | products |  |  |
| C | -3.842 | -2.697 | 0.814 | -3.714 | -2.605 | -0.811 | -4.717 | -2.601 | -0.096 |
| C | -5.106 | -1.882 | 1.048 | -4.424 | -2.152 | 0.463 | -5.852 | -1.590 | -0.009 |
| C | -4.712 | -0.436 | 1.373 | -3.450 | -1.323 | 1.307 | -5.353 | -0.331 | 0.710 |
| C | -2.679 | -0.617 | 0.070 | -2.245 | -0.603 | -0.630 | -3.078 | -0.726 | -0.059 |
| C | -2.965 | -2.077 | -0.261 | -3.099 | -1.438 | -1.576 | -3.487 | -2.008 | -0.770 |
| H | -5.720 | -1.900 | 0.128 | -5.287 | -1.517 | 0.186 | -6.170 | -1.324 | -1.036 |
| H | -3.272 | -2.699 | 1.767 | -2.890 | -3.285 | -0.511 | -4.442 | -2.887 | 0.940 |
| H | -2.063 | -0.548 | 0.986 | -1.370 | -1.199 | -0.296 | -2.724 | -0.949 | 0.969 |
| H | -3.482 | -2.112 | -1.236 | -3.905 | -0.790 | -1.968 | -3.742 | -1.739 | -1.814 |
| H | -4.125 | -0.419 | 2.311 | -2.585 | -1.954 | 1.592 | -5.081 | -0.588 | 1.752 |
| O | -3.920 | 0.075 | 0.288 | -3.004 | -0.220 | 0.514 | -4.204 | 0.167 | 0.010 |
| O | -2.055 | -0.003 | -1.002 | -1.849 | 0.546 | -1.284 | -2.100 | -0.103 | -0.807 |
| C | -0.995 | 0.903 | -0.665 | -0.779 | 1.287 | -0.681 | -1.234 | 0.834 | -0.148 |
| C | -1.488 | 2.305 | -0.291 | -1.320 | 2.638 | -0.217 | -1.850 | 2.249 | -0.102 |
| H | -0.453 | 0.480 | 0.195 | -0.372 | 0.750 | 0.192 | -1.043 | 0.501 | 0.889 |
| C | -0.269 | 3.178 | 0.012 | -0.174 | 3.566 | 0.164 | -0.794 | 3.317 | 0.173 |
| H | -2.028 | 2.736 | -1.158 | -1.867 | 3.105 | -1.060 | -2.284 | 2.450 | -1.102 |
| C | 0.826 | 3.032 | -1.054 | 0.913 | 3.551 | -0.922 | 0.441 | 3.111 | -0.700 |
| H | 0.158 | 2.820 | 0.971 | 0.276 | 3.210 | 1.109 | -0.464 | 3.217 | 1.227 |
| H | 0.486 | 3.521 | -1.994 | 0.499 | 4.027 | -1.839 | 0.161 | 3.187 | -1.775 |
| O | 1.128 | 1.673 | -1.328 | 1.365 | 2.244 | -1.239 | 0.951 | 1.789 | -0.477 |
| O | -2.308 | 2.290 | 0.864 | -2.181 | 2.474 | 0.897 | -2.837 | 2.338 | 0.912 |
| H | -3.038 | 1.671 | 0.680 | -2.810 | 1.772 | 0.653 | -3.450 | 1.596 | 0.746 |
| O | -0.681 | 4.528 | 0.101 | -0.686 | 4.877 | 0.300 | -1.362 | 4.587 | -0.079 |
| H | 0.116 | 5.040 | 0.313 | 0.058 | 5.441 | 0.558 | -0.628 | 5.216 | 0.006 |
| C | -0.022 | 0.985 | -1.835 | 0.328 | 1.403 | -1.729 | 0.059 | 0.799 | -0.958 |
| H | -0.455 | 1.580 | -2.663 | -0.099 | 1.848 | -2.648 | -0.192 | 1.002 | -2.019 |
| C | 0.423 | -0.366 | -2.389 | 0.858 | -0.012 | -1.994 | 0.793 | -0.531 | -0.895 |
| H | 0.625 | -1.067 | -1.562 | 0.897 | -0.564 | -1.046 | 1.095 | -0.798 | 0.126 |
| H | -0.408 | -0.793 | -2.968 | 0.142 | -0.512 | -2.659 | 0.164 | -1.334 | -1.295 |
| O | 1.530 | -0.227 | -3.249 | 2.120 | -0.105 | -2.646 | 1.933 | -0.435 | -1.769 |
| O | 1.975 | 3.641 | -0.546 | 2.007 | 4.265 | -0.431 | 1.400 | 4.031 | -0.346 |
| H | 2.713 | 3.464 | -1.159 | 2.772 | 4.031 | -0.980 | 2.122 | 3.959 | -1.020 |
| O | -1.722 | -2.783 | -0.343 | -2.265 | -1.907 | -2.618 | -2.395 | -2.905 | -0.716 |
| H | -1.951 | -3.724 | -0.419 | -2.798 | -2.531 | -3.134 | -2.736 | -3.760 | -1.023 |
| O | -4.120 | -4.026 | 0.405 | -4.596 | -3.267 | -1.701 | -5.084 | -3.751 | -0.842 |
| H | -4.704 | -4.402 | 1.083 | -5.038 | -3.959 | -1.185 | -5.892 | -4.093 | -0.427 |
| O | -5.780 | -2.524 | 2.130 | -4.853 | -3.353 | 1.095 | -6.904 | -2.245 | 0.700 |
| H | -6.714 | -2.274 | 2.108 | -5.381 | -3.130 | 1.874 | -7.739 | -1.805 | 0.490 |
| C | -5.892 | 0.513 | 1.521 | -4.027 | -0.698 | 2.570 | -6.357 | 0.815 | 0.730 |
| H | -6.431 | 0.559 | 0.553 | -4.870 | -0.034 | 2.291 | -6.590 | 1.095 | -0.317 |
| H | -6.581 | 0.103 | 2.277 | -4.413 | -1.488 | 3.233 | -7.287 | 0.455 | 1.202 |
| O | -5.511 | 1.789 | 1.987 | -3.031 | -0.014 | 3.296 | -5.918 | 1.914 | 1.498 |
| H | -4.998 | 2.231 | 1.293 | -2.665 | 0.672 | 2.712 | -5.223 | 2.384 | 1.010 |
| C | 4.037 | 1.165 | 0.410 | 3.523 | 0.245 | -0.538 | 3.435 | 0.379 | 0.050 |
| H | 3.171 | 1.832 | 0.340 | 2.923 | 1.153 | -0.434 | 2.586 | 0.633 | 0.694 |
| H | 4.511 | 1.272 | 1.396 | 4.585 | 0.514 | -0.548 | 4.156 | 1.204 | 0.096 |
| C | 3.575 | -0.298 | 0.246 | 3.265 | -0.645 | 0.692 | 4.103 | -0.901 | 0.595 |
| C | 2.302 | -0.493 | 1.098 | 3.934 | 0.017 | 1.912 | 4.661 | -0.621 | 2.002 |
| H | 1.651 | 0.383 | 0.975 | 3.631 | 1.068 | 2.004 | 3.840 | -0.293 | 2.660 |
| H | 2.571 | -0.568 | 2.163 | 5.025 | -0.011 | 1.778 | 5.419 | 0.172 | 1.981 |
| C | 1.508 | -1.714 | 0.696 | 3.606 | -0.692 | 3.202 | 5.276 | -1.863 | 2.601 |
| O | 1.928 | -2.610 | -0.014 | 2.975 | -1.721 | 3.313 | 5.126 | -2.994 | 2.171 |
| O | 0.255 | -1.669 | 1.168 | 4.113 | -0.031 | 4.260 | 6.013 | -1.598 | 3.690 |
| H | -0.309 | -2.329 | 0.689 | 3.859 | -0.531 | 5.058 | 6.355 | -2.456 | 4.008 |
| C | 5.047 | 1.519 | -0.655 | 3.272 | -0.446 | -1.870 | 3.020 | 0.270 | -1.411 |
| O | 6.149 | 1.044 | -0.774 | 3.854 | -1.434 | -2.222 | 3.710 | 0.751 | -2.293 |
| O | 4.570 | 2.473 | -1.509 | 4.201 | 1.091 | -2.888 | 3.216 | 3.533 | -2.311 |
| C | 4.683 | -1.226 | 0.783 | 3.935 | -2.020 | 0.510 | 5.287 | -1.263 | -0.323 |
| O | 5.029 | -1.233 | 1.943 | 5.128 | -2.196 | 0.523 | 6.403 | -0.812 | -0.191 |
| O | 5.208 | -2.021 | -0.160 | 3.031 | -3.007 | 0.371 | 4.931 | -2.108 | -1.304 |
| H | 5.894 | -2.549 | 0.288 | 3.533 | -3.828 | 0.219 | 5.720 | -2.213 | -1.867 |
| O | 3.336 | -0.509 | -1.131 | 1.859 | -0.743 | 0.879 | 3.116 | -1.910 | 0.628 |
| H | 3.108 | -1.452 | -1.233 | 1.697 | -1.575 | 1.353 | 3.565 | -2.705 | 0.971 |
| H | 2.252 | 0.102 | -2.683 | 3.236 | 1.169 | -3.188 | 2.787 | 3.553 | -3.180 |
| H | 5.274 | 2.617 | -2.169 | 4.629 | 0.578 | -3.589 | 3.562 | 2.616 | -2.261 |
| Hydrolysis (non-catalyst) | reactants |  |  | TS |  |  | products |  |  |
| C | 3.771 | -2.314 | 0.055 | 2.562 | -2.727 | 0.305 | 4.692 | -2.058 | 0.942 |
| C | 4.839 | -1.232 | 0.154 | 2.990 | -1.292 | 0.560 | 4.736 | -0.538 | 0.823 |
| C | 4.314 | 0.061 | -0.484 | 2.964 | -0.421 | -0.708 | 4.429 | -0.086 | -0.614 |
| C | 2.011 | -0.568 | -0.014 | 1.377 | -1.999 | -1.692 | 3.204 | -2.102 | -1.025 |
| C | 2.463 | -1.849 | 0.673 | 1.208 | -2.695 | -0.399 | 3.373 | -2.587 | 0.408 |
| H | 5.060 | -1.053 | 1.223 | 2.277 | -0.875 | 1.293 | 3.966 | -0.121 | 1.500 |
| H | 3.600 | -2.520 | -1.022 | 3.314 | -3.231 | -0.335 | 5.515 | -2.475 | 0.326 |
| H | 1.823 | -0.745 | -1.094 | 0.883 | -2.350 | -2.601 | 4.033 | -2.481 | -1.660 |
| H | 2.617 | -1.617 | 1.742 | 0.518 | -2.019 | 0.170 | 2.535 | -2.168 | 0.998 |
| H | 4.175 | -0.099 | -1.571 | 3.959 | -0.387 | -1.170 | 5.240 | -0.416 | -1.290 |
| O | 3.062 | 0.406 | 0.127 | 2.149 | -1.002 | -1.833 | 3.194 | -0.694 | -1.040 |
| O | 0.893 | -0.094 | 0.628 | -0.495 | -0.414 | -0.301 | -0.017 | -1.179 | 0.016 |
| C | 0.052 | 0.850 | -0.073 | -1.472 | 0.567 | -0.211 | -0.489 | 0.132 | -0.264 |
| C | 0.549 | 2.290 | 0.155 | -0.876 | 1.928 | -0.607 | 0.673 | 1.092 | -0.554 |
| H | 0.091 | 0.640 | -1.159 | -2.305 | 0.369 | -0.930 | -1.161 | 0.139 | -1.146 |
| C | -0.547 | 3.307 | -0.128 | -1.945 | 2.998 | -0.597 | 0.280 | 2.554 | -0.439 |
| H | 0.826 | 2.379 | 1.225 | -0.111 | 2.223 | 0.140 | 1.449 | 0.888 | 0.207 |
| C | -1.852 | 2.874 | 0.531 | -2.589 | 3.003 | 0.801 | -0.519 | 2.788 | 0.837 |
| H | -0.730 | 3.334 | -1.221 | -2.727 | 2.737 | -1.341 | -0.374 | 2.823 | -1.290 |
| H | -1.718 | 2.827 | 1.636 | -1.829 | 3.332 | 1.539 | 0.127 | 2.577 | 1.721 |
| O | -2.253 | 1.604 | 0.055 | -3.119 | 1.742 | 1.149 | -1.651 | 1.943 | 0.876 |
| O | 1.654 | 2.591 | -0.685 | -0.240 | 1.770 | -1.882 | 1.200 | 0.894 | -1.862 |
| H | 2.290 | 1.865 | -0.547 | -0.133 | 0.796 | -1.928 | 1.836 | 0.156 | -1.806 |
| O | -0.129 | 4.565 | 0.367 | -1.377 | 4.267 | -0.862 | 1.479 | 3.316 | -0.439 |
| H | -0.888 | 5.157 | 0.246 | -2.063 | 4.913 | -0.626 | 1.215 | 4.246 | -0.360 |
| C | -1.357 | 0.576 | 0.466 | -2.143 | 0.692 | 1.168 | -1.286 | 0.569 | 0.972 |
| H | -1.291 | 0.541 | 1.572 | -1.359 | 0.927 | 1.923 | -0.633 | 0.414 | 1.859 |
| C | -1.914 | -0.766 | -0.026 | -2.844 | -0.596 | 1.563 | -2.558 | -0.250 | 1.145 |
| H | -2.466 | -0.568 | -0.960 | -3.716 | -0.736 | 0.904 | -3.274 | 0.057 | 0.367 |
| H | -1.064 | -1.434 | -0.264 | -2.136 | -1.426 | 1.374 | -2.302 | -1.313 | 0.985 |
| O | -2.798 | -1.365 | 0.889 | -3.347 | -0.604 | 2.889 | -3.206 | -0.027 | 2.387 |
| O | -2.818 | 3.818 | 0.174 | -3.617 | 3.953 | 0.871 | -0.941 | 4.117 | 0.819 |
| H | -3.642 | 3.578 | 0.624 | -4.358 | 3.583 | 0.362 | -1.445 | 4.275 | 1.632 |
| O | 1.456 | -2.845 | 0.516 | 0.666 | -3.977 | -0.618 | 3.323 | -4.004 | 0.372 |
| H | 1.900 | -3.693 | 0.694 | 0.707 | -4.425 | 0.243 | 3.539 | -4.314 | 1.266 |
| O | 4.144 | -3.507 | 0.728 | 2.372 | -3.436 | 1.511 | 4.815 | -2.488 | 2.288 |
| H | 4.996 | -3.777 | 0.351 | 3.217 | -3.408 | 1.988 | 5.630 | -2.082 | 2.625 |
| O | 5.979 | -1.753 | -0.527 | 4.303 | -1.349 | 1.107 | 6.044 | -0.155 | 1.245 |
| H | 6.765 | -1.274 | -0.230 | 4.474 | -0.523 | 1.581 | 6.032 | 0.786 | 1.468 |
| C | 5.225 | 1.266 | -0.271 | 2.426 | 0.974 | -0.406 | 4.262 | 1.434 | -0.718 |
| H | 5.330 | 1.435 | 0.820 | 1.413 | 0.827 | -0.001 | 3.537 | 1.775 | 0.045 |
| H | 6.221 | 1.025 | -0.677 | 3.076 | 1.355 | 0.411 | 5.242 | 1.878 | -0.465 |
| O | 4.783 | 2.417 | -0.954 | 2.462 | 1.837 | -1.499 | 3.904 | 1.872 | -2.001 |
| H | 4.008 | 2.781 | -0.496 | 1.525 | 1.995 | -1.766 | 2.927 | 1.864 | -2.040 |
| H | -2.215 | -1.783 | 1.557 | -2.604 | -0.413 | 3.479 | -2.637 | -0.398 | 3.077 |
| O | -0.718 | -2.487 | 2.359 | -1.154 | -2.105 | -2.079 | 1.963 | -2.489 | -1.565 |
| H | 0.006 | -2.510 | 1.699 | -1.284 | -2.947 | -1.614 | 1.822 | -3.407 | -1.273 |
| H | -0.894 | -3.424 | 2.533 | -1.002 | -1.430 | -1.321 | 0.533 | -1.499 | -0.724 |
| Hydrolysis (H+ catalyst) | reactants |  |  | TS |  |  | products |  |  |
| C | 3.783 | -2.439 | -0.370 | 3.166 | -2.102 | -1.277 | 3.763 | -1.950 | 0.020 |
| C | 4.838 | -1.411 | 0.031 | 4.328 | -1.481 | -0.493 | 4.431 | -0.569 | 0.028 |
| C | 4.344 | -0.007 | -0.357 | 3.896 | -0.242 | 0.328 | 3.308 | 0.450 | -0.207 |
| C | 2.039 | -0.689 | -0.225 | 1.594 | -0.567 | -0.279 | 1.697 | -0.834 | 0.896 |
| C | 2.433 | -2.087 | 0.228 | 1.880 | -2.019 | -0.443 | 2.618 | -2.039 | 1.023 |
| H | 4.987 | -1.464 | 1.127 | 4.672 | -2.252 | 0.222 | 4.912 | -0.390 | 1.006 |
| H | 3.699 | -2.411 | -1.476 | 3.038 | -1.522 | -2.210 | 3.337 | -2.080 | -0.997 |
| H | 1.944 | -0.639 | -1.328 | 0.600 | -0.133 | -0.490 | 1.115 | -0.892 | -0.037 |
| H | 2.507 | -2.086 | 1.331 | 2.086 | -2.455 | 0.553 | 3.046 | -2.073 | 2.043 |
| H | 4.261 | 0.059 | -1.458 | 4.511 | 0.629 | 0.075 | 2.765 | 0.135 | -1.118 |
| O | 3.038 | 0.207 | 0.233 | 2.526 | 0.254 | -0.055 | 2.412 | 0.367 | 0.923 |
| O | 0.830 | -0.343 | 0.380 | -1.223 | -0.163 | 0.123 | -1.454 | -0.654 | 0.703 |
| C | 0.040 | 0.727 | -0.215 | -2.113 | 0.762 | -0.483 | -1.793 | 0.671 | 0.107 |
| C | 0.433 | 2.091 | 0.367 | -1.467 | 2.129 | -0.634 | -0.534 | 1.531 | -0.002 |
| H | 0.228 | 0.741 | -1.302 | -2.324 | 0.353 | -1.484 | -2.169 | 0.440 | -0.899 |
| C | -0.659 | 3.125 | 0.109 | -2.449 | 3.081 | -1.298 | -0.881 | 3.010 | -0.183 |
| H | 0.524 | 1.978 | 1.469 | -1.240 | 2.529 | 0.378 | 0.026 | 1.460 | 0.952 |
| C | -2.044 | 2.569 | 0.442 | -3.764 | 3.098 | -0.518 | -2.004 | 3.442 | 0.752 |
| H | -0.657 | 3.373 | -0.970 | -2.680 | 2.714 | -2.317 | -1.228 | 3.178 | -1.218 |
| H | -2.106 | 2.340 | 1.529 | -3.587 | 3.492 | 0.507 | -1.674 | 3.355 | 1.812 |
| O | -2.301 | 1.361 | -0.291 | -4.299 | 1.775 | -0.415 | -3.134 | 2.604 | 0.550 |
| O | 1.626 | 2.568 | -0.209 | -0.267 | 1.982 | -1.379 | 0.225 | 1.014 | -1.074 |
| H | 2.307 | 1.881 | -0.092 | 0.005 | 2.882 | -1.625 | 1.042 | 1.559 | -1.171 |
| O | -0.377 | 4.244 | 0.917 | -1.826 | 4.352 | -1.329 | 0.302 | 3.758 | 0.099 |
| H | -1.051 | 4.912 | 0.714 | -2.441 | 4.964 | -1.763 | 0.076 | 4.695 | -0.025 |
| C | -1.413 | 0.324 | 0.071 | -3.436 | 0.887 | 0.285 | -2.896 | 1.279 | 0.984 |
| H | -1.488 | 0.106 | 1.157 | -3.226 | 1.272 | 1.307 | -2.547 | 1.277 | 2.040 |
| C | -1.809 | -0.936 | -0.708 | -4.181 | -0.436 | 0.435 | -4.215 | 0.510 | 0.890 |
| H | -2.493 | -0.652 | -1.521 | -5.204 | -0.202 | 0.769 | -4.626 | 0.671 | -0.120 |
| H | -0.927 | -1.426 | -1.141 | -4.245 | -0.950 | -0.541 | -4.010 | -0.571 | 1.009 |
| O | -2.416 | -1.954 | 0.114 | -3.504 | -1.252 | 1.403 | -5.180 | 0.985 | 1.797 |
| O | -2.963 | 3.527 | 0.054 | -4.646 | 3.888 | -1.237 | -2.322 | 4.745 | 0.408 |
| H | -3.832 | 3.307 | 0.423 | -5.444 | 4.033 | -0.706 | -2.983 | 5.084 | 1.032 |
| O | 1.452 | -3.055 | -0.187 | 0.778 | -2.633 | -1.061 | 1.817 | -3.204 | 0.789 |
| H | 1.938 | -3.903 | -0.251 | 1.114 | -3.466 | -1.440 | 2.430 | -3.952 | 0.682 |
| O | 4.068 | -3.751 | 0.072 | 3.352 | -3.472 | -1.546 | 4.642 | -3.009 | 0.330 |
| H | 4.921 | -4.008 | -0.313 | 4.027 | -3.561 | -2.237 | 5.372 | -2.964 | -0.308 |
| O | 6.009 | -1.786 | -0.676 | 5.321 | -1.186 | -1.454 | 5.378 | -0.611 | -1.030 |
| H | 6.789 | -1.428 | -0.229 | 6.185 | -1.120 | -1.020 | 6.083 | 0.027 | -0.855 |
| C | 5.225 | 1.135 | 0.132 | 3.846 | -0.474 | 1.842 | 3.651 | 1.912 | -0.412 |
| H | 5.260 | 1.117 | 1.238 | 3.334 | -1.433 | 2.054 | 3.946 | 2.379 | 0.543 |
| H | 6.247 | 0.961 | -0.243 | 4.888 | -0.585 | 2.184 | 4.496 | 1.983 | -1.116 |
| O | 4.790 | 2.375 | -0.381 | 3.278 | 0.599 | 2.540 | 2.533 | 2.570 | -1.006 |
| H | 4.196 | 2.801 | 0.254 | 2.337 | 0.639 | 2.305 | 2.047 | 3.119 | -0.361 |
| H | -3.277 | -1.651 | 0.444 | -4.160 | -1.831 | 1.817 | -4.990 | 0.618 | 2.672 |
| O | 0.168 | -1.133 | 2.853 | 0.648 | -0.793 | 2.000 | 0.738 | -0.795 | 1.942 |
| H | 0.643 | -1.033 | 3.692 | 0.950 | -0.959 | 2.908 | 1.178 | -0.608 | 2.788 |
| H | 0.628 | -0.599 | 2.168 | -1.013 | 0.126 | 1.029 | -0.695 | -0.584 | 1.375 |
| H | -0.272 | -2.386 | 2.126 | 0.001 | -1.556 | 1.806 | -1.037 | -3.305 | -0.872 |
| O | -0.563 | -3.093 | 1.436 | -1.020 | -2.664 | 1.287 | -0.501 | -2.561 | -0.559 |
| H | 0.203 | -3.141 | 0.761 | -0.729 | -2.753 | 0.360 | 0.291 | -2.941 | -0.096 |
| H | -1.380 | -2.701 | 0.951 | -1.873 | -2.178 | 1.215 | -1.127 | -1.443 | 0.060 |

Reference

Lu, T. & Chen, F. (2012). Quantitative Analysis of Molecular Surface Based on Improved Marching Tetrahedra Algorithm. Journal of Molecular Graphics and Modelling, 38, 314-23.