Supplementary Information

In Situ Reduced MXene/AuNPs Composite toward Enhanced Charging/Discharging and Specific Capacitance

Zixiang Zheng1, Wei Wu1, Tao Yang1,*, Enhui Wang1, Zhentao Du2, Xinmei Hou1,*, Tongxiang Liang3, Hailong Wang4

1 Beijing Advanced Innovation Center for Materials Genome Engineering, Collaborative Innovation Center of Steel Technology, University of Science and Technology Beijing, Beijing 100083, China.

2 MOE Key Laboratory of New Processing Technology for Non-ferrous Metals and Materials, Guangxi Key Laboratory of Processing for Non-ferrous Metals and Featured Materials, Guangxi University, Nanning 530004, China

3 School of Materials Science and Engineering, Jiangxi University of Science and Technology, Ganzhou 341000, China

4 School of Materials Science Engineering, Zhengzhou University, Zhengzhou 450001, China

Experiment and calculation

Before any measurements, all cells were cycled for 50 times at scan rate of 20 mV s-1. The cells were tested from scan rates of 5 mV s-1 to 100 mV s-1. GCD measurements were performed at current density arranging from 1 A g-1 to 10 A g-1. In order to evaluate the cyclic performance of the MXene/AuNPs electrodes, CV measurements were performed at a scan rate of 50 mV s-1 over 10000 cycles.

The coulombic efficiency was calculated from GCDs according to the following equation:

CE = Δtd/Δtc ×100%                             (1)

Where, Δtd and Δtc are the times of discharging and charging, respectively, and CE is coulombic efficiency.

The specific capacitance (F g-1) was calculated from CV curves according to the following equation:

Cs=∫IⅆVmvΔV                             (2)

Where, ΔV (V) is the potential window, m (g) is the mass of the active material of single electrode, V (V) is the potential versus reference electrode, I (A) is the response current, ν (mV s-1) is the scan rate, Cs (F g-1) is specific capacitance.

In the two-electrode cell, Cs values of the electrodes in the symmetric supercapacitor can be obtained by the following equation using the CV curves.

Cs=2∫IⅆVmvΔV                             (3)

where m (g) is the mass of the single film electrode and s (V s-1) is the scan rate. Volumetric capacitance was obtained by multiplying the gravimetric capacitance by density (ρ) of free-standing film on the working electrode. Volumetric capacitance Cv (F cm-3) of the electrode in the symmetric supercapacitor is calculated by the following equation:

Cv=Cs×ρ                            (4)

Power density Pv (W L-1) and volumetric energy density Ev (Wh L-1) for the symmetric supercapacitor are calculated by the following equations:

Ev=CvΔv28×3.6                             (5)

Pv=3600EvΔt                            (6)

where ∆t is the discharge time according to the CV curves (∆t = ∆V / s). Therefore, when Cs = 278 F g-1 at 5 mV s-1, Cv is calculated as 917.4 F cm-3, where ρ of MXene/AuNPs is 3.3 g/cm3. Then Ev = 917.4×0.628×3.6 = 11.47 Wh L-1, and Pv=3600×11.47120 =344.1 W L-1.

The related content of O is calculated in element sensitivity factor method, using the XPS spectrums of O 1s and Ti 2p. The results is calculated by the following equations:

ni/nj = (Ii/Si)/(Ij/Sj)                            (7)

where Ii and Ij are the photoelectron intensity of i and j elements, respectively. Si and Sj are the relative sensitivity factor (RSF) of i and j elements, respectively.

Fig. S1 (a) SEM image of Ti3C2Tx film, (b) TEM image of Ti3C2Tx, (c) HRTEM image of Ti3C2Tx, (d) SAED pattern of Ti3C2Tx.

Fig. S2 EDS analysis of MXene/AuNPs-2

Table S1. EDS results of samples

| Element | Atom % |  |  |  |
| --- | --- | --- | --- | --- |
|  | Ti3C2Tx | MXene/AuNPs-1 | MXene/AuNPs-2 | MXene/AuNPs-3 |
| Ti | 31.88 | 27.72 | 36.35 | 36.73 |
| C | 36.61 | 46.33 | 36.61 | 34.80 |
| O | 12.99 | 13.46 | 14.56 | 13.40 |
| F | 13.05 | 9.45 | 9.80 | 10.91 |
| Cl | 3.43 | 2.76 | 3.94 | 3.69 |
| Au | - | 0.28 | 0.35 | 0.47 |

Fig. S3 Conductivity characterization of the Ti3C2Tx and MXene/AuNPs-2.

Fig. S4 Specific capacitance of the supercapacitor vs scan rate.

Table S2. Comparison of electrochemical performance of different MXene-based materials as supercapacitor electrodes

| Electrode material | Electrolyte | Ev (Wh L-1) | Pv (W L-1) | Ref |
| --- | --- | --- | --- | --- |
| MXene/AuNPs | 1 M H2SO4 | 8.82 | 264.6 | This work |
| rGO//MXene | PVA/H2SO4 gel | 8.6 | 200 | [1] |
| Ni-dMXNC//MXene | 1 M KOH | 10.4 | 220 | [2] |
| Ti3C2Tx paper | 1 M KOH | 18.5 | 240 | [3] |
| MP-MX1.5 | 3 M H2SO4 | 20.7 | 184.8 | [4] |

References

[1] Couly C, Alhabeb M, Van Aken KL, et al. Asymmetric flexible MXene‐reduced graphene oxide micro‐supercapacitor, Adv. Electron. Mater. 2018, 4: 1700339.

[2] Xia QX, Fu J, Yun JM, et al. High volumetric energy density annealed-MXene-nickel oxide/MXene asymmetric supercapacitor, RSC Adv. 2017, 7: 11000-11011.

[3] Lukatskaya MR, Mashtalir O, Ren CE, et al. Cation intercalation and high volumetric capacitance of two-dimensional titanium carbide, Science 2013, 341: 1502-1505.

[4] Fan Z, Wang Y, Xie Z, et al. A nanoporous MXene film enables flexible supercapacitors with high energy storage, Nanoscale 2018, 10: 9642-9652.

* Author to whom correspondence should be addressed e-mails:

houxinmeiustb@ustb.edu.cn (X. M. Hou), yangtaoustb@ustb.edu.cn (T. Yang)