Table 1. Optimization of the reaction conditions for the synthesis of 5aa

|  |  |  | Reaction condition |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | RT (25 ͦC) |  | Reflux (80 ͦC) |  | MW |  | US |  |  |
| Entry | Catalyst | Solvent | Time (min) | Yield (%)b | Time (min) | Yield (%)b | Time (min) | Yield (%)b | Power (w) | Time (min) | Yield (%)b |
| 1 | - | EtOH | 300 | - | 300 | trace | 10 | trace | 75 | 7 | Trace |
| 2 | Fe3O4@SiO2@PTS-APG MNPs | EtOH | 300 | 25 | 300 | 29 | 10 | 32 | 75 | 7 | 37 |
| 3 | FE3O4@SiO2@PTS-APG MNPs | H2O | 300 | 10 | 300 | 19 | 10 | 24 | 75 | 7 | 28 |
| 4 | Fe3O4@SiO2@PTS-APG MNPs | Toluene | 300 | 14 | 300 | 23 | 10 | 26 | 75 | 7 | 31 |
| 5 | Fe3O4@SiO2@PTS-APG MNPs | THF | 300 | 12 | 300 | 17 | 10 | 20 | 75 | 7 | 24 |
| 6 | Fe3O4@SiO2@PTS-APG MNPs | DMF | 300 | trace | 300 | 10 | 10 | 15 | 75 | 7 | 20 |
| 7 | Fe3O4@SiO2@PTS-APG MNPs | EtOH | 360 | 25 | 360 | 45 | 12 | 34 | 80 | 7 | 39 |
| 8 | Fe3O4@SiO2@PTS-APG MNPs | EtOH | 420 | 40 | 420 | 47 | 15 | 34 | 85 | 5 | 41 |
| 9 | Fe3O4@SiO2@PTS-APG MNPs | EtOH | 480 | 41 | 480 | 50 | 17 | 35 | 90 | 5 | 41 |
| 10 | Fe3O4@SiO2@PTS-APG MNPs c | EtOH | 300 | 43 | 300 | 53 | 20 | 58 | 85 | 10 | 82 |
| 11 | Fe3O4@SiO2@PTS-APG MNPs d | EtOH | 300 | 43 | 300 | 54 | 25 | 59 | 85 | 10 | 82 |
| 12 | Fe3O4@SiO2@PTS-APG MNPs e | EtOH | 420 | 44 | 420 | 58 | 30 | 62 | 85 | 10 | 84 |
| 13 | Fe3O4@SiO2@PTS-APG MNPs c | EtOH | 480 | 45 | 480 | 60 | 35 | 73 | 85 | 12 | 86 |
| 14 | Fe3O4@SiO2@PTS-APG MNPs c | EtOH | 600 | 46 | 600 | 63 | 40 | 77 | 85 | 20 | 90 |
| a Reaction conditions: 4-(Dimethylamino)benzaldehyde (1a, 1.0 mmol), ammonium acetate (2, 1.0 mmol), ethyl acetoacetate (3, 1.0 mmol), dimedone (4, 1.0 mmol), the catalyst (5 mg) and EtOH (5.0 mL) were charged in a 25 mL Flask. b Isolated yield. c 10 mg catalyst loading. d 15 mg catalyst loading. e 20 mg catalyst loading. |  |  |  |  |  |  |  |  |  |  |  |

Table 2. Synthesis of different polyhydroquinoline derivatives using Fe3O4@SiO2@PTS-APG NPs as a catalysta

| Entry | Aldehyde 1 | Product 5 | Time (min) | Yield (%) | Obs. m.p. ( ͦC) [Lit.] |
| --- | --- | --- | --- | --- | --- |
| 1 2 3 4 5 6 7 8 9 10 | 4-(Dimethylamino)benzaldehyde 4-Clorobenzaldehyde 4-Hydroxybenzaldehyde 4-Nitrobenzaldehyde 4-Methoxybenzaldehyde 4-Methylbenzaldehyde Benzaldehyde 4-Bromobenzaldehyde 2-Chlorobenzaldehyde 2-Nitrobenzaldehyde | 5a 5b 5c 5d 5e 5f 5g 5h 5i 5j | 20 10 15 10 12 10 10 15 15 12 | 90 96 92 94 94 92 95 89 90 92 | 231-233[77] 230-232[56] 231-233[78] 241-243[79] 254-256[79] 258-260[80] 203-205[77] 252-254[81] 207-209[82] 208-210[80] |
| a Reaction conditions: aldehyde derivatives (1a-k, 1.0 mmol), ammonium acetate (2, 1.0 mmol), ethyl acetoacetate (3, 1.0 mmol), dimedone (4, 1.0 mmol), and catalyst (10 mg) in 3 mL EtOH with ultrasonic irradiation. |  |  |  |  |  |

Table 3. Optimization of the reaction conditions for the synthesis of 6aa

|  |  |  | Reaction condition |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | RT (25 ͦC) |  | Reflux (80 ͦC) |  | MW |  | US |  |  |
| Entry | Catalyst | Solvent | Time (min) | Yield (%)b | Time (min) | Yield (%)b | Time (min) | Yield (%)b | Power (w) | Time (min) | Yield (%)b |
| 1 | - | EtOH | 300 | - | 300 | trace | 10 | - | 85 | 7 | trace |
| 2 | Fe3O4@SiO2@PTS-APG MNPs | EtOH | 300 | 42 | 300 | 52 | 12 | 62 | 85 | 7 | 71 |
| 3 | Fe3O4@SiO2@PTS-APG MNPs c | EtOH | 300 | 44 | 300 | 57 | 15 | 69 | 85 | 7 | 86 |
| 4 | Fe3O4@SiO2@PTS-APG MNPs d | EtOH | 300 | 46 | 300 | 59 | 15 | 71 | 85 | 7 | 87 |
| 5 | Fe3O4@SiO2@PTS-APG MNPs e | EtOH | 300 | 48 | 300 | 61 | 15 | 74 | 85 | 7 | 89 |
| 6 | Fe3O4@SiO2@PTS-APG MNPs c | EtOH | 420 | 50 | 420 | 62 | 20 | 77 | 85 | 12 | 94 |
| 7 | Fe3O4@SiO2@PTS-APG MNPs c | EtOH | 480 | 52 | 480 | 63 | 25 | 80 | 85 | 15 | 94 |
| 8 | Fe3O4@SiO2@PTS-APG MNPs c | EtOH | 600 | 54 | 600 | 66 | 30 | 82 | 85 | 20 | 95 |
| a Reaction conditions: 4-Chlorobenzaldehyde (1a, 1.0 mmol), ammonium acetate (2, 1.0 mmol), ethyl acetoacetate (3, 2.0 mmol), the catalyst (5 mg) and EtOH (5.0 mL) were charged in a 25 mL Flask. b Isolated yield. c 10 mg catalyst loading. d 15 mg catalyst loading. e 20 mg catalyst loading. |  |  |  |  |  |  |  |  |  |  |  |

Table 4. Synthesis of different 1,4-dihydropyridine derivatives using Fe3O4@SiO2@PTS-APG NPs as a catalysta

| Entry | Aldehyde 1 | Product 6 | Time (min) | Yield (%) | Obs. m.p. ( ͦC) [Lit.] |
| --- | --- | --- | --- | --- | --- |
| 1 2 3 4 5 6 7 8 9 10 11 | 4-Clorobenzaldehyde 4-Nitrobenzaldehyde 3-Nitrobenzaldehyde Benzaldehyde 4-Methylbenzaldehyde 4-Bromobenzaldehyde 4-Hydroxybenzaldehyde 2,4-Dichlorobenzaldehyde 4-Methoxybenzaldehyde Furan-2-carbaldehyde Butyraldehyde | 6a 6b 6c 6d 6e 6f 6g 6h 6i 6j 6k | 12 10 10 12 17 12 10 20 15 12 12 | 94 90 87 88 85 90 90 87 90 88 84 | 142-144[85] 129-131[85] 162-164[86] 156-158[87] 137-139[86] 162-164[87] 200-202[88] 188-190[85] 158-160[42] 160-162[42] 121-123[89] |
| a Reaction conditions: aldehyde derivatives (1a-j, 1.0 mmol), ammonium acetate (2, 1.0 mmol), ethyl acetoacetate (3, 2.0 mmol), dimedone (4, 1.0 mmol), and catalyst (10 mg) in 3 mL EtOH with ultrasonic irradiation. |  |  |  |  |  |

Table 5. A comparison on the efficiency of the Fe3O4@SiO2@PTS-APG MNPs with other reported catalysis in the synthesis of different PHQ and 1,4-DHP derivatives

| Entry | Product | Catalyst | Reaction condition | Time | Yield (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | (5a) | Bismuth (III) bromide (2 mol%) | EtOH, RT | 2.5 h | 87 | [90] |
|  |  | Fe3O4@SiO2@PTS-APG NMPs (10 mg) | EtOH, sonication | 20 min | 90 | This work |
| 2 | (5b) | Alginic acid (17.6 mg) | EtOH, reflux | 25 min | 95 | [20] |
|  |  | V-TiO2 NPs (5.85 nm, 2 mol%) | solvent-free, 80 ͦC | 14 min | 82 | [78] |
|  |  | Fe3O4@SiO2@PTS-APG NMPs (10 mg) | EtOH, sonication | 10 min | 96 | This work |
| 3 | (6a) | AFGONs (25 mg) | EtOH, RT | 2 h | 88 | [45] |
|  |  | Sulfated polyborated (5 wt%) | solvent-free, 90 ͦC | 25 min | 92 | [91] |
|  |  | Chitosan supported vanadium oxo (5 mg) | solvent-free, 85 ͦC | 45 min | 89 | [92] |
|  |  | Fe3O4@SiO2@PTS-APG NMPs (10 mg) | EtOH, sonication | 12 min | 94 | This work |
| 4 | (6k) | TBAHS (2:1.5:1 ratio) | solvent-free, 70 ͦC | 70 min | 65 | [85] |
|  |  | Fe3O4@SiO2@PTS-APG NMPs (10 mg) | EtOH, sonication | 15 min | 90 | This work |

Table 6. Spectral characterization of compounds 5a and 6a

| Product | M.p. (◦C) | FT-IR (KBr, cm-1) |  | 1H NMR (CDCl3, 500 MHz) |
| --- | --- | --- | --- | --- |
| (5a) | 231-233 | 756 | 1606 | 0.94 (s, 3H) |
|  |  | 783 | 1704 | 1.06 (s, 3H) |
|  |  | 854 | 2956 | 1.17-1.20 (t, 3H, j= 15 Hz) |
|  |  | 1029 | 3076 | 2.09-2.22 (m, 7H) |
|  |  | 1072 | 3205 | 2.29 (s, 6H) |
|  |  | 1107 | 3282 | 4.04-4.07 (q, 2H, j= 15 Hz) |
|  |  | 1213 | - | 5.35 (s, 1H) |
|  |  | 1278 | - | 6.69 (s, 1H) |
|  |  | 1380 | - | 7.10-7.12 (d, 2H, j= 10 Hz) |
|  |  | 1490 | - | 7.32-7.34 (d, 2H, j= 10 Hz) |
| (6a) | 142-144 | 669 | 1292 | 1.22-1.24 (t, 6H, j=10 Hz) |
|  |  | 744 | 1371 | 2.34 (s, 6H) |
|  |  | 783 | 1487 | 4.09-4.11 (q, 4H, j= 10 Hz) |
|  |  | 827 | 1649 | 4.97 (s, 1H) |
|  |  | 1016 | 1697 | 5.55 (s, 1H) |
|  |  | 1051 | 2958 | 7.17-7.19 (d, 2H, j=10 Hz) |
|  |  | 1091 | 2985 | 7.21-7.22 (d, 2H, j= 10 Hz) |
|  |  | 1213 | 3355 | - |