Ultrasound-Promoted preparation and application of novel bifunctional core-shell Fe3O4@SiO2@PTS-APG as a robust catalyst in the expeditious synthesis of Hantzsch esters

Peyman Shakib, Mohammad G. Dekamin*, Ehsan Valiey and Shahriar Karami a

aPharmaceutical and Heterocyclic Compounds Research Laboratory Department of Chemistry Iran University of Science and Technology. Email:  mdekamin@iust.ac.ir

| Contents | Page |
| --- | --- |
| FT-IR spectra of the Fe3O4, Fe3O4@SiO2, Fe3O4@SiO2@CPTS and Fe3O4@SiO2@PTS-APG | 2 |
| Energy dispersive spectroscopy (EDS) pattern of Fe3O4@SiO2@PTS-APG | 3 |
| Field emission scanning electron microscopy (FESEM) images of Fe3O4@SiO2@PTS-APG | 3 |
| X-Ray diffraction pattern (XRD) of Fe3O4@SiO2@PTS-APG | 4 |
| Thermal gravimetric analysis (TGA) of the Fe3O4@SiO2@PTS-APG | 4 |
| Vibrating sample magnetometer (VSM) study of the Fe3O4@SiO2@PTS-APG | 4 |
| Reusability of Fe3O4@SiO2@PTS-APG for the synthesis of 5b (red diagram) and 6a (blue diagram) | 5 |
| FT-IR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a) | 6 |
| 1H NMR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a) | 7 |
| FT-IR spectrum of Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a) | 13 |
| 1H NMR spectrum of Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a) | 14 |

Fig. 1 FTIR spectra of the (a)Fe3O4, (b)Fe3O4@SiO2, (c) Fe3O4@SiO2@CPTS and (d) Fe3O4@SiO2@PTS-APG

Counts

Counts

Energy (kev)

Energy (kev)

Fig. 2. Energy dispersive spectroscopy (EDS) pattern of the Fe3O4@SiO2@PTS-APG

| (a) (a) | (b) (b) |
| --- | --- |
| (c) (c) | (d) (d) |

Fig. 3. FESEM images of the Fe3O4@SiO2@PTS-APG catalyst.

Fig.4. X-Ray diffraction (XRD) pattern of the Fe3O4@SiO2@PTS-APG.

Fig. 5. TGA curve of the Fe3O4@SiO2@PTS-APG catalyst.

Fig. 6. Magnetization curves of the (red) Fe3O4, (blue) Fe3O4@SiO2, (green) Fe3O4@SiO2@PTS-APG.

Fig. 7. Reusability of Fe3O4@SiO2@PTS-APG for the synthesis of 5b (red diagram) and 6a

(blue diagram).

Selected spectral data:

Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a)

M.p. 231-233 oC; FT-IR (KBr, cm-1): υ = 3282, 3205, 3076, 2956, 1704, 1606, 1490, 1380, 1278, 1213, 1107, 1072, 1029, 854, 783, 756; 1HNMR (CDCl3, 500 MHz): 0.94 (s, 3H), 1.06 (s, 3H), 1.17-1.20 (t, 3H, j=15 Hz), 2.09-2.22 (m, 7H), 2.29 (s, 6H),  4.04-4.07 (q, 2H, j=15), 5.35 (s, 1H), 6.69 (s, 1H), 7.10-7.12 (d, 2H, j=10.0 Hz), 7.32-7.34 (d, 2H, j=10.0 Hz).

Fig. 8. FT-IR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a).

Fig. 9. 1H NMR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a).

Fig. 10. Expanded 1H NMR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a).

Fig. 11. Expanded 1H NMR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a).

Fig. 12. Expanded 1H NMR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a).

Fig. 13. Expanded 1H NMR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a).

Fig. 14. Expanded 1H NMR spectrum of Ethyl 1, 4, 5, 6, 7, 8 – hexahydro – 4 - (4- N, N - dimethyaminophenyl) -7, 7-dimethyl – 5 -oxoquinoline-3-carboxylate (5a).

Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a)

M.p. 142-144 oC; FT-IR (KBr, cm-1): υ = 3355, 2985, 2958, 1697, 1649, 1487, 1371, 1292, 1213, 1091, 1051, 1016, 827, 783, 744, 669; 1H NMR: (CDCl3, 500 MHz): δ =  1.22-1.24 (t, 6H, j= 10 Hz), 2.34 (s, 6H), 4.09-4.11 (q, 4H, j= 10 Hz), 4.97 (s, 1H), 5.55 (s, 1H), 7.17-7.19 (d, 2H, j= 10 Hz), 7.21-7.22 (d, 2H, j= 10 Hz).

Fig. 15. FT-IR spectrum of Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a).

Fig. 16. 1HNMR spectrum of Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a).

Fig. 17. 1HNMR spectrum of Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a).

Fig. 18. Expanded 1H NMR spectrum of Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a).

Fig. 19. Expanded 1H NMR spectrum of Diethyl 4-(4-chlorophenyl)-2,6-dimethyl-1,4- dihydropyridine-3,5-dicarboxylate (6a).