Supplementary Data for

The Effect of Metals on Zeolite Crystallization Kinetics with Relevance to Nuclear Waste Glass Corrosion

Adam J. Mallette1, Joelle T. Reiser2, Giannis Mpourmpakis3, Radha K. Motkuri2, James J. Neeway2,*, Jeffrey D. Rimer1,*

1Department of Chemical and Biomolecular Engineering, University of Houston, Houston, TX 77204, USA

2Pacific Northwest National Laboratory, Energy and Environment Directorate, Richland, WA 99354, USA

3Department of Chemical and Petroleum Engineering, University of Pittsburgh, Pittsburgh, PA 15213, USA

*Correspondence sent to: james.neeway@pnnl.gov and jrimer@central.uh.edu

Table of Contents

Supplementary Figures	2

Supplementary Tables	10

References	15

List of Figures and Tables

Figure S1: Crystallization kinetics of zeolite GIS in a conventional synthesis at 100°C

Figure S2: PXRD patterns of conventional GIS syntheses with elemental additives

Figure S3: PXRD patterns of products generated from glass-replicating syntheses

Figure S4: PXRD reference patterns of phases observed in glass-replicating syntheses

Figure S5: Correlations between GIS produced and elements besides calcium

Figure S6: Relationship between GIS product and calcium molar ratio by class

Figure S7: Correlations between burtite produced and elements besides tin

Figure S8: Periodic table comparisons of elemental effects in conventional and eLAW syntheses

Table S1: Compositions of eLAW glasses synthesized by Crum et al. [1]

Table S2: eLAW synthesis mixtures designed to replicate glass compositions

Table S3: Mass % of oxides in select representative eLAW glass formulations

Table S4: Molar ratio of oxides in select representative eLAW synthesis mixtures

Table S5: Crystal phase outcomes of glass-replicating syntheses

# Supplementary Figures

Figure S1. Time-resolved crystallization curve of zeolite GIS via the interzeolite transformation from FAU to GIS. A synthesis mixture with a molar composition of 9 SiO2:0.5 Al2O3:5.5 Na2O:190 H2O was heated at 100°C for various times (0–7 days). Product phases were quantified from PXRD patterns as amorphous (grey), FAU (green), FAU + GIS (green/purple), and GIS with polymorph P2 (purple). Figure adapted using data from ref. [2]

Figure S2. PXRD patterns of zeolite syntheses with elemental additives reveal the effect of each element on zeolite GIS crystallization kinetics as (A) a suppressor, (B) neutral, or (C) an accelerant. Syntheses possessing a molar composition of 9 Si:1 Al:11 Na:0.2 M:190 H2O, where M corresponds to the element added, were carried out for 3 days at 100°C. Circles indicate select peaks from phases present: GIS (P1), yellow; GIS (P2), purple; FAU, green; and PHI, orange. Given that crystallization follows the Ostwald rule of stages and undergoes conversion from amorphous to FAU to GIS, suppression is indicated by an increase in the amount of either FAU or amorphous material relative to the control (Fig. S1, 3 days). Amorphous material is represented by a broad peak from ~25-35 degrees (2q).

Figure S3. PXRD patterns of solids generated from 24 glass-mimicking syntheses. Synthesis number (corresponding to Table S1) is located at the right-hand side of each pattern, with “eLAW” omitted for brevity. Vertical dashed lines indicate peak positions for GIS (P1) (red), burtite (yellow), and MgO internal standard (blue). Additional peaks correspond to LTA (eLAW-1 and eLAW-23) and FAU (eLAW-20).

Figure S4. PXRD reference patterns for crystal phases observed as products of glass-mimicking syntheses: zeolites FAU, LTA, and GIS; burtite (calcium hexahydroxystannate – Ca[Sn(OH)6]); MgO internal standard; and ZrO2.

Figure S5. Zeolite GIS product yield as a function of molar ratios in the synthesis mixture besides calcium: (A) tin, (B) zirconium, (C) boron, and (D) aluminum. The absence of a clear trend in each graph suggests that Ca is the primary factor in determining the amount of GIS product, although tin may also be significant (Fig. 6). Color coding of data points is based on the classification of each glass according to Fig. 3A, which corresponds to alteration responses for glasses with low Ca (purple triangles); high Ca, Al, Zr (blue circles); high Ca, B, and low Al (green squares); and high Ca, Al, and low Zr (red diamonds).

Figure S6. Zeolite GIS product yield as a function of the Ca/Si molar ratio in the synthesis mixture separated based on glass classification (as denoted by the color coding used in Fig. 3b), which corresponds to alteration responses for glasses with low Ca (purple triangles); high Ca, Al, Zr (blue circles); high Ca, B, and low Al (green squares); and high Ca, Al, and low Zr (red diamonds).

Figure S7. Burtite product yield as a function of molar ratios in synthesis mixtures besides tin: (A) calcium, (B) zirconium, (C) boron, and (D) aluminum. The absence of a clear trend in each graph indicates that the amount of tin is the predominant factor determining the quantity of burtite formed. Color coding of data points is based on the classification of each glass according to Fig. 3a, which corresponds to alteration responses for glasses with low Ca (purple triangles); high Ca, Al, Zr (blue circles); high Ca, B, and low Al (green squares); and high Ca, Al, and low Zr (red diamonds).

A

B

Figure S8. Comparison of elemental species’ effect on zeolite GIS crystallization rates using (A) conventional synthesis conditions and (B) synthesis conditions designed to replicate eLAW glass compositions.

# Supplementary Tables

Table S1. eLAW glass compositions (mass %) [1]

| Glass ID | Al2O3 | B2O3 | CaO | Na2O | SiO2 | ZrO2 | SnO2 | Others |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| eLAW01 | 0.0922 | 0.0659 | 0.0127 | 0.2350 | 0.3978 | 0.0159 | 0.0394 | 0.1411 |
| eLAW02 | 0.0887 | 0.1467 | 0.0523 | 0.2441 | 0.3751 | 0.0232 | 0.0116 | 0.0585 |
| eLAW03 | 0.0637 | 0.1484 | 0.0733 | 0.1501 | 0.4546 | 0.0489 | 0.0055 | 0.0555 |
| eLAW04 | 0.0892 | 0.0628 | 0.0719 | 0.1924 | 0.3568 | 0.0452 | 0.0240 | 0.1577 |
| eLAW05 | 0.0696 | 0.1697 | 0.0021 | 0.2042 | 0.4291 | 0.0179 | 0.0481 | 0.0593 |
| eLAW06 | 0.1108 | 0.1571 | 0.0174 | 0.1829 | 0.3880 | 0.0463 | 0.0079 | 0.0894 |
| eLAW07 | 0.0754 | 0.0755 | 0.0962 | 0.1541 | 0.4236 | 0.0312 | 0.0211 | 0.1228 |
| eLAW08 | 0.0634 | 0.0617 | 0.0402 | 0.2498 | 0.4263 | 0.0420 | 0.0299 | 0.0867 |
| eLAW09 | 0.1138 | 0.0994 | 0.0667 | 0.1670 | 0.3800 | 0.0163 | 0.0048 | 0.1521 |
| eLAW10 | 0.1203 | 0.1701 | 0.0989 | 0.1567 | 0.3502 | 0.0262 | 0.0070 | 0.0706 |
| eLAW11 | 0.0793 | 0.1171 | 0.0577 | 0.1928 | 0.4348 | 0.0251 | 0.0024 | 0.0909 |
| eLAW12 | 0.0875 | 0.1404 | 0.0262 | 0.1778 | 0.4152 | 0.0108 | 0.0177 | 0.1244 |
| eLAW13 | 0.0940 | 0.1215 | 0.0837 | 0.1549 | 0.4095 | 0.0195 | 0.0499 | 0.0671 |
| eLAW14 | 0.0730 | 0.0977 | 0.0488 | 0.2162 | 0.3502 | 0.0427 | 0.0410 | 0.1305 |
| eLAW15 | 0.1013 | 0.0777 | 0.0739 | 0.2338 | 0.3937 | 0.0383 | 0.0012 | 0.0802 |
| eLAW16 | 0.0608 | 0.1370 | 0.0003 | 0.1662 | 0.4600 | 0.0207 | 0.0137 | 0.1414 |
| eLAW17 | 0.0862 | 0.0655 | 0.0874 | 0.1962 | 0.4681 | 0.0136 | 0.0095 | 0.0735 |
| eLAW18 | 0.0777 | 0.1312 | 0.0162 | 0.2239 | 0.3644 | 0.0326 | 0.0055 | 0.1485 |
| eLAW19 | 0.0690 | 0.1136 | 0.0316 | 0.1591 | 0.3900 | 0.0482 | 0.0327 | 0.1558 |
| eLAW20 | 0.0724 | 0.0686 | 0.0046 | 0.2412 | 0.4465 | 0.0496 | 0.0032 | 0.1140 |
| eLAW21 | 0.0978 | 0.0959 | 0.0355 | 0.1980 | 0.4063 | 0.0329 | 0.0317 | 0.1019 |
| eLAW22 | 0.1085 | 0.0880 | 0.0465 | 0.2262 | 0.4451 | 0.0152 | 0.0203 | 0.0503 |
| eLAW23 | 0.1246 | 0.1280 | 0.0103 | 0.2472 | 0.3528 | 0.0140 | 0.0166 | 0.1065 |
| eLAW24 | 0.0617 | 0.1301 | 0.0884 | 0.1801 | 0.3616 | 0.0152 | 0.0457 | 0.1172 |

Table S2. Molar ratios in growth mixtures of glass-mimicking syntheses

| Glass ID | H2O | Al2O3 | B2O3 | CaO | Na2O | SiO2 | ZrO2 | SnO2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| eLAW01 | 1270 | 8.6 | 8.8 | 2.1 | 29.8 | 60.1 | 1.2 | 2.6 |
| eLAW02 | 1270 | 8.4 | 17.4 | 9.5 | 29.8 | 60.1 | 1.6 | 0.8 |
| eLAW03 | 1270 | 4.9 | 15.2 | 10.2 | 30.4 | 60.3 | 2.7 | 0.3 |
| eLAW04 | 1270 | 8.6 | 8.6 | 12.5 | 29.7 | 60.2 | 3.6 | 1.8 |
| eLAW05 | 1270 | 6.0 | 18.5 | 0.5 | 30.0 | 60.4 | 1.2 | 2.7 |
| eLAW06 | 1270 | 9.8 | 19.5 | 2.9 | 29.7 | 60.2 | 3.2 | 0.5 |
| eLAW07 | 1270 | 5.7 | 8.4 | 14.5 | 29.4 | 60.6 | 2.1 | 1.1 |
| eLAW08 | 1270 | 5.4 | 7.7 | 6.6 | 30.5 | 62.2 | 2.6 | 1.8 |
| eLAW09 | 1270 | 10.0 | 12.1 | 11.7 | 29.1 | 60.2 | 1.4 | 0.4 |
| eLAW10 | 1270 | 11.3 | 21.0 | 18.1 | 30.5 | 60.0 | 1.9 | 0.7 |
| eLAW11 | 1270 | 6.3 | 12.2 | 9.2 | 30.3 | 59.9 | 2.0 | 0.2 |
| eLAW12 | 1270 | 7.4 | 15.0 | 4.4 | 30.1 | 59.5 | 0.7 | 0.8 |
| eLAW13 | 1270 | 7.8 | 13.3 | 13.2 | 30.3 | 59.6 | 1.2 | 3.0 |
| eLAW14 | 1270 | 7.5 | 15.2 | 9.7 | 30.7 | 59.8 | 3.3 | 2.8 |
| eLAW15 | 1270 | 9.0 | 9.3 | 12.4 | 30.2 | 60.9 | 2.5 | 0.1 |
| eLAW16 | 1270 | 5.3 | 13.9 | 0.1 | 31.2 | 60.1 | 1.2 | 0.8 |
| eLAW17 | 1270 | 6.1 | 6.7 | 12.9 | 30.7 | 60.0 | 0.8 | 0.4 |
| eLAW18 | 1270 | 7.9 | 17.5 | 3.2 | 30.8 | 60.4 | 2.7 | 0.4 |
| eLAW19 | 1270 | 6.2 | 13.9 | 5.4 | 30.3 | 60.0 | 3.4 | 2.0 |
| eLAW20 | 1270 | 6.1 | 8.0 | 0.6 | 29.6 | 59.9 | 2.9 | 0.2 |
| eLAW21 | 1270 | 8.7 | 11.3 | 6.1 | 29.8 | 60.5 | 2.0 | 2.1 |
| eLAW22 | 1270 | 9.0 | 9.9 | 7.4 | 29.7 | 60.6 | 0.8 | 1.3 |
| eLAW23 | 1270 | 13.5 | 17.9 | 2.3 | 30.0 | 60.7 | 1.1 | 1.3 |
| eLAW24 | 1270 | 6.3 | 17.0 | 17.8 | 30.2 | 60.5 | 1.1 | 3.4 |

Color coding of data points is based on the classification of each glass according to Fig. 3A, which corresponds to alteration responses for glasses with low CaO (Type 1, purple); high CaO, Al2O3, ZrO2 (Type 2, blue); high CaO, B2O3, and low Al2O3 (Type 3, green); and high CaO, Al2O3, and low ZrO2 (Type 4, red).

Table S3. Oxide percentage of the original glass compositions of 4 select eLAW glasses [1]

| Oxide | eLAW-1 | eLAW-2 | eLAW-7 | eLAW-17 |
| --- | --- | --- | --- | --- |
| Al2O3 | 9.2% | 8.9% | 7.5% | 8.6% |
| B2O3 | 6.6% | 14.7% | 7.6% | 6.5% |
| CaO | 1.3% | 5.2% | 9.6% | 8.7% |
| Cl- | 0.4% | 0.1% | 0.3% | 0.2% |
| Cr2O3 | 0.8% | 0.3% | 0.7% | 0.4% |
| F- | 0.5% | 0.2% | 0.5% | 0.3% |
| Fe2O3 | 1.0% | 0.4% | 0.9% | 0.5% |
| K2O | 1.7% | 0.7% | 1.5% | 0.9% |
| MgO | 1.1% | 0.5% | 1.0% | 0.6% |
| Na2O | 23.5% | 24.4% | 15.4% | 19.6% |
| P2O5 | 1.2% | 0.5% | 1.0% | 0.6% |
| SiO2 | 39.8% | 37.5% | 42.4% | 46.8% |
| SnO2 | 3.9% | 1.2% | 2.1% | 0.9% |
| SO3 | 0.9% | 0.4% | 0.7% | 0.4% |
| V2O5 | 1.7% | 0.7% | 1.5% | 0.9% |
| ZnO | 4.8% | 2.0% | 4.2% | 2.5% |
| ZrO2 | 1.6% | 2.3% | 3.1% | 1.4% |

Table S4. Oxide molar ratios of 4 select zeolite synthesis mixtures designed to replicate eLAW glass compositions.

| Oxide | eLAW-1 | eLAW-2 | eLAW-7 | eLAW-17 |
| --- | --- | --- | --- | --- |
| Al2O3 | 8.2 | 8.4 | 6.3 | 6.5 |
| B2O3 | 8.6 | 20.3 | 9.2 | 7.2 |
| CaO | 2.1 | 9.0 | 14.7 | 12.1 |
| Na2O | 30.1 | 30.1 | 30.1 | 30.1 |
| SiO2 | 60.2 | 60.2 | 60.2 | 60.2 |
| SnO2 | 2.4 | 0.7 | 1.2 | 0.5 |
| ZrO2 | 1.2 | 1.8 | 2.2 | 0.9 |
| H2O | 1270 | 1270 | 1270 | 1270 |

The molar composition of H2O, Na2O, and SiO2 are held constant across all synthesis mixtures to maintain consistency in Si concentration and pH.

Color coding of rows is based on the classification of each glass according to Fig. 3A, which corresponds to alteration responses for glasses with low CaO (purple); high CaO, Al2O3, ZrO2 (blue); high CaO, B2O3, and low Al2O3 (green); and high CaO, Al2O3, and low ZrO2 (red).

Table S5. Product phases (wt. %) in glass mimicking syntheses determined using TOPAS

| Glass ID | GIS | burtite | ZrO2 | FAU | LTA | amorphous |
| --- | --- | --- | --- | --- | --- | --- |
| eLAW01 | 3% | 7% | 1% | - | 10% | 79% |
| eLAW02 | 35% | - | 2% | - | - | 63% |
| eLAW03 | 26% | - | 2% | - | - | 72% |
| eLAW04 | 22% | - | 1% | - | - | 76% |
| eLAW05 | 1% | 1% | 1% | - | - | 97% |
| eLAW06 | 18% | 2% | 3% | - | - | 77% |
| eLAW07 | 14% | - | - | - | - | 85% |
| eLAW08 | 26% | 1% | 2% | - | - | 71% |
| eLAW09 | 31% | - | 1% | - | - | 68% |
| eLAW10 | 30% | - | 1% | - | - | 69% |
| eLAW11 | 42% | - | 2% | - | - | 56% |
| eLAW12 | 38% | 1% | 2% | - | - | 59% |
| eLAW13 | 33% | 3% | 1% | - | - | 63% |
| eLAW14 | 32% | 4% | 2% | - | - | 62% |
| eLAW15 | 39% | - | 2% | - | - | 58% |
| eLAW16 | - | 1% | 1% | - | - | 99% |
| eLAW17 | 32% | - | 1% | - | - | 67% |
| eLAW18 | 41% | - | 3% | - | - | 56% |
| eLAW19 | 17% | 2% | 3% | - | - | 79% |
| eLAW20 | 9% | - | 5% | 8% | - | 78% |
| eLAW21 | 58% | - | 4% | - | - | 36% |
| eLAW22 | 30% | - | 1% | - | - | 64% |
| eLAW23 | 2% | 2% | 1% | - | 8% | 88% |
| eLAW24 | 21% | 5% | 1% | - | - | 73% |

Color coding of rows is based on the classification of each glass according to Fig. 3A, which corresponds to alteration responses for glasses with low CaO (purple); high CaO, Al2O3, ZrO2 (blue); high CaO, B2O3, and low Al2O3 (green); and high CaO, Al2O3, and low ZrO2 (red).

# References

[1] J. V. Crum, J. T. Reiser, B. P. Parruzot, J. J. Neeway, J. F. Bonnett, S. N. Kerisit, S. K. Cooley, J. V. Ryan, G. L. Smith and R. M. Asmussen, Journal of the American Ceramic Society, 2021, 104, 4145-4162.

[2] Mallette, A. J. et al. Heteroatom Manipulation of Zeolite Crystallization: Stabilizing Zn-FAU against Interzeolite Transformation. JACS Au, doi:10.1021/jacsau.2c00325 (2022).