Sb/C Composite Embedded in SiOC Buffer Matrix via Sb/MOF-Driven Dispersion Property for Novel Anode Material in Sodium-Ion Batteries

Jeongeun Park1, Minjun Kim1, Minkyeong Ku1, Dayoung Kam1, Hyung-Seok Kim2,3,4, Sang-Ok Kim3,4, Hun-Gi Jung3,4, Kyung Yoon Chung3,4, and Wonchang Choi1*

1 Department of Energy Engineering, Konkuk University, 120, Neungdong-ro, Gwangjin-gu, Seoul 05029, Republic of Korea

2 KHU-KIST Department of Converging Science and Technology, Kyung Hee University, Seoul, Republic of Korea

3 Energy Storage Research Center, Korea Institute of Science and Technology (KIST), 5, Hwarang-ro 14-gil, Seongbuk-gu, Seoul 02792, Republic of Korea

4 Division of Energy & Environment Technology, KIST School, Korea University of Science and Technology, 5, Hwarang-ro 14-gil, Seongbuk-gu, Seoul 02792, Republic of Korea

Corresponding author

Wonchang Choi / Ph. D.

Address: Department of Energy Engineering, Konkuk University, 120, Neungdong-ro,

Gwangjin-gu, Seoul 05029, Republic of Korea

Email: wcchoi@konkuk.ac.kr

Calculation for weight ratio of Sb and SiOC in Sb/C–SiOC composite from TGA analysis

It is reported that 63.91% is Sb/C–SiOC composite and 48.72% is Sb/C composite at 900 °C from TGA data. Assuming the carbons in the Sb/C and Sb/C–SiOC samples are completely vaporization via CO2 gas, and assuming the Sb content is (x), the C content is (y), and the SiOC content is (z), the equations are as follows.

Equation S1 In the Sb/C composite

93.63 x + y = 48.72

y = 0

x = 0.52

Sb content = 52%

Equation S2 In the Sb/C–SiOC composite

93.63 x + y + 65.41 z = 63.91

65.41 z = 63.91 − 48.6876

z = 0.2327

SiOC content in Sb/C–SiOC sample = 23.27%

1 − x − z = y = 0.25

C content = 25%

∴ Sb content in Sb/C–SiOC sample = 52%

Fig. S1 SEM image of (a) Pure Sb, (b) SiOC, and (c) Sb/C composites.

Fig. S2 (a) The CV curves and (b) the charge/discharge curves of Sb electrode.

Fig. S2 shows the CV curve and voltage profile of the Sb material synthesized by reducing the SbCl3 material [1]. The CV curve of the Sb material is ​​​​​​​similar in shape to the CV curve of Sb in previous studies. However, a shoulder peak (around the 1.0 V) on the right of the oxidation peak of 0.87 V and a reduction peak around 0.1 V, which appeared in the second cycle, are assumed to be caused by the presence of Sb2O3 [2]. This is because the unstable pure Sb material reacts with O2 in the air to form Sb2O3 due to the large Gibbs free energy (−605 kJ/mol) and the standard molar enthalpy of reaction (−718 kJ/mol) [3]. On the other hand, since this phenomenon is not observed in the CV curve of the synthesized Sb/C–SiOC material, it can be said that the Sb material embedded in the SiOC is more stable because contact with air is effectively blocked [4].

Fig. S3 (a) Charge/discharge voltage profiles during the initial two cycles of SiOC between 0.001 V and 3.0 V vs. Na/Na+ at 100 mA·g−1. (b) The cycle performance of the SiOC anode material at 100 mA·g−1.

Fig. S4 Nitrogen adsorption–desorption isotherm and pore size distribution (inset) of the (a) Pure Sb, (b) Sb/C composite, and (c) Sb/C–SiOC composites.

The results of BET analysis show the type IV isotherm curve of the Sb/C–SiOC material, which is mainly due to the mesoporous properties of MOFs-derived carbon, which can provide pathways for the electrolyte toward the electrode [5]. Therefore, the Sb/C–SiOC composite rich in surface pores are expected to exhibit improved rate performance by the promoted sodium ion transport [6].

Table S1 Electrochemical Performance of the Sb-Based Anode Materials for SIBs

| Sample | First charge capacity at 0.1 A·g−1 (mA·h·g−1) | First charge capacity at 0.5 A·g−1 (mA·h·g−1) | Charge capacity of 100th cycle (mA·h·g−1) | Capacity retention after 100 cycles (%) | Charge capacity of 200th cycle (mA·h·g−1) | Capacity retention after 200 cycles (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Sb | 600.0 | 516.79 | - | - | - | - |
| Sb/C | 498.61 | 467.4 | 49.21 | 10.53% | 22.72 | 4.86% |
| Sb–SiOC | 441.76 | 423.54 | 331.9 | 78.36% | 147.96 | 34.93% |
| Sb/C–SiOC | 427.87 | 403.66 | 403.95 | 100% | 403.81 | 100% |

Table S2 Fitting results of the Nyquist plots of pure nanoparticulate Sb and Sb/SiOC composite electrodes using the equivalent circuit at various cycles.

|  | Before cycle |  |  |  | After 200 cycles |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Rs (Ω) | RSEI (Ω) | Rct (Ω) |  | Rs (Ω) | RSEI (Ω) | Rct (Ω) |
| Sb–SiOC | 3.082 | 23.19 | 112.9 |  | 4.227 | 30.19 | 283.7 |
| Sb/C–SiOC | 3.232 | 25.81 | 146.3 |  | 3.699 | 18.68 | 205.1 |

References

1. Z. Yi, N. Lin, W. Zhang, W. Wang, Y. Zhu, Y. Qian (2018) Preparation of Sb nanoparticles in molten salt and their potassium storage performance and mechanism. Nanoscale 10:13236-13241. https://doi.org/10.1039/c8nr03829e.

2. X. Zhou, Z. Zhang, X. Lu, X. Lv, G. Ma, Q. Wang, Z. Lei (2017) Sb2O3 Nanoparticles Anchored on Graphene Sheets via Alcohol Dissolution-Reprecipitation Method for Excellent Lithium-Storage Properties. ACS Appl. Mater. Interfaces 9:34927-34936. https://doi.org/10.1021/acsami.7b10107.

3. X. Liu, J. Chen, M. Luo, M. Leng, Z. Xia, Y. Zhou, S. Qin, D.J. Xue, L. Lv, H. Huang, D. Niu, J. Tang (2014) Thermal evaporation and characterization of Sb2Se3 thin film for substrate Sb2Se3/CdS solar cells. ACS Appl. Mater. Interfaces 6:10687-10695. https://doi.org/10.1021/am502427s.

4. M. Kong, Y. Liu, B. Zhou, K. Yang, J. Tang, P. Zhang, W.H. Zhang (2020) Rational Design of Sb@C@TiO2 Triple-Shell Nanoboxes for High-Performance Sodium-Ion Batteries. Small 16:2001976. https://doi.org/10.1002/smll.202001976.

5. H. Lim, S. Yu, W. Choi, S.O. Kim (2021) Hierarchically Designed Nitrogen-Doped MoS2/Silicon Oxycarbide Nanoscale Heterostructure as High-Performance Sodium-Ion Battery Anode. ACS Nano 15:7409-7420. https://doi.org/10.1021/acsnano.1c00797.

6. G. Wang, X. Xiong, Z. Lin, C. Yang, Z. Lin, M. Liu (2017) Sb/C composite as a high-performance anode for sodium ion batteries. Electrochim. Acta 242:159-164. https://doi.org/10.1016/j.electacta.2017.04.164.