Supplementary Information

Superconducting Characteristics of a Carbon/N-Alkane above Room Temperature

Yasushi Kawashima*

Department of Precision Engineering, School of Engineering, Tokai University, Hiratsuka, Kanagawa 259-1292, Japan

*Corresponding author. Email: kawasima@keyaki.cc.u-tokai.ac.jp

The PDF file includes:

Supporting Information text

Figures S1 to S2

Tables S1 to S4

References

1. Temperature increase of samples owing to measurement current

1.1 Calculation model of temperature distribution in the mixture

As the thermal conductivities of the pitch-based carbon fibers and tellurium–copper are several orders of magnitude higher than those of the PTFE tube and n-heptadecane, the carbon fiber/alkane mixture and tellurium–copper screws pressurizing the mixture can be regarded as being approximately completely thermally insulated during heating. Subsequently, the temperature distributions of the carbon fiber/alkane mixture and tellurium–copper screw generated by Joule heating owing to the measurement current were calculated to examine whether the mixture and screws were in a uniform temperature state, such that they could be treated as one body. The thermal conductivity of PTFE is 0.27–0.28 W m−1 K−1 at temperatures ranging from 293 to 523 K [1]. The thermal conductivities of the pitch-based carbon fiber (Nippon Graphite Fiber Co., Ltd., XN-100-25Z) and tellurium–copper at room temperature are 900 and 355 W m−1 K−1 (see Table S1), respectively. Because the thermal conductivities of the carbon fiber and tellurium–copper are approximately three orders of magnitude higher than that of PTFE, the heat flow in the radial direction of the PTFE tube can be ignored relative to that in the axial direction. Thus, the thermal conduction problem in the carbon fiber/alkane mixture and tellurium–copper screw can be treated as a one-dimensional problem in the axial direction of a PTFE tube.

As shown in Figs. 2–3, the electrical resistance value of the sample from the start of heating to just before the sudden increase in resistance was 0.8046 to 81.6232 Ω. As the shape of the carbon fiber/alkane mixture is 0.9 mm in diameter and 20 mm in length, the resistance can be converted to resistivity values of 2.5593 × 10−3 to 2.5963 × 10−1 Ω cm. The pitch-based carbon fiber (Nippon Graphite Fiber Co., Ltd., XN-100-25Z) has an electrical resistivity of 1.5 × 10−4 Ω cm, and the electrical conductivity of all alkanes is very low; for example, n-dodecane at 24 °C has an electrical conductivity of 1.10 × 10−14 S cm‒1 [2]. This indicates that the electrical resistance of the carbon fiber/alkane mixture depends primarily on the resistance of the carbon fiber. Furthermore, in carbon fiber/insulator mixtures, the electrical conductivity appears owing to the formation of carbon fiber networks arising from the contact between the fibers [3]. The contact state between the carbon fibers strongly pushed by the two tellurium–copper screws is considered to be hardly changed by heating, and the temperature characteristic of the electrical resistance of the carbon fiber/alkane mixture should be the same as that of the carbon fiber.

The temperature dependence of the electrical resistance of carbon fibers has the properties of sp2 carbon, and the electrical resistance should decrease with increasing temperature. In fact, the temperature coefficient of the electrical resistance of carbon fiber composites has been shown to be negative in the range of 293–413 K [4]. However, according to Figs. 2–3, contrary to this prediction, the resistance of the mixture increases with increasing temperature. This indicates that the contact resistance between the tellurium-copper screw and the carbon fiber/alkane mixture increased as the temperature increased. In fact, the average coefficient of thermal expansion of the PTFE tubes at temperatures between 298 and 473 K is 151 × 10−6 K−1 [5], whereas the mean transverse and longitudinal coefficients of thermal expansion of the carbon fibers at temperatures between 300 and 2500 K range from 5 × 10−6 K−1 to 10 × 10−6 K−1 and from 1.6 × 10−6 K−1 to 2.1 × 10−6 K−1, respectively [6]. The coefficient of thermal expansion of the PTFE tube is approximately two orders of magnitude higher than that of the carbon fiber. Thus, the increase in the electrical resistance of the sample owing to the temperature increase is caused by the increase in the contact resistance between the mixture and tellurium–copper screw, which is in turn due to the thermal expansion of PTFE. Hence, it can be assumed that most of the Joule heat generated in the sample owing to the resistance measurement current was caused by the contact resistance between the carbon fiber/alkane mixture and tellurium–copper screws.

Based on the above discussion, to calculate the axial temperature distribution of the carbon fiber/alkane mixture and tellurium–copper screw packed in the PTFE tube, we propose the one-dimensional calculation model shown in Fig. S1. In Fig. S1, the horizontal axis represents the axial coordinates of the PTFE tube, and the vertical axis represents the temperature. In Fig. S1, points b and d show the boundary between the carbon fiber/alkane mixture and tellurium–copper screw, points a and e are the boundaries between the tellurium and copper screw and n-heptadecane liquid, and point c is the center of the carbon fiber/alkane mixture. As the model in Fig. S1 is symmetric with respect to c, the temperature distribution can be considered symmetrical. Here, the carbon fiber/alkane mixture is regarded as a cylinder with a diameter of 0.9 mm and length of 20 mm, and the M1.2 tellurium–copper screw is regarded as a cylinder with a diameter of 0.9 mm and length of 6 mm. Considering that all the heat generation is due to the contact resistance, it can be assumed that the heat generation source is at the interface between the mixture and the tellurium–copper screw electrode. As shown in Fig. S1, the heat q is generated per unit time and unit area at boundary surfaces b and d. Interfaces b and d are assumed to be planar heat sources that emit a heat flow of q/2 per unit time and unit area evenly on the mixture side and tellurium–copper side. Additionally, Fig. S1 shows the temperature distribution immediately after heat generation occurs at the boundary surface and how the heat generated at the boundary surface propagates separately on the carbon fiber/alkane mixture side and the tellurium–copper screw side.

Fig. S1. One-dimensional calculation model. The vertical axis represents temperature, and the horizontal axis represents the X axis. a-b and d-e represent the tellurium–copper screw portions, b-d represents the carbon fiber/alkane mixture, and b and d represent the interface between the carbon fiber/alkane mixture and tellurium–copper screw. Point c is the center of the carbon fiber/alkane mixture, b-d. In this figure, it is assumed that the Joule heat in the sample is equally generated at interfaces b and d, and that the same amount of heat flows to the tellurium–copper screw side and carbon fiber/alkane mixture side.

If the resistance of the carbon fiber/alkane mixture is almost zero until it increases suddenly, then it is considered that almost all of the measured resistances are owing to the contact resistance; as such, the model in Fig. S1 can be applied almost precisely.

1.2 Heat conduction equation and its solution

Because the resistance measurement current is constant, the calorific value Q(t) per unit time in the mixture can be obtained from the measured resistance. If the calorific value due to the contact resistance at the boundary surface b is q, it is expressed by the following equation (see Fig. S1):

k2∂T∂xx→b-0-k1∂T∂xx→b+0=q.				(S1)

Here, k1 and k2 are the thermal conductivities of the carbon fiber/alkane mixture and tellurium–copper, respectively. As shown in Fig. S1, the heat generated at the interface between the tellurium–copper and mixture was conducted separately on the tellurium–copper and mixture sides. At interface b, the left side is tellurium–copper and the right side is the mixture. Assuming that the same amount of heat is transferred to the left and right at the boundary surface per unit time, the boundary conditions are satisfied at the boundary surface between the mixture and tellurium–copper screw as follows:

-k1∂T∂xx→b+0=q2.				(S2)

Additionally, the cylindrical carbon fiber/alkane mixture (diameter: d1 = 0.9 mm, length: 2L1 = 20 mm) is sandwiched between the same tellurium–copper screws at both ends and the same boundary conditions are applied to the left and right ends of the mixture, such that the temperature distribution in the mixture can be assumed to be symmetrical with respect to the center c of the mixture. Thus, q at each time at the interface was half of Q(t) at each time in the mixture. That is, q=12Q. As the calorific value in the mixture is equal at the left and right interfaces, the heat does not move to the right or left side of c in the mixture. Therefore, the boundary conditions hold at point c as follows:

∂T∂xx = L1=0.				(S3)

Here, point b is set to the origin, x = 0; subsequently, the coordinate of point c is x = L1. The boundary condition at point b can be expressed by Eq. (S4) based on Eq. (S2):

-k1∂T∂xx = 0=q2.				(S4)

From symmetry, the time change of the temperature distribution of the mixture can be obtained by solving the heat conduction equation between one end and the center of the mixture. Assuming that the temperature distribution of the mixture was constant and uniform at t = 0, the heat conduction equation and initial conditions were as follows:

∂2Tx,t∂x2=1α1∂Tx,t∂t, 0≤x≤L1, t>0,			(S5)

and

T=Ti, 0≤x≤L1, t=0.				(S6)

In Eqs. (S5) and (S6), α1 and Ti are the thermal diffusivity and the initial temperature, respectively. α1 is given as follows:

α1=k1ρ1cp1,				(S7)

where k1, ρ1, and cp1 are the thermal conductivity, specific gravity, and specific heat of the carbon-fiber/alkane mixture, respectively.

When the heat conduction equation (Eq. (S5)) is solved under the boundary conditions (Eq. (S3) and Eq. (S4)) and initial condition (Eq. (S6)), Tx, t, is given as follows:

Tx, t=Ti+qL12k1α1tL12+12xL12-xL1+13-2n = 1∞1nπ2cosnπxL1exp-n2π2α1L12t.	(S8)

When Eq. (S8) is transformed using Eq. (S7), Tx, t can be expressed as

Tx, t=Ti+q2ρ1cp1L1t+qL12k112xL12-xL1+13-2n = 1∞1nπ2cosnπxL1exp-n2π2α1L12t. (S9)

The difference between Tx, t and TL1, t is given as follows:

Tx, t-TL1, t=qL12k112xL12-xL1+12-2n = 1∞1nπ2cosnπxL1—exp-n2π2α1L12t.	(S10)

Eq. (S10) expresses the time change in the temperature distribution when the temperature at x = L1 is set to 0.

Next, a formula is obtained to calculate the temperature distribution of the tellurium–copper screw portion. Let point d be the origin of x = 0. We solved the heat conduction equation for the region to the right of point d (tellurium–copper). The thermal conductivity of liquid n-heptadecane is 0.146 W m−1 K−1 at 303.35 K [7] and decreases with increasing temperature. Because the thermal conductivity of liquid n-heptadecane is very small, it can be assumed that the boundary surface e is in a thermally insulated state. Hence, the boundary conditions at interface d between the tellurium–copper screw and mixture, and at the boundary surface e between the tellurium–copper screw and liquid n-heptadecane, are as follows (see Fig. S1):

∂T∂xx = L2=0,			(S11)

and

-k2∂T∂xx = 0=q2.				(S12)

Here, point d is set to the origin x = 0, and the coordinate of point e is x = L2. For the initial conditions, assuming that the temperature distribution of the tellurium–copper screw was constant and uniform, the heat conduction equation and initial conditions were as follows:

∂2Tx,t∂x2=1α2∂Tx,t∂t, 0≤x≤L2, t>0,			(S13)

and

T=Ti, 0≤x≤L2, t=0.				(S14)

Here, α2 and Ti are the thermal diffusivity and initial temperature of tellurium–copper, respectively. α2 is given as follows:

α2=k2ρ2cp2,				(S15)

where ρ2, cp2, and k2 are the specific gravity, specific heat, and thermal conductivity of tellurium–copper, respectively.

When the heat conduction Eq. (S13) is solved under the boundary conditions (S11) and (S12) and initial condition (S14), the temperature distribution function Tx, t, in the tellurium–copper screw is given as follows:

Tx, t=Ti+qL22k2α2tL22+12xL22-xL2+13-2n = 1∞1nπ2cosnπxL2exp-n2π2α2L22t.	(S16)

The difference between Tx, t and Tx, L2 is given as follows:

Tx, t-TL2, t=qL22k212xL22-xL2+12-2n = 1∞1nπ2cosnπxL2--1nexp-n2π2α2L22t. (S17)

1.3 Temperature distribution in the mixture and screws

First, using Eq. (S10), the time change of the temperature distribution in the carbon fiber/alkane mixture (in which the temperature of the c-plane was set to zero) was calculated. To calculate the temperature distribution, it is necessary to obtain the density ρ1, specific heat cp1, and thermal conductivity k1 of the carbon-fiber/alkane mixture. ρ1 and cp1 can be obtained from the densities and specific heats of the carbon fibers and alkanes, respectively, and the volume fraction of carbon fibers as follows:

ρ1=Vfibρfib+(1-Vfib)ρalk,			(S18)

and

cp1=Vfibρfibcp,fib+1-Vfibρalkcp, alkρ1,		(S19)

respectively. Here, ρfib and ρalk are the densities of the carbon fiber and alkanes, respectively; cp,fib and cp, alk are the specific heats of the carbon fiber and alkanes, respectively; and Vfib is the volume fraction of the carbon fiber. Therefore, the density and specific heat of the carbon fiber/alkane mixture can be obtained from the densities and specific heats of the carbon fiber and alkane and the volume fraction of the carbon fiber. However, it is difficult to determine the thermal conductivity definitively of the carbon fiber/alkane mixture from the data obtained thus far.

1.3.1 Thermal conductivity of carbon fiber/alkane mixture

The relationship between the electrical conductivity of the carbon fiber/polymer mixture and the volume fraction of carbon fibers in the mixture has been extensively studied [3, 8–10]. Based on those studies, when the volume fraction of the carbon fiber is small, the electrical conductivity of the mixture is approximately equal to the value of the electrical conductivity of the polymer of the insulator. However, when the volume fraction of the fiber exceeded a certain value (percolation threshold), a network of fibers began to form, and the electrical conductivity of the mixture increased rapidly (several orders of magnitude) with an increase in the volume fraction of the fiber. When the volume fraction exceeded a certain value, the electrical conductivity reached a plateau and did not change significantly.

In the case of thermal conductivity, the same phenomenon as in the case of electrical conductivity was observed. When the volume fraction of the fiber exceeded the percolation threshold, the formation of the fiber network caused the thermal conductivity of the mixture to increase rapidly. When the volume fraction of the fiber exceeded a certain value, the thermal conductivity reached a plateau, and there was almost no increase in the thermal conductivity.

Demain and Issi investigated the relationship between the volume fraction of fibers and the electrical resistivity and thermal conductivity of pitch-based carbon fiber/polycarbonate mixtures [11]. Their study showed that both the electrical and in-plane thermal conductivities of the mixture increased sharply when the volume fraction of the fiber exceeded the percolation threshold and changed little when the volume fraction exceeded a certain value. Furthermore, it has been shown that when the volume fraction of the carbon fiber reaches 0.2 [11], the thermal conductivity does not change as the volume fraction of the fiber increases further. The pitch-based carbon fiber used in their study was P55 (Amoco), which has a thermal conductivity of 100 W m−1 K−1, and the thermal conductivity of the polycarbonate was 0.20 W m−1 K−1 [11]. In their study, the thermal conductivity was shown to change little when the volume fraction of the fiber exceeded 0.2. The thermal conductivity (Kc) of the mixture in the carbon fiber direction in the absence of pores is given as follows [11]:

Kc = Km + (Kfα – Km)Vfib,				(S20)

where K is the thermal conductivity, Vfib is the volume fraction of the fiber, and the subscripts c, m, and f represent the composite material (carbon fiber/polycarbonate mixture), matrix (polycarbonate), and fiber (carbon fiber), respectively. α is an efficiency factor that accounts for the fiber orientation and partial reinforcement.

The carbon fibers (P55, Amoco) used by Demain and Issi were the same pitch-based fibers as the carbon fibers (Nippon Graphite Fiber Co., Ltd., XN-100-25Z, no sizing agent, true density: 2.2 g cm−3, resistivity: 1.5 × 10−4 Ω cm, thermal conductivity: 900 W m−1 K−1) used in our experiments. The density, resistivity, and thermal conductivity of P55 were 2.0 g cm‒3, 10−3 Ω cm, and 100 W m−1 K−1, respectively, and there was no significant difference in density between P55 and XN-100-25Z. However, the resistivity and thermal conductivity of XN-100-25Z were 1/15 and nine times those of P55, respectively. Although there were some differences in the resistivity and thermal conductivity between P55 and XN-100-25Z, the thermal conductivity of the carbon fiber/alkane mixture was estimated with reference to the results obtained for this pitch-based carbon fiber/polycarbonate mixture.

The pitch-based carbon fiber packed in the PTFE tube ranges in mass from 0.013 to 0.018 g and the density of the carbon fiber is 2.22 × 10−3 g mm‒3; thus, the volume of the inserted graphite fiber (Vfib) is 5.856 to 8.108 mm3. As the volume of the sample chamber of the PTFE tube (Vtube) is πd12L1/2, d1 = 0.9 mm and 2L1 = 20 mm, and Vtube = 12.723 mm3. Therefore, the volume fraction of carbon fiber in the carbon fiber/alkane mixture inserted into the sample chamber of the PTFE tube ranged from 0.460 to 0.637. As the volume fraction of the fiber exceeds 0.2 in all samples, it can be assumed that their thermal conductivities reached a plateau. Thus, the thermal conductivity of the carbon-fiber/alkane mixture can be obtained using Eq. (S20).

The thermal conductivities of n-octane, n-nonane, n-decane, n-dodecane, n-tridecane, and n-hexadecane were ~0.15 W m−1 K−1 at room temperature [12]. The thermal conductivity of the pitch-based carbon fibers used in our study was 900 W m−1 K−1. Thus, we set Km = 0.15 W m−1 K−1 and Kf = 900 W m−1 K−1 in Eq. (S20). Furthermore, as in the literature, assuming that the thermal conductivity becomes saturated when the volume fraction of the pitch-carbon fiber reaches 0.2 and while setting α = 0.48 and Vfib = 0.2, the thermal conductivity Kc (= k1) of the carbon fiber/alkane mixture inserted into the PTFE tube is estimated as 86.5 W m−1 K−1 = 0.0865 W mm−1 K−1 from Eq. (S20). This value is approximately one-tenth of the thermal conductivity of the pitch-based carbon fiber (900 W m−1 K−1). This ratio is almost equal to the ratio of the thermal conductivity of the polycarbonate/pitch-based carbon fiber P55 (Amoco) composite material (10 W m−1 K−1) to that of carbon fiber P55 (100 W m−1 K−1).

The polycarbonate liquefies at approximately 240 °C. In the Demain and Issi experiments, a pitch-based carbon fiber/polycarbonate mixture was heated and pressurized at 270 °C. The viscosity of polycarbonate at 280 °C is ~1000 Pa⸳s [13], whereas that of n-hexadecane is 3.486 mPa⸳s at room temperature [14], and it decreases with increasing temperature. The lower the viscosity, the easier it is for the fibers to move and form a network. The viscosity of hexadecane is approximately five orders of magnitude lower than that of molten polycarbonate. Thus, it can be estimated that the thermal conductivity of carbon fiber/hexadecane, as estimated from the thermal conductivity obtained for carbon fiber/polycarbonate (86.5 W m−1 K−1), is considerably smaller than the actual value. Therefore, the actual temperature distribution reached a steady state faster than the temperature distribution obtained using this thermal conductivity value and was uniform. In other words, the actual difference between the maximum and minimum temperatures in the mixture was considered smaller than that calculated using the thermal conductivity, as estimated from the Demain and Issi experiments.

1.3.2 Calculation of temperature distribution of the mixture and screw

The greater the calorific value of the sample, the greater the temperature difference between the maximum and minimum temperatures in the sample, that is, the lower the uniformity of the temperature. In the relationship diagram between the temperature and resistance shown in Figs. 2–3, the maximum resistance (Rmax) from the start of heating to the temperature at which the resistance suddenly increases is 81.62 Ω in the case of hexadecane (Fig. 3f). The largest calorific value Qmax per unit time in all the samples was obtained by multiplying the maximum resistance (Rmax) by the square of the measured current i (Qmax=Rmaxi2). In the experiment conducted in this study, the largest amount of heat was generated in the case of hexadecane. When the measurement current i was 10 mA, the maximum calorific value was 8.162 × 10−3 W. Thus, the temperature distribution in the hexadecane sample shown in Fig. 3f was calculated. Because the amount of heat generated per unit time on the two heat-generating surfaces b and d are equal to symmetry, q/2 on the right side of Eq. (S4) is given as follows:

q2=Qmax4÷πd124=3.207 × 10-3 W mm−2,			(S21)

where d1 = 0.9 mm.

In the case of n-hexadecane, which generates the maximum calorific value (Fig. 3f), the temperature distribution of the carbon fiber/n-hexadecane mixture was calculated using the physical properties at room temperature according to Eq. (S10).

The values of the density (ρfib) and specific heat (cp, fib) of graphite fiber at room temperature are 2.22 g cm‒3 and 0.7132 J g−1 K−1 [15], respectively, and the values of the density (ρalk) and specific heat (cp, alk) of n-hexadecane at room temperature are 0.772 g cm‒3 Ref. [16] and 2.142 J g−1 K−1 [17], respectively. The ρ1 and cp1 of the carbon fiber/n-hexadecane mixture can be obtained from the densities and specific heats of the carbon fiber and n-hexadecane and the volume fraction of the fiber (Vfib) using Eqs. (S18) and (S19). From Eqs. (S18) and (S19), when the volume fraction of carbon fiber in the mixture ranged from 0.460 to 0.637, ρ1cp1 ranged from 1.609 to 1.621 J cm−3 K−1. Hence, there was no significant difference in ρ1cp1 between the Vfib values of 0.460 and 0.637. Therefore, the calculation proceeded with ρ1cp1 = 1.615 × 10–3 J mm−3 K−1. Substituting q/2 = 3.207 × 10−3 W mm−2, k1 = 0.0865 W mm−1 K−1, L1 = 10 mm, and α1 = 53.6 mm2 s−1 in Eq. (S10), the time change T(x, t) − T(L1, t) of the temperature distribution, at which the temperature at x = L1 (point c) is set as 0, was calculated. The results are presented in Fig. S2a. The steady state is reached 0.8 s after heating, the highest temperature positions in the carbon fiber/n-hexadecane mixture are across the heating surfaces b and d, and the lowest temperature positions are in the center c of the mixture. The difference between the maximum and minimum temperatures of the mixture in the steady state was 0.185 K, and the temperature distribution in the carbon fiber/n-hexadecane mixture could be regarded as almost uniform. As mentioned in Section 1.3.1, the thermal conductivity of the carbon fiber/alkane mixture is considered significantly higher than that estimated from experiments on the carbon fiber/polycarbonate mixture; therefore, the temperature distribution will reach a steady state earlier than 0.8 s. It is estimated that the difference between the maximum and minimum temperatures of the mixture in steady state will be considerably less than 0.185 K.

Next, in the case of n-hexadecane, which generated the maximum amount of heat (Fig. 3f), the temperature distribution of the tellurium–copper screw, in which the temperature at x = L2 (boundary surface e) was set to 0, was calculated using Eq. (S17). Table S1 shows the density, specific heat, thermal conductivity, and thermal diffusivity of tellurium–copper at room temperature [18].

Table S1. Density, specific heat, thermal conductivity, and thermal diffusivity of tellurium–copper.

| Density (ρ2) | Specific heat (cp2) | Thermal conductivity (k2) | Thermal diffusivity (α2) |
| --- | --- | --- | --- |
| 8.94 × 10−3 g mm−3 | 0.385 J g−1 K−1 | 0.355 W mm−1 K−1 | 103.14 mm2 s−1 |

By substituting q/2 = 3.207 × 10−3 W mm−2, k2 = 0.355 W mm−1 K−1, L2 = 6 mm, and α2 = 103.14 mm2 s−1 in Eq. (S17), T(x, t) − T(L2, t) of the temperature distribution, in which the temperature at x = L2 (point e) is set as 0, was calculated. In this way, the time change of the temperature distribution in the tellurium–copper part in the case of n-hexadecane, where the largest amount of heat was generated on the heat-generating surface during the experiment (Fig. 3f), was calculated. As shown in Fig. S2b, the steady state is reached 0.15 s after heating, the highest temperature position in the tellurium–copper screw is across the heat-generating surface d, and the lowest temperature position is across the contact surface e between the n-heptadecane liquid and tellurium–copper screw. Because the difference between the maximum and minimum temperatures of the tellurium–copper screw is 0.027 K, the temperature distribution of the tellurium–copper screw can be regarded as uniform. Furthermore, the temperature of the tellurium–copper screw can be considered approximately equal to the temperature of the contact surface between the carbon fiber/n-hexadecane mixture and the tellurium–copper screw. From the above calculations, the carbon fiber/n-alkane mixture and tellurium–copper screw can be regarded as one body, and can be assumed to increase in temperature while maintaining a nearly uniform temperature distribution.

Fig. S2. Time changes of temperature distribution of carbon fiber/n-alkane mixture and tellurium–copper screw: a carbon fiber/n-alkane mixture and b tellurium–copper screw.

1.4 Temperature increase of the mixture owing to measurement current

From the calculation results in Section 1.3.2, the carbon fiber/n-alkane mixture and tellurium–copper screw can be treated as a single body. Furthermore, the thermal conductivities of PTFE [1] and heptadecane [7] were approximately three orders of magnitude lower than those of the carbon fiber/alkane mixture and tellurium–copper. Thus, it was possible to determine the temperature increase of the carbon fiber/alkane mixture owing to the resistance measurement currents in the experiments, assuming that the mixture and tellurium–copper screws were heated in a completely thermally insulated state. Thus, by assuming that all the Joule heat generated in the sample from the start of heating the sample to the temperature at which the resistance increased suddenly was used only to raise the temperature of the carbon fiber/n-alkane mixture and tellurium–copper screw, the temperature increase of the carbon fiber/n-alkane mixture could be easily calculated.

To determine the heat capacity of the carbon fiber/n-alkane mixture, we first obtained the temperature when the measured resistance was equal to the average resistance from the start of heating to the sudden increase in resistance (i.e., Tm) from the temperature-resistance curves obtained by each measurement based on the measurement data from Figs. 2–3. In the cases shown in Figs. 2a–e and 3a–h, ρalk and cp,alk of each n-alkane and ρfib and cp,fib of the carbon fiber at Tm were determined from the equations for the relationship between the density and temperature, and that between the specific heat and temperature for each n-alkane and carbon fiber. The relationship between the density and temperature for each n-alkane used is provided in Ref. [16], where the density of the n-alkane is expressed as a function of the carbon number of the alkane and temperature. As an equation for the relationship between the specific heat and temperature of each alkane, an equation expressing the constant-pressure specific heat as a function of the carbon number of the alkane and temperature was used, as shown in Ref. [17]. To obtain an equation for the relationship between the density and temperature of the carbon fiber, a linear function showing the relationship between density and temperature was obtained from the density data measured at each temperature of isotropic graphite G348 in Ref. [19] using the least squares method. This function was transformed so that it became 2.22 g cm‒3 at room temperature (20 °C, 293.15 K). The reason for the conversion was that the density of the carbon fiber used (XN-100-25Z) was 2.22 g cm‒3 at room temperature. The formula for the relationship between the density of the carbon fiber and temperature obtained in this way is as follows:

ρfib = 2.230254 − 0.00003497986 × T(K).			(S22)

The polynomial expression for absolute temperature T given in Ref. [15] was used to express the relationship between the specific heat at constant pressure and the temperature of the carbon fiber. Table S2 lists ρalk, cp,alk, ρfib, and cp,fib at Tm.

Table S2. Tm, density, ρalk, specific heat at a constant pressure of the alkane at Tm, cp,alk, and density, ρfib, and specific heat at a constant pressure of carbon fiber at Tm, cp,fib.

| Sample name | Tm (K) | cp, alk ( J g-1 K-1) | ρ alk (g mm-3) | cp, fib (J g-1 K-1) | ρ fib (g mm-3) |
| --- | --- | --- | --- | --- | --- |
| n-octane |  |  |  |  |  |
| 2a | 323.09 | 2.3105 | 0.6750 × 10−3 | 0.7801 | 2.2190 × 10−3 |
| 2b | 342.20 | 2.3886 | 0.6588 × 10−3 | 0.8356 | 2.2183 × 10−3 |
| 2c | 335.29 | 2.3603 | 0.6647 × 10−3 | 0.8156 | 2.2185 × 10−3 |
| n-nonane |  |  |  |  |  |
| 2d | 340.78 | 2.3694 | 0.6759 × 10−3 | 0.8315 | 2.2183 × 10−3 |
| 2e | 357.71 | 2.4375 | 0.6620 × 10−3 | 0.8798 | 2.2177 × 10−3 |
| n-decane |  |  |  |  |  |
| 3a | 347.30 | 2.3846 | 0.6844 × 10−3 | 0.8502 | 2.2181 × 10−3 |
| 3b | 369.85 | 2.4741 | 0.6665 × 10−3 | 0.9138 | 2.2173 × 10−3 |
| n-dodecane |  |  |  |  |  |
| 3c | 356.60 | 2.4041 | 0.6999 × 10−3 | 0.8767 | 2.2178 × 10−3 |
| 3d | 371.07 | 2.4604 | 0.6892 × 10−3 | 0.9172 | 2.2173 × 10−3 |
| n-tridecane |  |  |  |  |  |
| 3e | 372.84 | 2.4600 | 0.6976 × 10−3 | 0.9221 | 2.2172 × 10−3 |
| n-hexadecane |  |  |  |  |  |
| 3f | 394.47 | 2.5257 | 0.7057 × 10−3 | 0.9806 | 2.2165 × 10−3 |
| 3g | 423.57 | 2.6360 | 0.6852 × 10−3 | 1.0553 | 2.2154 × 10−3 |
| 3h | 440.54 | 2.7003 | 0.6729 × 10−3 | 1.0965 | 2.2148 × 10−3 |

Furthermore, the density (ρfib+alk (1)) and specific heat (cfib+alk(1)) of the carbon fiber/n-alkane mixture at Tm when the volume fraction of the carbon fiber in the mixture were 0.460 were obtained using Eqs. (S18) and (S19). Then, in the same manner, ρfib+alk (2) and cfib+alk(2) of the carbon fiber/n-alkane mixture at Tm when the volume fraction of the carbon fiber in the mixture is 0.637 were obtained using Eqs. (S18) and (S19). Table S3 shows the values of ρfib+alk (1), ρfib+alk (2), cfib+alk(1), and cfib+alk(2) of the mixture when the volume fractions of carbon fibers in the mixture are 0.460 and 0.637, and the products ρfib+alk (1) cfib+alk(1) and ρfib+alk (2) cfib+alk(2). Additionally, ρtel ctel for the density and specific heat of tellurium–copper is shown in Table S3. For tellurium–copper, the density and specific heat at room temperature were used (see Table S1).

Table S3. Specific heat cfib+alk(k) (k = 1, 2) and density ρfib+alk (k) (k = 1, 2) of carbon fiber/alkane mixture; product of density and specific heat of the mixture, ρfib+alk (k) cfib+alk(k) (k = 1, 2); and product of density and specific heat of tellurium–copper, ρtel ctel.

| Sample name | Tm (K) | cp,fib+alk(1) (J g-1 K-1) | cp,fib+alk(2)(J g-1 K-1) | ρfib+alk(1) (g mm-3) | ρfib+alk(2) (g mm-3) | ρfib+alk(1)cp,fib+alk(1) (J mm-3 K-1) | ρfib+alk(2)cp,fib+alk(2) (J mm-3 K-1) | ρtel ctel (J mm-3 K-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| n-octane |  |  |  |  |  |  |  |  |
| 2a | 323.09 | 1.1828 | 1.0062 | 1.3852 × 10−3 | 1.6585 × 10−3 | 1.6385 × 10−3 | 1.6688 × 10−3 | 3.4419 × 10−3 |
| 2b | 342.20 | 1.2371 | 1.0604 | 1.3762 × 10−3 | 1.6522 × 10−3 | 1.7024 × 10−3 | 1.7520 × 10−3 | 3.4419 × 10−3 |
| 2c | 335.29 | 1.2175 | 1.0409 | 1.3795 × 10−3 | 1.6545 × 10−3 | 1.6795 × 10−3 | 1.7221 × 10−3 | 3.4419 × 10−3 |
| n-nonane |  |  |  |  |  |  |  |  |
| 2d | 340.78 | 1.2367 | 1.0590 | 1.3854 × 10−3 | 1.6584 × 10−3 | 1.7133 × 10−3 | 1.7563 × 10−3 | 3.4419 × 10−3 |
| 2e | 357.71 | 1.2840 | 1.1063 | 1.3776 × 10−3 | 1.6530 × 10−3 | 1.7689 × 10−3 | 1.8286 × 10−3 | 3.4419 × 10−3 |
| n-decane |  |  |  |  |  |  |  |  |
| 3a | 347.30 | 1.2582 | 1.0797 | 1.3899 × 10−3 | 1.6614 × 10−3 | 1.7488 × 10−3 | 1.7937 × 10−3 | 3.4419 × 10−3 |
| 3b | 369.85 | 1.3208 | 1.1420 | 1.3799 × 10−3 | 1.6544 × 10−3 | 1.8225 × 10−3 | 1.8893 × 10−3 | 3.4419 × 10−3 |
| n-dodecane |  |  |  |  |  |  |  |  |
| 3c | 356.60 | 1.2896 | 1.1095 | 1.3981 × 10−3 | 1.6668 × 10−3 | 1.8030 × 10−3 | 1.8493 × 10−3 | 3.4419 × 10−3 |
| 3d | 371.07 | 1.3298 | 1.1494 | 1.3921 × 10−3 | 1.6626 × 10−3 | 1.8512 × 10−3 | 1.9110 × 10−3 | 3.4419 × 10−3 |
| n-tridecane |  |  |  |  |  |  |  |  |
| 3e | 372.84 | 1.3369 | 1.1559 | 1.3966 × 10−3 | 1.6656 × 10−3 | 1.8672 × 10−3 | 1.9253 × 10−3 | 3.4419 × 10−3 |
| n-hexadecane |  |  |  |  |  |  |  |  |
| 3f | 394.47 | 1.4010 | 1.2179 | 1.4007 × 10−3 | 1.6681 × 10−3 | 1.9623 × 10−3 | 2.0315 × 10−3 | 3.4419 × 10−3 |
| 3g | 423.57 | 1.4763 | 1.2922 | 1.3891 × 10−3 | 1.6599 × 10−3 | 2.0508 × 10−3 | 2.1449 × 10−3 | 3.4419 × 10−3 |
| 3h | 440.54 | 1.5181 | 1.3332 | 1.3822 × 10−3 | 1.6551 × 10−3 | 2.0983 × 10−3 | 2.2066 × 10−3 | 3.4419 × 10−3 |

The heat capacity of an object consisting of a carbon-fiber/n-alkane mixture and two tellurium–copper screws considered as a single unit was calculated as follows:

Cfib+alk+tel(k)=ρfib+alk (k) cfib+alk(k)Vfib+alk+ρtel ctelVtel (k = 1, 2),		(S23)

where Vfib+alk is the volume of the carbon fiber/n-alkane mixture and Vtel is twice the volume of the tellurium–copper screw. That is, Vfib+alk=πd12L14 and Vtel=πd22L22, where d1=d2. Table S4 shows the values of Cfib+alk+tel(k) (k = 1, 2) in the cases of Figs. 2–3. For reference, Table S4 also shows the values of Cfib+alk(k)=ρfib+alk (k) cfib+alk(k)Vfib+alk (k=1, 2).

Table S4. Heat capacity of carbon fiber/alkane mixture, Cfib+alk(k) (k = 1, 2), and total heat capacity of the mixture and tellurium–copper screws, Cfib+alk+tel(k) (k = 1, 2).

| Sample name | Tm (K) | Cfib+alk(1) (J K-1) | Cfib+alk(2) (J K-1) | Cfib+alk+tel(1) (J K-1) | Cfib+alk+tel(2) (J K-1) |
| --- | --- | --- | --- | --- | --- |
| n-octane |  |  |  |  |  |
| 2a | 323.09 | 2.0847 × 10−2 | 2.1233 × 10−2 | 4.7123 × 10−2 | 4.7509 × 10−2 |
| 2b | 342.20 | 2.1661 × 10−2 | 2.2291 × 10−2 | 4.7936 × 10−2 | 4.8567 × 10−2 |
| 2c | 335.29 | 2.1369 × 10−2 | 2.1911 × 10−2 | 4.7645 × 10−2 | 4.8187 × 10−2 |
| n-nonane |  |  |  |  |  |
| 2d | 340.78 | 2.1799 × 10−2 | 2.2346 × 10−2 | 4.8074 × 10−2 | 4.8622 × 10−2 |
| 2e | 357.71 | 2.2506 × 10−2 | 2.3266 × 10−2 | 4.8782 × 10−2 | 4.9542 × 10−2 |
| n-decane |  |  |  |  |  |
| 3a | 347.30 | 2.2250 × 10−2 | 2.2822 × 10−2 | 4.8526 × 10−2 | 4.9098 × 10−2 |
| 3b | 369.85 | 2.3188 × 10−2 | 2.4038 × 10−2 | 4.9464 × 10−2 | 5.0314 × 10−2 |
| n-dodecane |  |  |  |  |  |
| 3c | 356.60 | 2.2941 × 10−2 | 2.3530 × 10−2 | 4.9216 × 10−2 | 4.9806 × 10−2 |
| 3d | 371.07 | 2.3553 × 10−2 | 2.4315 × 10−2 | 4.9829 × 10−2 | 5.0590 × 10−2 |
| n-tridecane |  |  |  |  |  |
| 3e | 372.84 | 2.3757 × 10−2 | 2.4496 × 10−2 | 5.0032 × 10−2 | 5.0772 × 10−2 |
| n-hexadecane |  |  |  |  |  |
| 3f | 394.47 | 2.4967 × 10−2 | 2.5848 × 10−2 | 5.1243 × 10−2 | 5.2124 × 10−2 |
| 3g | 423.57 | 2.6093 × 10−2 | 2.7290 × 10−2 | 5.2369 × 10−2 | 5.3566 × 10−2 |
| 3h | 440.54 | 2.6698 × 10−2 | 2.8075 × 10−2 | 5.2974 × 10−2 | 5.4351 × 10−2 |

The AC resistance value of the carbon fiber/alkane mixture packed in the PTFE tube was stored in the computer every second, and the current value applied to measure the sample resistance was constant (effective value was 10 mA). The total Joule heat used to heat the mixture and tellurium–copper screws from the start of heating to the occurrence of a sudden increase in resistance (Qtotal) was obtained by multiplying the time integral of the resistance from the start of heating to the occurrence of a sudden increase in resistance by the square of the measurement current (10 mA). The values of Qtotal at this Joule heat for each measurement are shown in Table 4 of the main text. The temperature increase of the sample consisting of the mixture and the two tellurium–copper screws owing to the resistance measurement current (∆Tfib+alk+tel(k)) was calculated as follows:

∆Tfib+alk+tel(k)=QtotalCfib+alk+tel(k) (k = 1, 2).			(S24)

The calculation results for the temperature increase due to the measured current are shown in Table 4 in the main text. It is found that when the volume fraction of carbon fiber is 0.460 or 0.637, the magnitude of the temperature increase of the sample owing to the measurement current is almost no different between ∆Tfib+alk+tel(1) and ∆Tfib+alk+tel(2) (within 1%–3%). Table 4 shows the boiling point (Tboil) of each alkane, the temperature at which the resistance increases suddenly (Tincrease), and the difference between the two (Tboil-Tincrease). Comparing Tboil-Tincrease and ∆Tfib+alk+tel(k) (k = 1, 2), it can be observed that the former is considerably larger than the latter. This indicates that Tincrease does not reach Tboil for the alkane contained in the mixture, even if the temperature increase owing to the measurement current is considered. The results show that the observed sudden increase in resistance cannot be explained by the rapid increase in the contact resistance between the carbon fiber/n-alkane mixture and tellurium–copper screw caused by the volume expansion of the alkane (owing to the boiling of the alkane in the mixture). As ∆Tfib+alk+tel(k) (k = 1, 2) is the rising temperature obtained by assuming that the mixture and tellurium–copper screws are in a completely thermally insulated state, these are the upper limit values of the temperature increase of the mixture owing to the measurement current. Thus, for all the samples, the temperature of the alkane contained in the carbon fiber/alkane mixture did not reach the boiling point of the alkane when the resistance of the mixture increased rapidly.

References

1. Pan, C., Zhang, J., Kou, K., Zhang, Y., Wu, G.: Investigation of the through-plane thermal conductivity of polymer composites with in-plane oriented hexagonal boron nitride. Int. J. Heat Mass Transf. 120, 1–8 (2018)

2. Taylor, S.E., Zeng, H.: Electrical conductivity and viscosity in binary organic liquid mixtures: Participation of molecular interactions and nanodomains. Colloids Interfaces 4, 44 (2020)

3. Taipalus, R., Harmia, T., Zhang, M.Q., Friedrich, K.: The electrical conductivity of carbon-fibre-reinforced polypropylene/polyaniline complex-blends: Experimental characterisation and modelling. Compos. Sci. Technol. 61, 801–814 (2001)

4. Khan, J.B., Smith, A.C., Tuohy, P.M., Gresil, M., Soutis, C., Lambourne, A.: Experimental electrical characterisation of carbon fibre composites (CFCs) for use in future aircraft applications. IET Sci. Meas. Technol. 13, 1131–1138 (2019)

5. Kirby, R.K.: Thermal expansion of polytetrafluoroethylene (Teflon) from −190̊ to +300̊C. J. Res. NBS 57, 91–94 (1956)

6. Pradere, C., Sauder, C.: Transverse and longitudinal coefficient of thermal expansion of carbon fibers at high temperatures (300–2500 K). Carbon 46, 1874–1884 (2008)

7. Vélez, C., de Zárate, J.M.O., Khayet, M.: Thermal properties of n-pentadecane, n-heptadecane and n-nonadecane in the solid/liquid phase change region. Int. J. Therm. Sci. 94, 139–146 (2015)

8. Weber, M., Kamal, M.R.: Estimation of the volume resistivity of electrically conductive composites. Polym. Compos. 18, 711–725 (1997)

9. Taherian, R., Hadianfard, M.J., Golikand, A.N.: A new equation for predicting electrical conductivity of carbon-filled polymer composites used for bipolar plates of fuel cells. J. Appl. Polym. Sci. 128, 1497–1509 (2013)

10. Heiser, J.A., King, J.A., Konell, J.P., Sutter, L.L.: Electrical conductivity of carbon filled nylon 6,6. Adv. Polym. Technol. 23, 135–146 (2004)

11. Demain, A., Issi, J -P.: The effect of fiber concentration on the thermal conductivity of a polycarbonate/pitch-based carbon fiber composite. J. Compos. Mater. 27, 668–683 (1993)

12. Konstantinov, V.A.: Heat transfer in molecular crystals, in: A Belmiloudi(Ed.) Heat Transfer – Theoretical Analysis, Experimental Investigations and Industrial Systems. IntechOpen, chap. 6 (2011)

13. Lomellini, P.: Viscosity-temperature relationships of a polycarbonate melt: Williams-Landel-Ferry versus Arrhenius behaviour. Makromol. Chem. 193, 69–79 (1992)

14. Klein, T., Yan, S., Cui, J., Magee, J.W., Kroenlein, K., Rausch, M.H., Koller, T.M., Fröba, A.P.: Liquid viscosity and surface tension of n-hexane, n-octane, n-decane, and n-hexadecane up to 573 K by surface light scattering. J. Chem. Eng. Data 64(9), 4116–4131 (2019)

15. Butland, A.T.D., Maddison, R.J.:The specific heat of graphite: An evaluation of measurements. J. Nucl. Mater. 49, 45–56 (1973/74)

16. Sazhin, S.: Droplets and Sprays, Appendix K, pp. 335–336, Springer, Heidelberg (2014)

17. Regueira, T., Varzandeh, F., Stenby, E.H., Yan, W.: Heat capacity and Joule-Thomson coefficient of selected n-alkanes at 0.1 and 10 MPa in broad temperature ranges. J. Chem. Thermodyn. 111, 250–264 (2017)

18. Concast. C14500: Standard-Stocked Product. https://www.concast.com/files/C14500.pdf

19. McEligot, D.M., Swank, W.D., Cottle, D.L., Valentin, F.I.: Thermal properties of G-348 graphite. (2016) https://www.osti.gov/servlets/purl/1330693