TABLES

| Table 1 Geotechnical characteristics and classification of Bentonite soil |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Colour | United soil classification | Clay(%) | Silt (%) | Sand (%) | Plasticity index (%) | Plastic limit (%) | Liquid limit (%) | Property |
| White | CH | 78 | 22 | 0 | 356.2 | 40 | 396.2 |  |

| Table 2 Mineralogical composition of Bentonite soil (wt% of the total amount). |  |  |  |
| --- | --- | --- | --- |
| Cristobalite (%) | Albite (%) | Quartz (%) | Montmorillonite (%) |
| SiO2 | (Na,Ca)(Si,Al)4O8 | SiO2 | Ca0.2(Al,Mg)2Si4O10(OH)2,xH2O |
| 12 | 26 | 14 | 45 |

| Table 3 Chemical Analysis of cement (%, by weight) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cement Type | SiO2 | Al2O3 | Fe2O3 | CaO | MgO | SO3 | Free CaO | Alkalies (Na2O%+0.658K2O%) | L.O.I | Insoluble Residue |
| II | 21.50 | 4.95 | 3.97 | 63.52 | 1.75 | 2.20 | 1.4 | 1 | 1.19 | 0.5 |

| Table 4 Physical and appearance characteristics of epoxy resin |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Viscosity of the compound at 25 °C | Density | Curing time at room temperature | Composition time of the components | The combination ratio of the resin to the hardener | Color | Appearance |
| 440 cp | 1.1gr/cm3 | 360 min | 5 min | 2:1 | Clear colorless | Liquid |