Solvent-free synthesis and characterization of bimetallic UiO-66(Zr/Sn) heterogeneous catalyst for biodiesel production

Ahmed S. Abou- Elyazeda,b*, Ebtehal A. Shabanb , Yinyong Suna*, Ahmed M. El-Nahasb, Tahani I. Kasharb

aMIIT Key Laboratory of Critical Materials Technology for New Energy Conversion and Storage, School of Chemistry and Chemical Engineering, Harbin Institute of Technology, Harbin, 150001, China.

bChemistry Department, Faculty of Science, Menoufia University, Shebin El-Kom, Egypt.

*Corresponding author: yysun@hit.edu.cn, Tel: (+86)-45186413708

Ahmedphysical90@gmail.com, Tel: (+2)-01090674437

Experimental:

Synthesis of UiO-66(Zr)-solvent and UiO-66(Zr)-green

Synthesis of UiO-66(Zr)-solvent: UiO-66(Zr) was prepared via a solvothermal technique, as follows the metal precursor ZrOCl2.8H2O (1.5 mmol) and the organic linker BDC (1.5 mmol) were dissolved in 50 mL DMF at room temperature in a Teflon-lined stainless-steel autoclave. The uniform mixture was packed and heated for 24 h at 130 °C in a preheated oven. After cooling to room temperature, the gel was washed with ethanol at 70 °C and then stored in CH2Cl2 for two days before being centrifuged and dried in an oven at 100 °C after that activated under vacuum at 150 °C for 24 h. The catalyst was referred to as UiO-66(Zr)-solvent.

Synthesis of UiO-66(Zr)-green: was synthesized by green method; ZrOCl2·8H2O (1.5 mmol) as metal precursor and BDC-linker (1.5 mmol) were pulverized together for about 10 min at room temperature. Then the pulverized materials were moved into an autoclave at 130 ºC for 12 h. After cooling to room temperature, the resulting white solid was washed with 70 ºC ethanol and dried for 12 h at 150 ºC under vacuum.

Table S1. Textural properties of mixed-metal MOFs (UiO-66(Zr/Sn).

| Sample name | SnIV content % | BET surface area (m2 g-1) | Langmuir surface area (m2 g-1) | Pore volume (cm3 g-1) |
| --- | --- | --- | --- | --- |
| UiO-66(Zr)-green-24 h | - | 701 | 945 | 0.68 |
| UiO-66(Zr/Sn)-130-24 h | 2.5 | 1158 | 1482 | 0.82 |
| UiO-66(Zr/Sn)- 130-24 h | 5 | 1170 | 1561 | 0.84 |
| UiO-66(Zr/Sn)- 130-24 h | 10 | 1104 | 1420 | 0.64 |
| UiO-66(Zr/Sn)- 130-24 h | 15 | 1056 | 1394 | 0.60 |
| UiO-66(Zr/Sn)- 130-24 h | 20 | 1075 | 1388 | 0.60 |
| UiO-66(Zr/Sn)- 130-24 h | 25 | 968 | 1303 | 0.65 |

Table S2. NH3-TPD results of UiO-66(Zr)-green and UiO-66(Zr/Sn)-5-130-24.

| Samples | Desorption temperature (below 200 °C) |  | Desorption temperature (200~400 °C) |  |
| --- | --- | --- | --- | --- |
|  | Number of acid sites (mmol) | Number of acid sites/adsorbent (mmol/g) | Number of acid sites (mmol) | Number of acid sites/adsorbent (mmol/g) |
| UiO-66(Zr)-green | 0.003 | 0.053 | 0.004 | 0.072 |
| UiO-66(Zr/Sn)-5-130-24 | 0.009 | 0.173 | 0.015 | 0.291 |