Supporting information

Design and Applications of a Promising Powerful Colorimetric Sensor for glutathione detection based on Mesoporous Silica Nanoparticle loaded by Copper

Morvarid Aghayana, Ali Mahmoudia,*, Mohammad Reza Sazegara, khodadad Nazarib, Alireza Jahanafarina, Omid Nazaria, Forogh Adhamic, Zeynab Poorhasana, Parisa Hamidia, Batoul Sadat Shafaeia

aDept. of Chemistry, Faculty of science, Islamic Azad University, North Tehran Branch, Tehran, Iran

bFuture Bioenergy Solutions Inc., North Vancouver, BC, V7P3P9, Canada

c.Dep. of chemistry, Faculty of science, Islamic Azad University, Yadegar-e-Imam Khomeini (RAH), Shahre Rey Branch, Tehran, Iran.

* Corresponding Authors

E-mail: mahmoudiali.ac@gmail.com

Tel.: +98 9123377127

A

B

Fig. S1 (A) long-term stability and (b) recyclability of catalytic activity of Cu-MSN, respectively.

(1)

Table S1. Comparison of Kinetic parameters of Cu-MSN and other peroxidase-mimics

|  | Enzyme mimics |  | km(mM) |  | Vmax(mM.S-1) |  | kcat(S-1) |  | kcat/km(mM-1.S-1) |  |  |  | References |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TMB | Cu-MSN |  | 0.1009 |  | 4.5×10-5 |  | 1.4×10-1 |  |  | 1.72 | This work |  |  |
|  | HRP |  | 0.434 |  | 1×10-4 |  | 4×103 |  |  | 9.21×103 | [32] |  |  |
|  | Porous CuO |  | 0.14 |  | 1.45×10-5 |  | 2.12×10-6 |  |  | 1.5×10-5 | [33] |  |  |
|  | PtPd NPs |  | 1.78 |  | 3.46×10-4 |  | 1.42×10-2 |  |  | 7.9×10-3 | [34] |  |  |
|  | Fe-MSN |  | 0.407 |  | 7.6×10-5 |  | 4.6×10-3 |  |  | 1.13×10-2 | [35] |  |  |
|  | Ag nanowire |  | 108 |  | 2.84×10-6 |  | 6.35×10-5 |  |  | 5.87×10-3 | [36] |  |  |
| H2O2 | Cu-MSN |  | 0.0226 |  | 6.5×10-5 |  | 2×10-1 |  |  | 1.08×101 | This work |  |  |
|  | HRP |  | 3.70 |  | 8.71×10-5 |  | 4×103 |  |  | 9.4×102 | [32] |  |  |
|  | PtPd NPs |  | 0.053 |  | 9.26×10-5 |  | 3.6×10-3 |  |  | 6.7×10-2 | [34] |  |  |
|  | Fe-MSN |  | 0.01 |  | 4.33×10-5 |  | 2.9×10-3 |  |  | 2.6×10-1 | [35] |  |  |
| ABTS | Cu-MSN | 0.0854 |  | 2.9 ×10-4 |  | 9.2 |  |  |  | 1.07×102 |  | This work |  |
|  | Pd@Fe2O3 | 0.049 |  | 1.02 ×10-4 |  | 7.5 ×10-2 |  |  |  | 0.15×101 |  | [37] |  |
|  | HRPa | 0.472 |  | 55 ×10-5 |  | 4.8 ×103 |  |  |  | 1.01×104 |  | [38] |  |
|  | AuNPs | 0.033 |  | 8.1 ×10-6 |  | 5.67 |  |  |  | - |  | [38] |  |
|  | Co-MSN | 0.07 |  | 33 ×10-5 |  | 1.62 ×10-2 |  |  |  | 2.22 ×10-1 |  | [39] |  |
|  | Zn-CuO NPs | 0.01 |  | 2.87×10-5 |  | - |  |  |  | - |  | [40] |  |
| H2O2 | Cu-MSN | 0.0885 |  | 1.5×101 |  | 4.96×102 |  |  |  | 4.72×103 |  | This work |  |
|  | Pd@Fe2O3 | 0.254 |  | 1.28×10-4 |  | 9.4×10-2 |  |  |  | 3.7×10-1 |  | [37] |  |
|  | Co-MSN | 0.34 |  | 13.2×10-5 |  | - |  |  |  | - |  | [39] |  |
|  | Zn-CuO | 0.071 |  | 0.3×10-5 |  | - |  | - |  |  |  | [40] |  |
| an HRP: Horseradish peroxidase |  |  |  |  |  |  |  |  |  |  |  |  |  |

(2)

Table S2. Detection of GSH amount in diverse human serum samples

| Samples | Added (µM) | Found (µM) | Recovery (%) | RSD(%) |
| --- | --- | --- | --- | --- |
| 1 | 1 | 0.996±0.018 | 99.6 | 2.2 |
|  | 10 | 9.982±0.018 | 99.8 | 0.18 |
|  | 30 | 29.93±0.051 | 99.7 | 0.2 |
| 2 | 1 | 0.99±0.014 | 99 | 1.41 |
|  | 10 | 9.986±0.092 | 99.8 | 0.32 |
|  | 30 | 29.95±0.091 | 99.8 | 0.31 |
| 3 | 1 | 0.973±0.03 | 97.3 | 3.08 |
|  | 10 | 9.996±0.057 | 99.9 | 0.78 |
|  | 30 | 29.93±0.087 | 99.7 | 0.3 |

(3)