Supporting Information

for

A dihydropyridine derivative as a highly selective fluorometric probe for quantification of Au3+ residue in the gold nanoparticle solution

Waroton Paisuwana, Mongkol Sukwattanasinittb, Mamoru Tobisuc,d, Anawat Ajavakomb,*

aDepartment of Chemistry, Faculty of Science, Chulalongkorn University, Phyathai Road, Pathumwan, Bangkok 10330, Thailand

bNanotec-CU Center of Excellence on Food and Agriculture, Department of Chemistry, Faculty of Science, Chulalongkorn University, Phyathai Road, Pathumwan, Bangkok 10330, Thailand

cDepartment of Applied Chemistry, Graduate School of Engineering, Osaka University, Suita, Osaka 565-0871

dInnovative Catalysis Science Division, Institute for Open and Transdisciplinary Research Initiatives (ICS-OTRI), Osaka University, Suita, Osaka 565-0871, Japan

| (c) (c) TABLE OF CONTENTS | PAGE |
| --- | --- |
| S1. 1H NMR spectra of DHP in acetone-d6 | 2 |
| S2. 1H NMR spectra of DHP-OH in acetone-d6 | 2 |
| S3. 13C NMR spectra of DHP in acetone-d61H | 3 |
| S4. 13C NMR spectra of DHP-OH in acetone-d6 | 3 |
| S5. HRMS spectra of DHP | 4 |
| S6. HRMS spectra of DHP-OH | 4 |
| S7. IR spectra of DHP | 5 |
| S8. IR spectra of DHP-OH | 5 |
| S9. Molar absorptivity of DHP and DHP-OH | 6 |
| S10. Fluorescence quantum efficiency of DHP and DHP-OH | 7 |
| S11. Fluorescence response of DHP and [DHP+Au3+] in various pHs | 8 |
| S12. Fluorescence response of DHP-OH and [DHP-OH+Au3+] in various pHs | 8 |
| S13. Time dependent fluorescence quenching profile in Tris-HCl pH 6.0 for 60 minutes | 9 |
| S14. Comparison of fluorescent probes for Au3+ detection | 9-10 |
| S15. Absorption spectra of DHP-OH, Au3+, and the mixture of DHP-OH and Au3+ in Tris-HCl pH 6.0. | 10 |
| S16. 13C NMR spectra of [DHP-OH+Au3+] | 11 |
| S17. HRMS spectra of [DHP-OH+Au3+] | 11 |
| S18. Absorption and morphology of AuNPs | 12 |

S1. 1H NMR spectra of DHP in acetone-d6

S2. 1H NMR spectra of DHP-OH in acetone-d6

S3. 13C NMR spectra of DHP in acetone-d6

S4. 13C NMR spectra of DHP-OH in acetone-d6

S5. HRMS spectra of DHP

S6. HRMS spectra of DHP-OH

S7. IR spectra of DHP

S8. IR spectra of DHP-OH

S9. Molar absorptivity of DHP and DHP-OH

S10. Fluorescence quantum efficiency of DHP and DHP-OH

S11. Fluorescence response of DHP and [DHP+Au3+] in various pHs

S12. Fluorescence response of DHP-OH and [DHP-OH+Au3+] in various pHs

S13. Time dependent fluorescence quenching profile in Tris-HCl pH 6.0 for 60 minutes

S14. Comparison of fluorescent probes for Au3+ detection

| Entry | Fluorescent Probe | Synthetic step | LOD (nM) | Fluorescent Mode | Solvent (v/v) | Application | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  | 1 | 48 | Turn on | DMSO/ H2O (1/1) | Synthetic waste water | Dyes and Pigments, 2019, 164, 14-19. |
| 2 |  | 1 | 70 | Turn on | HEPES (pH 7.4) | Cell imaging | Sensors and Actuators B, 2015, 209, 1005-1010. |
| 3 |  | 3 | 100 | Turn on | EtOH/ PBS (1/1, pH 7.4) | Human blood, serum and cell imaging | Sensors and Actuators B, 2016, 226, 364-369. |
| 4 |  | 1 | 60 | Turn on | PBS/ EtOH (7:3, pH 7.0) | Cell imaging | Biosensors and Bioelectronics, 2016, 77, 812-817. |
| 5 |  | 4 | 15 | Turn on and ratiometric | EtOH/ PBS (1/1, pH 7.4) | Cell imaging | Biosensors and Bioelectronics, 2016, 80, 288-293. |
| 6 |  | 1 | R1=100 R2=120 | Turn on | EtOH/ HEPES (1/1, pH 7.4) | Cell imaging | Biosensors and Bioelectronics, 2016, 86, 939-943. |
| 7 |  | 1 | 9.4 | Turn on | MeOH/ H2O (8:2) | Tap water and cell imaging | Dyes and Pigments, 2021, 191, 109341. |
| 8 |  | 2 | 9.8 | Turn off | DMSO/NaCl-HCl (1/99, pH 2.0) | Drinking, rain, tap, pond, and river water | Journal of Photochemistry and Photobiology A: Chemistry, 2020, 112823, |
| 9 |  | 1 | 167 (32.8 ppb) | Turn off | Tris-HCl pH 6.0 | Strip test, Real water samples, and Au3+ residue in AuNPs solution | This work |

S15. Absorption spectra of DHP-OH, Au3+, and the mixture of DHP-OH and Au3+ in Tris-HCl pH 6.0.

S16. 13C NMR spectra of [DHP-OH+Au3+]

1-(2-hydroxyethyl)-4-(2-methoxy-2-oxoethyl)-3,5-bis(methoxycarbonyl)pyridin-1-ium (Oxidized product): 13C NMR (125 MHz, D2O:DMSO-d6 (99:1, v/v)) δ (ppm): 171.29, 163.23, 155.09, 148.76, 131.93, 64.03, 59.87, 54.11, 53.16, 37.99.

S17. HRMS spectra of [DHP-OH+Au3+]

S18. Absorption and morphology of AuNPs

a) absorption spectra, b) DLS spectra, and c) TEM images of the Au3+/HEPES solution at the molar ratio of 1:1 and 1:5.