Table 1 Weight loss and water absorbency of P(KA) and P(Am-co-KA) after being buried in soil for ten weeks.

Polymers	 Weight loss 	Water absorbency 	Reduction in water absorbency 
(% (w/w))	(g/g)*  	(%)

P(KA) 	53 ± 3	183 ± 7 	52 ± 6

P(Am-co-KA) 	43 ± 2	165 ± 11	51 ± 9

Data are presented as mean ± one standard deviation derived from three replicates (N = 3).

*Water absorbency of the controls, P(KA) and P(Am-co-KA), were 370 ± 10 g/g and 326 ± 9 g/g, respectively.

Table 2 Weight loss and water absorbency of P(KA) and P(Am-co-KA) after incubation with different concentrations of crude peroxidase at room temperature (28±3C) for 16 h.

concentration

Crude peroxidase	  P(KA) 		P(Am-co-KA)

Weight loss	Water absorbency 	Weight loss	Water absorbency

(U/g)	(% (w/w)) 	(g/g)	(% (w/w))	(g/g)

0	<1	383  22c	<1	342  16

5 	<1	375  13bc	<1	339  12

10	<1	363  11bc	<1	338  22

15	  6.5  0.5a	352  11b	<1	335  18

20	15.0  0.3b	336 ± 12a	<1	333  9

Data are presented as mean ± one standard deviation derived from three replicates (N = 3). Different superscript letters in the same column indicated the values were significantly different (t-test or ANOVA followed by DMRT where applicable, P < 0.05).

Table 3 Weight loss and water absorbency of P(KA) and P(Am-co-KA) after incubation in different concentrations of hydrogen peroxide at room temperature (28±3C) for 2 h.

concentration

Hydrogen peroxide 	  P(KA) 		P(Am-co-KA)

Weight loss	Water absorbency 	Weight loss	Water absorbency

(% (v/w))	(% (w/w)) 	(g/g)	(% w/w) 	(g/g)

0	<1	386  19d	<1	330.1  20.0b

4	26.3  1.0a	347  18c	16.9  1.1a	308.2  17.0b

8	37.7  1.5b	305  17b	23.3  1.7b	301.0  19.5b

12	53.0  3.4c	232 ± 18a	53.4  2.6c	185.8  15.1a

Data are presented as mean ± one standard deviation derived from three replicates (N = 3). Different superscript letters in the same column indicated the values were significantly different (ANOVA and DMRT, P < 0.05).

Table 4 Weight loss and water absorbency of P(KA) and P(Am-co-KA) after incubation in 12% (v/w) of hydrogen peroxide at different temperatures for 2 h.

Temperature (ºC) 	  P(KA) 		P(Am-co-KA)

Weight loss	Water absorbency 	Weight loss	Water absorbency

(% (w/w)) 	(g/g)	(% w/w) 	(g/g)

30	53.0  4.2a	237.0 ± 8.2c	52.5  2.6a	187.5  7.26d

40	59.7  4.4ab	184.9 ± 10.9b	58.8  2.6ab	149.2  10.3c

50 	64.9  5.2b	139.3 ± 10.1a	61.2  2.6ab	137.8  7.0b

60	66.8  5.7b	121.6 ± 10.3a	63.6  2.6c	99.6  9.0a

Data are presented as mean ± one standard deviation derived from three replicates (N = 3). Different superscript letters in the same column indicated the values were significantly different (ANOVA and DMRT, P < 0.05).

Table 5 Box-Behnken design matrix of P(KA) degradation at different hydrogen peroxide concentrations, incubation times and temperatures

Trial	Variable factor			Weight loss	Prediction value

H2O2 concentration	Time 	Temperature	(% w/w)	 (% w/w)

(% v/w)	(h) 	(ºC)

1	0(-1)	2(-1)	60(0)	13.2  0.7	13.8  1.9

2	20(+1)	2(-1)	60(0)	36.5  2.8	32.6  1.9

3	0(-1)	10(+1)	60(0)	10.8  1.0	15.8  1.9

4	20(+1)	10(+1)	60(0)	82.7  5.9	83.0  1.9

5	0(-1)	6(0)	50(-1)	  7.2  0.1	13.3  1.9

6	20(+1)	6(0)	50(-1)	30.4  1.9	32.7  1.9

7	0(-1)	6(0)	70(+1)	  4.4  0.3	  6.6  1.9

8	20(+1)	6(0)	70(+1)	57.7  4.4	64.0  1.9

9	10(0)	2(-1)	50(-1)	42.7  2.4	48.6  1.9

10	10(0)	10(+1)	50(-1)	81.7  5.7	83.4  1.9

11	10(0)	2(-1)	70(+1)	76.8  5.8	76.2  1.9

12	10(0)	10(+1)	70(+1)	99.2  6.2	94.0  1.9

13	10(0)	6(0)	60(0)	95.0  2.6	92.9  1.9

14	10(0)	6(0)	60(0)	94.5  3.0	92.9  1.9

15	10(0)	6(0)	60(0)	93.1  2.3	92.9  1.9

* Data are presented as the mean ± one standard deviation derived from triplicate experiments. Numbers in parenthesis (-1, 0 or +1) are the coded value (low, normal or high). The second-order regression equation provided weight loss of P(KA) as a function of the variables. This model was significant, based on the F-value (25.09) and the model terms value of Prob > F (0.001).

Table 6 Box-Behnken design matrix of P(Am-co-KA) degradation at different hydrogen peroxide concentrations, incubation times and temperatures

Trial	Variable factor			Weight loss	Prediction value

H2O2 concentration	Time 	Temperature	(% w/w)	 (% w/w)

(% v/w)	(h) 	(ºC)

1	0(-1)	 2(-1)	60(0)	  3.7  3.2	  3.1  2.2

2	20(+1)	 2(-1)	60(0)	64.3  2.2	 58.1  2.2

3	0(-1)	10(+1)	60(0)	17.2  1.0	 25.3  2.2

4	20(+1)	10(+1)	60(0)	87.9  3.9	 95.9  2.2

5	0(-1)	 6(0)	50(-1)	  5.6  0.3	  7.0  2.2

6	20(+1)	 6(0)	50(-1)	61.7  3.5	 62.8  2.2

7	0(-1)	 6(0)	70(+1)	12.4  2.0	 28.8  2.2

8	20(+1)	 6(0)	70(+1)	82.7  5.7	 88.6  2.2

9	10(0)	 2(-1)	50(-1)	41.8  2.4	 50.5  2.2

10	10(0)	10(+1)	50(-1)	99.7  6.4	100.0  2.2

11	10(0)	 2(-1)	70(+1)	86.5  4.4	100.0  2.2

12	10(0)	10(+1)	70(+1)	90.2  2.8	 99.3   2.2

13	10(0)	 6(0)	60(0)	87.6  6.4	 94.8   2.2

14	10(0)	 6(0)	60(0)	85.6  4.7	 94.8   2.2

15	10(0)	 6(0)	60(0)	85.7  3.2	 94.8   2.2

* Data are presented as the mean ± one standard deviation derived from triplicate experiments. Numbers in parenthesis (-1, 0 or +1) are the coded value (low, normal or high). The second-order regression equation provided weight loss of P(Am-co-KA) as a function of the variables. This model was significant, based on the F-value (15.15) and the model terms value of Prob > F (0.001).

Table 7 Phytotoxicity tests of untreated and treated P(KA) and P(Am-co-KA).

Treatment                                            Germination rate (%)

Mung bean 	Sweet corn

Control	98.8  0.2	96.0 ± 1.2d

P(KA)	97.3  2.4	60.0 ± 4.0a

P(Am-co-KA)	98.7  1.3	70.7 ± 2.3b

Treated P(KA)	97.3  2.2	86.7 ± 3.4c

Treated P(Am-co-KA)	98.4  1.0	90.3 ± 2.3c

Data are presented as mean ± one standard deviation derived from three replicates (N = 3). Different superscript letters in the same column indicated the values were significantly different (ANOVA and DMRT, P < 0.05).