Supplementary data I

Weight loss and water absorbency of P(KA) and P(Am-co-KA) after cultivation in a culture of Trametes polyzona for 20 days.

Polymers	 Weight loss 	Water absorbency 	Reduction in water absorbency 
(% (w/w))	(g/g)*  	(%)

P(KA) 	<1	376 ± 2 	2.76 ± 0.54

P(Am-co-KA) 	<1	330 ± 3	2.17 ± 0.90

Data are presented as mean ± one standard deviation derived from three replicates (N = 3).

*Water absorbency of the controls, P(KA) and P(Am-co-KA), were 377 ± 5 g/g and 329 ± 8 g/g, respectively.

Supplementary data II

The effects of crude peroxidase on weight loss and water absorbency of P(KA) and P(Am-co-KA) after incubation in 12% (v/w) of hydrogen peroxide at 50ºC for 2 h.

concentration

Crude peroxidase	  P(KA) 		P(Am-co-KA)

Weight loss	Water absorbency 	Weight loss	Water absorbency

(U/g)	(% (w/w)) 	(g/g)	(% (w/w))	(g/g)

0	66.8  5.7	122.1 ± 4.9	63.6  2.6	99.6  9.0

20	66.1  2.5	121.6 ± 10.3	63.7  1.4	99.5  8.6

Data are presented as mean ± one standard deviation derived from three replicates (N = 3).