Figure S1. Comparison of the water uptake values for untreated and vacuum treated seeds. Sub-Figures (a) and (b) illustrate the water uptake values of chilli and papaya seeds respectively, for the ageing time of 60 days.

Figure S2. Comparison of the electrical conductivity values for untreated and vacuum treated seeds. Sub-Figures (a) and (b) illustrate the electrical conductivity values of chili and papaya seeds respectively, for the ageing time of 60 days.

Figure S3. Component fitting of high-resolution C1s spectra of (a) untreated and (b) vacuum-treated chilli seeds.

Figure S4. Component fitting of high-resolution C1s spectra of (a) untreated and (b) vacuum-treated papaya seeds.

Table S1. The atomic percentage of the different elements present in Bambara, chilli and papaya seeds.

| Chili seeds using oxygen plasma |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Untreated | Vacuum-treated | Plasma-treated day 4 | Plasma-treated day 21 | Plasma-treated day 51 |
| C (%) | 81.7 | 83.8 | 65.6 | 67.7 | 72.5 |
| O (%) | 16.9 | 15.1 | 30.2 | 29.0 | 24.4 |
| N (%) | 1.4 | 1.1 | 4.2 | 3.3 | 3.1 |
| O/C (%) | 0.2 | 0.2 | 0.5 | 0.4 | 0.3 |
| N/C (%) | 0.2 | 0.1 | 0.6 | 0.5 | 0.4 |
| C-C or C-H (%) | 62.3 | 61.9 | 34.8 | 34.8 | 43.4 |
| C-O or C-N (%) | 14.8 | 16.9 | 23.2 | 23.2 | 21.6 |
| C=O (%) | 4.2 | 5.0 | 9.7 | 9.7 | 7.5 |
| Papaya seeds using oxygen plasma |  |  |  |  |  |
|  | Untreated | Vacuum-treated | Plasma-treated day 4 | Plasma-treated day 21 | Plasma-treated day 51 |
| C (%) | 63.3 | 61.8 | 45.1 | 52.6 | 61.8 |
| O (%) | 29.4 | 29.7 | 43.9 | 40.8 | 33.6 |
| N (%) | 6.8 | 7.0 | 4.8 | 3.6 | 4.0 |
| F (%) | 0.0 | 0.0 | 0.9 | 0.0 | 0.0 |
| Mg (%) | 0.0 | 0.0 | 1.5 | 0.5 | 0.6 |
| Si (%) | 0.5 | 1.5 | 1.9 | 1.2 | 0.0 |
| S (%) | 0.0 | 0.0 | 0.6 | 0.0 | 0.0 |
| Ca (%) | 0.0 | 0.0 | 1.3 | 0.5 | 0.0 |
| O/C (%) | 0.4 | 0.4 | 1.0 | 0.8 | 0.5 |
| N/C (%) | 0.1 | 0.1 | 0.1 | 0.1 | 0.1 |
| C-C or C-H (%) | 25.9 | 27.4 | 13.2 | 14.1 | 14.1 |
| C-O or C-N (%) | 19.6 | 16.7 | 21.3 | 22.9 | 20.1 |
| C=O (%) | 17.8 | 17.7 | 10.6 | 15.2 | 13.9 |
| Bambara seeds using H2O plasma |  |  |  |  |  |
|  | C (%) | O (%) | N (%) | O/C | N/C |
| Untreated | 81.0 | 15.0 | 4.0 | 0.2 | 0.05 |
| Plasma-treated | 67.8 | 27.2 | 5.0 | 0.4 | 0.07 |

Table S2. Statistical analysis results for water uptake and electrical conductivity

| p- values for water uptake |  |  |  |
| --- | --- | --- | --- |
|  | Plasma-treated vs. Untreated | Plasma-treated vs. Vacuum-treated | Vacuum-treated vs. Untreated |
| Bambara | 0.000 | ---- | ---- |
| Chilli | 0.001 | 0.056 | 0.099 |
| Papaya | 0.004 | 0.501 | 0.043 |
| p- values for electrical conductivity |  |  |  |
|  | Plasma-treated vs. Untreated | Plasma-treated vs. Vacuum-treated | Vacuum-treated vs. Untreated |
| Bambara | 0.001 | ---- | ---- |
| Chilli | 0.000 | 0.000 | 0.799 |
| Papaya | 0.002 | 0.002 | 0.984 |