Supplementary Information

Unraveling the complex causality behind the Fe-N-C degradation in fuel cell

Geunsu Bae,1 Song Jin,2,3 Man Ho Han,4 Hyung-Suk Oh,4 Moulay-Tahar Sougrati,5 Kug-Seung Lee,6 Min Ho Seo,*,7 Frédéric Jaouen,*,5 and Chang Hyuck Choi*,1

1Department of Chemistry, Pohang University of Science and Technology (POSTECH), Pohang 37673, Republic of Korea.
2School of Materials Science and Engineering, Gwangju Institute of Science and Technology (GIST), Gwangju 61005, Republic of Korea.
3Department of Hydrogen Energy Materials, Surface Technology Division, Korea Institute of Materials Science (KIMS), Changwon 51508, Republic of Korea.
4Clean Energy Research Center, Korea Institute of Science and Technology (KIST), Seoul 02792, Republic of Korea.
5ICGM, Univ. Montpellier, CNRS, ENSCM, 34293 Montpellier, France.
6Beamline Department, Pohang Accelerator Laboratory, Pohang University of Science and Technology (POSTECH), Pohang 37673, Republic of Korea.
7Department of Nanotechnology and Engineering, Pukyong National University, Busan 48547, Republic of Korea.

*Corresponding authors: foifrit@pknu.ac.kr (M.H.S), frederic.jaouen@umontpellier.fr (F.J.), and chchoi@postech.ac.kr (C.H.C.)

Supplementary Notes

Supplementary Note 1. Summary of previous analytical methods.

Till now, two analytical methods, 57Fe Mössbauer spectroscopy and Fourier-transform alternating current voltammetry, have been successfully developed to understand the deactivation mechanism of Fe-N-C catalysts in PEMFCs. For the convenience of readers, we have summarized the detailed procedures of the analytical methods in Supplementary Table 1.

Supplementary Table 1. Summary of the procedure of previous diagnostic methods.

| Method | Procedure | Reference |
| --- | --- | --- |
| 57Fe Mössbauer spectroscopy | - In situ: acquire Mössbauer spectrum in PEMFC during a 36 h potentiostatic hold, with N2 /H2 feeds at anode/cathode. - Post-mortem: acquire Mössbauer spectrum after PEMFC operation at a fixed potential with O2/H2 or N2/H2 feed. | Nat. Catal. 4, 10–19 (2021) |
| Fourier-transform alternating current voltammetry (FTaCV) | - Break-in procedure. - Polarization measurement at the beginning-of-life. - Change cathodic gas to N2. - Electricity disconnection to the fuel cell station. - Connection with the potentiostat. - Measure CV. - Measure EIS. - Measure FTaCV. | Nat. Catal. 5, 163–170 (2022) |

Supplementary Note 2. Physicochemical characteristics of Fe0.5NC

The XRD and Raman spectrum of Fe0.5NC confirmed the successful carbonization of the precursor mixture after the pyrolysis at 1323 K (Supplementary Fig. 1a and b). N1s XPS revealed the functionalization of the carbon support with N moieties, which served as anchoring sites for the stabilization of isolated Fe ions (Supplementary Fig. 1c). The FT-EXAFS spectrum showed a strong Fe-N(O) interaction at R ~1.8 Å without Fe-Fe coordination at R ~2.5 Å (Supplementary Fig. 1d). Similarly, the WT-EXAFS contour map exhibited an intense peak at R ~1.9 Å and k ~6.3 Å–1 for the Fe–N(O) first shell and a less intense signal at R ~2.9 Å and k ~10.3 Å–1 for the Fe-(N)-C second shell (Supplementary Fig. 1e). No fingerprint of Fe particles in a signal from the Fe-Fe first shell at R ~2.5 Å and k ~9.7 Å–1 was not found (Supplementary Fig. 1f). In addition, its 57Fe Mössbauer spectrum could be fitted with two doublets of D1 and D2 (Supplementary Fig. 1g and Supplementary Table 2), which were assigned to different types of Fe-N4 moieties.1 The EXAFS and 57Fe Mössbauer spectra thus supported the predominant existence of the isolated Fe-N4 moieties without noticeable amounts of bulk Fe species in Fe0.5NC. The atomic dispersion of Fe species was further visualized by HAADF-STEM (Supplementary Fig. 1h).

Supplementary Note 3. Description of online GDE/EFC/ICP-MS system

A homemade EFC in which the GDE served as the working electrode was used for online ICP-MS measurements (Fig. 1a). Ar or O2 gas flowed into the graphite serpentine flow channel and diffused into the catalyst-electrolyte interface through the GDE. The operating temperature was controlled using a heating pad attached to the back of graphite serpentine. To prevent the accumulation of gas bubbles in the electrolyte flow channel, which mainly resulted from gaseous CO or CO2 evolution at the graphite counter electrode, a vacuum trap with a PTFE membrane was additionally implemented. Note that all measurements were conducted without a polymer membrane to obtain clear ICP-MS signals2 and high specificity for catalytic activity without interference from other components.3

Prior to electrochemical analysis with online GDE/EFC/ICP-MS, we cleaned the graphite rod counter electrode to avoid any Fe contamination during the analysis (Supplementary Fig. 2). When the counter electrode was contacted with a 0.1 M HClO4 electrolyte, ca. 200 ppb Fe was dissolved. However, Fe dissolution was reduced to almost zero within a few minutes. After the stabilization step, almost negligible leaching of Fe from the counter electrode was observed even under extremely harsh electrochemically conditions, CVs with an upper potential limit of 4.5 VRHE. In addition, the Fe0.5NC/GDE was cleaned through 200 fast CVs (200 mV s−1, 1.0–0.0 VRHE) at room temperature to remove any unexpected bulk Fe species (Supplementary Fig. 3). No distinct ICP-MS signal was observed from Fe leaching for Fe0.5NC/GDE which was in line with our previous report.4

Finally, the ORR polarization curve of the Fe0.5NC/GDE measured using the GDE/EFC/ICP-MS system showed a current density-potential response comparable to that measured using a conventional RDE system in the low overpotential region. However, unlike the RDE system, the GDE/EFC/ICP-MS system exhibited no mass transport-controlled region, even in the high overpotential region of 0.2 VRHE (Supplementary Fig. 4). Therefore, the results confirmed that the homemade EFC successfully reflected the realistic fuel cell environment of the catalyst layer compared to the RDE system.

Supplementary Note 4. Calculation of SD and TOF losses

1. SD loss

The fraction of dissolved Fe to the total bulk Fe content of Fe0.5NC was calculated using the following equation:

Dissolved Febulk (%) = vFe diss.×s÷mFe×100 = mFe diss.÷%Fe100×100		(Eq. S1)

where vFe diss. is the rate of Fe dissolution, s is the operation time, mFe is the bulk Fe content in the catalyst, mFe diss. is the total amount of dissolved Fe, and %Fe is the weight percentage of Fe in the catalyst. Similarly, the fraction of dissolved Fe to the surface Fe content of Fe0.5NC (i.e., SD loss) can be expressed by the following equation:

Dissolved Fesurf (%) = Dissolved Febulk÷U100 						(Eq. S2)

where U is the utilization factor of Fe0.5NC, which represents the electrochemically accessible active Fe-N4 sites to the total number of Fe atoms in the catalyst (i.e., 25% as confirmed by cyanide poisoning and nitrite stripping methods).5

2. TOF loss

The ORR activity of Fe0.5NC can be expressed in terms of the intrinsic TOF and the absolute amount (i.e., SD) of Fe-N4 sites using the following equation:

J [A g-1]= TOF×SD×FNA 							(Eq. S3)

where J is the catalytic mass activity at a given potential, NA is the Avogadro constant, and F is the Faraday constant. Similarly, the ORR activity of the deactivated Fe0.5NC can be expressed by the following equation:

JDEACT. [A g-1]= TOFDEACT.×SDDEACT.×FNA 					(Eq. S4)

where JDEACT., TOFDEACT., and SDDEACT. are the J, TOF, and SD values of the deactivated Fe0.5NC, respectively. The relative loss in the J value for deactivated Fe0.5NC can then be estimated using Eqs. S3 and S4:

J'= (J-JDEACT.)J=1-JDEACT.J=1-TOFDEACT.TOF×SDDEACT.SD 		(Eq. S5)

where J' is the relative loss of J for the deactivated Fe0.5NC. Similarly, the relative losses in the SD and TOF values for the deactivated Fe0.5NC can be expressed by the following equations:

TOF'= (TOF-TOFDEACT.)TOF=1-TOFDEACT.TOF				(Eq. S6)

SD'= (SD-SDDEACT.)SD=1-SDDEACT.SD					(Eq. S7)

where TOF' and SD' are the relative losses of TOF and SD for deactivated Fe0.5NC, respectively. Subsequently, by substituting Eqs. S6 and S7 with Eq. S5, we can finally obtain Eq.S8 which describes the relationship between the relative losses in J, SD, and TOF values for deactivated Fe0.5NC:

J'=1-1-TOF'×1-SD',  TOF'=1-1-J'1-SD'				(Eq. S8)

Supplementary Figures

Supplementary Fig. 1. Physicochemical characterizations of Fe0.5NC. a, XRD pattern, b, Raman spectrum, and c, XPS-N1s spectrum of Fe0.5NC. The XPS peak was deconvoluted with four N-components: pyridinic-N (398.5 eV), pyrrolic-N (400.1 eV), graphitic-N (401.1 eV), and pyridinic-oxide (403.2 eV).6 d, k3-weighted Fe K-edge FT-EXAFS of Fe0.5NC and Fe foil. e,f, k3-weighted Fe K-edge WT-EXAFS contour plots of Fe0.5NC (e) and Fe foil (f). g, 57Fe Mössbauer spectrum of Fe0.5NC, which was fitted with two doublets (i.e., D1 and D2, indicating ferric and ferrous Fe-N4 moieties of high and low/medium spins, respectively).1 h, HAADF-STEM image of Fe0.5NC (scale bar = 2 nm).

Supplementary Fig. 2. Fe dissolution from graphite rod counter electrode. a,b, Fe dissolution from graphite rod obtained after the contact with 0.1 M HClO4 electrolyte (a) and during the CVs with various upper potential limits (b). For b, the graphite rod was used as a working electrode.

Supplementary Fig. 3. Electrochemical activation of Fe0.5NC/GDE. Fe dissolution rate of Fe0.5NC/GDE obtained by online GDE/EFC/ICP-MS during the CVs in a potential range of 1.0–0.0 VRHE under Ar flow at 298 K.

Supplementary Fig. 4. ORR performance of Fe0.5NC. a,b, ORR polarization curves of Fe0.5NC fabricated on RDE or GDE (a), and corresponding Tafel plots (b). On the conventional RDE system, Fe0.5NC showed a Tafel slope of 60 mV dec−1. However, in the GDE/EFC/ICP-MS system, the same catalyst revealed a higher Tafel slope of 110 mV dec−1 at a low overpotential region and it increased to 200 mV dec−1 as the overpotential increased. This phenomenon, i.e., doubling of the Tafel slope, can be interpreted as a flooded GDE, where the measured Tafel slope is a consequence of combined O2 diffusion outside the GDE and the ORR kinetics inside the active layer.7

Supplementary Fig. 5. Change in ORR activity after the CVs at various temperatures. a–d, ORR polarization curves of Fe0.5NC/GDE obtained before and after the three CVs in a potential range of 1.0–0.0 VRHE under Ar flow at various temperatures; 298 K (a), 313 K (b), 333 K (c), and 353 K (d).

Supplementary Fig. 6. Post-mortem TEM analysis. a–e, TEM images of Fe0.5NC/GDE before (a) and after (b–e) the three CVs in a potential range of 1.0–0.0 VRHE under Ar flow at various temperatures; 298 K (b), 313 K (c), 333 K (d), and 353 K (e).

Supplementary Fig. 7. Change in ORR activity after the CVs under different gas atmospheres. a,b, ORR polarization curves of Fe0.5NC/GDE obtained before and after the three CVs in a potential range of 1.0–0.0 VRHE under Ar (a) or O2 flow (b) at 353 K.

Supplementary Fig. 8. Post-mortem TEM analysis. a–c, TEM images of Fe0.5NC/GDE after 2 h potential hold at 0.6 VRHE and 353 K under O2 flow.

Supplementary Fig. 9. Post-mortem EDS analysis. a, TEM and b, EDS elemental mapping (Fe and O) results of Fe0.5NC/GDE after 2 h potential hold at 0.6 VRHE and 353 K under O2 flow.

Supplementary Fig. 10. Selective leaching of Fe oxide. a–c, Fe dissolution of Fe0.5NC and Fe2O3/NC in 0.5 M HClO4 solution at various temperatures; 373 K (a), 353 K (b), and 333 K (c). For comparison, the results obtained without any catalysts (labeled ‘No Cat.’) and with Fe-free NC catalyst are also provided.

Additional discussion: To quantify the Fe oxide formed on Fe0.5NC during ORR, we selectively dissolved the Fe oxides from the aged catalyst without loss of the remaining Fe-N4 sites and measured their amount using ICP-MS. For this, we optimized the acid leaching conditions in a 0.5 M HClO4 solution. With a pristine Fe0.5NC, we prepared Fe2O3 nanoparticles supported on NC (labeled ‘Fe2O3/NC’), and the samples were acid-treated for 24 h at various leaching temperatures, one of the critical parameters determining the dissolution rate of Fe oxide.8 At 373 K, most of the Fe oxide was dissolved out from Fe2O3/NC. However, the Fe-N4 sites from Fe0.5NC were also damaged and dissolved after acid treatment at 373 K (Supplementary Fig. 10a). When leaching temperature decreased to 353 K and further to 333 K, the undesirable Fe-N4 site loss could be avoided, and ca. 80% of Fe oxide was leached out at 333 K (Supplementary Fig. 10b and c). Hence, we chose this condition, i.e., 0.5 M HClO4, 24 h, and 333 K, for the selective leaching of Fe oxide without undesirable loss of Fe-N4 sites. It is of note that 80% of imperfect Fe oxide leaching under such condition was 20% post-compensated for estimating the total amount of Fe oxide formed upon Fe0.5NC during ORR (see details in Supplementary Fig. 13).

Supplementary Fig. 11. Fe dissolution from Fe0.5NC/GDE at a constant potential of 0.6 VRHE. a–d, Real-time Fe dissolution of Fe0.5NC/GDE obtained by online GDE/EFC/ICP-MS during the potential hold at 0.6 VRHE and 353 K under O2 flow with various reaction times; 30 min (a), 60 min (b), 90 min (c), and 120 min (d). The relative change in ORR current density is also shown.

Supplementary Fig. 12. Post-leaching of aged Fe0.5NC/GDEs. a, 57Fe concentration in the solution obtained after the acid-treatment of Fe0.5NC/GDEs which are aged under various ORR durations. For comparison, the results obtained without any catalysts (labeled ‘No Cat.’) and with carbon paper, MPL, or pristine Fe0.5NC/GDE are also shown. The 57Fe concentration was measured using ICP-MS. The results showed non-negligible amounts of Fe dissolution from the carbon paper and MPL because Fe is typically ubiquitous. b, Fe dissolution from Fe oxides of aged Fe0.5NC/GDE was thus estimated by subtracting 57Fe concentration obtained with aged Fe0.5NC/GDEs from that of pristine Fe0.5NC/GDE. The sample solutions were diluted to one-tenth concentration with 0.1 M HClO4 solution.

Supplementary Fig. 13. Cumulative amounts of dissolved Fe under O2 flow. a, Cumulative amounts of dissolved Fe from Fe0.5NC/GDEs during the potential hold at 0.6 VRHE and 353 K under O2 flow as a function of operation time, i.e., the sum of both cumulative Fe-N4 dissolution (measured by GDE/EFC/ICP-MS) and Fe oxide amounts (measured by post-leaching). Owing to the incomplete leaching of Fe oxides under the optimized acid-leaching condition (Supplementary Fig. 10), the dissolved Fe oxide amounts was 20% post-compensated by multiplying 1.25 (i.e., the inverse of 80%). b, Comparison of cumulative amounts of dissolved Fe from Fe0.5NC/GDEs under O2 and Ar flows. Those under the Ar flow was cumulative Fe-N4 dissolution only (measured by GDE/EFC/ICP-MS) owing to the lack of Fe oxide formation.

Supplementary Fig. 14. Change in ORR current of Fe0.5NC/GDE. Change in ORR current density of Fe0.5NC/GDE obtained during 2 h potential hold at 0.6 VRHE and 353 K. The slope indicates the decay rate for each zone. It is of note that the decay rate obtained from the GDE/EFC/ICP-MS system was higher than that obtained during the fuel cell operation (i.e., 6.7 × 10−3 and 2.9 × 10−2 mA cm−2 min−1 for 1st and 2nd zone, respectively).9 The faster degradation rate in the GDE/EFC/ICP-MS system is probably due to the continuous flow of electrolyte and the fast removal of dissolved Fe ions, hardly arriving at equilibrium between non-dissolved and dissolved Fe species.

Supplementary Fig. 15. Post-mortem XPS analysis. XPS O1s spectra of Fe0.5NC/GDE after 2 h potential hold at 0.6 VRHE and 353 K under Ar or O2 flow. For comparison, the spectra of pristine Fe0.5NC/GDE were also shown. After aging Fe0.5NC/GDE under O2 flow, higher amounts of oxygen functional groups were identified compared to that aged under Ar flow.

Additional discussion: Although much larger apparent Fe dissolution was identified under Ar than that under O2 flow during the GDE/EFC/ICP-MS operation, it was later found that the total loss of active Fe-N4 sites was almost the same regardless of the gas flow (Supplementary Fig. 13). Despite the quantitatively similar loss of catalytic sites, the ORR activity drop after cycling was slightly larger for O2 than for Ar (Fig. 2b), which can be attributed to the formation of ROS that modifies the carbon surface and consequently decreases the TOF of the Fe-N4 sites.10

Supplementary Fig. 16. a, Pristine Fe-N4 and b, Pt-N4 were designed as reference models. Gray, blue, orange, and white balls indicate carbon, nitrogen, iron, and platinum atoms, respectively.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 71 (C65Fe1N4Pt1) | −1.198 |
| 2 |  | −1.196 |
| 3 |  | −1.140 |
| 4 |  | −1.142 |
| 5 |  | −1.195 |
| 6 (#1) | 70 (C64Fe1N4Pt1) | −1.238 |
| 7 |  | −1.217 |
| 8 |  | −1.202 |
| 9 |  | −1.205 |
| 10 |  | −1.228 |
| 11 |  | −1.221 |
| 12 |  | −1.209 |
| 13 |  | −1.203 |
| 14 |  | −1.200 |
| 15 |  | −1.200 |

Supplementary Fig. 17. Various configurations of Fe-N4 with a single-atom Pt for searching the most stable structure. Model volumes were 71 (1–5) or 70 (6–15). Model No. 6 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/Pt model (#1) for the cohesive energy comparison. Gray, blue, orange, and white balls indicate carbon, nitrogen, iron, and platinum atoms, respectively.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 70 (C60Fe1N8Pt1) | −1.637 |
| 2 (#2) |  | −1.647 |
| 3 |  | −1.640 |
| 4 |  | −1.634 |
| 5 |  | −1.622 |
| 6 | 70 (C61Fe1N7Pt1) | −1.643 |
| 7 | 70 (C62Fe1N6Pt1) | −1.446 |
| 8 |  | −1.442 |

Supplementary Fig. 18. Various configurations of Fe-N4 with a Pt-N4 for searching the most stable structure. Model volume was 70. Model No. 2 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/Pt-N4 model (#2) for the cohesive energy comparison. Gray, blue, orange, and white balls indicate carbon, nitrogen, iron, and platinum atoms, respectively.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 72 (C62Cl2Fe1N6Pt1) | −1.858 |
| 2 | 72 (C60Cl2Fe1N8Pt1) | −2.027 |
| 3 (#3) |  | −2.037 |
| 4 |  | −2.034 |
| 5 |  | −2.029 |
| 6 |  | −2.012 |
| 7 | 72 (C61Cl2Fe1N7Pt1) | −1.944 |

Supplementary Fig. 19. a, Optimized structure of Pt-N4Cl2 model. b, Various configurations of Fe-N4 with a Pt-N4Cl2 for searching the most stable structure. Model volume was 72. Model No. 3 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/Pt-N4Cl2 model (#3) for the cohesive energy comparison. Gray, blue, green, orange, and white balls indicate carbon, nitrogen, chlorine, iron, and platinum atoms, respectively.

Supplementary Fig. 20. a,b, Summary of theoretically possible configurations for trans-/cis-Pt-N2Cl2 into graphene sheet with edge sites (a) and basal planes (b) before/after structural optimization.

Additional note: The abbreviation of carbon vacancy is “v”, and the numbering indicates that 1: trans-PtN2Cl2-1; 2: trans-PtN2Cl2-2; 3: trans-PtN2Cl2-v; 4: cis-PtN2Cl2; 5: cis-PtN2Cl2-v.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 70 (C62Cl2Fe1N4Pt1) | −1.407 |
| 2 | 70 (C60Cl2Fe1N6Pt1) | −1.600 |
| 3 (#4-1) |  | −1.610 |
| 4 |  | −1.588 |
| 5 | 70 (C61Cl2Fe1N5Pt1) | −1.491 |

Supplementary Fig. 21. a, Optimized structure of the trans-Pt-N2Cl2-1 model. b, Various configurations of Fe-N4 with a trans-Pt-N2Cl2-1 for searching the most stable structure. Model volume was 70. Model No. 3 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/trans-Pt-N2Cl2-1 model (#4-1) for the cohesive energy comparison. Gray, blue, green, orange, and white balls indicate carbon, nitrogen, chlorine, iron, and platinum atoms, respectively.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 72 (C64Cl2Fe1N4Pt1) | −1.468 |
| 2 | 72 (C62Cl2Fe1N6Pt1) | −1.654 |
| 3 |  | −1.657 |
| 4 (#4-2) |  | −1.663 |
| 5 |  | −1.646 |
| 6 |  | −1.657 |
| 7 | 72 (C63Cl2Fe1N5Pt1) | −1.559 |

Supplementary Fig. 22. a, Optimized structure of the trans-Pt-N2Cl2-2 model. b, Various configurations of Fe-N4 with a trans-Pt-N2Cl2-2 for searching the most stable structure. Model volume was 72. Model No. 4 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/trans-Pt-N2Cl2-2 model (#4-2) for the cohesive energy comparison. Gray, blue, green, orange, and white balls indicate carbon, nitrogen, chlorine, iron, and platinum atoms, respectively.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 70 (C62Cl2Fe1N4Pt1) | −1.425 |
| 2 | 72 (C61Cl2Fe1N5Pt1) | −1.588 |
| 3 |  | −1.522 |
| 4 | 70 (C60Cl2Fe1N6Pt1) | −1.623 |
| 5 |  | −1.614 |
| 6 |  | −1.622 |
| 7 (#4-3) |  | −1.642 |
| 8 |  | −1.620 |

Supplementary Fig. 23. a, Optimized structure of the trans-Pt-N2Cl2-v model. b, Various configurations of Fe-N4 with a trans-Pt-N2Cl2-v for searching the most stable structure. Model volumes were 70 (1, 4–8) or 72 (2 and 3). Model No. 7 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/trans-Pt-N2Cl2-v model (#4-3) for the cohesive energy comparison. Gray, blue, green, orange, and white balls indicate carbon, nitrogen, chlorine, iron, and platinum atoms, respectively.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 72 (C62Cl2Fe1N6Pt1) | −1.842 |
| 2 |  | −1.843 |
| 3 |  | −1.845 |
| 4 (#5-1) |  | −1.848 |
| 5 |  | −1.838 |
| 6 | 72 (C63Cl2Fe1N5Pt1) | −1.770 |
| 7 |  | −1.770 |

Supplementary Fig. 24. a, Optimized structure of the cis-Pt-N2Cl2 model. b, Various configurations of Fe-N4 with a cis-Pt-N2Cl2 for searching the most stable structure. Model volume was 72. Model No. 4 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/cis-Pt-N2Cl2 model (#5-1) for the cohesive energy comparison. Gray, blue, green, orange, and white balls indicate carbon, nitrogen, chlorine, iron, and platinum atoms, respectively.

| No. | Volume | Formation energy (eV) |
| --- | --- | --- |
| 1 | 70 (C61Cl2Fe1N5Pt1) | −1.733 |
| 2 | 70 (C61Cl2Fe1N5Pt1) | −1.810 |
| 3 |  | −1.818 |
| 4 |  | −1.811 |
| 5 |  | −1.818 |
| 6 |  | −1.818 |
| 7 (#5-2) |  | −1.820 |

Supplementary Fig. 25. a, Optimized structure of the cis-Pt-N2Cl2-v model. b, Various configurations of Fe-N4 with a cis-Pt-N2Cl2-v for searching the most stable structure. Model volume was 70. Model No. 7 showed the lowest formation energy among the models, and thus, was used as the representative Fe-N4/cis-Pt-N2Cl2-v model (#5-2) for the cohesive energy comparison. Gray, blue, green, orange, and white balls indicate carbon, nitrogen, chlorine, iron, and platinum atoms, respectively.

Supplementary Fig. 26. Physical characterizations of Fe0.5NC-Pt. a, XRD patterns and b, Raman spectra of Fe0.5NC and Fe0.5NC-Pt. The XRD patterns show (002) and (101) planes of graphite at ca. 24° and 44°, respectively. In Raman spectra, clear D- and G-band peaks appeared at ca. 1352 and 1588 cm−1, respectively. The intensity ratio between the two bands (ID/IG), representing the degree of disorder in the carbon lattice, remained almost constant between the catalysts.

Supplementary Fig. 27. Electrochemical characterizations of Fe0.5NC-Pt. a, FAOR polarization curves measured in Ar-saturated 0.1 M HClO4 electrolyte containing 20 mM HCOOH. b, MOR experiments conducted at 0.7 VRHE in O2-saturated 0.1 M HClO4 electrolyte. 50 mM methanol was injected into the electrolyte after 1 min. For comparison, those for Fe0.5NC or Pt/C are also shown.

Supplementary Fig. 28. Electrochemical characterization of NC-Pt. a, ORR polarization curves measured in O2-saturated 0.1 M HClO4 electrolyte. b, PRR polarization curves measured in Ar-saturated 0.1 M HClO4 electrolyte containing 1.3 mM H2O2. c, FAOR polarization curves measured in Ar-saturated 0.1 M HClO4 electrolyte containing 20 mM HCOOH. d, MOR experiments conducted at 0.7 VRHE in O2-saturated 0.1 M HClO4 electrolyte. 50 mM methanol was injected into the electrolyte after 1 min. For comparison, those for NC or Pt/C are also shown.

Supplementary Fig. 29. Fe and Pt dissolutions from Fe0.5NC-Pt/GDE. a,b, Real-time Fe and Pt dissolutions of Fe0.5NC-Pt/GDE obtained by online GDE/EFC/ICP-MS during 2 h potential hold at 0.6 VRHE and 353 K under Ar (a) or O2 flow (b). The relative change in ORR current density is also shown.

Supplementary Fig. 30. Stability diagram of Fe0.5NC-Pt. Relative loss of j, SD, and TOF values of Fe0.5NC-Pt as a function of operation time obtained during 2 h potential hold at 0.6 VRHE and 353 K under O2 flow. The SD change was measured under Ar flow due to qualitatively similar loss of Fe-N4 sites regardless of gas flows.

Supplementary Fig. 31. FT-EXAFS of pristine and aged Fe0.5NC-Pt. k3-weighted Pt L3-edge FT-EXAFS spectra of Fe0.5NC-Pt before and after 50 h of PEMFC operation at 0.5 V.

Supplementary Fig. 32. H2O2 formation profile of Fe0.5NC and Fe0.5NC-Pt. The Pt ring, equipped at the rotating ring-disk electrode, was polarized at a constant potential of 1.2 VRHE during ORR polarization on the disk electrode. The collection efficiency of 0.42 was used after FeⅡ/FeⅢ redox calibration.

Supplementary Table 2. Parameters derived from the fittings of the 57Fe Mössbauer spectrum of Fe0.5NC: relative area (RA), isomer shift (IS), and quadrupole splitting (QS) of each fitted spectral component.

| Sample | Component | RA (%) | IS (mm s−1) | QS (mm s−1) | Assignment |
| --- | --- | --- | --- | --- | --- |
| Fe0.5NC powder | D1 | 59 | 0.33 | 0.88 | High spin O-FeⅢ-N4 |
|  | D2 | 41 | 0.37 | 2.73 | Low/medium spin FeⅡ-N4 |

Supplementary Table 3. Volume and cohesive energy values of the defined model for various configurations.

| Defined model | Volume | Cohesive energy (eV) |
| --- | --- | --- |
| Fe-N4 | 71 (C66Fe1N4) | −6.503 |
| Pt-N4 | 71 (C66Pt1N4) | −7.015 |
| #1 (No.6) | 70 (C64Fe1N4Pt1) | −6.774 |
| #2 (No.2) | 70 (C60Fe1N8Pt1) | −6.527 |
| #3 (No.3) | 72 (C60Cl2Fe1N8Pt1) | −6.553 |
| #4-1 (No.3) | 70 (C60Cl2Fe1N6Pt1) | −6.515 |
| #4-2 (No.4) | 72 (C62Cl2Fe1N6Pt1) | −6.923 |
| #4-3 (No.7) | 70 (C60Cl2Fe1N6Pt1) | −7.583 |
| #5-1 (No.4) | 72 (C62Cl2Fe1N6Pt1) | −6.849 |
| #5-2 (No.7) | 70 (C60Cl2Fe1N6Pt1) | −6.834 |

Supplementary Table 4. Best-fit parameters obtained from FT-EXAFS analysis of Fe0.5NC-Pt: coordination number (CN), interatomic distance (R), and Debye-Waller factor (σ2) of each path. The errors are given in the parentheses.

| Sample | Path | CN | R (Å) | σ2 (Å2) | R-factor |
| --- | --- | --- | --- | --- | --- |
| Fe0.5NC-Pt powder | Pt-N | 3.44 | 2.04 (3) | 0.008 (8) | 0.011 |
|  | Pt-Cl | 1.06 | 2.24 (4) | 0.008 (8) |  |

References

1	Mineva, T. et al. Understanding active sites in pyrolyzed Fe–N–C catalysts for fuel cell cathodes by bridging density functional theory calculations and 57Fe Mössbauer spectroscopy. ACS Catal. 9, 9359-9371 (2019).

2	Ehelebe, K. et al. Platinum dissolution in realistic fuel cell catalyst layers. Angew. Chem. Int. Ed. 60, 8882-8888 (2021).

3	Martinez, U., Komini Babu, S., Holby, E. F. & Zelenay, P. Durability challenges and perspective in the development of PGM-free electrocatalysts for the oxygen reduction reaction. Curr. Opin. Electrochem. 9, 224-232 (2018).

4	Choi, C. H. et al. Minimizing operando demetallation of Fe-N-C electrocatalysts in acidic medium. ACS Catal. 6, 3136-3146 (2016).

5	Bae, G. et al. Quantification of active site density and turnover frequency: from single-atom metal to nanoparticle electrocatalysts. JACS Au 1, 586-597 (2021).

6	Guo, D. et al. Active sites of nitrogen-doped carbon materials for oxygen reduction reaction clarified using model catalysts. Science 351, 361 (2016).

7	Jaouen, F. d. r., Lindbergh, G. r. & Sundholm, G. r. Investigation of mass-transport limitations in the solid polymer fuel cell cathode. J. Electrochem. Soc. 149, A437 (2002).

8	Taxiarchou, M., Panias, D., Douni, I., Paspaliaris, I. & Kontopoulos, A. Dissolution of hematite in acidic oxalate solutions. Hydrometallurgy 44, 287-299 (1997).

9	Chenitz, R. et al. A specific demetalation of Fe–N4 catalytic sites in the micropores of NC_Ar + NH3 is at the origin of the initial activity loss of the highly active Fe/N/C catalyst used for the reduction of oxygen in PEM fuel cells. Energy Environ. Sci. 11, 365-382 (2018).

10	Choi, C. H. et al. The Achilles' heel of iron-based catalysts during oxygen reduction in an acidic medium. Energy Environ. Sci. 11, 3176-3182 (2018).