Support Information

S1. Optical images of schematic illustration the treatment

Optical images indicating the treatment of superhydrophobic SA/CMC aerogel.

S2. Measurement for the water stability of samples in the water

All aerogels would float on the water surface when them were placed in. The aerogels were dipped in the water with tweezers for a while, then released them to observe. The SA/CMC aerogel will float in the water and dissolve completely within a day. The SA/CMC aerogel with silane reagent modification will swell in the water without solubilization until it becomes a soft and easily deformable wet gel that floats on the surface. The Ca2+ crosslinked SA/CMC aerogel with silane reagent modification mostly floats below the surface of water. The superhydrophobic SA/CMC aerogel mostly floats above the surface of water. Obviously, the superhydrophobic SA/CMC aerogel has a best water stability. The excellent water stability would be beneficial to the application of the aerogel in water or wet environment.

The water stability of the prepared aerogels in different processing stages. The morphology of prepared aerogels was observed at 15 min, 3 h, 1 day and 7 days, respectively in the water. The aerogels in the beaker from left to right are the SA/CMC aerogel, the SA/CMC aerogel with silane reagent modification, the Ca2+ crosslinked SA/CMC aerogel with silane reagent modification and the superhydrophobic SA/CMC aerogel.

S3. Measurement for the water stability for the superhydrophobic SA/CMC aerogel

As shown in Figure S3(a), the water contact angles (WCAs, °) of SA/CMC aerogel with various concentration are 0°. All the hydrophobic modification steps promoted the hydrophobic properties of aerogels. Figure S3(b) demonstrates the WCAs of the superhydrophobic SA/CMC aerogel with various polysaccharide concentrations decrease gradually with time. Figure S3(c) and (d) verify the optimal WCAs of aerogels with various polysaccharide concentrations by adding different amount of SiO2 nanoparticles and MTMS.

(a) The water contact angles (WCAs, °) of the SA/CMC aerogel and the superhydrophobic SA/CMC aerogel with two kinds of polysaccharide concentrations in different processing stages at different times; WCAs (°) of the superhydrophobic SA/CMC aerogel with (b) various polysaccharide concentrations at various time (c) different addition ratio of SiO2 and MTMS (d) various polysaccharide concentrations under two kinds of addition ratio of SiO2 and MTMS. Data are mean ± SD (n = 3).

S4. Measurement for the standard curve of MB solution

(a) UV absorption wavelengths of methylene blue (MB) at different concentrations; (b) The standard curve of MB solution.

S5. Measurement for the selective competitive adsorption process of the superhydrophobic SA/CMC aerogel

The superhydrophobic SA/CMC aerogel can quickly remove oil droplets from the water surface within 15 s. And chloroform has the best effect in the selective competitive adsorption process of the superhydrophobic SA/CMC aerogel.

The selective competitive adsorption process and effect of the superhydrophobic SA/CMC aerogel in oil/water mixture: (a, b) paraffin liquid (red)/water mixture; (c, d) chloroform (red)/water mixture; (e) hexane (red)/water mixtures.