| Table 1 Previous Work on the Mechanical Properties of Earth-based Composites |  |  |  |  |
| --- | --- | --- | --- | --- |
| Composites | Compressive Strength (MPa) | Flexural Strength (MPa) | Fracture Toughness (MPam) | Reference |
| Laterite Reinforced with Polyethylene, Biochar, Calcium Phosphate andPhosphogypsum Composites Laterite Reinforced with Polyethylene Compsoite | 4.2 4.1 | 10.1 6.1 | 1.2 0.76 | Azeko et al., 2022 [10] Azeko et al., 2018; 2016 [1, 9] |
| Laterite and Clay Reinforced with Natural Straw Composite | 3.03 | 9 | 1.4 | Kabiru et al., 2016a,b [26, 27] |
| Waste Sisal and Eucalyptus Grandis Pulp Cement Composites | Not measured | 19.2 | 0.64 | Savastano et al., 2005 [28] |
| Cement Blocks Reinforced with Sisal and Banana Pulp Fibres | Not measured | 20 | 1.5 | Savastano et al., 2000 [29] |
| Concrete Blocks Reinforced with Crumb Rubber | 23 | Not measured | 0.39 | Sukontasukku and Chaikaew, 2006 [30] |
| Fly Ash Concrete | 26.7 | 3.6 | Not measured | Siddique, 2004 [31] |