	Table 1
Previous Work on the Mechanical Properties of Earth-based Composites

	Composites
	Compressive Strength (MPa)
	Flexural Strength (MPa)
	Fracture Toughness (MPam)
	Reference

	Laterite Reinforced with Polyethylene, Biochar, Calcium Phosphate andPhosphogypsum Composites
Laterite Reinforced with Polyethylene Compsoite
	4.2
4.1
	10.1
6.1
	1.2
0.76
	Azeko et al., 2022 [10]
Azeko et al., 2018; 2016 [1, 9]

	Laterite and Clay Reinforced with Natural Straw Composite
	3.03
	9
	1.4
	Kabiru et al., 2016a,b [26, 27]

	Waste Sisal and Eucalyptus Grandis Pulp Cement Composites
	Not measured
	19.2
	0.64
	Savastano et al., 2005 [28]

	Cement Blocks Reinforced with Sisal and Banana Pulp Fibres
	Not measured
	20
	1.5
	Savastano et al., 2000 [29]

	Concrete Blocks Reinforced with Crumb Rubber
	23
	Not measured
	0.39
	Sukontasukku and Chaikaew, 2006 [30]

	Fly Ash Concrete
	26.7
	3.6
	Not measured
	Siddique, 2004 [31]



