Table B1. The main chemical component of body of Yuezhou porcelain（%）[1].

No.  Na2O  MgO  Al2O3  SiO2  K2O  CaO  TiO2  Fe2O3

DH-1  0.90  0.61  20.34  71.42  3.15  0.25  0.65  1.67

DH-2  0.03  0.69  21.27  70.48  3.65  0.23  0.63  2.02

JD-3  0.40  1.07  25.54  65.24  2.86  0.32  0.82  2.74

JD-4  0.03  1.15  26.32  65.13  3.01  0.23  0.66  2.47

JD-5  0.41  1.28  21.44  69.10  3.77  0.30  0.71  1.98

JD-6  0.49  1.17  21.41  69.49  4.02  0.57  0.47  1.38

NC-7  0.58  0.74  20.78  71.64  3.03  0.38  0.61  1.24

NC-8  0.88  1.26  23.02  66.34  2.98  0.31  0.68  3.53

NC-9  0.41  0.87  18.28  74.32  2.88  0.25  0.45  1.55

NC-10  0.32  0.80  19.06  72.82  3.28  0.22  0.59  1.91

NC-11  0.57  0.68  19.00  72.34  3.67  0.30  0.52  1.92

NC-12  0.34  1.13  19.01  71.75  3.57  0.28  0.62  2.31

NC-13  1.76  1.58  17.94  72.17  2.90  0.26  0.54  1.86

NC-14  0.46  1.30  30.02  60.99  3.04  0.29  0.75  2.14

NC-15  0.69  1.29  19.48  72.25  2.51  0.48  0.42  1.88

NC-16  0.53  0.99  19.79  72.03  3.03  0.17  0.58  1.86

NC-17  1.16  0.85  20.25  70.15  3.34  0.33  0.48  2.44

SC-18  0.21  1.01  25.42  64.67  3.64  0.34  0.61  3.12

SC-19  0.73  0.75  15.68  76.32  2.87  0.24  0.45  1.96

SC-20  0.73  1.69  20.61  69.13  2.73  0.28  0.59  3.25

SC-21  0.90  1.05  27.22  62.85  3.51  0.39  0.74  2.33

SC-22  0.28  0.86  18.98  71.68  3.29  0.25  0.61  3.05

SC-23  0.03  1.11  19.26  72.55  3.29  0.40  0.55  1.82

SC-24  0.03  0.36  15.32  77.08  2.79  0.17  0.75  2.50

SC-25  0.63  1.28  24.39  67.55  2.24  0.24  0.49  2.18

SC-26  0.54  1.22  22.92  67.04  3.89  0.23  0.70  2.46

SC-27  0.03  1.23  27.45  63.23  3.91  0.28  0.64  2.22

TC-28  0.71  1.08  28.15  62.20  3.38  0.22  0.58  2.67

TC-29  0.53  0.66  22.84  67.91  3.67  0.21  0.57  2.60

TC-30  0.58  1.14  19.75  71.33  3.16  0.28  0.63  2.13

Table B2. The minor chemical component of body of Yuezhou porcelain (μg/g) [1].

No         MnO    CuO    ZnO    PbO2  Rb2O    SrO    Y2O3   ZrO2    P2O5

DH-1  170  80  130  0  250  80  50  460  200

DH-2  210  20  180  110  310  80  40  380  250

JD-3  210  130  400  80  270  60  70  350  340

JD-4  250  80  140  70  240  50  30  290  490

JD-5  200  120  330  120  360  90  70  490  290

JD-6  230  80  50  80  290  50  50  400  360

NC-7  170  110  270  0  200  40  50  170  180

NC-8  320  60  300  60  240  40  50  360  460

NC-9  330  120  280  50  230  40  40  380  300

NC-10  150  60  180  20  250  80  50  480  200

NC-11  160  50  160   50  240  40  40  280  260

NC-12  250  30  200  100  290  100  50  900  320

NC-13  230  70  120  50  240  50  40  320  370

NC-14  340  100  170  110  330  50  60  320  780

NC-15  190  110  130  60  260  70  50  420  300

NC-16  180  80  110  0  280  50  90  420  430

NC-17  200  60  140  90  170  20  40  1060  670

SC-18  280  40  190  160  390  150  180  580  320

SC-19  160  210   150  80  220  30  40  240  280

SC-20  370  120  190  50  250  80  70  360  750

SC-21  170  60  240  140  310  120  40  600  360

SC-22  200  70  160  130  310  80  70  820  290

SC-23  210  120  310  60  270  140  50  480  230

SC-24  210  80  400  70  270  80  60  250  260

SC-25  260  120  200  50  300  110  60  400  820

SC-26  300  120  160  60  300  70  50  640  220

SC-27  230  100  190  120  300  60  40  370  720

TC-28  230  30  110  110  270  60  50  890  220

TC-29  160  60  160  110  300  130  50  560  570

TC-30  230  30  160  40  250  60  50  330  150

Table B3. The REE composition of the clay body of celadons from Hongzhou kiln by NAA analysis [2,3].

| No. | Date | Ba | Ce | Co | Cr | Cs | Eu | Fe2O3* | Hf | La | Lu | Na2O* | Nd | Rb | Sb | Sc | Sm | Ta | Tb | Th | U | Yb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| JXHZ369 | Eastern Han | 593 | 107 | 15.5 | 100 | 13.1 | 1.95 | 6.11 | 5.9 | 70.2 | 0.59 | 0.46 | 42 | 132 | 1.4 | 19.1 | 11.1 | 1.4 | 1.56 | 17.8 | 5.1 | 3.5 |
| JXHZ370 | Eastern Han | 599 | 103 | 12.7 | 102 | 14.9 | 1.81 | 5.14 | 6.4 | 66.7 | 0.62 | 0.50 | 40 | 162 | 1.4 | 19.6 | 10.1 | 1.6 | 1.42 | 18.4 | 5.3 | 3.8 |
| JXHZ371 | Eastern Han | 555 | 98.6 | 13.9 | 108 | 12.8 | 1.95 | 6.27 | 6.4 | 67.6 | 0.56 | 0.42 | 39 | 123 | 1.4 | 20.1 | 10.3 | 1.3 | 1.38 | 17.0 | 5.3 | 3.3 |
| JXHZ372 | Eastern Han | 591 | 97.3 | 15.6 | 107 | 11.9 | 1.87 | 6.37 | 6.1 | 71.4 | 0.52 | 0.49 | 45 | 150 | 1.7 | 19.5 | 10.8 | 1.2 | 1.34 | 16.9 | 4.9 | 3.2 |
| JXHZ373 | Eastern Han | 619 | 110 | 12.4 | 99 | 12.2 | 1.89 | 5.10 | 6.2 | 69.8 | 0.58 | 0.51 | 42 | 137 | 1.0 | 17.7 | 10.7 | 1.5 | 1.35 | 17.0 | 5.2 | 3.8 |
| JXHZ374 | Eastern Han | 585 | 105 | 13.6 | 104 | 13.2 | 2.21 | 5.27 | 6.2 | 71.0 | 0.58 | 0.47 | 43 | 136 | 1.3 | 19.3 | 10.7 | 1.3 | 1.58 | 17.0 | 5.9 | 4.1 |
| JXHZ375 | Eastern Han | 564 | 108 | 10.9 | 101 | 12.3 | 1.75 | 4.17 | 6.5 | 65.0 | 0.55 | 0.53 | 38 | 144 | 1.2 | 19.2 | 10.4 | 1.5 | 1.29 | 17.6 | 4.9 | 3.7 |
| JXHZ376 | Eastern Han | 603 | 116 | 13.6 | 107 | 13.0 | 1.96 | 5.01 | 6.2 | 70.6 | 0.57 | 0.57 | 44 | 138 | 1.2 | 20.2 | 11.2 | 1.2 | 1.42 | 17.1 | 4.7 | 3.8 |
| JXHZ377 | Eastern Han | 453 | 112 | 9.1 | 118 | 13.1 | 1.90 | 5.49 | 6.1 | 72.8 | 0.53 | 0.31 | 45 | 118 | 1.0 | 18.7 | 10.7 | 1.3 | 1.46 | 17.6 | 6.3 | 3.3 |
| JXHZ378 | Eastern Han | 650 | 127 | 10.9 | 111 | 13.0 | 2.29 | 4.83 | 7.9 | 83.4 | 0.61 | 0.58 | 53 | 142 | 1.4 | 20.5 | 12.5 | 1.5 | 1.72 | 17.6 | 6.1 | 3.5 |
| JXHZ379 | Eastern Han | 456 | 111 | 12.5 | 114 | 12.3 | 2.00 | 5.40 | 6.2 | 67.1 | 0.52 | 0.40 | 41 | 117 | 1.4 | 20.0 | 10.4 | 1.7 | 1.40 | 17.6 | 4.9 | 3.5 |
| JXHZ380 | Eastern Han | 595 | 114 | 14.1 | 109 | 14.2 | 2.20 | 5.33 | 6.1 | 70.0 | 0.53 | 0.37 | 45 | 148 | 1.4 | 21.5 | 11.4 | 1.5 | 1.33 | 18.8 | 5.9 | 3.7 |
| JXHZ381 | Eastern Han | 554 | 98.7 | 12.2 | 103 | 11.9 | 1.93 | 5.01 | 7.1 | 65.5 | 0.59 | 0.62 | 38 | 125 | 1.5 | 18.8 | 10.3 | 1.3 | 1.40 | 16.3 | 4.9 | 3.8 |
| JXHZ382 | Eastern Han | 661 | 105 | 15.7 | 117 | 13.1 | 1.80 | 5.49 | 6.6 | 73.3 | 0.60 | 0.56 | 42 | 148 | 1.4 | 21.8 | 11.3 | 1.4 | 1.29 | 18.7 | 5.4 | 4.0 |
| JXHZ383 | Eastern Han | 628 | 102 | 14.9 | 102 | 12.3 | 1.75 | 5.16 | 6.9 | 63.8 | 0.55 | 0.63 | 34 | 130 | 1.8 | 18.3 | 9.8 | 1.5 | 1.34 | 16.9 | 4.9 | 3.5 |
| JXHZ384 | Eastern Han | 551 | 115 | 14.5 | 114 | 13.1 | 1.91 | 5.50 | 6.0 | 69.7 | 0.56 | 0.38 | 39 | 131 | 1.5 | 20.0 | 11.0 | 1.4 | 1.41 | 18.0 | 5.3 | 3.7 |
| JXHZ385 | Eastern Han | 505 | 110 | 11.4 | 104 | 12.4 | 1.67 | 4.09 | 6.9 | 68.1 | 0.56 | 0.42 | 40 | 140 | 1.3 | 16.6 | 10.7 | 1.4 | 1.48 | 19.1 | 5.5 | 3.1 |
| JXHZ386 | Eastern Han | 550 | 96.5 | 12.6 | 98 | 12.6 | 1.73 | 5.57 | 5.9 | 63.0 | 0.51 | 0.57 | 39 | 140 | 1.4 | 18.9 | 9.7 | 1.3 | 1.27 | 16.3 | 5.6 | 3.3 |
| JXHZ387 | Eastern Han | 622 | 107 | 18.1 | 118 | 15.1 | 1.86 | 5.74 | 6.8 | 69.0 | 0.60 | 0.30 | 34 | 148 | 1.5 | 20.9 | 9.9 | 1.6 | 1.33 | 19.7 | 6.6 | 3.5 |
| JXHZ388 | Eastern Han | 534 | 104 | 11.3 | 103 | 11.9 | 1.45 | 5.26 | 6.4 | 64.4 | 0.52 | 0.43 | 40 | 139 | 0.7 | 18.4 | 9.7 | 1.3 | 1.11 | 17.5 | 5.3 | 3.7 |
| JXHZ389 | Eastern Han | 511 | 89.3 | 9.5 | 94 | 13.3 | 1.49 | 4.84 | 5.5 | 56.9 | 0.46 | 0.39 | 34 | 144 | 0.9 | 16.3 | 8.7 | 1.2 | 1.22 | 17.1 | 6.0 | 3.0 |
| No. | Date | Ba | Ce | Co | Cr | Cs | Eu | Fe2O3* | Hf | La | Lu | Na2O* | Nd | Rb | Sb | Sc | Sm | Ta | Tb | Th | U | Yb |
| JXHZ001 | Sui Dynasty | 769 | 113 | 9.3 | 74 | 17.0 | 1.45 | 3.29 | 14.5 | 66.4 | 0.58 | 0.34 | 47 | 208 | 1.5 | 14.6 | 8.9 | 2.7 | 1.47 | 31.5 | 7.5 | 4.2 |
| JXHZ002 | Sui Dynasty | 216 | 32.1 | 3.5 | 27 | 6.0 | 0.59 | 1.17 | 3.7 | 68.0 | 0.17 | 0.35 |  | 63 |  | 5.6 | 9.8 | 0.9 | 1.37 | 9.8 | 8.6 | 1.2 |
| JXHZ003 | Sui Dynasty | 437 | 43.9 | 5.3 | 38 | 7.0 | 1.10 | 1.74 | 5.3 | 62.7 | 0.27 | 0.37 |  | 129 | 1.2 | 7.9 | 8.5 | 1.8 | 0.66 | 12.0 | 6.6 | 1.2 |
| JXHZ004 | Sui Dynasty | 214 | 36.9 | 4.9 | 22 | 5.4 | 0.62 | 1.44 | 4.8 | 68.7 | 0.16 | 0.36 |  | 91 |  | 5.1 | 9.6 | 1.1 | 1.62 | 10.0 | 7.8 | 1.2 |
| JXHZ005 | Sui Dynasty | 316 | 28.5 | 4.6 | 22 | 4.9 | 0.61 | 1.11 |  | 64.5 | 0.17 | 0.42 |  | 72 | 1.1 | 5.5 | 8.9 | 0.8 | 1.66 | 8.5 | 7.3 | 1.2 |
| JXHZ006 | Sui Dynasty | 254 | 26.4 | 3.5 | 23 | 5.9 | 0.67 | 1.26 | 4.0 | 62.9 | 0.19 | 0.31 |  | 79 |  | 5.0 | 9.0 | 0.9 | 1.86 | 9.6 | 7.4 | 1.3 |
| JXHZ007 | Sui Dynasty | 855 | 121 | 8.5 | 86 | 16.5 | 1.82 | 2.87 | 9.5 | 72.4 | 0.59 | 0.37 | 56 | 204 | 1.7 | 17.0 | 9.9 | 2.4 | 1.42 | 27.6 | 6.2 | 3.9 |
| JXHZ008 | Sui Dynasty | 576 | 85.8 | 10.4 | 80 | 12.2 | 1.41 | 4.81 | 13.0 | 57.1 | 0.52 | 0.22 | 38 | 179 | 1.5 | 13.1 | 7.8 | 2.6 | 1.01 | 22.1 | 5.1 | 2.7 |
| JXHZ009 | Sui Dynasty | 710 | 117 | 10.9 | 77 | 16.3 | 1.63 | 3.06 | 13.0 | 71.5 | 0.67 | 0.46 | 51 | 225 | 1.5 | 15.3 | 10.1 | 2.9 | 1.46 | 33.2 | 7.7 | 3.8 |
| JXHZ010 | Sui Dynasty | 709 | 109 | 11.4 | 82 | 18.2 | 1.69 | 3.04 | 14.2 | 70.2 | 0.65 | 0.38 | 44 | 231 | 1.4 | 16.0 | 9.7 | 2.8 | 1.15 | 29.9 | 8.3 | 3.4 |
| JXHZ011 | Sui Dynasty | 398 | 98.5 | 7.2 | 78 | 10.1 | 1.51 | 2.33 | 9.5 | 60.7 | 0.54 | 0.25 | 47 | 123 | 1.3 | 14.5 | 8.2 | 1.9 | 1.24 | 18.1 | 5.1 | 4.5 |
| JXHZ012 | Sui Dynasty | 452 | 94.4 | 10.0 | 65 | 12.3 | 1.38 | 2.89 | 9.6 | 57.9 | 0.49 | 0.26 | 42 | 156 | 1.4 | 13.1 | 7.7 | 2.2 | 0.99 | 18.0 | 6.0 | 4.2 |
| JXHZ013 | Sui Dynasty | 525 | 105 | 10.5 | 75 | 13.5 | 1.49 | 3.66 | 8.9 | 62.0 | 0.54 | 0.37 | 50 | 177 | 1.3 | 14.6 | 8.3 | 2.2 | 1.13 | 18.7 | 6.1 | 4.6 |
| JXHZ014 | Sui Dynasty | 535 | 104 | 9.1 | 67 | 14.5 | 1.48 | 3.43 | 9.6 | 60.8 | 0.50 | 0.29 | 49 | 184 | 1.4 | 14.1 | 8.4 | 2.2 | 1.09 | 20.4 | 7.1 | 4.4 |
| JXHZ015 | Sui Dynasty | 574 | 108 | 10.2 | 71 | 14.9 | 1.63 | 2.54 | 10.3 | 66.9 | 0.56 | 0.42 | 51 | 200 | 1.2 | 15.1 | 9.1 | 2.3 | 1.23 | 22.5 | 7.5 | 4.9 |
| JXHZ016 | Sui Dynasty | 467 | 104 | 8.5 | 68 | 13.0 | 1.33 | 3.34 | 11.7 | 62.8 | 0.53 | 0.27 | 49 | 173 | 1.3 | 13.9 | 8.6 | 2.5 | 1.13 | 20.0 | 6.6 | 4.5 |
| JXHZ017 | Sui Dynasty | 492 | 106 | 10.2 | 65 | 12.1 | 1.45 | 2.70 | 11.5 | 63.2 | 0.51 | 0.35 | 50 | 166 | 1.4 | 13.2 | 8.6 | 2.1 | 1.11 | 20.2 | 7.0 | 4.3 |
| JXHZ018 | Sui Dynasty | 493 | 90.6 | 9.6 | 71 | 11.9 | 1.35 | 4.00 | 8.9 | 56.7 | 0.48 | 0.26 | 42 | 149 | 1.4 | 14.2 | 7.5 | 2.0 | 1.05 | 17.5 | 5.6 | 4.1 |
| JXHZ019 | Sui Dynasty | 635 | 115 | 10.7 | 76 | 15.1 | 1.64 | 3.54 | 8.7 | 68.4 | 0.54 | 0.39 | 55 | 204 | 1.3 | 15.4 | 9.5 | 2.4 | 1.21 | 22.9 | 7.5 | 4.7 |
| JXHZ020 | Sui Dynasty | 596 | 103 | 10.8 | 70 | 15.7 | 1.54 | 3.03 | 9.2 | 62.7 | 0.51 | 0.36 | 49 | 210 | 1.4 | 14.7 | 8.7 | 2.4 | 1.13 | 21.6 | 8.0 | 4.5 |
| JXHZ021 | Sui Dynasty | 518 | 100 | 8.4 | 83 | 12.9 | 1.46 | 4.16 | 8.0 | 62.0 | 0.52 | 0.22 | 47 | 157 | 1.2 | 16.4 | 8.1 | 2.2 | 1.14 | 20.4 | 6.3 | 4.5 |
| JXHZ022 | Sui Dynasty | 505 | 105 | 9.6 | 66 | 12.5 | 1.35 | 3.30 | 11.4 | 63.6 | 0.59 | 0.29 | 52 | 175 | 1.2 | 13.5 | 8.9 | 2.3 | 1.29 | 22.2 | 7.2 | 5.1 |
| JXHZ023 | Sui Dynasty | 579 | 98.4 | 9.3 | 67 | 14.6 | 1.45 | 3.03 | 11.7 | 61.1 | 0.52 | 0.34 | 47 | 207 | 1.2 | 14.0 | 8.3 | 2.2 | 1.09 | 19.8 | 7.0 | 4.2 |
| JXHZ024 | Sui Dynasty | 663 | 132 | 9.5 | 71 | 17.0 | 2.16 | 2.59 | 8.8 | 86.9 | 0.61 | 0.30 | 47 | 255 | 1.3 | 18.8 | 13.1 | 2.2 | 1.37 | 23.1 | 8.6 | 3.8 |
| JXHZ025 | Sui Dynasty | 599 | 107 | 11.6 | 72 | 15.3 | 1.48 | 3.30 | 9.0 | 64.6 | 0.52 | 0.36 | 49 | 204 | 1.3 | 15.0 | 8.8 | 2.4 | 1.09 | 21.8 | 7.2 | 4.4 |
| JXHZ026 | Sui Dynasty | 528 | 106 | 12.0 | 80 | 15.3 | 1.52 | 4.71 | 8.9 | 70.7 | 0.59 | 0.34 | 32 | 214 | 1.3 | 19.0 | 10.5 | 2.2 | 1.22 | 22.9 | 8.7 | 3.9 |
| JXHZ027 | Sui Dynasty | 512 | 104 | 9.9 | 74 | 13.3 | 1.55 | 3.39 | 8.1 | 64.0 | 0.49 | 0.24 | 49 | 168 | 1.4 | 14.4 | 8.8 | 2.0 | 1.14 | 20.0 | 6.8 | 4.4 |
| No. | Date | Ba | Ce | Co | Cr | Cs | Eu | Fe2O3* | Hf | La | Lu | Na2O* | Nd | Rb | Sb | Sc | Sm | Ta | Tb | Th | U | Yb |
| JXHZ189 | Tang Dynasty | 728 | 113 | 13.9 | 87 | 22.8 | 1.68 | 4.40 | 7.7 | 79.5 | 0.56 | 0.39 | 36 | 303 | 1.4 | 20.2 | 10.9 | 2.1 | 1.35 | 24.1 | 10.8 | 4.2 |
| JXHZ190 | Tang Dynasty | 626 | 127 | 13.3 | 83 | 19.0 | 2.01 | 4.43 | 7.9 | 66.3 | 0.69 | 0.26 | 61 | 229 | 1.5 | 17.0 | 6.3 | 2.6 | 1.80 | 24.2 | 6.4 | 5.6 |
| JXHZ191 | Tang Dynasty | 672 | 123 | 15.0 | 83 | 20.2 | 1.82 | 4.56 | 7.6 | 63.9 | 0.58 | 0.20 | 54 | 256 | 1.5 | 17.2 | 5.8 | 2.8 | 1.37 | 24.3 | 6.1 | 5.2 |
| JXHZ192 | Tang Dynasty | 663 | 127 | 17.7 | 76 | 19.7 | 1.78 | 5.27 | 7.7 | 63.1 | 0.58 | 0.20 | 55 | 245 | 1.5 | 16.7 | 5.9 | 2.8 | 1.39 | 24.7 | 6.3 | 5.1 |
| JXHZ193 | Tang Dynasty | 571 | 126 | 8.1 | 86 | 14.4 | 1.23 | 2.56 | 6.2 | 64.1 | 0.60 | 0.21 | 61 | 127 | 0.8 | 14.1 | 6.0 | 1.4 | 1.00 | 23.2 | 4.9 | 5.1 |
| JXHZ194 | Tang Dynasty | 460 | 123 | 9.8 | 80 | 15.5 | 2.30 | 3.24 | 7.1 | 65.7 | 0.64 | 0.17 | 58 | 151 | 0.9 | 12.9 | 6.6 | 1.8 | 0.94 | 23.2 | 6.1 | 5.5 |
| JXHZ195 | Tang Dynasty | 608 | 124 | 9.1 | 82 | 15.8 | 1.35 | 2.13 | 6.6 | 63.6 | 0.57 | 0.23 | 56 | 162 | 1.1 | 14.7 | 6.0 | 1.9 | 1.61 | 23.2 | 5.1 | 4.8 |
| JXHZ196 | Tang Dynasty | 698 | 115 | 11.7 | 88 | 21.3 | 1.78 | 5.53 | 6.7 | 78.4 | 0.62 | 0.20 | 59 | 244 | 1.4 | 17.7 | 10.6 | 2.7 | 1.44 | 25.7 | 11.0 | 5.1 |
| JXHZ197 | Tang Dynasty | 648 | 121 | 11.6 | 82 | 21.2 | 1.59 | 5.41 | 7.1 | 78.7 | 0.62 | 0.24 | 60 | 241 | 1.3 | 16.4 | 10.8 | 2.8 | 1.34 | 25.9 | 11.9 | 5.3 |
| JXHZ198 | Tang Dynasty | 737 | 131 | 12.2 | 89 | 19.4 | 1.80 | 3.97 | 7.4 | 78.4 | 0.60 | 0.37 | 60 | 243 | 1.6 | 17.8 | 10.6 | 2.8 | 1.31 | 26.0 | 9.8 | 5.1 |
| JXHZ199 | Tang Dynasty | 630 | 126 | 13.0 | 86 | 16.9 | 1.92 | 4.17 | 7.7 | 82.7 | 0.66 | 0.33 | 42 | 207 | 1.4 | 17.2 | 11.8 | 2.3 | 1.31 | 23.9 | 9.5 | 4.3 |
| JXHZ200 | Tang Dynasty | 618 | 118 | 14.2 | 69 | 17.8 | 1.64 | 5.19 | 8.4 | 75.0 | 0.66 | 0.29 | 55 | 233 | 1.2 | 15.0 | 10.6 | 2.7 | 1.43 | 23.7 | 11.2 | 5.2 |
| JXHZ201 | Tang Dynasty | 722 | 122 | 9.5 | 85 | 17.6 | 1.80 | 3.07 | 7.0 | 74.9 | 0.62 | 0.33 | 57 | 227 | 1.4 | 17.5 | 10.5 | 2.4 | 1.29 | 24.0 | 9.4 | 5.4 |
| JXHZ202 | Tang Dynasty | 598 | 125 | 14.0 | 81 | 18.9 | 1.85 | 4.19 | 7.4 | 75.9 | 0.62 | 0.30 | 57 | 233 | 1.3 | 17.3 | 10.6 | 2.7 | 1.18 | 25.0 | 10.0 | 5.4 |
| JXHZ203 | Tang Dynasty | 611 | 117 | 12.0 | 76 | 15.6 | 1.60 | 3.74 | 9.8 | 73.5 | 0.67 | 0.38 | 35 | 215 | 1.2 | 14.5 | 10.8 | 2.2 | 1.19 | 23.0 | 9.9 | 4.2 |
| JXHZ204 | Tang Dynasty | 565 | 123 | 12.3 | 84 | 18.2 | 2.01 | 4.60 | 7.3 | 73.6 | 0.69 | 0.25 | 59 | 203 | 1.6 | 17.3 | 10.7 | 2.5 | 1.50 | 23.8 | 9.7 | 5.3 |
| JXHZ205 | Tang Dynasty | 685 | 131 | 14.4 | 83 | 18.4 | 2.03 | 5.07 | 8.3 | 81.0 | 0.66 | 0.36 | 61 | 245 | 1.5 | 17.6 | 11.0 | 2.7 | 1.54 | 24.1 | 9.8 | 5.2 |
| JXHZ206 | Tang Dynasty | 661 | 123 | 16.3 | 78 | 19.0 | 1.87 | 4.94 | 8.1 | 75.0 | 0.65 | 0.30 | 54 | 235 | 1.4 | 16.4 | 10.8 | 2.5 | 1.67 | 24.1 | 10.8 | 5.7 |
| JXHZ207 | Tang Dynasty | 673 | 129 | 15.1 | 74 | 18.1 | 1.94 | 4.46 | 7.3 | 76.5 | 0.61 | 0.23 | 58 | 218 | 1.6 | 16.1 | 10.7 | 2.6 | 1.42 | 22.8 | 10.0 | 5.3 |
| JXHZ208 | Tang Dynasty | 680 | 117 | 11.8 | 78 | 18.6 | 1.76 | 3.91 | 8.0 | 71.2 | 0.60 | 0.32 | 53 | 243 | 1.7 | 16.7 | 10.0 | 2.8 | 1.20 | 23.6 | 9.3 | 5.0 |
| JXHZ210 | Tang Dynasty | 698 | 122 | 13.0 | 89 | 17.5 | 1.59 | 4.11 | 7.3 | 76.0 | 0.57 | 0.40 | 40 | 233 | 1.4 | 17.9 | 11.2 | 2.3 | 1.26 | 25.2 | 9.9 | 3.8 |
| JXHZ211 | Tang Dynasty | 637 | 125 | 16.0 | 82 | 19.1 | 2.05 | 5.04 | 7.5 | 80.0 | 0.62 | 0.24 | 62 | 233 | 1.0 | 16.8 | 11.0 | 2.8 | 1.42 | 23.6 | 10.4 | 5.2 |
| JXHZ212 | Tang Dynasty | 622 | 122 | 13.1 | 83 | 21.8 | 1.81 | 5.93 | 6.6 | 79.4 | 0.61 | 0.18 | 56 | 261 | 1.7 | 18.0 | 10.6 | 2.5 | 1.42 | 24.5 | 11.0 | 5.0 |
| JXHZ213 | Tang Dynasty | 679 | 134 | 15.4 | 81 | 19.9 | 1.99 | 5.37 | 7.4 | 82.4 | 0.63 | 0.26 | 64 | 226 | 1.3 | 17.3 | 11.6 | 2.6 | 1.64 | 24.1 | 10.9 | 5.5 |
| JXHZ214 | Tang Dynasty | 643 | 122 | 15.2 | 79 | 19.6 | 1.79 | 5.53 | 7.5 | 77.6 | 0.61 | 0.24 | 57 | 234 | 1.6 | 16.7 | 10.9 | 2.6 | 1.58 | 24.4 | 11.0 | 5.4 |
| JXHZ215 | Tang Dynasty | 652 | 119 | 13.9 | 71 | 19.5 | 1.70 | 5.39 | 8.0 | 76.1 | 0.58 | 0.29 | 56 | 247 | 1.1 | 16.0 | 10.6 | 2.8 | 1.60 | 23.3 | 11.0 | 5.4 |
| JXHZ216 | Tang Dynasty | 683 | 135 | 18.8 | 90 | 20.2 | 2.01 | 6.59 | 6.0 | 86.3 | 0.57 | 0.19 | 59 | 244 | 1.2 | 18.2 | 10.9 | 2.6 | 1.40 | 23.7 | 11.0 | 5.1 |
| JXHZ217 | Tang Dynasty | 630 | 130 | 14.7 | 81 | 19.1 | 1.94 | 5.30 | 7.6 | 80.4 | 0.61 | 0.30 | 56 | 228 | 1.7 | 17.0 | 11.2 | 2.5 | 1.60 | 24.9 | 11.0 | 5.2 |
| JXHZ218 | Tang Dynasty | 606 | 121 | 16.0 | 79 | 19.2 | 1.87 | 5.76 | 7.7 | 75.8 | 0.59 | 0.28 | 55 | 230 | 1.2 | 16.1 | 10.3 | 2.7 | 1.48 | 24.8 | 11.4 | 5.3 |
| JXHZ219 | Tang Dynasty | 602 | 118 | 14.3 | 72 | 18.4 | 1.96 | 5.16 | 8.8 | 74.3 | 0.59 | 0.32 | 54 | 233 | 1.2 | 15.4 | 10.5 | 2.6 | 1.22 | 24.1 | 10.9 | 5.0 |

Table B4. The chemical composition of the clay body of celadons from Wuzhou kiln [4].

| Time period | Location | SiO2 | A2O3 | CaO | MgO | K2O | Na2O | FeO | TiO2 | P2O5 | MnO | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tang | LYFT | 67.37 | 20.67 | 0.9 | 0.77 | 5.98 | 1.76 | 2.12 | 0.38 | 0.02 | 0.03 | 100 |
| Tang | JSLL | 70.56 | 19.35 | 0.35 | 0.66 | 5.08 | 0.56 | 3.14 | 0.25 | 0.02 | 0.04 | 100 |
| Tang | JHHZ | 69.36 | 19.94 | 0.71 | 0.65 | 5.1 | 1.69 | 2.25 | 0.25 | 0.02 | 0.05 | 100 |
| Song | QZDGT | 58 | 33.74 | 0.09 | 1 | 3.13 | 0.1 | 3.46 | 0.39 | 0.04 | 0.04 | 100 |
| Yuan | JYT1 | 69.65 | 20.83 | 0.13 | 1.56 | 4.18 | 0.11 | 3.21 | 0.27 | 0.02 | 0.03 | 100 |
| Yuan | JHTD | 71.31 | 19.46 | 0.16 | 0.99 | 4.11 | 0.2 | 3.32 | 0.36 | 0.04 | 0.04 | 100 |
| Yuan | JSYJS | 69.38 | 22.36 | 0.27 | 1.2 | 3.44 | 0.1 | 2.96 | 0.24 | 0.03 | 0.03 | 100 |
| Song-Yuan | JSWY | 70.58 | 21.96 | 0.16 | 0.6 | 3.86 | 0.08 | 2.49 | 0.29 | 0.03 | 0.02 | 100 |
| Ming | LYGC | 75.75 | 16.68 | 0.17 | 0.62 | 3.41 | 0.22 | 2.81 | 0.29 | 0.02 | 0.05 | 100 |

Table B5. The chemical composition of the glaze of celadons from Wuzhou kiln [4].

| Time period | Location | SiO2 | A2O3 | CaO | MgO | K2O | Na2O | FeO | TiO2 | P2O5 | MnO | Total |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tang | LYFT | 55.42 | 10.81 | 21.36 | 3.96 | 2.09 | 0.74 | 2.28 | 0.62 | 2.03 | 0.69 | 100 |
| Tang | JSLL | 57.6 | 12.61 | 19.27 | 3.01 | 2.28 | 0.3 | 2.61 | 0.57 | 1.07 | 0.67 | 100 |
| Tang | JHHZ | 59.63 | 12.15 | 17.9 | 2.6 | 1.66 | 0.62 | 2.87 | 0.74 | 1.32 | 0.51 | 100 |
| Song | QZDGT | 54.22 | 14 | 19.56 | 3.1 | 2.4 | 0.17 | 3.5 | 0.58 | 1.55 | 0.97 | 100 |
| Yuan | JYT1 | 59.32 | 10.35 | 18.51 | 3.54 | 2.35 | 0.14 | 2.74 | 0.59 | 1.5 | 0.96 | 100 |
| Yuan | JHTD | 61.38 | 12.6 | 14.78 | 3.2 | 2.58 | 0.26 | 2.86 | 0.53 | 1.01 | 0.82 | 100 |
| Yuan | JSYJS | 62.56 | 12.12 | 14.02 | 2.37 | 1.95 | 0.09 | 4.6 | 0.53 | 1.06 | 0.7 | 100 |
| Song-Yuan | JSWY | 64.94 | 16.84 | 10.99 | 1.02 | 3.91 | 0.12 | 1.86 | 0.12 | 0.09 | 0.12 | 100 |
| Ming | LYGC | 59.05 | 14.06 | 15.53 | 3.5 | 2.52 | 0.25 | 2.39 | 0.43 | 1.38 | 0.88 | 100 |

Table B6. The chemical composition of the clay body of celadons from Yue kiln [5].

| No. | Na2O | MgO | Al2O3 | SiO2 | K2O | CaO | TiO2 | MnO | Fe2O3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| hyt - 1 | 1.25 | 0.45 | 15.95 | 76.17 | 2.4 | 0.52 | 0.84 | 0.05 | 2.29 |
| hyt -3 | 0.77 | 0.42 | 16.54 | 76.41 | 2.87 | 0.42 | 0.84 | 0.02 | 1.73 |
| hyt-2 | 0.64 | 0.32 | 14.92 | 78.05 | 3.36 | 0.37 | 0.78 | 0.01 | 1.57 |
| hys - 1 | 0.76 | 0.36 | 15.23 | 77.53 | 2.8 | 0.44 | 0.82 | 0.04 | 2.04 |
| hys -2 | 1.43 | 0.51 | 15.35 | 76.81 | 2.78 | 0.4 | 0.76 | 0.04 | 1.93 |
| hys -3 | 0.74 | 0.37 | 15.53 | 77.59 | 2.92 | 0.42 | 0.73 | 0.01 | 1.72 |
| pd41 -1 | 1.02 | 0.38 | 16.44 | 76.36 | 2.74 | 0.42 | 0.78 | 0.01 | 1.86 |
| pd41 -2 | 1.2 | 0.42 | 16.3 | 76.3 | 2.99 | 0.43 | 0.69 | 0.02 | 1.66 |
| pd41 -3 | 0.69 | 0.37 | 16.2 | 76.54 | 3.2 | 0.53 | 0.71 | 0.01 | 1.76 |
| pd43 -1 | 0.69 | 0.28 | 15.29 | 77 | 3.21 | 0.55 | 0.87 | 0.04 | 2.08 |
| pd43-2 | 0.55 | 0.44 | 15.28 | 77.78 | 2.84 | 0.43 | 0.72 | 0.02 | 1.94 |
| pd43-3 | 1.18 | 0.38 | 14.88 | 77.56 | 2.83 | 0.52 | 0.8 | 0.05 | 1.82 |
| DLTEP-47 | 0.71 | 0.35 | 17.28 | 75.67 | 2.99 | 0.35 | 0.79 | 0.01 | 1.86 |
| DLTEP-29 | 0.96 | 0.4 | 17.47 | 74.84 | 3.2 | 0.38 | 0.75 | 0.03 | 1.99 |
| DLTEP -17 | 0.74 | 0.36 | 15.96 | 76.75 | 2.93 | 0.47 | 0.81 | 0.03 | 1.95 |
| DLTEP-0 | 0.69 | 0.39 | 17.41 | 74.83 | 3.35 | 0.43 | 0.81 | 0.01 | 2.08 |
| GTJSLH -1 | 0.96 | 0.36 | 15.8 | 77.01 | 2.85 | 0.47 | 0.79 | 0.04 | 1.72 |
| GTJSLH -14 | 1.26 | 0.42 | 17.27 | 74.68 | 3.07 | 0.49 | 0.79 | 0.03 | 2 |
| GTJSLH-2 | 1.36 | 0.48 | 16.01 | 75.67 | 3.34 | 0.43 | 0.84 | 0.01 | 1.86 |
| GTJSLH-21 | 0.75 | 0.42 | 17.42 | 75.09 | 3.06 | 0.43 | 0.75 | 0.03 | 2.05 |
| GTJSLH-26 | 1.1 | 0.49 | 16.78 | 75.35 | 2.92 | 0.57 | 0.79 | 0.03 | 1.97 |
| GTJSLH-27 | 0.87 | 0.44 | 17.23 | 75.59 | 2.79 | 0.46 | 0.77 | 0.02 | 1.83 |
| GTJSLH-3 | 0.89 | 0.46 | 17.81 | 74.81 | 2.93 | 0.44 | 0.74 | 0.02 | 1.9 |
| GTJSLH-6 | 0.46 | 0.38 | 17.34 | 75.42 | 3.04 | 0.46 | 0.8 | 0.02 | 2.08 |
| GTJSLH-7 | 1.17 | 0.57 | 16.33 | 76.06 | 2.68 | 0.47 | 0.79 | 0.01 | 1.93 |
| GTJSLH-8 | 0.71 | 0.41 | 16.28 | 76.87 | 2.65 | 0.48 | 0.78 | 0.03 | 1.8 |
| shl | 1.01 | 0.33 | 16.25 | 76.96 | 2.68 | 0.29 | 0.8 | 0.02 | 1.66 |
| sh2 | 0.74 | 0.29 | 16.46 | 76.54 | 2.81 | 0.35 | 0.78 | 0.02 | 2.03 |
| sh3 | 0.6 | 0.27 | 16.48 | 76.91 | 2.55 | 0.35 | 0.85 | 0.02 | 1.97 |
| sh4 | 0.7 | 0.25 | 15.72 | 76.93 | 3.04 | 0.39 | 0.97 | 0.01 | 1.99 |
| sh5 | 0.79 | 0.17 | 15.7 | 77.71 | 3.07 | 0.31 | 0.78 | 0.01 | 1.47 |
| WPYY-1 | 0.56 | 0.34 | 16.15 | 77.25 | 2.65 | 0.37 | 0.8 | 0.03 | 1.85 |
| WPYY-11 | 0.43 | 0.35 | 15.95 | 77.71 | 2.75 | 0.35 | 0.84 | 0.03 | 1.55 |
| WPYY -12 | 0.18 | 0.11 | 15.47 | 77.98 | 3.17 | 0.54 | 0.87 | 0.01 | 1.67 |
| WPYY-2 | 0.95 | 0.28 | 14.69 | 78.63 | 2.86 | 0.29 | 0.78 | 0.01 | 1.42 |
| WPYY-3 | 0.67 | 0.21 | 16.25 | 77.14 | 2.92 | 0.45 | 0.94 | 0.01 | 1.43 |
| WPYY-4 | 0.79 | 0.38 | 16.27 | 77 | 2.6 | 0.46 | 0.86 | 0.02 | 1.62 |
| WPYY-6 | 0.31 | 0.25 | 16.64 | 77.73 | 2.5 | 0.3 | 0.78 | 0.03 | 1.47 |
| WPYY-7 | 0.69 | 0.28 | 15.99 | 77.43 | 2.84 | 0.35 | 0.8 | 0.01 | 1.62 |
| YC04 | 0.84 | 0.37 | 16.01 | 76.55 | 3.09 | 0.67 | 0.79 | 0.01 | 1.6 |
| YC05 | 0.64 | 0.26 | 16.4 | 77.03 | 2.82 | 0.35 | 0.73 | 0.02 | 1.76 |
| YC06 | 0.72 | 0.34 | 16.09 | 76.78 | 3.08 | 0.37 | 0.84 | 0.01 | 1.75 |
| YC07 | 0.82 | 0.33 | 16.06 | 75.84 | 3.27 | 0.57 | 0.79 | 0.04 | 2.29 |
| YC09 | 0.14 | 0.2 | 16.17 | 77.53 | 3 | 0.46 | 0.78 | 0.02 | 1.69 |
| YC11 | 1.24 | 0.43 | 16.25 | 76.43 | 2.88 | 0.45 | 0.75 | 0.02 | 1.53 |
| YC12 | 0.83 | 0.37 | 16.35 | 76.01 | 3.06 | 0.4 | 0.75 | 0.02 | 2.18 |
| YC13 | 0.47 | 0.27 | 16.09 | 76.98 | 3.07 | 0.52 | 0.76 | 0.04 | 1.81 |
| YC14 | 0.98 | 0.38 | 16.32 | 76.39 | 2.97 | 0.51 | 0.72 | 0.02 | 1.71 |

Table B7. The chemical composition of the glaze of celadons from Yue kiln [5].

| No. | Na2O | MgO | Al2O3 | SiO2 | K2O | CaO | TiO2 | MnO | Fe2O3 | P2O5 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| hhx - y37 - 2w | 0.24 | 1.39 | 11.67 | 61.47 | 1.23 | 18.46 | 0.28 | 0.67 | 2.77 | 1.28 |
| hhx - y37 - 1w | 0.12 | 1.41 | 13.01 | 62.06 | 1.25 | 17.22 | 0.29 | 0.86 | 2.03 | 1.55 |
| hhx - y37 -5w | 0.28 | 1.19 | 11.75 | 63.83 | 1.64 | 17.34 | 0.26 | 0.44 | 1.35 | 1.19 |
| hyt - 1 | 0.19 | 1.77 | 11.85 | 58.28 | 1.46 | 18.16 | 0.3 | 0.86 | 3.17 | 1.61 |
| hyt — 3 | 0.21 | 1.56 | 12.47 | 60.99 | 1.41 | 17.78 | 0.28 | 0.46 | 2.77 | 1.54 |
| hys -1 | 0.18 | 1.86 | 11.58 | 53.16 | 3.49 | 22.99 | 0.26 | 0.83 | 2.74 | 1.91 |
| hys -2 | 0.23 | 1.87 | 12.39 | 56.31 | 1.69 | 21.72 | 0.27 | 0.82 | 2.18 | 2.32 |
| hys -3 | 0.36 | 2.04 | 13.44 | 59.53 | 1.75 | 17.45 | 0.26 | 0.53 | 1.87 | 2.77 |
| pd41 -1 | 0.35 | 1.84 | 13.55 | 58.05 | 1.45 | 19.19 | 0.28 | 0.72 | 2.63 | 1.61 |
| pd41 -2 | 0.37 | 1.66 | 12.27 | 59.14 | 1.4 | 19.55 | 0.27 | 0.68 | 2.38 | 2.04 |
| pd41 -3 | 0.15 | 1.47 | 11.78 | 60.61 | 1.63 | 18.87 | 0.27 | 0.5 | 2.36 | 2.22 |
| pd43 -1 | 0.34 | 1.92 | 11.01 | 60.7 | 1.46 | 18.89 | 0.25 | 0.85 | 1.95 | 2.48 |
| pd43-2 | 0.1 | 1.67 | 11.85 | 60.04 | 1.5 | 18.92 | 0.27 | 0.94 | 1.84 | 2.7 |
| pd43-3 | 0.22 | 1.8 | 12.19 | 63.56 | 1.66 | 14.59 | 0.29 | 1.12 | 1.99 | 2.45 |
| pd43 - 4 | 0.16 | 1.96 | 11.56 | 59.8 | 1.22 | 19.01 | 0.27 | 0.68 | 2.86 | 2.4 |
| pd43-5 | 0.06 | 1.7 | 11.59 | 60.15 | 1.29 | 19.27 | 0.25 | 0.88 | 2.46 | 2.35 |
| pd43 -6 | 0.04 | 1.64 | 11.76 | 62.98 | 1.23 | 17.32 | 0.26 | 1.05 | 1.43 | 2.3 |
| dltep -47 | 0.09 | 1.27 | 12.65 | 63.89 | 1.78 | 16.86 | 0.11 | 0.72 | 1.47 | 1.16 |
| dltep - 29 | 0.01 | 0.8 | 13.29 | 62.52 | 2.45 | 17.05 | 0.11 | 0.92 | 1.6 | 1.27 |
| dltep - 17 | 0.31 | 1.29 | 12.74 | 64.02 | 2 | 15.94 | 0.14 | 0.66 | 1.77 | 1.11 |
| dltep - 0 | 0.13 | 1.15 | 12.24 | 63.69 | 2.18 | 16.89 | 0.11 | 0.74 | 1.29 | 1.61 |
| GTJSLH -1 | 0.13 | 1.4 | 12.38 | 66.9 | 1.81 | 12.48 | 0.28 | 0.69 | 2.22 | 1.72 |
| GTJSLH -14 | 0.14 | 1.59 | 12.05 | 61.24 | 1.51 | 17.57 | 0.27 | 0.8 | 2.5 | 1.86 |
| GTJSLH-2 | 0.1 | 1.34 | 12.57 | 64.24 | 1.7 | 15.52 | 0.31 | 0.44 | 1.95 | 1.61 |
| GTJSLH-21 | 0.09 | 1.36 | 13.97 | 60.93 | 1.52 | 17.75 | 0.28 | 0.5 | 1.93 | 1.55 |
| GTJSLH-26 | 0.2 | 1.82 | 12.13 | 60.34 | 1.26 | 18.41 | 0.26 | 0.56 | 2.78 | 2.16 |
| GTJSLH-27 | 0.22 | 1.09 | 11.31 | 64.14 | 3.05 | 17.22 | 0.23 | 0.28 | 1.3 | 1.16 |
| GTJSLH-3 | 0.31 | 1.7 | 12.73 | 61.13 | 1.4 | 18.09 | 0.25 | 0.57 | 1.98 | 1.84 |
| GTJSLH-6 | 0.23 | 1.6 | 12.69 | 61.98 | 1.46 | 17.44 | 0.28 | 0.64 | 1.86 | 1.78 |
| GTJSLH-7 | 0.38 | 1.66 | 12.98 | 61.15 | 1.24 | 17.96 | 0.31 | 0.73 | 1.94 | 1.63 |
| GTJSLH-8 | 0.25 | 1.63 | 11.74 | 62.15 | 1.34 | 16.99 | 0.29 | 0.82 | 2.49 | 1.93 |
| shl | 0.21 | 1.18 | 11.33 | 66.26 | 2.67 | 14.15 | 0.23 | 0.56 | 2.13 | 1.12 |
| sh2 | 0.04 | 1.51 | 12.49 | 62.55 | 1.27 | 16.31 | 0.29 | 0.78 | 2.38 | 2.39 |
| sh3 | 0.31 | 1.5 | 13.29 | 61.14 | 2.42 | 16.51 | 0.29 | 0.71 | 2.41 | 1.42 |
| sh4 | 0.17 | 1.68 | 11.74 | 60.54 | 1.3 | 19.34 | 0.28 | 0.69 | 2.07 | 2.19 |
| sh5 | 0.23 | 1.15 | 12.48 | 66.19 | 1.65 | 14.01 | 0.28 | 0.36 | 2.3 | 1.34 |
| WPYY-1 | 0.27 | 1.74 | 11.73 | 60.94 | 1.53 | 18.42 | 0.32 | 0.44 | 2.15 | 2.27 |
| WPYY -11 | 0.31 | 1.56 | 11.37 | 59.2 | 1.21 | 21.52 | 0.31 | 0.4 | 1.69 | 2.45 |
| WPYY -12 | 0.21 | 1.93 | 11.86 | 60.37 | 1.22 | 19.47 | 0.3 | 0.48 | 1.65 | 2.52 |
| WPYY-2 | 0.26 | 1.78 | 11.79 | 61.03 | 1.34 | 18.26 | 0.3 | 0.36 | 2.4 | 2.44 |
| WPYY-3 | 0.1 | 1.2 | 11.8 | 60.53 | 1.26 | 21.17 | 0.3 | 0.36 | 1.77 | 1.52 |
| WPYY-4 | 0.06 | 1.2 | 10.67 | 65.32 | 1.22 | 16.59 | 0.32 | 0.48 | 2.45 | 1.69 |
| WPYY-6 | 0.18 | 1.2 | 12.36 | 62.55 | 1.17 | 18.55 | 0.31 | 0.4 | 1.56 | 1.71 |
| WPYY-7 | 0.17 | 1.61 | 10.89 | 60.52 | 1.28 | 20.9 | 0.32 | 0.43 | 1.36 | 2.52 |
| YC04 | 0.23 | 1.13 | 12.73 | 63.5 | 1.6 | 16.72 | 0.31 | 0.39 | 2.12 | 1.2 |
| YC05 | 0.08 | 1.27 | 12.87 | 62.15 | 1.48 | 18.31 | 0.27 | 0.41 | 1.72 | 1.41 |
| YC06 | 0.18 | 1.55 | 13.67 | 63.34 | 1.46 | 14.81 | 0.29 | 0.32 | 2.26 | 1.76 |
| YC07 | 0.19 | 1.64 | 13.51 | 58.6 | 1.2 | 19.62 | 0.28 | 0.5 | 2.43 | 1.78 |
| YC09 | 0.34 | 1.56 | 12.81 | 61.09 | 1.49 | 18.54 | 0.28 | 0.39 | 2.19 | 1.11 |
| YC11 | 0.41 | 1.4 | 13.57 | 63.24 | 1.82 | 15.53 | 0.3 | 0.46 | 1.95 | 1.19 |
| YC12 | 0.31 | 2.07 | 12.18 | 57.21 | 1.36 | 20.9 | 0.27 | 0.68 | 2.7 | 2.31 |
| YC13 | 0.21 | 1.22 | 12.89 | 61.57 | 1.42 | 18.55 | 0.27 | 0.46 | 1.84 | 1.57 |
| YC14 | 0.22 | 1.35 | 13.03 | 62.68 | 1.52 | 16.48 | 0.28 | 0.42 | 2.06 | 1.76 |

Table B8. The chemical composition of the clay body of celadons from Shouzhou kiln [6].

| No. | Na2O | MgO | Al2O3 | SiO2 | P2O5 | K2O | CaO | TiO2 | MnO | Fe2O3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S-l | 0.59 | 0.56 | 23 | 68.44 | 0.09 | 1.57 | 0.52 | 1.12 | 0.03 | 3.16 |
| S-2 | 0.8 | 0.56 | 22.98 | 68.98 | 0.15 | 1.31 | 0.48 | 1.18 | 0.06 | 2.65 |
| S—3 | 0.59 | 0.6 | 24.49 | 66.85 | 0.1 | 1.72 | 0.61 | 1.25 | 0.03 | 2.86 |
| S—4 | 0.67 | 0.58 | 22.81 | 68.41 | 0.12 | 1.53 | 0.5 | 1.32 | 0.04 | 3.14 |
| S—5 | 0.93 | 0.54 | 23.79 | 66.68 | 0.11 | 1.82 | 0.58 | 1.18 | 0.05 | 3.44 |
| S—6 | 0.82 | 0.55 | 23.07 | 67.39 | 0.13 | 1.64 | 0.71 | 1.09 | 0.04 | 3.68 |
| S—7 | 0.71 | 0.49 | 23.97 | 67.29 | 0.09 | 1.96 | 0.6 | 1.28 | 0.05 | 2.64 |
| S—8 | 0.74 | 0.78 | 24.25 | 65.11 | 0.1 | 1.6 | 0.77 | 1.19 | 0.07 | 4.51 |
| S—9 | 0.83 | 0.64 | 24.49 | 66.04 | 0.18 | 1.73 | 0.52 | 1.18 | 0.05 | 3.53 |
| S-10 | 0.72 | 0.82 | 21.63 | 68.86 | 0.16 | 2.07 | 0.67 | 1.01 | 0.08 | 3.14 |
| S—11 | 0.89 | 0.75 | 25.21 | 66.28 | 0.12 | 1.7 | 0.53 | 1.26 | 0.06 | 2.32 |
| S—12 | 0.43 | 0.67 | 24.2 | 66.63 | 0.24 | 1.79 | 1.02 | 1.35 | 0.1 | 2.81 |
| S—13 | 0.43 | 0.61 | 24.99 | 65.36 | 0.13 | 1.56 | 0.75 | 1.39 | 0.11 | 3.8 |
| S—14 | 0.95 | 0.55 | 25.77 | 63.99 | 0.1 | 1.84 | 0.58 | 1.22 | 0.11 | 3.97 |
| S—15 | 0.4 | 0.55 | 25.78 | 65.69 | 0.08 | 1.59 | 0.81 | 1 | 0.06 | 3.12 |
| S—16 | 0.41 | 0.51 | 26.18 | 66.13 | 0.16 | 1.2 | 0.52 | 1.21 | 0.07 | 2.77 |
| S—17 | 0.71 | 0.67 | 25.32 | 64.59 | 0.14 | 1.48 | 0.48 | 1.23 | 0.19 | 4.34 |
| S—18 | 0.63 | 1.01 | 26.86 | 64.02 | 0.14 | 1.74 | 0.55 | 1.02 | 0.03 | 3.15 |
| S—19 | 1.01 | 0.74 | 23.58 | 65.87 | 0.14 | 1.83 | 0.56 | 1.57 | 0.08 | 3.76 |
| S—20 | 0.86 | 0.56 | 23.01 | 68.21 | 0.12 | 1.5 | 0.79 | 1.21 | 0.05 | 2.81 |
| S—21 | 0.96 | 0.95 | 20.8 | 68.82 | 0.1 | 2.26 | 0.69 | 0.96 | 0.09 | 3.47 |
| S—22 | 0.94 | 1.04 | 24.96 | 65.02 | 0.16 | 2.15 | 0.6 | 0.86 | 0.07 | 3.36 |
| S—23 | 1.09 | 0.53 | 22.2 | 68.15 | 0.14 | 1.68 | 0.76 | 1.09 | 0.08 | 3.41 |
| S—24 | 0.43 | 0.69 | 23.9 | 65.23 | 0.1 | 1.62 | 0.89 | 1.13 | 0.08 | 5.02 |
| S—25 | 0.63 | 0.85 | 23.12 | 67.06 | 0.08 | 1.46 | 0.93 | 1.03 | 0.05 | 3.88 |
| S—26 | 1.27 | 0.6 | 19.89 | 70.01 | 0.14 | 2.54 | 0.62 | 0.86 | 0.12 | 3.1 |
| S—27 | 0.58 | 0.6 | 24.2 | 66.23 | 0.08 | 1.88 | 0.67 | 1.02 | 0.09 | 3.73 |
| S—28 | 0.8 | 0.5 | 20.81 | 68.87 | 0.15 | 1.66 | 1.22 | 1.19 | 0.19 | 3.76 |
| S—29 | 1.05 | 0.57 | 23.01 | 67.55 | 0.18 | 1.4 | 0.65 | 1.56 | 0.06 | 3.16 |
| S—30 | 0.83 | 0.55 | 23.38 | 66.56 | 0.04 | 1.85 | 0.57 | 1.09 | 0.09 | 4.08 |
| S—31 | 0.69 | 0.7 | 21.49 | 69.43 | 0.12 | 1.48 | 0.75 | 1.07 | 0.07 | 3.31 |
| S—32 | 0.84 | 0.73 | 26.59 | 64.14 | 0.14 | 1.31 | 0.76 | 1.29 | 0.05 | 3.29 |
| S—33 | 0.42 | 0.71 | 24.61 | 66.24 | 0.1 | 1.5 | 0.94 | 1.16 | 0.04 | 3.38 |
| S—34 | 0.72 | 0.83 | 24.38 | 65.55 | 0 | 1.78 | 0.89 | 1.2 | 0.08 | 3.57 |
| S—35 | 0.92 | 0.52 | 20.62 | 71.95 | 0.17 | 1.42 | 0.33 | 0.82 | 0.03 | 2.4 |
| S—36 | 0.58 | 0.41 | 22.68 | 70.07 | 0.23 | 1.11 | 0.51 | 1.11 | 0.07 | 2.47 |
| S—37 | 0.58 | 0.72 | 27.68 | 63.5 | 0.14 | 2.11 | 0.6 | 1.25 | 0.02 | 2.54 |
| S—38 | 0.75 | 0.69 | 22.05 | 68.42 | 0.13 | 1.48 | 0.7 | 1.15 | 0.08 | 3.68 |
| S—39 | 0.72 | 0.78 | 25.29 | 66.33 | 0.14 | 1.7 | 0.45 | 1.21 | 0.04 | 2.47 |
| S—40 | 0.95 | 0.25 | 24.33 | 67.05 | 0.15 | 0.88 | 0.53 | 2.18 | 0.06 | 2.75 |
| S—41 | 1.18 | 0.68 | 23.2 | 64.8 | 0.07 | 1.75 | 0.79 | 1.44 | 0.06 | 5.11 |
| S—42 | 1.56 | 0.54 | 22.86 | 66.17 | 0.12 | 1.65 | 0.69 | 2.16 | 0.07 | 3.3 |
| S—43 | 1.09 | 0.61 | 19.97 | 69.88 | 0.15 | 1.72 | 0.8 | 1.09 | 0.08 | 3.75 |
| S—44 | 0.75 | 0.49 | 25.07 | 66.74 | 0.14 | 1.6 | 0.44 | 1.25 | 0.09 | 2.58 |
| S—45 | 1.11 | 0.54 | 19.22 | 73.11 | 0.13 | 1.5 | 0.5 | 0.88 | 0.13 | 2.01 |
| S—46 | 0.49 | 0.46 | 18.26 | 74.26 | 0.11 | 1.23 | 0.48 | 1 | 0.06 | 2.75 |
| S—47 | 0.72 | 0.68 | 25.45 | 65.57 | 0.23 | 1.48 | 0.63 | 1.41 | 0.06 | 2.99 |
| S—48 | 1.11 | 0.63 | 24.76 | 66.34 | 0.15 | 1.27 | 0.92 | 1.37 | 0.04 | 2.54 |
| S—49 | 1.03 | 0.69 | 23.57 | 66.55 | 0.16 | 1.7 | 0.72 | 1.03 | 0.04 | 3.68 |
| S—50 | 0.94 | 0.44 | 24.78 | 67.55 | 0.1 | 1.26 | 0.45 | 1.66 | 0.05 | 1.87 |
| S—52 | 1.11 | 0.52 | 21.57 | 70.97 | 0.16 | 0.9 | 0.59 | 1.13 | 0.04 | 2.17 |
| S—53 | 1.03 | 0.72 | 23.81 | 66.47 | 0.18 | 1.58 | 0.88 | 1.06 | 0.08 | 3.38 |
| S—54 | 0.68 | 0.67 | 24.41 | 67.33 | 0.19 | 1.27 | 0.65 | 1.22 | 0.06 | 2.71 |
| S—55 | 0.79 | 0.69 | 23.21 | 66.86 | 0.15 | 1.53 | 0.7 | 1.35 | 0.07 | 3.8 |
| S—56 | 0.75 | 0.3 | 22.54 | 71.1 | 0.2 | 0.75 | 0.42 | 1.26 | 0.05 | 1.81 |
| S—57 | 1.14 | 0.64 | 24.38 | 65.64 | 0.18 | 2.6 | 0.45 | 1.32 | 0.17 | 2.65 |
| S—58 | 1.14 | 0.88 | 24.14 | 65.48 | 0.19 | 2.65 | 0.6 | 1.12 | 0.06 | 2.92 |
| S—59 | 0.4 | 0.48 | 22.88 | 69.27 | 0.12 | 1.4 | 0.6 | 1.09 | 0.03 | 2.85 |

Table B9. The chemical composition of the clay body of celadons from Yaozhou kiln [7].

| number | dynasty | Major wt% |  |  |  |  |  |  |  | Minorμg/g |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Na2O | MgO | Al2O3 | SiO2 | K2O | CaO | TiO2 | Fe2O3 | MnO | CuO | Rb2O | SrO | ZrO2 | P2O5 |
| T1 | Tang | 0.37 | 0.53 | 20.42 | 70.05 | 4.94 | 0.96 | 0.17 | 1.55 | 100 | 40 | 220 | 190 | 90 | 190 |
| T2 |  | 0.15 | 0.43 | 20.28 | 70.45 | 5.27 | 0.54 | 0.19 | 1.69 | 90 | 30 | 220 | 150 | 170 | 190 |
| T3 |  | 0.07 | 0.88 | 21.74 | 68.48 | 5.05 | 0.63 | 0.36 | 1.79 | 100 | 20 | 230 | 160 | 190 | 150 |
| T4 |  | 0.46 | 0.68 | 21.93 | 68.14 | 5.36 | 0.53 | 0.25 | 1.65 | 150 | 10 | 260 | 120 | 130 | 150 |
| T5 |  | 0.5 | 0.46 | 20.35 | 69.84 | 5.07 | 0.84 | 0.17 | 1.77 | 120 | 50 | 240 | 180 | 110 | 160 |
| WD1 | Five Dynasty | 0.22 | 1.18 | 31.87 | 59.11 | 2.03 | 0.86 | 1.2 | 2.53 | 110 | 100 | 140 | 180 | 600 | 280 |
| WD2 |  | 0.23 | 0.88 | 28.78 | 62.81 | 1.84 | 1.01 | 1.11 | 2.34 | 120 | 50 | 120 | 170 | 750 | 330 |
| WD3 |  | 0.24 | 1.01 | 27.62 | 63.93 | 1.69 | 0.63 | 1.14 | 2.75 | 120 | 20 | 120 | 160 | 660 | 150 |
| WD4 |  | 0.18 | 1.07 | 27.37 | 64.25 | 1.62 | 0.87 | 1.16 | 2.48 | 110 | 70 | 130 | 190 | 640 | 100 |
| WD5 |  | 0.22 | 1.17 | 26.77 | 64.55 | 1.59 | 1.26 | 1.04 | 2.4 | 100 | 80 | 120 | 140 | 690 | 250 |
| S1 | Song | 0.57 | 0.91 | 24.03 | 67.91 | 2.46 | 0.27 | 0.83 | 2.02 | 90 | 40 | 190 | 190 | 470 | 130 |
| S2 |  | 0.25 | 0.71 | 25.63 | 67.2 | 1.95 | 0.37 | 0.9 | 1.99 | 90 | 50 | 130 | 110 | 640 | 120 |
| S3 |  | 0.07 | 0.72 | 23.38 | 69.77 | 2.28 | 0.31 | 0.71 | 1.76 | 80 | 60 | 150 | 100 | 440 | 140 |
| S4 |  | 0.4 | 0.85 | 27.38 | 64.61 | 2.25 | 0.47 | 0.71 | 2.32 | 120 | 100 | 130 | 160 | 400 | 170 |
| S5 |  | 0.19 | 0.96 | 26.24 | 65.69 | 2.48 | 0.5 | 0.71 | 2.24 | 130 | 90 | 170 | 160 | 430 | 140 |
| J1 | Jin | 0.54 | 1.05 | 19.33 | 72.97 | 2.35 | 0.3 | 0.72 | 1.75 | 100 | 20 | 190 | 200 | 390 | 180 |
| J2 |  | 0.55 | 0.95 | 20.93 | 71.06 | 2.51 | 0.39 | 0.68 | 1.92 | 80 | 10 | 140 | 280 | 540 | 160 |
| J3 |  | 0.27 | 0.93 | 19.95 | 72.66 | 2.32 | 0.28 | 0.65 | 1.93 | 90 | 80 | 160 | 250 | 520 | 130 |
| J4 |  | 0.44 | 1.07 | 21.09 | 70.43 | 2.62 | 0.68 | 0.63 | 2.03 | 110 | 60 | 170 | 270 | 510 | 180 |
| J5 |  | 0.17 | 1.16 | 25.51 | 66.29 | 2.51 | 0.4 | 0.7 | 2.28 | 110 | 80 | 180 | 180 | 420 | 160 |
| Y1 | Yuan | 0.49 | 1.12 | 21.04 | 70.71 | 2.64 | 0.45 | 0.66 | 1.89 | 130 | 110 | 180 | 240 | 370 | 240 |
| Y2 |  | 0.19 | 0.96 | 27.08 | 65.11 | 2.16 | 0.81 | 0.62 | 2.08 | 200 | 80 | 150 | 190 | 440 | 110 |
| Y3 |  | 0.4 | 1.08 | 19.52 | 72.84 | 2.14 | 0.44 | 0.58 | 2.01 | 80 | 60 | 160 | 200 | 740 | 270 |
| Y4 |  | 0.29 | 0.9 | 24.52 | 67.32 | 2.49 | 0.57 | 0.67 | 2.25 | 180 | 70 | 150 | 140 | 350 | 230 |
| Y5 |  | 0.3 | 0.69 | 23.02 | 70.02 | 1.99 | 0.45 | 0.87 | 1.66 | 70 | 70 |  |  |  |  |

Table B10. The chemical composition of the clay body of celadons from Yingou kiln in Fuping area (Dingzhou kiln) [8].

| No. | Na2O | MgO | Al2O3 | SiO2 | P2O5 | K2O | CaO | TiO2 | Fe2O3 | Cr | Mn | Ni | Cu | Zn | Rb | Sr | Zr | Pb |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | wt% | wt% | wt% | wt% | wt% | wt% | wt% | wt% | wt% | μg/g | μg/g | μg/g | μg/g | μg/g | μg/g | μg/g | μg/g | μg/g |
| Q09# | 1.45 | 1.37 | 21.75 | 67.29 | 0.04 | 2.23 | 2.25 | 0.74 | 2.87 | 155 | 301 | n.d. | 39 | 13 | 125 | 117 | 491 | 22 |
| Q08# | 1.62 | 1.29 | 20.41 | 70 | n.d. | 2.21 | 1.46 | 0.65 | 2.36 | 167 | 284 | n.d. | n.d. | 7 | 120 | 150 | 333 | 36 |
| Q12# | 1.64 | 1.13 | 21.55 | 69.71 | 0.02 | 2.36 | 0.6 | 0.64 | 2.32 | 154 | 336 | n.d. | n.d. | 15 | 138 | 188 | 357 | 47 |
| Q05# | 0.9 | 0.32 | 19.96 | 66.25 | 0.04 | 4.46 | 3.92 | 0.86 | 3.28 | 139 | 322 | n.d. | n.d. | 55 | 121 | 127 | 380 | 31 |
| Q01# | 1.58 | 1.3 | 25.61 | 64.8 | 0.06 | 2.19 | 1.02 | 0.76 | 2.67 | 112 | 325 | 14 | n.d. | 20 | 118 | 132 | 418 | 27 |
| Q02# | 1.64 | n.d. | 18.49 | 72.43 | n.d. | 2.12 | 1.82 | 0.74 | 2.75 | 106 | 306 | 30 | n.d. | 10 | 88 | 76 | 261 | 19 |
| Q11# | 1.41 | 1.32 | 25.34 | 63.55 | n.d. | 2.27 | 1.33 | 1.06 | 3.72 | 158 | 306 | 31 | n.d. | 12 | 110 | 146 | 431 | 36 |
| Q17# | 1.84 | n.d. | 13.68 | 74.89 | n.d. | 2.06 | 4.07 | 0.73 | 2.74 | 144 | 319 | 12 | n.d. | 12 | 84 | 107 | 335 | 28 |
| YG-Q-1 | 1.79 | 2.33 | 27.41 | 62.65 | 0.1 | 1.98 | 0.57 | 0.76 | 2.41 | 162 | 288 | 37 | 8 | 29 | 131 | 158 | 477 | 67 |
| YG-Q-2 | 1.78 | 1.37 | 22.17 | 66.08 | 0.05 | 5.65 | 1.13 | 0.23 | 1.54 | 43 | 276 | 11 | n.d. | 25 | 248 | 108 | 122 | 72 |
| YG-Q-3 | 1.63 | 1.73 | 24.71 | 63.63 | 0.05 | 5.26 | 0.9 | 0.24 | 1.85 | 21 | 223 | 8 | n.d. | 7 | 226 | 143 | 103 | 69 |
| YG-Q-3 | 1.79 | 1.97 | 24.95 | 63.03 | 0.11 | 5.19 | 0.87 | 0.24 | 1.84 | 38 | 244 | 25 | n.d. | n.d. | 241 | 133 | 111 | 103 |
| YG-Q-4 | 1.78 | 1.82 | 22.53 | 66 | 0.15 | 4.75 | 1.13 | 0.2 | 1.64 | 83 | 218 | 10 | n.d. | 56 | 238 | 129 | 114 | 45 |
| YG-Q-5 | 1.79 | 1.73 | 21.81 | 66.14 | 0.17 | 5.32 | 0.83 | 0.2 | 2.01 | 38 | 259 | 22 | n.d. | 29 | 234 | 124 | 128 | 93 |
| YG-Q-6 | 1.81 | 1.71 | 22.15 | 66.39 | 0.13 | 4.49 | 1.79 | 0.21 | 1.32 | 45 | 220 | n.d. | n.d. | 42 | 234 | 121 | 148 | 34 |
| YG-Q-7 | 1.5 | 1.84 | 30.54 | 60.1 | 0.03 | 2.09 | 0.6 | 1.04 | 2.28 | 132 | 316 | 33 | n.d. | 37 | 114 | 127 | 500 | 33 |
| X-3 | 1.97 | 1.7 | 18.59 | 71.82 | 0.12 | 2.14 | 0.89 | 0.59 | 2.18 | 159 | 313 | 5 | n.d. | 16 | 124 | 241 | 463 | 36 |
| X-10 | 1.71 | 2.12 | 28.16 | 60.95 | 0.11 | 1.68 | 0.85 | 0.99 | 3.42 | 130 | 325 | 40 | 60 | 24 | 120 | 164 | 581 | 45 |
| SF3 | 1.73 | 1.51 | 25.31 | 65.52 | 0.1 | 2.47 | 0.33 | 0.74 | 2.29 | 110 | 316 | 24 | n.d. | 31 | 147 | 145 | 420 | 48 |
| SF4 | 1.91 | 1.86 | 21.34 | 69.87 | 0.13 | 2.25 | 0.25 | 0.66 | 1.74 | 132 | 244 | 8 | n.d. | n.d. | 146 | 185 | 444 | 32 |
| SXY6 | 1.61 | 1.68 | 25.85 | 64.86 | 0.06 | 2.7 | 0.95 | 0.65 | 1.63 | 94 | 318 | 16 | n.d. | 43 | 153 | 99 | 367 | 28 |
| SXY7 | 1.51 | 1.61 | 26.48 | 64.89 | 0.03 | 2.47 | 0.71 | 0.61 | 1.68 | 112 | 288 | 18 | n.d. | n.d. | 138 | 74 | 330 | 56 |
| SXY8 | 1.59 | 1.92 | 26.27 | 64.69 | 0.04 | 1.67 | 0.33 | 0.92 | 2.57 | 113 | 289 | 9 | 44 | n.d. | 112 | 146 | 600 | 16 |

Reference

1. Xiong W. The Technical Analysis of Yuezhou Kiln Celaond and Comparative study of Hongzhou Kiln [Master’s thesis]. [Jingdezhen]: Jingdezhen Ceramic Institute; 2018.

2. Feng X, Feng S, Zhang W, Fan C, Quan K. Study on Hongzhou Kiln Porcelains of Successive Dynastyies by NAA. Nuclear Physics Review. 2005;22:142–6.

3. Feng X, Feng S, Fan C, Zhang W, Quan K. Provenance and indirect dating study on Hongzhou Kiln porcelains by INAA. Journal of radioanalytical and nuclear chemistry. Akadémiai Kiadó, co-published with Springer Science+ Business Media BV …; 2007;272:551–6.

4. Yin M. Unearthing the potential of celadon civilian wares: scientific analysis of ceramic sherds from Wuzhou. 2009;

5. Xiong Y, Gong Y, Xia J, Wu Ji. The analysis of porcelains from Yue kiln by EDXRF. Sciences of Conservation and Archaeology. 2010;22:28–34.

6. Li H, Chen C, Wang M. Study on Composition Characteristics of Yellow Glazed Porcelain Unearthed From Shouzhou Kiln in Anhui Province. China Ceramics. 2022;58:67–73.

7. Sang Z, Wang F, Duan X, Mu T, Ren Z, Wei X, et al. Analysis of the celadon characteristics of the Yaozhou kiln. Ceramics International. Elsevier; 2019;45:22215–25.

8. Liu S, Li Q, Zhou S. Chemical Analysis of Glaze and Body for Ceramic Wres Collected from Yingou Site in Fuping. China Ceramics. 2017;4:66–81.