Supporting Information

Constructing Interconnected Asymmetric Conductive Network in TPU Fibrous Film：Achieving Low-Reflection Electromagnetic Interference Shielding and Surperior Thermal Conductivity

Yang Zhang a,b, Shengdu Yang a, Qi Zhang a,b, Zhuyu Ma a, YingJian Guo a,b, Meng Shi a,b, Hong Wu a,b,*, Shaoyun Guo a,b

a The State Key Laboratory of Polymer Materials Engineering, Polymer Research Institute of Sichuan University, Chengdu 610065, China

b Sichuan Provincial Engineering Laboratory of Plastic/Rubber Complex Processing Technology, Chengdu 610065, China

* Corresponding Authors

E-mail: wh@scu.edu.cn (H.Wu.)

S1. Calculation formulas

The power of reflection (R), transmission (T), and absorption (A) are used to calculated by measured S-parameters. Finally, total SE (SET), reflected SE (SER) and absorbed SE (SEA) are calculated using the below equations:

R=S112(1)

T=S212 (2)

A=1-R-T 3

SER=-10∙log101-R (4)

SEA=-10∙log10(T/1-R) (5)

SET=-10∙log10T (6)

Figure S1. TEM of MFs.

Figure S2. SEM images (a-a1) TM-20 and (b-b1) TM-50 (The TPU/Fe3O4@MWCNT film was designated as TM-X, where X indicates the different modification time.).

Figure S3. Digital photographs of (a) pure TPU film, and (b-d) TMA-20.

Figure S4. SEM images of AgNWs layer on the TM film.

Figure S5. Cross-sectional SEM images of (a) TMA-0, (b) TMA-2.5, (c) TMA-5 and  (d) TMA-10 (TMA-Y represents the TM-40 coated with AgNWs, where Y was the filtered mass of AgNWs.).

Figure S6. XRD spectra of TPU fibrous film, TMA-0 film and TMA-20 film.

Figure S7. A-R coefficients in the X-band of TMA-Y when electromagnetic waves are incident from the (a) AgNWs layer and (b)TM layer, respectively.

Figure S8. Variation of EMI SE of the TMA-20 before and after bending for 1000 cycles (one bending cycle shown in the insets)

Table S1. Comparison of EMI shielding performances for different materials

| Samples | Thickness（mm） | EMI SE (dB) | Ref. |
| --- | --- | --- | --- |
| MXene/AgNWs/Textiles | 0.120 | 54 | [1] |
| MXene/ANF | 0.012 | 34.71 | [2] |
| CNT/Graphene | 1.6 | 47.5 | [3] |
| AgNWs/PU/Textile | 0.6 | 63.9 | [4] |
| CNT/UHMWPE | 1 | 25.7 | [5] |
| CuNWs/PS | 0.2 | 35 | [6] |
| CNT film | 0.15 | 35 | [7] |
| CNT/WPU | 0.8 | 80 | [8] |
| MXene/PVA | 0.027 | 44 | [9] |
| Graphene/SiC/PVDF | 1.2 | 32.5 | [10] |
| MXene/CNT/TPU | 0.6 | 43 | [11] |
| AgNWs/Cellulose | 0.16 | 48.6 | [12] |
| MXene/Cellulose | 0.035 | 39.6 | [13] |
| MXene/PEDOT:PSS | 0.011 | 42.1 | [14] |
| CF/Fe3O4/EP | 0.2 | 20 | [15] |
| CNT@Fe3O4/ AgNWs/TPU | 0.081 | 78.48 | This Work |

Table S2. Comparison of EMI SE and TC for different materials

| Samples | TC (W m-1K-1) | EMI SE (dB) | R | Ref. |
| --- | --- | --- | --- | --- |
| rGO-WPU/cotton | 2.13 | 46.0 | 0.65 | [16] |
| rGO@Fe3O4/epoxy | 1.2 | 13.0 | 0.86 | [17] |
| GNSs/CINAP/CE | 4.13 | 56.0 | 0.85 | [18] |
| MXene/Graphene/PE | 9.26 | 61.0 | 0.83 | [19] |
| MXene/Chitosan | 6.3 | 40.8 | 0.52 | [20] |
| CNTs/Fe3O4/PW/PP | 0.59 | 41.2 | 0.77 | [21] |
| (GnPs/MWCNTs)@PBZ/PEEK | 6.27 | 54.4 | 0.85 | [22] |
| MXene/GR/PEG | 0.58 | 36.0 | 0.76 | [23] |
| GNPs/PS | 4.72 | 33 | 0.75 | [24] |
| Fe3O4/CNT/cellulose | 9.53 | 30.3 | 0.93 | [25] |
| Fe3O4/MXene /PVA | 2.86 | 40.0 | 0.94 | [26] |
| Cu/PCPES | 1.75 | 59.7 | 0.73 | [27] |
| MXene/AgNWs/Epoxy | 2.34 | 94.1 | 0.86 | [28] |
| CNT@Fe3O4/ AgNWs/TPU | 7.83 | 78.5 | 0.56 | This Work |

References

[1] Liu LX, Chen W, Zhang HB, Wang QW, Guan F, Yu ZZ. Flexible and Multifunctional Silk Textiles with Biomimetic Leaf‐Like MXene/Silver Nanowire Nanostructures for Electromagnetic Interference Shielding, Humidity Monitoring, and Self‐Derived Hydrophobicity. Advanced Functional Materials. 2019;29(44).

[2] Wei H, Wang M, Zheng W, Jiang Z, Huang Y. 2D Ti3C2Tx MXene/aramid nanofibers composite films prepared via a simple filtration method with excellent mechanical and electromagnetic interference shielding properties. Ceramics International. 2020;46(5):6199-204.

[3] Song Q, Ye F, Yin X, Li W, Li H, Liu Y, et al. Carbon Nanotube-Multilayered Graphene Edge Plane Core-Shell Hybrid Foams for Ultrahigh-Performance Electromagnetic-Interference Shielding. Adv Mater. 2017;29(31).

[4] Jia L-C, Ding K-Q, Ma R-J, Wang H-L, Sun W-J, Yan D-X, et al. Highly Conductive and Machine-Washable Textiles for Efficient Electromagnetic Interference Shielding. Advanced Materials Technologies. 2019;4(2).

[5] Yu W-C, Zhang G-Q, Liu Y-H, Xu L, Yan D-X, Huang H-D, et al. Selective electromagnetic interference shielding performance and superior mechanical strength of conductive polymer composites with oriented segregated conductive networks. Chemical Engineering Journal. 2019;373:556-64.

[6] Al-Saleh MH, Gelves GA, Sundararaj U. Copper nanowire/polystyrene nanocomposites: Lower percolation threshold and higher EMI shielding. Composites Part A: Applied Science and Manufacturing. 2011;42(1):92-7.

[7] Wang L-L, Tay B-K, See K-Y, Sun Z, Tan L-K, Lua D. Electromagnetic interference shielding effectiveness of carbon-based materials prepared by screen printing. Carbon. 2009;47(8):1905-10.

[8] Zeng Z, Chen M, Jin H, Li W, Xue X, Zhou L, et al. Thin and flexible multi-walled carbon nanotube/waterborne polyurethane composites with high-performance electromagnetic interference shielding. Carbon. 2016;96:768-77.

[9] Jin X, Wang J, Dai L, Liu X, Li L, Yang Y, et al. Flame-retardant poly(vinyl alcohol)/MXene multilayered films with outstanding electromagnetic interference shielding and thermal conductive performances. Chemical Engineering Journal. 2020;380.

[10] Liang C, Hamidinejad M, Ma L, Wang Z, Park CB. Lightweight and flexible graphene/SiC-nanowires/ poly(vinylidene fluoride) composites for electromagnetic interference shielding and thermal management. Carbon. 2020;156:58-66.

[11] Zhang D, Yin R, Zheng Y, Li Q, Liu H, Liu C, et al. Multifunctional MXene/CNTs based flexible electronic textile with excellent strain sensing, electromagnetic interference shielding and Joule heating performances. Chemical Engineering Journal. 2022;438.

[12] Lee TW, Lee SE, Jeong YG. Highly Effective Electromagnetic Interference Shielding Materials based on Silver Nanowire/Cellulose Papers. ACS Appl Mater Interfaces. 2016;8(20):13123-32.

[13] Zhou B, Zhang Z, Li Y, Han G, Feng Y, Wang B, et al. Flexible, Robust, and Multifunctional Electromagnetic Interference Shielding Film with Alternating Cellulose Nanofiber and MXene Layers. ACS Appl Mater Interfaces. 2020;12(4):4895-905.

[14] Liu R, Miao M, Li Y, Zhang J, Cao S, Feng X. Ultrathin Biomimetic Polymeric Ti3C2T x MXene Composite Films for Electromagnetic Interference Shielding. ACS Appl Mater Interfaces. 2018;10(51):44787-95.

[15] Crespo M, Méndez N, González M, Baselga J, Pozuelo J. Synergistic effect of magnetite nanoparticles and carbon nanofibres in electromagnetic absorbing composites. Carbon. 2014;74:63-72.

[16] Wang Y, Wang W, Xu R, Zhu M, Yu D. Flexible, durable and thermal conducting thiol-modified rGO-WPU/cotton fabric for robust electromagnetic interference shielding. Chemical Engineering Journal. 2019;360:817-28.

[17] Liu Y, Lu M, Wu K, Yao S, Du X, Chen G, et al. Anisotropic thermal conductivity and electromagnetic interference shielding of epoxy nanocomposites based on magnetic driving reduced graphene oxide@Fe3O4. Composites Science and Technology. 2019;174:1-10.

[18] Ren F, Song D, Li Z, Jia L, Zhao Y, Yan D, et al. Synergistic effect of graphene nanosheets and carbonyl iron–nickel alloy hybrid filler on electromagnetic interference shielding and thermal conductivity of cyanate ester composites. Journal of Materials Chemistry C. 2018;6(6):1476-86.

[19] Tan X, Liu TH, Zhou W, Yuan Q, Ying J, Yan Q, et al. Enhanced Electromagnetic Shielding and Thermal Conductive Properties of Polyolefin Composites with a Ti3C2Tx MXene/Graphene Framework Connected by a Hydrogen-Bonded Interface. ACS Nano. 2022.

[20] Tan Z, Zhao H, Sun F, Ran L, Yi L, Zhao L, et al. Fabrication of Chitosan/MXene multilayered film based on layer-by-layer assembly: Toward enhanced electromagnetic interference shielding and thermal management capacity. Composites Part A: Applied Science and Manufacturing. 2022;155.

[21] Li X, Sheng M, Gong S, Wu H, Chen X, Lu X, et al. Flexible and multifunctional phase change composites featuring high-efficiency electromagnetic interference shielding and thermal management for use in electronic devices. Chemical Engineering Journal. 2022;430.

[22] Chen R, He Q, Li X, Wen F, Cheng L, Li L, et al. Significant enhancement of thermal conductivity in segregated(GnPs&MWCNTs)@Polybenzoxazine/(Polyether ether ketone) -based composites with excellent electromagnetic shielding. Chemical Engineering Journal. 2022;431.

[23] Jin L, Wang P, Cao W, Song N, Ding P. Isolated Solid Wall-Assisted Thermal Conductive Performance of Three-Dimensional Anisotropic MXene/Graphene Polymeric Composites. ACS Appl Mater Interfaces. 2022;14(1):1747-56.

[24] Guo Y, Pan L, Yang X, Ruan K, Han Y, Kong J, et al. Simultaneous improvement of thermal conductivities and electromagnetic interference shielding performances in polystyrene composites via constructing interconnection oriented networks based on electrospinning technology. Composites Part A: Applied Science and Manufacturing. 2019;124.

[25] Li Y, Xue B, Yang S, Cheng Z, Xie L, Zheng Q. Flexible multilayered films consisting of alternating nanofibrillated cellulose/Fe3O4 and carbon nanotube/polyethylene oxide layers for electromagnetic interference shielding. Chemical Engineering Journal. 2021;410.

[26] Zhang Y, Ruan K, Gu J. Flexible Sandwich-Structured Electromagnetic Interference Shielding Nanocomposite Films with Excellent Thermal Conductivities. Small. 2021:e2101951.

[27] Zhao H, Huang Y, Han Y, Yun J, Wang X, Jin L, et al. Flexible and lightweight porous polyether sulfone/Cu composite film with bidirectional differential structure for electromagnetic interference shielding and heat conduction. Chemical Engineering Journal. 2022;440.

[28] Liu H, Huang Z, Chen T, Su X, Liu Y, Fu R. Construction of 3D MXene/Silver nanowires aerogels reinforced polymer composites for extraordinary electromagnetic interference shielding and thermal conductivity. Chemical Engineering Journal. 2022;427.