Supporting Information

Effect of the ambient factor over spinel CuMn2O4 for toluene catalytic ozonation: Enhancement of the synergy and the generation of ROS

Guanjie Wang a,b, Bo Zhao c, Zhiping Ye a,d,e, Liang Zhao a, Xiuwen Zhang a, Jiade Wang a,*

a College of Environment, Zhejiang University of Technology, Hangzhou, 310014 China

b Collaborative Innovation Center of Yangtze River Delta Region Green Pharmaceuticals, Zhejiang University of Technology, Hangzhou, 310014, China

c Zhejiang TUNA Environmental Science & Technology Co., Ltd. Shaoxing, 312000, China

d State Environmental Protection Key Laboratory of Sources and Control of Air Pollution Complex, Beijing, 100084, China

e Department of Chemical Engineering, Sichuan University, Chengdu 610065, Sichuan, China

*Corresponding author, Jiade Wang
E-mail: jdwang@zjut.edu.cn
Mailing address: College of Environment, Zhejiang University of Technology, Hangzhou, 310014, China

This Supporting Information provides:

Total number of pages: 5

Total number of Figures: 7

Total number of Tables: 2

Figure

Fig. S1 Schematic experiment of catalyst activity evaluation.

Fig. S2 SEM of CuMn2O4 at different O3 concentrations, (A) 1000 ppm, (B) 1400 ppm, and (C) 2100 ppm.

Fig. S3 SEM of CuMn2O4 at different temperatures, (A) 50℃, (B) 100℃, and (C) 150℃.

Fig. S4 XPS of CuMn2O4 at different temperatures, (A) Cu 2p, (B) Mn 2p, and (C) O 1s.

Fig. S5 GC-MS spectra.

Fig. S6 SEM of CuMn2O4 at different humidity, (A) 0%, (B) 30% and (C) 60%.

Fig. S7 XPS of CuMn2O4 at different humidity, (A) Cu 2p, (B) Mn 2p, and (C) O 1s.

Table

Table S1 The relevant data about the post-reaction CuMn2O4 (O3 concentration).

Table S2 The relevant data about the post-reaction CuMn2O4 (humidity).

Figure

Fig. S1 Schematic experiment of catalyst activity evaluation.

Fig. S2 SEM of CuMn2O4 at different O3 concentrations, (A) 1000 ppm, (B) 1400 ppm, and (C) 2100 ppm.

Fig. S3 SEM of CuMn2O4 at different temperatures, (A) 50 ℃, (B) 100 ℃, and (C) 150 ℃.

Fig. S4 XPS of CuMn2O4 at different temperatures, (A) Cu 2p, (B) Mn 2p, and (C) O 1s.

Fig. S5 GC-MS spectra.

Fig. S6 SEM of CuMn2O4 at different humidity, (A) 0%, (B) 30% and (C) 60%.

Fig. S7 XPS of CuMn2O4 at different humidity, (A) Cu 2p, (B) Mn 2p, and (C) O 1s.

Table

Table S1 The relevant data about the post-reaction CuMn2O4 (O3 concentration).

| Samples | SBETa (m2/g) | Vpb (cm³/g) | Dpc (nm) |
| --- | --- | --- | --- |
| CuMn2O4-10 | 27.6 | 0.1 | 19.8 |
| CuMn2O4-14 | 23.6 | 0.1 | 15.8 |
| CuMn2O4-21 | 17.8 | 0.1 | 14.8 |

a Surface Area.

b Desorption cumulative volume of pores.

c Desorption average pore diameter.

Table S2 The relevant data about the post-reaction CuMn2O4 (humidity).

| Samples | SBETa (m2/g) | Vpb (cm³/g) | Dpc (nm) |
| --- | --- | --- | --- |
| CuMn2O4-0 % | 17.8 | 0.1 | 14.8 |
| CuMn2O4-30 % | 24.9 | 0.1 | 18.5 |
| CuMn2O4-60 % | 25.2 | 0.1 | 18.3 |

a Surface Area.

b Desorption cumulative volume of pores.

c Desorption average pore diameter.