Table 1. The textural and porosity characteristics of the 3D-NC and the 3D-NC without Ni (Ⅱ) and Mn (Ⅱ).
	Parameters
	Sample

	
	3D-NC
	3D-NC without Ni (Ⅱ) and Mn (Ⅱ)

	SBET (m2/g)
	20.113
	13.902

	Vt (cm2/g)
	0.059
	0.051


SBET: specific surface area measured by the BET method, Vt: total pore volume measured by the BJH method.

