Table 1. The textural and porosity characteristics of the 3D-NC and the 3D-NC without Ni (Ⅱ) and Mn (Ⅱ).

| Parameters | Sample |  |
| --- | --- | --- |
|  | 3D-NC | 3D-NC without Ni (Ⅱ) and Mn (Ⅱ) |
| SBET (m2/g) | 20.113 | 13.902 |
| Vt (cm2/g) | 0.059 | 0.051 |

SBET: specific surface area measured by the BET method, Vt: total pore volume measured by the BJH method.