Table 2. Fitting data of kinetic model for Hg (Ⅱ) adsorption on the 3D-NC.

| Ions | Qe,e (mg/g) | Pseudo-first-order equation |  |  | Pseudo-second-order equation |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Qe,c (mg/g) | R2 | k1(h-1) | Qe,c (mg/g) | R2 | k2(g/(mg•min)) |
| Hg (Ⅱ) | 403.20 | 666.5792 | 0.9667 | 2.9526 | 403.2927 | 0.9997 | 0.00445 |