Supplementary Material

Preparation of Self-assembled Starch-based Organometallic Polymers and Their Efficient Adsorption of Mercury Ion in Water

Chao Geng, PeiLin Yang, Ruikang Lin, Li Guo, Chao Yuan, Bo Cui, Yishan Fang,

State Key Laboratory of Biobased Material and Green Papermaking, School of Food Science and Engineering, Qilu University of Technology, Shandong Academy of Sciences, Jinan, 250353 , China.

Tel. /fax: +86 0531 89631195 (Y. Fangi)

E-mail address: fangysh123@qlu.edu.cn (Y. Fang)

Experimental details

Materials

All chemical reagents were used as received without further purification unless otherwise specified. The Glycerol was purchased from Tianjin FUYU CHEMICAL Co., LTD and the tungsten chloride was purchased from Shanghai Maclin Biochemical Technology Co., LTD. The potato starch was obtained by Gansu harvest Agricultural Technology Co., Ltd and The thiourea was purchased from Tianjin Zhiyuan Chemical Reagent Co. LTD. Potassium dihydrogen phosphate, dipotassium hydrogenphosphate, hydrochloric acid and sodium hydroxide were purchased from Tianjin Dingsheng Xinhua Co., LTD. The solutions were prepared with ultrapure water.

Apparatus

The structure of the materials was performed by Scanning electron microscopy (Regulus 8220, Hitachi High-Technologies Corporation, Japan) and the structural stability of the materials were investigated using a thermal analyzer (STA 6000, PerkinElmer, Shelton, USA). 3 mg of the sample was tested from 30 °C to 800 °C under nitrogen atmosphere with 20 mL/min flow rate and the heating rate was 10 °C/min. Zeta potential of the materials was determined by Zetasizer Nano-ZS90 (Malvern Instruments, Westborough, MA, USA). Prior to the test, the materials were dispersed in a solution of pH 1-10 to determine the potential. The X-ray diffraction pattern was measured from 4 to 70° with a scanning speed of 4°/min by using a D8-Advance X-ray diffractometer (Bruker AXS Co., Ltd., Karlsruhe, Germany) and the Cu-Kα radiation was used under the 20 mA and 40 kV conditions. The FTIR was performed by using a Fourier transform infrared spectrometer (PerkinElmer, Shelton, USA) with a resolution of 4 cm−1. X-ray photoelectron spectroscopy was analyzed by EscaLab Xi+ X-ray photoelectron spectrometer (Thermo Scientific, West Sussex, UK) with a monochromatic Al-Kα radiation. The spectrum was previously calibrated and the energy was referenced to C1s at 284.8 eV. Electrochemical behaviors were measured on CHI 660E (Shanghai Chenhua Instrument Co., LTD, Shanghai, China) by differential pulse voltammetry (DPV) with conventional three electrode system.

Figures and Tables

Table S1. Fitting equations of the adsorption kinetics for Hg (Ⅱ) adsorption and MB adsorption on TH@WOx/SP.

| Object | Pseudo-first-order equation | Pseudo-second-order equation |
| --- | --- | --- |
|  | y=ax+b | y=ax+b |
| Hg (Ⅱ) | y=0.00555x+2.6621 | y=0.000449x+0.00176 |
| MB | y=0.00946x+1.7957 | y=0.00535x+0.0483 |

Table S2. Fitting data of kinetic model for Hg (Ⅱ) adsorption and MB adsorption on TH@WOx/SP.

| Object | qe,e(mg/g) | Pseudo-first-order equation |  |  | Pseudo-second-order equation |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qe,c (mg/g) | R2 | K1(h-1) | qe,c (mg/g) | R2 | K1(h-1) |
| Hg(Ⅱ) | 2201.16 | 432.7449 | 0.4632 | 0.7669 | 2227.1715 | 0.9991 | 0.00687 |
| MB | 175.01 | 62.7735 | 0.8305 | 1.3072 | 186.7258 | 0.9981 | 0.03556 |

Table S3. Fitting equations of the adsorption isotherms for Hg (Ⅱ) adsorption and MB adsorption on TH@WOx/SP.

| Object | Langmuir equation | Freundlich equation |
| --- | --- | --- |
|  | y=ax+b | y=ax+b |
| Hg(Ⅱ) | y=0.0004x+0.00406 | y=0.4335x+2.4981 |
| MB | y=0.00553x+0.00481 | y=0.2536x+1.8436 |

Table S4. Fitting data of adsorption isotherm for Hg (Ⅱ) and MB adsorption on TH@WOx/SP.

| Object | Langmuir equation |  |  | Freundlich equation |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qm (mg/g) | b | R2 | n | Kf | R2 |
| Hg(Ⅱ) | 2305.66 | 0.1068 | 0.9961 | 2.3068 | 314.8473 | 0.9171 |
| MB | 180.83 | 1.1497 | 0.9998 | 3.9432 | 69.7590 | 0.8884 |

Table S5. Comparison of the equilibrium time and adsorption capacities with other

adsorbents for Hg(II) and MB .

| Adsorbents | Adsorption capacity m Q (mg/g) /Equilibrium time (min) |  | References |
| --- | --- | --- | --- |
|  | Hg(II) | MB |  |
| Melamine-grafted chitosan | 490.7/240 | - | (Ge &Du 2020) |
| MOF-MA | 1080/10 | - | (Wang et al. 2020) |
| MnFe2O4@Zn-Al LDHs@Cel@AGB | 1200/30 | 19.28/25 | (Mahmoud et al. 2021) |
| GO-EDTA-CS nanocomposite | 324/120 | 141/180 | (Verma et al. 2022) |
| Silica-polyamide | - | 44.6/50 | (Osman et al. 2020) |
| Oxone modified hydrochar | - | 86.7/480 | (Madduri et al. 2020) |
| GONRs | 33.02/12 | - | (Sadeghi et al. 2020) |
| BSH–MMT | 104.79/360 | - | (Pei et al. 2022) |
| Salecan/GO sponge | 463/60 | - | (Hu et al. 2021) |
| TH@WOx/SP | 2201.16/30 | 175.01/90 | this work |

Table S6. Binding energy before and after adsorption of Hg (Ⅱ) and MB on TH@WOx/SP.

| Object |  | Original (eV) | Loded with Hg (eV) | Loded with MB (eV) |
| --- | --- | --- | --- | --- |
| Hg4f | Hg4f7/2 | - | 103.30 | - |
|  | Hg4f5/2 | - | 106.22 | - |
| W4f | W4f7/2(Ⅵ) | 36.10 | 36.09 | 36.15 |
|  | W4f5/2(Ⅵ) | 38.24 | 38.23 | 38.29 |
|  | W4f7/2(Ⅴ) | 35.31 | - | 35.53 |
|  | W4f5/2(Ⅴ) | 37.38 | - | 37.60 |
| S2p | S2p3/2 | 163.61 | 164.04 | 163.64 |
|  | S2p1/2 | 164.71 | 165.14 | 164.74 |
| N1s | C–N | 399.93 | 400.09 | 400.02 |
|  | N–H | 401.89 | 402.15 | 401.85 |
| C1s | C–C | 284.80 | 284.80 | 284.80 |
|  | C–O/C–N/C–S | 286.21 | 286.31 | 286.23 |
|  | C=O | 289.04 | 289.15 | 289.05 |
| O1s | O–W | 531.12 | 531.55 | 531.15 |
|  | O–C/O=C | 532.44 | 532.75 | 532.43 |
|  | –OH | 533.37 | 533.64 | 533.40 |

Figure S1. Comparison of the XPS spectra before and after adsorption of MB on TH@WOx/SP.

References

Ge H, Du J (2020): Selective adsorption of Pb(II) and Hg(II) on melamine-grafted chitosan. International Journal of Biological Macromolecules 162, 1880-1887

Hu X, Yan L, Wang Y, Xu M (2021): Ion-imprinted sponge produced by ice template-assisted freeze drying of salecan and graphene oxide nanosheets for highly selective adsorption of mercury (II) ion. Carbohydrate Polymers 258, 117622

Madduri S, Elsayed I, Hassan EB (2020): Novel oxone treated hydrochar for the removal of Pb(II) and methylene blue (MB) dye from aqueous solutions. Chemosphere 260, 127683

Mahmoud ME, El-Bahy SM, Elweshahy SMT (2021): Decorated Mn-ferrite nanoparticle@Zn–Al layered double hydroxide@Cellulose@ activated biochar nanocomposite for efficient remediation of methylene blue and mercury (II). Bioresource Technology 342, 126029

Osman AM, Hendi AH, Saleh TA (2020): Simultaneous adsorption of dye and toxic metal ions using an interfacially polymerized silica/polyamide nanocomposite: Kinetic and thermodynamic studies. Journal of Molecular Liquids 314, 113640

Pei P, Xu Y, Wang L, Liang X, Sun Y (2022): Thiol-functionalized montmorillonite prepared by one-step mechanochemical grafting and its adsorption performance for mercury and methylmercury. Science of The Total Environment 806, 150510

Sadeghi MH, Tofighy MA, Mohammadi T (2020): One-dimensional graphene for efficient aqueous heavy metal adsorption: Rapid removal of arsenic and mercury ions by graphene oxide nanoribbons (GONRs). Chemosphere 253, 126647

Verma M, Lee I, Oh J, Kumar V, Kim H (2022): Synthesis of EDTA-functionalized graphene oxide-chitosan nanocomposite for simultaneous removal of inorganic and organic pollutants from complex wastewater. Chemosphere 287, 132385

Wang C, Lin G, Xi Y, Li X, Huang Z, Wang S, Zhao J, Zhang L (2020): Development of mercaptosuccinic anchored MOF through one-step preparation to enhance adsorption capacity and selectivity for Hg(II) and Pb(II). Journal of Molecular Liquids 317, 113896