Figure S1. Estimation of the effects (at 95% confidence level) using the Pareto chart according to the 22-rotational central composite design for the response variable lignin extracted (%) in the delignification process of the straw and bagasse mixture.

Table S1 - ANOVA for dependent variable lignin extraction (%) for 22-rotational central composite design for the delignification process of the straw and bagasse mixture.

| Factor | SQ | GL | MQ | F | p-value |
| --- | --- | --- | --- | --- | --- |
| Regression | 1283.888 | 3 | 427.963 | 8.0338 | 0.01143 |
| Residues | 372.887 | 7 | 53.270 |  |  |
| Lack of Fit | 363.452 | 5 | 72.6903 | 15.4094 | 0.062058 |
| Pure error | 9.435 | 2 | 4.7173 |  |  |
| Total | 1656.775 | 10 |  |  |  |

R2=0.77493; R2adj = 0.67847

Figure S2. Response surface that relates lignin extraction (%) to time and NaOH concentration for delignification process of the straw and bagasse mixture.

Figure S3. Estimation of the effects (at 95% confidence level) using the Pareto chart according to the 22-rotational central composite design for the response variable lignin precipitate (g) in the recovery process of lignin using the liquid fraction obtained by delignification process.

Table S2. ANOVA for dependent variable lignin precipitate (g) for 22-rotational central composite design for the recovery process of lignin using the liquid fraction obtained by delignification process.

| Factor | SQ | GL | MQ | F | p-value |
| --- | --- | --- | --- | --- | --- |
| Regression | 0.236276 | 3 | 0.078759 | 19.91727 | 0.00083 |
| Residues | 0.027680 | 7 | 0.003954 |  |  |
| Lack of Fit | 0.027028 | 5 | 0.005406 | 16.5741 | 0.057876 |
| Pure error | 0.000652 | 2 | 0.000326 |  |  |
| Total | 0.263956 | 10 |  |  |  |

R2=0.89513; R2adj = 0.85019.

Figure S4. Response surface that relates lignin precipitate (g) to time and pH for the recovery process of lignin using the liquid fraction obtained by delignification process.

Figure S5. FTIR-ATR of lignin untreated (LIG), carbonized lignin at 600ºC (LIGTc-600) and sulfonated carbonaceous solids (Tc = 600ºC) with (SCSTc-600[Adj.]) and without (SCSTc-600) sulfonation adjustment.