Supporting Information

In vivo bioluminescence imaging of natural bacteria via ATP-binding cassette sugar transporter

Qian Zhang,1,‡ Bin Song,1,‡ Yunmin Yang,1,‡ Yanan Xu,1 Jian Ji,2 Wenjun Cao,2 Jianping Lu,1 Jiali Ding,1 Haiting Cao,1 Binbin Chu,1 Jiaxu Hong,2,* Houyu Wang1,* & Yao He1,*

1Suzhou Key Laboratory of Nanotechnology and Biomedicine, Institute of Functional Nano & Soft Materials & Collaborative Innovation Center of Suzhou Nano Science and Technology (NANO-CIC), Soochow University, Suzhou 215123, China

2Department of Ophthalmology and Vision Science, Shanghai Eye, Ear, Nose and Throat Hospital, Fudan University, Shanghai, China.

*Corresponding authors. Email: jiaxu.hong@fdeent.org; houyuwang@suda.edu.cn; yaohe@suda.edu.cn

‡ These authors contributed equally.

Calculation of FRET efficiency and BRET ratio.

FRET efficiencies between Cy5 and ICG in GP-Si-BPs were calculated according to the following equation:

E=1-F'D/FD         (1)

where F'D and FD were the donor fluorescence intensities with and without an acceptor, respectively. The optimal FRET efficiency between Cy5 and ICG was calculated to be 32% (Fig. 2c).

The Förster distances (R0) of these two steps were also calculated to be 1.03 nm according to the following equations:

Jλ=[0∞FDλεAλλ4dλ]/[0∞FDλdλ]    (2)

R0=0.0211[κ2n-4ΦDJλ]1/6    (3)

where FDλ was the area-normalized emission spectrum of donor, εAλ was the molar absorption spectrum of the acceptor in M-1cm-1, λ was the wavelength in nm, κ2 was orientation factor (κ2=2/3 due to dynamic averaging donor-acceptor systems), ΦD was quantum yield of the donor, and n=1.35 was the refractive index of the surrounding medium.

Supplementary Fig. 1. The DLS analysis of SiNPs, GP-Si-Luc and GP-Si-BPs. Source data are provided as a Source data file.

Supplementary Fig. 2. SEM images of bacteria treated with Trojan BLI probes. a, SEM images of MRSA or MDR E. coli treated by PBS (control), 0.06 mM of Si-BPs or GP-Si-BPs at 37 oC for 2.5 h. After incubation, the treated bacteria were rinsed with PBS buffer for several times. b, SEM images of MRSA or MDR E. coli treated by PBS (control), 0.06 mM of Si-Luc or GP-Si-Luc at 37 oC for 2.5 h. After incubation, the treated bacteria were rinsed with PBS buffer for several times. The bacterial cell concentration was ~1.0 ×107 CFU. Scale bars, 200 nm.

Supplementary Fig. 3. Comparison of ATP contents inside bacteria and outside bacteria determined by ATP assay kit. a, Linear correlation between luminescence intensities and ATP concentrations in ATP kit assay. b, Comparison of ATP contents inside MDR E. coli and outside MDR E. coli. The bacterial cell concentration was ~1.0 ×107 CFU. Statistical analysis was performed using a one-way ANOVA analysis. Error bars represent the standard deviation obtained from three independent measurements. Source data are provided as a Source data file.

Supplementary Fig. 4. Attenuation of the luminescence at 0.06 mM GP-Si-BPs in the presence of 0.06 mM GP-Si-Luc by addition of the ATP inhibitor of dicyclohexylcarbodiimide (DCC). All imaging experiments were repeated three times with similar results. Error bars represent the standard deviation obtained from three independent measurements. Source data are provided as a Source data file.

Supplementary Fig. 5. Quantification curves of GP, Cy5, ICG, D-Luciferin and Luciferase. a, UV-vis absorption spectra of GP with various concentrations ranged from 20 to 100 μg mL-1 and corresponding calibration curve. b, UV-vis absorption spectra of Cy5 with various concentrations ranged from 2 to 10 μg mL-1 and corresponding calibration curve. c, UV-vis absorption spectra of ICG with various concentrations ranged from 2 to 10 μg mL-1 and corresponding calibration curve. d, UV-vis absorption spectra of D-luciferin with various concentrations ranged from 10 to 100 μg mL-1 and corresponding calibration curve. e, Calibration curve of luciferase protein using the BCA assay. Error bars represent the standard deviation obtained from three independent measurements. Source data are provided as a Source data file.

Supplementary Fig. 6. The effects of GP concentration and incubation time on the uptake of GP-Si-BPs by bacteria. a, Flow cytometry analysis of MRSA co-incubated with GP-Si-BPs with GP concentration (0, 0.14, 0.28, 0.56, 1.12 mM) at 37 oC for 0.5 h, 1.5 h, 2.5 h and 3.5 h, respectively. b, Flow cytometry analysis of MDR E. coli co-incubated with GP-GP-Si-BPs with GP concentration (0, 0.14, 0.28, 0.56, 1.12 mM) at 37 oC for 0.5 h, 1.5 h, 2.5 h and 3.5 h, respectively.

Supplementary Fig. 7. CLSM images of bacteria treated with GP-Si-BPs, GP-Si-Luc or GP-Si-BPs + GP-Si-Luc. a, Confocal images of S. aureus or Salmonella typhimurium (STm) after the incubation with 0.06 mM GP-Si-BPs and corresponding flow cytometry analysis of uptake rates. b, Confocal images of S. aureus or STm after the incubation with 0.06 mM GP-Si-Luc and corresponding flow cytometry analysis of uptake rates. c, Confocal images of S. aureus or STm after the incubation with 0.06 mM GP-Si-BPs + GP-Si-Luc. After incubation, the treated bacteria were rinsed with PBS buffer for several times. The bacterial cell concentration is ~107 CFU. Scale bars, 25 μm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 8. CLSM images of bacteria treated with Si-BPs, Si-Luc or Si-BPs + Si-Luc. a, Confocal images of MRSA or MDR E. coli after the incubation with 0.06 mM Si-BPs and corresponding flow cytometry analysis of uptake rates. b, Confocal images of MRSA or MDR E. coli after the incubation with 0.06 mM Si-Luc and corresponding flow cytometry analysis of uptake rates. c, Confocal images of MRSA or MDR E. coli after the incubation with 0.06 mM Si-BPs + Si-Luc. After incubation, the treated bacteria were rinsed with PBS buffer for several times. The bacterial cell concentration is ~107 CFU. Scale bars, 25 μm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 9. CLSM images of bacteria treated with Si-BPs, Si-Luc and Si-BPs + Si-Luc. a, Confocal images of S. aureus or Salmonella typhimurium (STm) after the incubation with 0.06 mM Si-BPs and corresponding flow cytometry analysis of uptake rates. b, Confocal images of S. aureus or STm after the incubation with 0.06 mM Si-Luc and corresponding flow cytometry analysis of uptake rates. c, Confocal images of S. aureus or STm after the incubation with 0.06 mM Si-BPs + Si-Luc. After incubation, the treated bacteria were rinsed with PBS buffer for several times. The bacterial cell concentration is ~107 CFU. Scale bars, 25 μm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 10. Confirmation of the successful construction of ΔlamB and ΔmalE. a, A scheme illustrating the location of primers of ΔlamB-seqF and ΔlamB-seqR relative to lamB. b, Confirmation of lamB knockout by PCR. c, A scheme illustrating the location of primers of ΔmalE-seqF and ΔmalE-seqR relative to malE. d, Confirmation of malE knockout by PCR.

Supplementary Fig. 11. Flow cytometry analysis of uptake rates of bacteria mutants of ΔlamB and ΔmalE after incubation with 0.06 mM GP-Si-BPs or GP-Si-Luc. The bacterial cell concentration is ~107 CFU.

-

Supplementary Fig. 12. CLSM images of the GP-Si-BPs-treated bacteria after treatments of pure GP, glucose and maltotriose with different concentrations. a-b, Confocal fluorescence images of S. aureus (a) or E. coli (b) incubated with GP with different concentrations (e.g., 0, 0.28, 1.12 mM) for 5 min and then incubated with 0.06 mM GP-Si-BPs for another 2.5 h. c-d, Confocal fluorescence images of S. aureus incubated with glucose (c) or maltotriose (d) with different concentrations (e.g., 0, 0.28, 1.12 mM) for 5 min and then incubated with 0.06 mM GP-Si-BPs for another 2.5 h. e, Corresponding histograms of fluorescent intensity images of S. aureus incubated with glucose or maltotriose. The bacterial cell concentration is ~107 CFU. Scale bars, 25 μm. Statistical analysis was performed using a one-way ANOVA analysis. Error bars represent the standard deviation obtained from three independent measurements. All imaging experiments were repeated three times with similar results. Source data are provided as a Source data file.

Supplementary Fig. 13. Evaluation of the selectivity of GP-Si-BPs and GP-Si-Luc for bacteria over mammalian cells. a, Confocal fluorescence images of pure human blood, the mixture of human blood and MRSA or MDR E. coli after incubation with GP-Si-BPs, GP-Si-Luc and GP-Si-BPs + GP-Si-Luc. Arrows indicate red blood cells (RBCs). Scale bars, 25 μm. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 14. Ex vivo bioluminescence imaging of kidney tissues isolated from S. aureus (~1.0 × 108 CFU) nephritis-bearing mice with different treatments as indicated. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 15. Ex vivo bioluminescence imaging of kidney tissues isolated from S. aureus nephritis-bearing mice at different treating time points using Trojan BLI probes. All imaging experiments were repeated three times with similar results.

Supplementary Fig. 16. Evaluation of cytotoxicity of Trojan BLI probes. a, Morphology of HEK-293T, HeLa, MCF-7 and mREC cells treated with GP-Si-BPs + GP-Si-Luc (0.06 mM) for 24 h, respectively. b, Cell viability of HEK-293T, HeLa, MCF-7 and mREC cells treated with GP-Si-BPs + GP-Si-Luc with different dosages for 24 h, respectively. All error bars represent the standard deviation determined from three independent assays. Scale bar, 50μm. All imaging experiments were repeated three times with similar results. Source data are provided as a Source data file.

Supplementary Fig. 17. Representative histological images of major organs of healthy mice treated with 0.06 mM GP-Si-BPs or GP-Si-Luc for 24 h. a, H&E staining of different organs (heart, liver, spleen, lung and kidney) harvested from treated mice. Scale bars, 20 μm. b, Masson’s trichrome staining of different organs (heart, liver, spleen, lung and kidney) harvested from treated mice. Scale bars, 20 μm.

Supplementary Fig. 18. a, Ex vivo fluorescence imaging of organs resected from healthy mice after intravenous injection of 0.06 mM GP-Si-BPs at different time points. First row (from left to right): heart (He), liver (Li), spleen (Sp); second row (from left to right): lung (Lu), and kidney (Ki). b, Ex vivo fluorescence imaging of urine from healthy mice treated with PBS (control) or 0.06 mM GP-Si-BPs after 24 h post-injection.

Supplementary Table 1. Blood biochemical analysis of health mice treated with PBS, GP-Si-Luc or GP-Si-BPs for 24 h.

| Analysis index | PBS |  | GP-Si-Luc |  | GP-Si-BPs |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Mean | Standard deviation | Mean | Standard deviation | Mean | Standard deviation |
| Albumin and globulin ratio | 2.15 | 0.11 | 2.18 | 0.13 | 1.81 | 0.12 |
| Alanine aminotransferase (U/L) | 14.04 | 0.84 | 18.59 | 1.19 | 13.26 | 3.40 |
| Aspartate aminotransferase (U/L) | 45.53 | 7.49 | 46.43 | 10.08 | 47.19 | 7.08 |
| Alkaline phosphatase (U/L) | 46.88 | 13.81 | 46.20 | 4.35 | 52.66 | 3.52 |
| Urea (mmol/L) | 10.64 | 0.10 | 10.51 | 0.26 | 10.61 | 0.33 |
| Creatinine (μmol/L) | 6.47 | 0.63 | 9.06 | 1.78 | 8.04 | 0.67 |
| Total protein (mmol/L) | 18.54 | 0.56 | 17.70 | 0.45 | 18.70 | 0.70 |
| Albumin (g/L) | 12.66 | 0.34 | 12.12 | 0.09 | 12.02 | 0.17 |
| Globulin (g/L) | 5.89 | 0.33 | 5.58 | 0.38 | 6.68 | 0.54 |

Supplementary Table 2. Blood routine analysis of mice injected with PBS, GP-Si-Luc or GP-Si-BPs for 24 h.

| Analysis index | PBS |  | GP-Si-Luc |  | GP-Si-BPs |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Mean | Standard deviation | Mean | Standard deviation | Mean | Standard deviation |
| White blood cell (1.0×103 cells/μL) | 0.62 | 0.27 | 0.89 | 0.12 | 0.63 | 0.20 |
| Red blood cell (1.0×106 cells/μL) | 1.96 | 1.56 | 1.96 | 1.24 | 8.03 | 2.12 |
| Hemoglobin (g/dL) | 2.77 | 0.49 | 2.77 | 0.32 | 3.13 | 0.51 |
| Hematocrit (%) | 11.53 | 2.27 | 11.30 | 1.21 | 13.17 | 2.61 |
| Mean corpuscular volume (fL) | 59.10 | 0.62 | 57.70 | 1.42 | 59.37 | 1.19 |
| Mean corpuscular hemoglobin (pg) | 14.03 | 0.38 | 14.37 | 0.32 | 14.17 | 0.55 |
| Mean corpuscular hemoglobin concentration (g/dL) | 23.80 | 0.82 | 24.83 | 0.58 | 23.83 | 0.55 |
| Mean corpuscular hemoglobin concentration (g/dL) | 22.53 | 0.15 | 23.03 | 0.40 | 22.37 | 0.35 |
| Cholesterol (pg) | 13.27 | 0.15 | 13.27 | 0.25 | 13.23 | 0.06 |
| Red cell volume distribution width (%) | 12.33 | 0.12 | 12.03 | 0.25 | 12.30 | 0.35 |
| Hemoglobin content distribution width (g/dL) | 1.71 | 0.02 | 1.68 | 0.04 | 1.68 | 0.06 |
| Platelet (1.0×103 cells/μL) | 109.33 | 13.05 | 100.00 | 8.72 | 108.33 | 4.51 |
| Mean platelet volume (fL) | 10.13 | 0.72 | 9.13 | 0.42 | 10.03 | 0.32 |

Supplementary Notes:

Table of supplementary notes

1. Confirmation of lamB knockout by Sanger sequencing

2. Confirmation of malE knockout by Sanger sequencing

1. Confirmation of lamB knockout by Sanger sequencing

AAAGCCGTGATGTCCAGGTTGGAGCCAATATGTCGCTGGGTATTCGCCCGGAACATCTACTGCCGAGTGATATCGCTGACGTCATCCTTGAGGGTGAAGTTCAGGTCGTCGAGCAACTCGGCAACGAAACTCAAATCCATATCCAGATCCCTTCCATTCGTCAAAACCTGGTGTACCGCCAGAACGACGTGGTGTTGGTAGAAGAAGGTGCCACATTCGCTATCGGCCTGCCGCCAGAGCGTTGCCATCTGTTCCGTGAGGATGGCACTGCATGTCGTCGACTGCATAAGGAGCCGGGCGTTTAAGCACCCCACAAAACACACAAAGCCTGTCACAGGTGATGTGAAAAAAGAAAAGCAATGACTCAGGAGATAGATAGCAAAACCTGGGCCGGATAAGGCGTTTACGCCGCATTCGGCAACCAACGCCTGATGCGACGCTTGCGCGTCTTATCAGGCCTACAACGGCTGTCAAATGTAGGCCGGATAAGGCGTTTACGCCGCATCCGGCATAAAAACAGGTTGTCATTATCTGAAAGGGGCGAAAGCCCCTCTGATTATCGGGTTTAGCGCGCTATTGCCTGGCTACCGCTGAGCTCCAGATTTTGAGGTGAAAACAATGAAAATGAATAAAAGTCTCATCGTCCTCTGTTTATCAGCAGGGTTACTGGCAAGCGCGCCTGGAATTAGCCTTGCCGATGTTAACTACGTACCGCAAAACACCAGCGACGCGCCAGCCATTCCATCTGCTGCGCTGCAACAACTCACCTGGACACCGGTCGATCAATCT

2. Confirmation of malE knockout by Sanger sequencing

GCTGTACGCTCGCCATGCCCTTCTCCCTTTGTAACAACCTGTCATCGACAGCAACATTCATGATGGGCTGACTATGCGTCATCAGGAGATGGCTTAAATCCTCCACCCCCTGGCTTTTTTATGGGGGAGGAGGCGGGAGGATGAGAACACGGCTTCTGTGAACTAAACCGAGGTCATGTAAGGAATTTCGTGATGTTGCTTGCAAAAATCGTGGCGATTTTATGTGCGCATCTCCACATTACCGCCAATTCTGTAACAGAGATCACACAAAGCGACGGTGGGGCGTAGGGGCAAGGAGGATGGAAAGAGGTTGCCGTATAAAGAAACTAGAGTCCGTTTAGGTGTTTTCACGAGCACTTCACCAACAAGGACCATAGATTTGCTGTGAAATGCCGGATGCGGCGTGAACGCCTTGTCCGGCCTACAAAACCGAAACGTATGTAGGCCTGATAAGACGCGTCAGCGTCGCATCAGGCAGTTGTTGTCGGATAAGGCGTGAAAGCCTTATCCGTCCTGGAATGAGGAAGAACCCCATGGATGTCATTAAAAAGAAACATTGGTGGCAAAGCGACGCGCTGAAATGGTCAGTGCTAGGTCTGCTCGGCCTGCTGGTGGGTTACCTTGTTGTTTTAATGTACGCACAAGGGGAATACCTGTTCGCCATTACCACGCTGATATTGAGTTCAGCGGGGCTGTATATTTTCGCCAATCGTAAAGCCTACGCCTGGCGCTATGTTTACCCGGGAATGGCTGGAATGGGATTATTCGTCCTCTTCCCTCTGGTCTGCACCATCGCCATTGCCTTCACCA