Ni-P based Alloy Coatings Prepared by Direct and Pulsed Electrodeposition for Hydrogen Evolution Reaction in Alkaline Media

A. P. Gaikwada, Atindra Mohan Banerjeea, c, *, M. R. Paia, c, Rajat Dheemana#, Sanjay Kumarb, A. K. Tripathia, c

# a - Chemistry Division, b - Materials Science Division, Bhabha Atomic Research Centre, Mumbai-400085

# c - Homi Bhabha National Institute, Anushaktinagar, Mumbai-400094

| Spectrum No. | Ni | P | Ni/p |
| --- | --- | --- | --- |
| 1 | 5.9 | 0 | - |
| 2 | 4.9 | 0 | - |
| 3 | 5.8 | 0 | - |
| 4 | 5.9 | 0 | - |
| 5 | 6.2 | 0 | - |
| 6 | 5.5 | 0.4 | 13.75 |
| 7 | 5.2 | 0.4 | 13 |

| Spectrum No. | Ni | P | Ni/P |
| --- | --- | --- | --- |
| 8 | 2.7 | 0.2 | 13.5 |
| 9 | 4 | 0.3 | 13.33 |
| 10 | 3.2 | 0.5 | 6.4 |
| 11 | 3.7 | 0.6 | 6.17 |
| 12 | 3.5 | 0.5 | 7 |
| 13 | 3.7 | 0.5 | 7.4 |

| No. | Ni | P | Ni/P |
| --- | --- | --- | --- |
| 27 | 85.9 | 11.5 | 7.47 |
| 28 | 93.8 | 0.7 | 134 |
| 29 | 89.4 | 9.4 | 9.50 |
| 30 | 87.8 | 12.2 | 7.20 |
| 31 | 93.4 | 4.6 | 20.30 |
| 32 | 88 | 11.1 | 7.30 |
| 33 | 90.1 | 9.9 | 9.10 |
| 34 | 88.5 | 9.4 | 9.41 |
| 35 | 86.7 | 12.4 | 7 |
| 36 | 95.4 | 4.3 | 22.19 |