Investigation of electrode combinations to electricity generation from the pulp and paper industry’s wastewater

Humayun Iqbal1,2, Arup Bhowmik1,2, Sabina Yasmin3, Shahin Aziz4, Dipa Islam5, Mohammad Shah Jamal*1, Mosharof Hossain*1

Affiliations

1Institute of Fuel Research and Development, Bangladesh Council of Scientific and Industrial Research (BCSIR), Dhaka 1205, Bangladesh

2Department of Chemistry, Jahangirnagar University, Savar, Dhaka 1342, Bangladesh

3Institute of National Analytical Research & Services, Bangladesh Council of Scientific and Industrial Research (BCSIR), Dhaka 1205, Bangladesh

4BCSIR Laboratories, Dhaka, Dr. Qudrat-I-Khuda Road, Dhanmondi, Dhaka-1205, Bangladesh

5Biomedical and Toxicological Research Institute, Bangladesh Council of Scientific and Industrial Research (BCSIR), Dhaka 1205, Bangladesh

*Authors to whom correspondence should be addressed: mosharof@bcsir.gov.bd, msjdubd@gmail.com

Tel.: +8801741511376

SUPPORTING INFORMATION

Tables

Table S1 Fifteen days data of output voltage, current, power and power densities of MFC – 1 constructed with Zn & Cu electrodes

| Serial | Voltage (mV) | Current (mA) | Power (mW) | Power Density (mW/m2) |
| --- | --- | --- | --- | --- |
| 1 | 923 | 1.07 | 0.99 | 164.60 |
| 2 | 959 | 1.23 | 1.18 | 196.60 |
| 3 | 998 | 1.41 | 1.41 | 234.53 |
| 4 | 1034 | 1.6 | 1.65 | 275.73 |
| 5 | 1071 | 1.84 | 1.97 | 328.44 |
| 6 | 1103 | 2.1 | 2.32 | 386.05 |
| 7 | 1131 | 2.22 | 2.51 | 418.47 |
| 8 | 1152 | 2.35 | 2.71 | 451.20 |
| 9 | 1155 | 2.39 | 2.76 | 460.08 |
| 10 | 1143 | 2.32 | 2.65 | 441.96 |
| 11 | 1133 | 2.29 | 2.59 | 432.43 |
| 12 | 1107 | 2.07 | 2.29 | 381.92 |
| 13 | 1081 | 1.84 | 1.99 | 331.51 |
| 14 | 1043 | 1.67 | 1.74 | 290.30 |
| 15 | 1011 | 1.52 | 1.54 | 256.12 |

Table S2 Fifteen days data of voltage, current, power and power densities of MFC – 2 constructed with Zn mesh & Carbon electrodes

| Serial | Voltage (mV) | Current (mA) | Power (mW) | Power Density (mW/m2) |
| --- | --- | --- | --- | --- |
| 1 | 998 | 1.21 | 1.21 | 201.26 |
| 2 | 1039 | 1.48 | 1.54 | 256.29 |
| 3 | 1080 | 1.74 | 1.88 | 313.20 |
| 4 | 1115 | 2.02 | 2.25 | 375.38 |
| 5 | 1147 | 2.29 | 2.63 | 437.77 |
| 6 | 1171 | 2.54 | 2.97 | 495.72 |
| 7 | 1193 | 2.69 | 3.21 | 535.02 |
| 8 | 1188 | 2.64 | 3.14 | 522.72 |
| 9 | 1175 | 2.53 | 2.97 | 495.46 |
| 10 | 1137 | 2.46 | 2.80 | 466.17 |
| 11 | 1101 | 2.31 | 2.54 | 423.89 |
| 12 | 1070 | 2.12 | 2.27 | 378.07 |
| 13 | 1041 | 1.97 | 2.05 | 341.80 |
| 14 | 1011 | 1.69 | 1.71 | 284.77 |
| 15 | 987 | 1.40 | 1.38 | 230.30 |

Table S3 Fifteen days data of voltage, current, power and power densities of MFC – 3 constructed with Al mesh & Carbon electrodes

| Serial | Voltage (mV) | Current (mA) | Power (mW) | Power Density (mW/m2) |
| --- | --- | --- | --- | --- |
| 1 | 281 | 0.06 | 0.02 | 3.61 |
| 2 | 298 | 0.07 | 0.03 | 4.57 |
| 3 | 309 | 0.09 | 0.03 | 5.61 |
| 4 | 316 | 0.10 | 0.04 | 6.27 |
| 5 | 321 | 0.12 | 0.04 | 6.79 |
| 6 | 325 | 0.14 | 0.04 | 7.21 |
| 7 | 326 | 0.16 | 0.04 | 7.10 |
| 8 | 324 | 0.15 | 0.04 | 7.02 |
| 9 | 325 | 0.15 | 0.04 | 7.04 |
| 10 | 323 | 0.15 | 0.04 | 6.84 |
| 11 | 322 | 0.14 | 0.04 | 6.60 |
| 12 | 320 | 0.12 | 0.04 | 6.40 |
| 13 | 318 | 0.11 | 0.04 | 6.10 |
| 14 | 317 | 0.10 | 0.04 | 6.02 |
| 15 | 314 | 0.09 | 0.03 | 5.67 |

Table S4 Fifteen days data of voltage, current, power and power densities of MFC – 4 constructed with carbon electrodes in both anode and cathode

| Serial | Voltage (mV) | Current (mA) | Power (mW) | Power Density (mW/m2) |
| --- | --- | --- | --- | --- |
| 1 | 512 | 0.15 | 0.08 | 12.89 |
| 2 | 575 | 0.17 | 0.10 | 16.68 |
| 3 | 616 | 0.20 | 0.12 | 20.74 |
| 4 | 643 | 0.24 | 0.15 | 25.72 |
| 5 | 655 | 0.27 | 0.18 | 29.58 |
| 6 | 674 | 0.29 | 0.20 | 32.69 |
| 7 | 686 | 0.28 | 0.19 | 31.67 |
| 8 | 677 | 0.27 | 0.18 | 30.01 |
| 9 | 661 | 0.24 | 0.16 | 26.44 |
| 10 | 638 | 0.20 | 0.13 | 21.48 |
| 11 | 601 | 0.18 | 0.11 | 18.33 |
| 12 | 566 | 0.17 | 0.09 | 15.00 |
| 13 | 521 | 0.16 | 0.08 | 12.68 |
| 14 | 495 | 0.14 | 0.07 | 11.39 |
| 15 | 472 | 0.13 | 0.05 | 9.04 |

Table S5 Fifteen days data of voltage, current, power and power densities of MFC – 5 constructed with Zn & Cu electrodes in presence of 1M CuSO4.5H2O

| Serial | Voltage (mV) | Current (mA) | Power (mW) | Power Density (mW/m2) |
| --- | --- | --- | --- | --- |
| 1 | 1023 | 2.57 | 2.63 | 438.19 |
| 2 | 1045 | 2.93 | 3.06 | 510.31 |
| 3 | 1068 | 3.41 | 3.64 | 606.98 |
| 4 | 1095 | 3.87 | 4.24 | 706.28 |
| 5 | 1121 | 4.29 | 4.81 | 801.52 |
| 6 | 1149 | 4.58 | 5.26 | 877.07 |
| 7 | 1171 | 4.64 | 5.43 | 905.57 |
| 8 | 1182 | 4.74 | 5.60 | 933.78 |
| 9 | 1185 | 4.79 | 5.68 | 946.03 |
| 10 | 1174 | 4.54 | 5.33 | 888.33 |
| 11 | 1151 | 4.07 | 4.68 | 780.76 |
| 12 | 1126 | 3.64 | 4.10 | 683.11 |
| 13 | 1102 | 3.27 | 3.60 | 600.59 |
| 14 | 1085 | 2.92 | 3.17 | 528.03 |
| 15 | 1071 | 2.59 | 2.77 | 462.32 |

Table S6 Fifteen days data of voltage, current, power and power densities of MFC – 6 constructed with carbon electrodes in both anode and cathode in presence of 1M Fe2(SO4)3

| Serial` | Voltage (mV) | Current (mA) | Power (mW) | Power Density (mW/m2) |
| --- | --- | --- | --- | --- |
| 1 | 723 | 0.97 | 0.70 | 116.89 |
| 2 | 749 | 1.06 | 0.79 | 132.32 |
| 3 | 778 | 1.17 | 0.91 | 151.71 |
| 4 | 811 | 1.32 | 1.07 | 178.42 |
| 5 | 843 | 1.51 | 1.27 | 212.16 |
| 6 | 878 | 1.68 | 1.48 | 245.84 |
| 7 | 905 | 1.86 | 1.68 | 280.55 |
| 8 | 928 | 2.07 | 1.92 | 320.16 |
| 9 | 947 | 2.21 | 2.09 | 348.81 |
| 10 | 962 | 2.35 | 2.26 | 376.98 |
| 11 | 959 | 2.30 | 2.21 | 367.62 |
| 12 | 951 | 2.24 | 2.13 | 355.04 |
| 13 | 928 | 2.09 | 1.94 | 323.25 |
| 14 | 897 | 1.91 | 1.71 | 285.55 |
| 15 | 864 | 1.60 | 1.46 | 243.36 |

Table S7 Percent of Water recovery after MFC treatment

| Sample | BOD | Conductivity | TSS | TDS | Turbidity |
| --- | --- | --- | --- | --- | --- |
| MFC - 1 | 89% | 94% | 74% | 68% | 80% |
| MFC - 2 | 92% | 97% | 77% | 70% | 82% |
| MFC - 3 | 37% | 46% | 30% | 26% | 33% |
| MFC - 4 | 72% | 86% | 68% | 63% | 74% |
| MFC - 5 | 93% | 98% | 79% | 72% | 87% |
| MFC - 6 | 86% | 97% | 73% | 68% | 85% |