Fabrication of highly crystalline covalent organic framework for solid-phase extraction of three dyes from food and water samples

Junji Wang, Yongqing Tao, Luchun Wang, Meng Tian, Yulian Yang, Qiuyi Liu, Yuemeng Zou, Shaochi Liu, Hong Niu, Dandan Wang*, Die Gao*

School of Pharmacy, Southwest Medical University, Luzhou, Sichuan, 646000, China.

* To whom correspondence should be addressed: Dr. Die Gao and Dr. Dandan Wang, School of Pharmacy, Southwest Medical University, Luzhou, Sichuan 646000, P.R. China. Email address: gaodie_1203@126.com (D. Gao) and wangdanan_93@163.com

- The conditions of HPLC analysis

Analysis of congo red and direct red 80 were performed on an Agilent 1260 Infinity Ⅱ coupled with a DAD detector. Separation and analysis were conducted on an Eclipse XDB-C18 (4.6×250 mm, 5 μm particle size). For three dyes, the mobile phase was 60% acetonitrile (A) and 40% water (B) at a flow rate of 0.8 mL·min-1 with a detection wavelength of 500, 520 and 580 nm, respectively. The sample volume injected was 20 μL and the column temperature was maintained at 30 ℃ for all HPLC analysis.

- The calculation of the adsorption capacity of three dyes

The equilibrium adsorption capacity Q (mg⋅g-1) is calculated by the following equation.

Q = (C0-Ce )×Vm                             (1)

Where C0 was the initial concentration of sample solution μg⋅mL-1, Ce was the equilibrium concentration of sample solution μg⋅mL-1, V is the volume of sample solution added (mL), m is the mass of adsorbent used (mg).

- Calculation of the enrichment factors

Enrichment factor (EF) was calculated by the following equations:

EF =Ca/Cs

Where Ca and Cs are the concentrations of the target dyes in analytical and sample solutions, respectively.

Figure S1 The structures of the selected dyes

Figure S2 A. Particle size distribution of COF-TFTP. B. XPS pattern of C1s. C. XPS pattern of N1s. D. XPS pattern of O1s. E. Pore size distribution of the COF-TFTP.

Figure S3 Langmuir isotherms adsorption model curves of the dyes. A. Congo red. B. Methyl blue. C. Direct red 80. Freundlich isotherms adsorption model curves of the dyes. D. Congo red. E. Methyl blue. F. Direct red 80.

Figure S4 Pseudo-first order model curves of the dyes. A. Congo red. B. Methyl blue. C. Direct red 80. Pseudo-second order model curves of the dyes. D. Congo red. E. Methyl blue. F. Direct red 80.

Figure S5 The recycle test of the COF-TFTP.

Figure S6 Optimization of A. Loading dosage of COF-TFTP for SPE column. B. The sample flow rate. C. Desorption solvent volume.

Figure S7 HPLC chromatograms of pork sample water (A) and waste water (B) (Congo red).

Table S1 Method comparisons for the adsorption of three dyes

| Analytes | Absorbent | Adsorption capacity (mg·g-1) | Method | Ref |
| --- | --- | --- | --- | --- |
| Congo red | Magnetic lignin-based | 198.8 | UV-vis | (Jiang, et al., 2019) |
| Congo red | Carbon composite lignin-based | 198.5 | UV-vis | (Wang, et al., 2018) |
| Congo red | Amino-functionalized magnetic graphene oxide nanocomposite | 250 | UV-vis | (Sricharoen, et al., 2021) |
| Congo red | Ultrasound-assisted dispersive liquid antisolvent precipitation (UA-DLAP) | 250 | UV-vis | (Hosseini, Madrakian, Ahmadi, & Afkhami, 2020) |
| Congo red | COF-COOCa, COF-COONi | 704.23, 781.25 | UV-vis | (Yue, et al., 2019) |  |
| Congo red | S-doped Fe2O3/C magnetic nanocomposite | 270.2 | UV-vis | (Khoshsang, Ghaffarinejad, Kazemi, Wang, & Arandiyan, 2018) |  |
| Congo red | FexCo3-xO4 nanoparticles | 128.6 | UV-vis | (Liu, Wang, Zhang, & Baeyens, 2019) |  |
| Methyl blue | Sodium-doped graphitic carbon nitride | 360 | UV-vis | (Fronczak, Krajewska, Demby, & Bystrzejewski, 2017) |  |
| Methyl blue | Triptycene-based hyper-crosslinked porous polymer | 159.80 | UV-vis | (He, et al., 2022) |  |
| Methyl blue | Multi-hydroxyl containing organo-vermiculites | 178.3 | UV-vis | (Han, et al., 2022) |  |
| Methyl blue | Metal-modified barium lanthanum titanate | 37.6 | UV–vis | (Chang, Nguyen, Nguyen, & Hu, 2022) |  |
| Direct red 80 | Copper oxide nanoparticles | 14.07 | UV–vis | (Hamami & Javanbakht, 2021) |  |
| Direct red 80 | Almond shells | 20.5 | UV-vis | (Ardejani, Badii, Limaee, Shafaei, & Mirhabibi, 2008) |  |
| Congo red, methyl blue, direct red 80 | COF-TFTP | 284.10, 177.62 and 55.25 | HPLC-DAD | This work |  |

Table S2 Adsorption isotherm parameters of the dyes on COF-TFTP

| Compound | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Qmax (mg⋅g-1) | KL (mL/mg) | R2 | KF (mg1-1/nL1/ng-1) | n | R2 |
| Congo red | 526.32 | 0.0019 | 0.9933 | 4.448 | 1.558 | 0.9449 |
| methyl blue | 285.71 | 0.0019 | 0.9959 | 1.380 | 1.360 | 0.9813 |
| Direct red 80 | 56.50 | 0.0190 | 0.9653 | 13.870 | 4.830 | 0.8318 |

Table S3 Constants of Pseudo-first-order and Pseudo-second-order for the dyes

| Compound | Pseudo-first-order constants |  | Pseudo-second-order constants |  |
| --- | --- | --- | --- | --- |
|  | K1 (min-1) | R2 | K2 (g·mg-1·min-1) | R2 |
| Congo red | 0.0017 | 0.5074 | 0.0046 | 0.9998 |
| methyl blue | 0.0016 | 0.4476 | 0.0225 | 0.9978 |
| Direct red 80 | 0.0161 | 0.5316 | 0.0080 | 0.9962 |

Table S4 Linearity, LODs, LOQs and precision for developed methods

| Analytes | Linear ranges (μg⋅mL-1) | r | LODs | LOQs | Intra-day (%) |  |  | Inter-day (%) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | (μg⋅mL-1) | (μg⋅mL-1) | Low | Medium | High |  | Low | Medium | High |
| Methyl blue | 0.25-100 | 0.9993 | 0.10 | 0.25 | 2.47 | 6.64 | 3.72 |  | 2.22 | 1.79 | 1.17 |
| Congo red | 1-100 | 0.9991 | 0.34 | 1.00 | 4.70 | 2.60 | 1.34 |  | 4.76 | 2.56 | 0.18 |
| Direct red 80 | 0.5-100 | 0.9994 | 0.17 | 0.50 | 3.45 | 2.32 | 0.38 |  | 2.70 | 1.97 | 0.28 |

References

Ardejani, F. D., Badii, K., Limaee, N. Y., Shafaei, S. Z., & Mirhabibi, A. R. (2008). Adsorption of Direct Red 80 dye from aqueous solution onto almond shells: Effect of pH, initial concentration and shell type. J Hazard Mater, 151(2-3), 730-737. https://doi.org/10.1016/j.jhazmat.2007.06.048.

Chang, A. L., Nguyen, B. S., Nguyen, V. H., & Hu, C. C. (2022). Adsorption kinetics of methyl blue using metal-modified barium lanthanum titanate as an effective absorbent. Mater Chem Phys, 276. https://doi.org/10.1016/j.matchemphys.2021.125363.

Fronczak, M., Krajewska, M., Demby, K., & Bystrzejewski, M. (2017). Extraordinary Adsorption of Methyl Blue onto Sodium-Doped Graphitic Carbon Nitride. J Phys Chem C, 121, 15756-15766. https://doi.org/10.1021/acs.jpcc.7b03674.

Hamami, Z., & Javanbakht, V. (2021). Biosynthesis of copper oxide nanoparticles using biomass, peel, and extract polysaccharides of Solanum Tuberosum for ultrasound-assisted adsorption of azo direct red 80 contaminants. Ceram Int 47, 24170-24181. https://doi.org/10.1016/j.ceramint.2021.05.128.

Han, L., Wang, T. T., Gong, J. C., Li, X., Ji, Y. X., & Wang, S. F. (2022). Multi-hydroxyl containing organo-vermiculites for enhanced adsorption of coexisting methyl blue and Pb(II) and their adsorption mechanisms. Colloid Surface A, 650. https://doi.org/10.1016/j.colsurfa.2022.129542.

He, Y., Bao, W. L., Hua, Y. C., Guo, Z. L., Fu, X. L., Na, B., Yuan, D. Z., Peng, C. J., & Liu, H. L. (2022). Efficient adsorption of methyl orange and methyl blue dyes by a novel triptycene-based hyper-crosslinked porous polymer. RSC Adv, 12, 5587-5594. https://doi.org/10.1039/d1ra08589a.

Hosseini, Z., Madrakian, T., Ahmadi, M., & Afkhami, A. (2020). Ultrasound-assisted dispersive liquid antisolvent precipitation for extraction of polar organic compounds in water. Anal Chim Acta, 1135, 91-98. https://doi.org/10.1016/j.aca.2020.08.027.

Jiang, C. L., Wang, X. H., Qin, D. M., Da, W. X., Hou, B. X., Hao, C., & Wu, J. B. (2019). Construction of magnetic lignin-based adsorbent and its adsorption properties for dyes. J Hazard Mater, 369, 50-61. https://doi.org/10.1016/j.jhazmat.2019.02.021.

Khoshsang, H., Ghaffarinejad, A., Kazemi, H., Wang, Y., & Arandiyan, H. (2018). One-pot synthesis of S-doped Fe2O3/C magnetic nanocomposite as an adsorbent for anionic dye removal: equilibrium and kinetic studies. J Nanostructure Chem, 8, 23-32. https://doi.org/10.1007/s40097-017-0251-4.

Liu, J., Wang, N., Zhang, H. L., & Baeyens, J. (2019). Adsorption of Congo red dye on FexCo3-xO4 nanoparticles. J Environ Manage, 238, 473-483. https://doi.org/10.1016/j.jenvman.2019.03.009.

Sricharoen, P., Chanthai, S., Lamaiphan, N., Sakaew, C., Limchoowong, N., Nuengmatcha, P., & Oh, W. C. (2021). Sono-synthesized Fe3O4-GO-NH2 nanocomposite for highly efficient ultrasound-assisted magnetic dispersive solid-phase microextraction of hazardous dye Congo red from water samples. J Korean Ceram Soc, 58, 201-211. https://doi.org/10.1007/s43207-020-00089-y.

Wang, X. H., Jiang, C. L., Hou, B. X., Wang, Y. Y., Hao, C., & Wu, J. B. (2018). Carbon composite lignin-based adsorbents for the adsorption of dyes. Chemosphere, 206, 587-596. https://doi.org/10.1016/j.chemosphere.2018.04.183.

Yue, J. Y., Wang, L., Ma, Y., Yang, P., Zhang, Y. Q., Jiang, Y., & Tang, B. (2019). Metal ion-assisted carboxyl-containing covalent organic frameworks for the efficient removal of Congo red. Dalton Transactions, 48(48), 17763-17769. Dalton T, 48, 17763-17769. https://doi.org/10.1039/c9dt04175c.