# Supporting Information

Carbon Nanotubes Encapsulated Transition Metals for Efficient Hydrogen Evolution Reaction: Coupling Effect of 3d Orbital and π-Bond

Yun Han1, Xin Mao2, Xuecheng Yan*3, Qilong Wu4, Hongzhe Xu1, Qingchao Fang2, Yi Jia5, Xiangdong Yao6, Qin Li*1, Aijun Du*2

1 School of Engineering and Built Environment, Queensland Micro- and Nanotechnology Centre, Griffith University, Nathan Campus, Queensland, 4111, Australia, qin.li@griffith.edu.au.

2 School of Chemistry and Physics and Centre for Materials Science, Queensland University of Technology, Gardens Point Campus, Brisbane 4001, Australia, aijun.du@qut.edu.au.

3 Queensland Micro- and Nanotechnology Centre, Griffith University, Nathan Campus, QLD 4111, Australia, x.yan@griffith.edu.au.

4 Intelligent Polymer Research Institute and ARC Centre of Excellence for Electromaterials Science, Australian Institute for Innovative Materials, University of Wollongong, Wollongong, NSW 2500, Australia.

5 College of Chemical Engineering and Zhejiang Carbon Neutral Innovation Institute, Zhejiang University of Technology, Hangzhou 310032, P. R. China.

6 School of Advanced Energy, Sun Yat-Sen University (Shenzhen), Shenzhen, Guangdong 518107, P. R. China.

Figure S1. (a) Top-view and (b) side-view of Fe@CNT. (c) Side-view of Fe@CNT-H (one hydrogen atom adsorbed on Fe@CNT). (d) Top-view and (e) side-view of Co@CNT. (e) Side-view of Co@CNT-H (one hydrogen atom adsorbed on Co@CNT). The Fe, Co, C, and H atoms are shown in gold, navy, brown and pink, respectively.

Figure S2. (a), (c) and (e) show the top-view of TM@G (TM = Fe, Co, Ni). (b), (d) and (f) show the side-view of TM@G-H (one hydrogen atom adsorbed on TM@G, TM = Fe, Co, Ni). The Fe, Co, Ni, C, and H atoms are shown in gold, navy, grey, brown and pink, respectively.

Figure S3. (a) Local density of states (LDOS) of Fe and C atoms in Fe@CNT, and total LDOS of Fe@CNT and pristine CNTs. The black dashed line indicates the Fermi level relative to vacuum. (c) Differential charge density distributions of Fe@CNT and (d) a H atom chemisorbed on it (Fe@CNT-H). The yellow and blue colours represent electron accumulation and depletion regions, respectively, the isosurface value for (c) is 3×10-3 e/Å3, and for (d) is 1.8×10-3 e/Å3.

Figure S4. (a) Local density of states (LDOS) of Co and C atoms in Co@CNT, and total LDOS of Co@CNT and pristine CNT. The black dashed line indicates the Fermi level relative to vacuum. (c) Differential charge density distributions of Co@CNT and (d) a H atom chemisorbed on it (Co@CNT-H). The yellow and blue colours represent electron accumulation and depletion regions, respectively, the isosurface value for (c) is 3×10-3 e/Å3, and for (d) is 1.8×10-3 e/Å3.

Figure S5. (a) Local density of states (LDOS) of Ni and C atoms in Ni@G, and total LDOS of Ni@G and pristine graphene nanosheets. The black dashed line indicates the Fermi level relative to vacuum. (c) Differential charge density distributions of Ni@G and (d) a H atom chemisorbed on it (Ni@G-H). The yellow and blue colours represent electron accumulation and depletion regions, respectively, the isosurface value for (c) is 3×10-3 e/Å3, and for (d) is 1.8×10-3 e/Å3.