Table 1: The actual and coded values used for doing the RSM study in methylene blue photodegradation by ZB21.

| Std. dev. | Mean | High | Low | Unit | Factors |
| --- | --- | --- | --- | --- | --- |
| 5.10 | 12.5 | 20 | 5 | mg/L | A: Initial concentration |
| 3.06 | 7.5 | 12 | 3 | – | B: pH |
| 0.255 | 0.875 | 1.25 | 0.5 | mg/L | C: Catalysis dosage |
| 4.76 | 11 | 18 | 4 | W | D: Light intensity |

Table 2: All suggested performances by the software and the answer variable.

| Removal (%) |  | X4 | X3 | X2 | X1 | Run |
| --- | --- | --- | --- | --- | --- | --- |
| Pred. | Exp. |  |  |  |  |  |
| 11.95 | 12.26 | 4 | 0.875 | 3 | 12.5 | 1 |
| 27.37 | 28.02 | 18 | 0.875 | 7.5 | 20 | 2 |
| 16.58 | 17.64 | 11 | 0.875 | 3 | 5 | 3 |
| 74.68 | 74.74 | 11 | 0.5 | 12 | 12.5 | 4 |
| 82.73 | 82.79 | 11 | 0.875 | 12 | 5 | 5 |
| 16.67 | 16.67 | 11 | 0.875 | 7.5 | 12.5 | 6 |
| 22.84 | 22.64 | 11 | 0.875 | 3 | 20 | 7 |
| 13.10 | 12.86 | 11 | 0.5 | 7.5 | 5 | 8 |
| 11.31 | 11.02 | 4 | 0.5 | 7.5 | 12.5 | 9 |
| 77.35 | 76.93 | 18 | 0.875 | 12 | 12.5 | 10 |
| 22.45 | 23.35 | 4 | 0.875 | 7.5 | 20 | 11 |
| 15.86 | 16.01 | 18 | 1.25 | 7.5 | 12.5 | 12 |
| 13.84 | 14.06 | 11 | 1.25 | 3 | 12.5 | 13 |
| 16.67 | 15.67 | 11 | 0.875 | 7.5 | 12.5 | 14 |
| 20.15 | 19.52 | 18 | 0.875 | 7.5 | 5 | 15 |
| 78.38 | 79.09 | 11 | 1.25 | 12 | 12.5 | 16 |
| 19.06 | 17.73 | 4 | 1.25 | 7.5 | 12.5 | 17 |
| 26.15 | 26.3 | 11 | 1.25 | 7.5 | 5 | 18 |
| 11.62 | 11.18 | 11 | 0.5 | 3 | 12.5 | 19 |
| 17.70 | 18.9 | 18 | 0.5 | 7.5 | 12.5 | 20 |
| 27.09 | 26.83 | 11 | 0.5 | 7.5 | 20 | 21 |
| 16.29 | 15.37 | 18 | 0.875 | 3 | 12.5 | 22 |
| 78.49 | 79.3 | 4 | 0.875 | 12 | 12.5 | 23 |
| 19.96 | 20.09 | 11 | 1.25 | 7.5 | 20 | 24 |
| 21.88 | 21.505 | 4 | 0.875 | 7.5 | 5 | 25 |
| 84.28 | 83.08 | 11 | 0.875 | 12 | 20 | 26 |
| 16.67 | 17.67 | 11 | 0.875 | 7.5 | 12.5 | 27 |

Table 3 : Sequential model sum of squares.

| Source | Sum of Squares | df | Mean Square | F-value | P-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mean vs Total | 27470.5 | 1 | 27470.5 |  |  |  |
| Linear vs Mean | 12289.6 | 4 | 3072.4 | 12.03 | < 0.0001 |  |
| 2FI vs Linear | 149.5 | 6 | 24.9 | 0.0729 | 0.9980 |  |
| Quadratic vs 2FI | 5454.7 | 4 | 1363.7 | 1324 | < 0.0001 | Suggested |
| Cubic vs Quadratic | 10.15 | 8 | 1.27 | 2.30 | 0.2201 | Aliased |
| Residual | 2.21 | 4 | 0.5527 |  |  |  |
| Total | 45376.7 | 27 | 1680.6 |  |  |  |

Table 4: Lack of fit test.

| Source | Sum of Squares | df | Mean Square | F-value | P-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Linear | 5614.6 | 20 | 280.7 | 280.7 | 0.0036 |  |
| 2FI | 5465.1 | 14 | 390.4 | 390.4 | 0.0026 |  |
| Quadratic | 10.36 | 10 | 1.04 | 1.04 | 0.5863 | Suggested |
| Cubic | 0.2110 | 2 | 0.1055 | 0.1055 | 0.9046 | Aliased |
| Pure error | 2.00 | 2 | 1.00 |  |  |  |

Table 5: ANOVA for Quadratic model.

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 17894 | 14 | 1278 | 1241 | < 0.0001 | Significant |
| X1 | 45.6 | 1 | 45.6 | 44.3 | < 0.0001 |  |
| X2 | 12210 | 1 | 12210 | 11855 | < 0.0001 |  |
| X3 | 26.3 | 1 | 26.3 | 25.6 | 0.0003 |  |
| X4 | 7.7 | 1 | 7.7 | 7.4 | 0.0184 |  |
| X12 | 5.5 | 1 | 5.5 | 5.4 | 0.0387 |  |
| X13 | 101.8 | 1 | 101.8 | 98.8 | < 0.0001 |  |
| X14 | 11.1 | 1 | 11.1 | 10.8 | 0.0066 |  |
| X23 | 0.5402 | 1 | 0.5402 | 0.5245 | 0.4828 |  |
| X24 | 7.51 | 1 | 7.51 | 7.3 | 0.0193 |  |
| X34 | 23.04 | 1 | 23.04 | 22.4 | 0.0005 |  |
| X12 | 188.3 | 1 | 188.3 | 182.8 | < 0.0001 |  |
| X22 | 4485 | 1 | 4485 | 4355 | < 0.0001 |  |
| X32 | 5.7 | 1 | 5.7 | 5.5 | 0.0365 |  |
| X42 | 0.6665 | 1 | 0.6665 | 0.6471 | 0.4368 |  |
| Residual | 12.4 | 12.0 | 1.03 |  |  |  |
| Lack of Fit | 10.36 | 10 | 1.04 | 1.04 | 0.5863 | Not significant |
| Pure Error | 2.00 | 2 | 1.00 |  |  |  |
| Cor Total | 17906 | 26 |  |  |  |  |

summary statistics.  Table 6: Model

| Source | Std. Dev. | R² | Adjusted R² | Predicted R² | Press |  |
| --- | --- | --- | --- | --- | --- | --- |
| Linear | 15.98 | 0.6863 | 0.6293 | 0.5248 | 8510 |  |
| 2FI | 18.48 | 0.6947 | 0.5039 | 0.0655 | 16733 |  |
| Quadratic | 1.01 | 0.9993 | 0.9985 | 0.9964 | 64.2 | Suggested |
| Cubic | 0.7435 | 0.9999 | 0.9992 | 0.9981 | 34.9 | Aliased |