Supplementary Information

Cellulose nanocrystal films – Effect of electrolyte and lignin addition on self-assembly, optical, and mechanical properties

Mahesh Parita,b, Zhihua Jiang* a,b

- Department of Chemical Engineering, Auburn University, 212 Ross Hall, Auburn, AL 36849, USA

- Alabama Center for Paper and Bioresource Engineering, Auburn University, 356 Ross Hall, Auburn, AL 36849, USA

d

b

c

a

e

Fig.S1. Transmission spectra of CNC films with various electrolyte concentrations (a) NaOH (b) NaCl (c) CsCl (d) CaCl2 (e) AlCl3.

a

b

c

d

e

h

i

g

f

Fig.S2. CNC films at various NaOH concentrations (a) 0.125 mmol/g (b) 0.25 mmol/g (c) 0.375 mmol/g (d) 0.5 mmol/g (e) 0.75 mmol/g (f) 0.875 mmol/g (g) 1.75 mmol/g (h) 2.5 mmol/g (i) 3.75 mmol/g.

a

b

Fig.S3. (a) Dried dialyzed CNC film (b) Transmission spectra comparison of different CNC samples.

Fig.S4. 5 wt.% aqueous samples of dialyzed CNC (left) and as received CNC (right).

Fig.S5. XRD plots for pure CNC films and CNC films containing 1.25 mmol/g of various electrolytes

Fig.S6. Crystallinity of CNC films containing electrolytes at different concentrations.

Fig.S7.Crystallinity of CNC film samples added with 1.25 mmol/g electrolyte before and after dialysis.

Fig.S8. Dialyzed and redispersed samples after treating with CsCl, NaCl, NaOH, CaCl2 and AlCl3 (from left to right).

1595 cm-1

1512 cm-1

1702 cm-1

Fig.S9. FTIR spectra of KL and peroxide bleached KL samples.

b

a

Fig.S10. Scanning electron microscopy images of the CNC/lignin film cross sections showing the lignin dispersibility in 10 wt.% CNC/PBKL150.

Table S1. Effect of H2O2 concentration on lignin optical properties. (%T550 nm and %UV blocking at 400 nm obtained for 0.1 wt.% lignin solution and extinction coefficient obtained using absorbance at 255 nm).

| H2O2 Conc. (wt%) | H2O2/KL | %T at 550 nm | % UV blocking at 400 nm | Extinction coefficient at 255 nm (wt.%-1 cm-1) |
| --- | --- | --- | --- | --- |
| 0 | 0 | 31.2 | 99.7 | 223.8 |
| 50 | 0.5 | 62.5 | 99.3 | 206 |
| 150 | 1.5 | 85.5 | 93.7 | 187.3 |
| 200 | 2 | 87.6 | 90.8 | 185 |
| 400 | 4 | 90.3 | 89.8 | 175.2 |
| 600 | 6 | 91.6 | 89.4 | 157.3 |
| 1000 | 10 | 94.3 | 88.4 | 148.9 |

Table S2. %UV A, %UV B, %UV blocking at 400 nm and %T at 400 nm for CNC and CNC nanocomposites.

| Sample | %UV A blocking | %UV B blocking | %T at 550 nm | % UV blocking at 400 nm |
| --- | --- | --- | --- | --- |
| CNC | 19.9 | 26.6 | 86.8 | 18.8 |
| CNC/KL (10 wt.%) | 99.9 | 100.0 | 33.4 | 99.5 |
| CNC/4-ABA (10 wt.%) | 54.3 | 99.5 | 75.3 | 46.2 |
| CNC/PB-KL150 (4 wt.%) | 87.5 | 99.9 | 76.1 | 66.2 |
| CNC/PB-KL150 (10 wt.%) | 99.3 | 100.0 | 65.6 | 95.3 |