Supplementary Information: Multi-Task Mixture Density Graph Neural Networks for Predicting Cu-based Single-Atom Alloy Catalysts for CO2 Reduction

Figure S1 | Side and top views of structures of the four outliers Sb-doped single-atom alloys with adsorption energies of CO larger than 10 eV before and after relaxation. (a)-(d) Initial unrelaxed structures constructed by researchers. (e)-(h) Relaxed structures of the unrelaxed counterparts on the left panel. Positions of sublayer atoms and Sb atoms in the relaxed structures deviate a lot from their initial counterparts.

Figure S2 | Average MAE of baseline graph neural network (GNN) models on I2I task before and after modified with doping atom node embeddings. The results of original models are drawn in green bars. The yellow bars exhibit the average mean absolute errors (MAEs) of modified GNNs, which are also tested 10 times on I2I task using the same datasets.

Table S1. Results of multiple models on I2I tasks, with and without label normalization

| Model | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | 0.120 | 0.0178 | 0.457 | 0.299 | 0.758 | 6.83 | \ |
| Localized cos + GBR (normed) | 0.119 | 0.0178 | 0.456 | 0.301 | 0.760 | 6.83 | \ |
| Gaussian-cos + GBR | 0.130 | 0.0192 | 0.482 | 0.271 | 0.738 | 6.82 | \ |
| Gaussian-cos + GBR (normed) | 0.130 | 0.0192 | 0.479 | 0.271 | 0.737 | 6.87 | \ |
| Gaussian-tanh + GBR | 0.132 | 0.0201 | 0.485 | 0.268 | 0.735 | 6.71 | \ |
| Gaussian-tanh + GBR (normed) | 0.132 | 0.0198 | 0.483 | 0.267 | 0.735 | 6.71 | \ |
| SchNet | 0.257 | 0.113 | 0.421 | 0.103 | 0.409 | 1845.45 | 541697 |
| SchNet (normed) | 0.201 | 0.114 | 0.400 | 0.158 | 0.552 | 1896.88 | 541697 |
| CGCNN | 0.182 | 0.0887 | 0.401 | 0.147 | 0.557 | 1712.22 | 703361 |
| CGCNN (normed) | 0.220 | 0.124 | 0.432 | 0.152 | 0.548 | 1702.50 | 703361 |
| DimeNet | 0.099 | 0.0157 | 0.358 | 0.329 | 0.792 | 7741.72 | 2100070 |
| DimeNet (normed) | 0.0985 | 0.0146 | 0.366 | 0.347 | 0.799 | 7563.84 | 2100070 |
| Dimenet++ | 0.0966 | 0.0146 | 0.350 | 0.312 | 0.802 | 5335.63 | 1887110 |
| Dimenet++ (normed) | 0.0962 | 0.0149 | 0.353 | 0.323 | 0.800 | 5074.19 | 1887110 |
| DimeNet++ (emb256) | 0.0938 | 0.0148 | 0.356 | 0.337 | 0.821 | 5906.27 | 3545542 |
| DimeNet++ (emb256) (normed) | 0.0939 | 0.0140 | 0.355 | 0.350 | 0.810 | 5945.16 | 3545542 |

Table S2. Results of multiple models on R2R tasks, with and without label normalization

| Model | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | 0.116 | 0.0237 | 0.585 | 0.311 | 0.792 | 26.25 | \ |
| Localized cos + GBR (normed) | 0.118 | 0.0219 | 0.622 | 0.308 | 0.793 | 26.33 | \ |
| Gaussian-cos + GBR | 0.108 | 0.0138 | 0.594 | 0.361 | 0.800 | 25.42 | \ |
| Gaussian-cos + GBR (normed) | 0.110 | 0.0153 | 0.599 | 0.362 | 0.797 | 25.39 | \ |
| Gaussian-tanh + GBR | 0.117 | 0.0122 | 0.643 | 0.358 | 0.801 | 26.03 | \ |
| Gaussian-tanh + GBR (normed) | 0.117 | 0.0122 | 0.644 | 0.360 | 0.803 | 25.97 | \ |
| SchNet | 0.183 | 0.150 | 0.386 | 0.201 | 0.628 | 1904.08 | 541697 |
| SchNet (normed) | 0.263 | 0.162 | 0.434 | 0.147 | 0.480 | 1796.93 | 541697 |
| CGCNN | 0.139 | 0.102 | 0.355 | 0.198 | 0.683 | 1780.57 | 703361 |
| CGCNN (normed) | 0.136 | 0.0591 | 0.357 | 0.198 | 0.643 | 1659.76 | 703361 |
| DimeNet | 0.0556 | 0.0138 | 0.312 | 0.569 | 0.908 | 7678.62 | 2100070 |
| DimeNet (normed) | 0.0548 | 0.0142 | 0.311 | 0.585 | 0.908 | 7643.32 | 2100070 |
| Dimenet++ | 0.0603 | 0.0116 | 0.315 | 0.466 | 0.898 | 5171.22 | 1887110 |
| Dimenet++ (normed) | 0.0591 | 0.0122 | 0.314 | 0.486 | 0.902 | 5325.82 | 1887110 |
| DimeNet++ (emb256) | 0.0551 | 0.0137 | 0.312 | 0.544 | 0.911 | 5893.75 | 3545542 |
| DimeNet++ (emb256) (normed) | 0.0545 | 0.0135 | 0.313 | 0.568 | 0.911 | 5988.79 | 3545542 |

Table S3. Results of multiple models on R2I tasks, with and without label normalization

| Model | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | 0.381 | 0.0153 | 0.729 | 0.145 | 0.468 | 26.22 | \ |
| Localized cos + GBR (normed) | 0.381 | 0.0141 | 0.730 | 0.147 | 0.468 | 26.05 | \ |
| Gaussian-cos + GBR | 0.279 | 0.0312 | 0.608 | 0.138 | 0.445 | 25.93 | \ |
| Gaussian-cos + GBR (normed) | 0.280 | 0.0304 | 0.609 | 0.137 | 0.442 | 25.70 | \ |
| Gaussian-tanh + GBR | 0.280 | 0.0287 | 0.590 | 0.137 | 0.436 | 25.45 | \ |
| Gaussian-tanh + GBR (normed) | 0.280 | 0.0282 | 0.590 | 0.136 | 0.432 | 25.45 | \ |
| SchNet | 0.380 | 0.0460 | 0.567 | 0.0788 | 0.337 | 1818.69 | 541697 |
| SchNet (normed) | 0.379 | 0.0440 | 0.520 | 0.0618 | 0.281 | 1754.04 | 541697 |
| CGCNN | 0.300 | 0.0426 | 0.514 | 0.0874 | 0.395 | 1688.66 | 703361 |
| CGCNN (normed) | 0.280 | 0.0720 | 0.492 | 0.101 | 0.412 | 1744.21 | 703361 |
| DimeNet | 0.389 | 0.0265 | 0.620 | 0.135 | 0.465 | 7618.01 | 2100070 |
| DimeNet (normed) | 0.385 | 0.0273 | 0.615 | 0.135 | 0.467 | 7564.23 | 2100070 |
| Dimenet++ | 0.343 | 0.0203 | 0.546 | 0.120 | 0.442 | 5554.01 | 1887110 |
| Dimenet++ (normed) | 0.345 | 0.0236 | 0.548 | 0.129 | 0.443 | 5031.37 | 1887110 |
| DimeNet++ (emb256) | 0.334 | 0.0269 | 0.540 | 0.130 | 0.457 | 5835.03 | 3545542 |
| DimeNet++ (emb256) (normed) | 0.338 | 0.0323 | 0.545 | 0.130 | 0.456 | 5784.33 | 3545542 |

Table S4. Comparison between DimeNet++ and multi-task mixture density (MT-MD) DimeNet++ with different architectures

| Model | Test MAE AEVR. (eV) | Test MAE STD. (eV) | Test STDAE AEVR. (eV) | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. (s) | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MB4 (DimeNet++ (emb256)) | 0.0938 | 0.0148 | 0.356 | 0.337 | 0.821 | 5906.27 | 3545542 |
| MT-MD DimeNet++ (MB1-SRB1) | 0.0926 | 0.0149 | 0.347 | 0.348 | 0.813 | 4421.92 | 2099199 |
| MT-MD DimeNet++ (MB1-SRB2) | 0.0924 | 0.0150 | 0.349 | 0.348 | 0.817 | 5230.02 | 2727039 |
| MT-MD DimeNet++ (MB1-SRB3) | 0.0931 | 0.0144 | 0.346 | 0.325 | 0.810 | 6125.86 | 3354879 |
| MT-MD DimeNet++ (MB1-SRB4) | 0.0924 | 0.0163 | 0.344 | 0.338 | 0.810 | 6814.34 | 3982719 |
| MT-MD DimeNet++ (MB2-SRB1) | 0.0899 | 0.0154 | 0.349 | 0.369 | 0.822 | 5367.75 | 2889279 |
| MT-MD DimeNet++ (MB2-SRB2) | 0.0884 | 0.0121 | 0.316 | 0.368 | 0.822 | 6278.26 | 3779775 |
| MT-MD DimeNet++ (MB2-SRB3) | 0.0902 | 0.0130 | 0.352 | 0.380 | 0.817 | 7076.83 | 4407615 |
| MT-MD DimeNet++ (MB2-SRB4) | 0.0936 | 0.0156 | 0.363 | 0.353 | 0.820 | 7852.64 | 5035455 |
| MT-MD DimeNet++ (MB3-SRB1) | 0.0897 | 0.0142 | 0.354 | 0.372 | 0.824 | 6260.88 | 3679359 |
| MT-MD DimeNet++ (MB3-SRB2) | 0.0875 | 0.0135 | 0.310 | 0.384 | 0.823 | 7258.57 | 4569855 |
| MT-MD DimeNet++ (MB3-SRB3) | 0.0900 | 0.0141 | 0.332 | 0.374 | 0.824 | 8077.66 | 5460351 |
| MT-MD DimeNet++ (MB3-SRB4) | 0.0888 | 0.0131 | 0.351 | 0.389 | 0.831 | 9038.58 | 6088191 |
| MT-MD DimeNet++ (MB4-SRB1) | 0.0901 | 0.0146 | 0.351 | 0.378 | 0.824 | 7332.32 | 4469439 |
| MT-MD DimeNet++ (MB4-SRB2) | 0.0894 | 0.0134 | 0.350 | 0.388 | 0.826 | 8208.96 | 5359935 |
| MT-MD DimeNet++ (MB4-SRB3) | 0.0870 | 0.0114 | 0.303 | 0.398 | 0.829 | 9231.51 | 6250431 |
| MT-MD DimeNet++ (MB4-SRB4) | 0.0872 | 0.0132 | 0.310 | 0.393 | 0.827 | 10033.02 | 7140927 |

Table S5. Results of surface extrapolation tests using MT-MD DimeNet++

| Model | Target Surface | Test MAE AEVR. (eV) | Test MAE STD. (eV) | Test STDAE AEVR. (eV) | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. (s) | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MT-MD DimeNet++ | 100 | 0.161 | 0.0224 | 0.207 | 0.116 | 0.506 | 3634.34 | 4569855 |
| MT-MD DimeNet++ | 110 | 0.362 | 0.0947 | 1.42 | 0.0879 | 0.399 | 3456.47 | 4569855 |
| MT-MD DimeNet++ | 111 | 0.122 | 0.0197 | 0.111 | 0.122 | 0.522 | 3648.22 | 4569855 |
| MT-MD DimeNet++ | 210 | 0.170 | 0.0232 | 0.210 | 0.0853 | 0.443 | 3576.67 | 4569855 |
| MT-MD DimeNet++ | 411 | 0.175 | 0.0324 | 0.350 | 0.104 | 0.490 | 3522.97 | 4569855 |

Table S6. Results of Cu(751) surface extrapolation tests using multiple algorithms

| Model | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | 0.139 | 0.00141 | 0.157 | 0.0778 | 0.667 | 10.64 | \ |
| Gaussian-cos + GBR | 0.146 | 0.00793 | 0.139 | 0.0944 | 0.478 | 10.52 | \ |
| Gaussian-tanh + GBR | 0.135 | 0.00672 | 0.149 | 0.172 | 0.589 | 10.52 | \ |
| SchNet | 0.126 | 0.00160 | 0.171 | 0.333 | 0.667 | 2761.71 | 541697 |
| CGCNN | 0.126 | 0.000490 | 0.173 | 0.300 | 0.661 | 2730.44 | 703361 |
| DimeNet | 0.0968 | 0.00476 | 0.129 | 0.189 | 0.705 | 18107.20 | 2100070 |
| DimeNet++ | 0.0938 | 0.00463 | 0.117 | 0.167 | 0.711 | 8814.08 | 3545542 |
| MT-MD DimeNet++ | 0.0893 | 0.000518 | 0.117 | 0.183 | 0.728 | 10613.00 | 4569855 |

Table S7. Results of different element extrapolation tests

| Model | Element | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| MT-MD DimeNet++ | Ag | 0.138 | 0.0489 | 0.133 | 0.141 | 0.531 | 10469.84 | 4569855 |
| MT-MD DimeNet++ | Al | 0.122 | 0.0251 | 0.119 | 0.141 | 0.589 | 10506.85 | 4569855 |
| MT-MD DimeNet++ | As | 0.200 | 0.0485 | 0.310 | 0.107 | 0.547 | 10556.14 | 4569855 |
| MT-MD DimeNet++ | Au | 0.213 | 0.0136 | 0.192 | 0.0481 | 0.315 | 10575.96 | 4569855 |
| MT-MD DimeNet++ | B | 0.215 | 0.0238 | 0.178 | 0.0773 | 0.320 | 10574.01 | 4569855 |
| MT-MD DimeNet++ | Bi | 0.179 | 0.0483 | 0.173 | 0.0961 | 0.443 | 10932.39 | 4569855 |
| MT-MD DimeNet++ | Cd | 0.100 | 0.0194 | 0.111 | 0.192 | 0.680 | 10617.72 | 4569855 |
| MT-MD DimeNet++ | Co | 0.275 | 0.0721 | 0.227 | 0.0773 | 0.347 | 10540.12 | 4569855 |
| MT-MD DimeNet++ | Cr | 0.431 | 0.0659 | 0.338 | 0.064 | 0.326 | 10541.96 | 4569855 |
| MT-MD DimeNet++ | Fe | 0.165 | 0.0842 | 0.157 | 0.163 | 0.544 | 10606.80 | 4569855 |
| MT-MD DimeNet++ | Ga | 0.142 | 0.0239 | 0.181 | 0.187 | 0.552 | 10503.52 | 4569855 |
| MT-MD DimeNet++ | Ge | 0.149 | 0.0367 | 0.188 | 0.155 | 0.565 | 10520.09 | 4569855 |
| MT-MD DimeNet++ | Hf | 0.161 | 0.0686 | 0.16 | 0.133 | 0.539 | 10578.01 | 4569855 |
| MT-MD DimeNet++ | In | 0.180 | 0.00768 | 0.200 | 0.0908 | 0.413 | 10581.84 | 4569855 |
| MT-MD DimeNet++ | Ir | 0.392 | 0.0812 | 0.360 | 0.101 | 0.368 | 10537.45 | 4569855 |
| MT-MD DimeNet++ | Mn | 0.404 | 0.0759 | 0.345 | 0.117 | 0.389 | 10414.96 | 4569855 |
| MT-MD DimeNet++ | Mo | 0.487 | 0.244 | 0.373 | 0.0587 | 0.262 | 10833.56 | 4569855 |
| MT-MD DimeNet++ | N | 0.623 | 0.0118 | 0.627 | 0.0293 | 0.189 | 10467.38 | 4569855 |
| MT-MD DimeNet++ | Nb | 0.294 | 0.0938 | 0.317 | 0.0800 | 0.411 | 10467.59 | 4569855 |
| MT-MD DimeNet++ | Ni | 0.125 | 0.0839 | 0.143 | 0.213 | 0.701 | 10496.00 | 4569855 |
| MT-MD DimeNet++ | P | 0.184 | 0.0264 | 0.232 | 0.109 | 0.488 | 10420.82 | 4569855 |
| MT-MD DimeNet++ | Pd | 0.101 | 0.0339 | 0.0953 | 0.173 | 0.635 | 10491.69 | 4569855 |
| MT-MD DimeNet++ | Pt | 0.153 | 0.0312 | 0.144 | 0.197 | 0.507 | 10429.56 | 4569855 |
| MT-MD DimeNet++ | Re | 0.699 | 0.141 | 0.534 | 0.0694 | 0.267 | 10495.81 | 4569855 |
| MT-MD DimeNet++ | Rh | 0.305 | 0.115 | 0.263 | 0.0747 | 0.384 | 10464.45 | 4569855 |
| MT-MD DimeNet++ | Ru | 0.581 | 0.0343 | 0.439 | 0.0587 | 0.253 | 10907.55 | 4569855 |
| MT-MD DimeNet++ | S | 0.150 | 0.00784 | 0.138 | 0.0933 | 0.488 | 10652.04 | 4569855 |
| MT-MD DimeNet++ | Sb | 0.971 | 0.0567 | 3.42 | 0.0799 | 0.440 | 10555.20 | 4569855 |
| MT-MD DimeNet++ | Sc | 0.150 | 0.00784 | 0.138 | 0.0933 | 0.488 | 10652.04 | 4569855 |
| MT-MD DimeNet++ | Se | 0.225 | 0.0212 | 0.289 | 0.109 | 0.421 | 10575.81 | 4569855 |
| MT-MD DimeNet++ | Si | 0.165 | 0.00808 | 0.166 | 0.0881 | 0.456 | 10567.24 | 4569855 |
| MT-MD DimeNet++ | Sn | 0.135 | 0.0148 | 0.128 | 0.139 | 0.525 | 10589.69 | 4569855 |
| MT-MD DimeNet++ | Ta | 0.226 | 0.0901 | 0.249 | 0.128 | 0.475 | 10556.03 | 4569855 |
| MT-MD DimeNet++ | Tc | 0.561 | 0.137 | 0.439 | 0.0854 | 0.323 | 10638.90 | 4569855 |
| MT-MD DimeNet++ | Te | 0.233 | 0.00610 | 0.252 | 0.0827 | 0.411 | 10576.33 | 4569855 |
| MT-MD DimeNet++ | Ti | 0.187 | 0.0408 | 0.198 | 0.123 | 0.504 | 10572.16 | 4569855 |
| MT-MD DimeNet++ | V | 0.265 | 0.147 | 0.241 | 0.128 | 0.432 | 10631.11 | 4569855 |
| MT-MD DimeNet++ | W | 0.553 | 0.113 | 0.453 | 0.0747 | 0.291 | 10671.00 | 4569855 |
| MT-MD DimeNet++ | Y | 0.166 | 0.0182 | 0.132 | 0.0667 | 0.413 | 10658.10 | 4569855 |
| MT-MD DimeNet++ | Zn | 0.134 | 0.0466 | 0.145 | 0.0853 | 0.605 | 10633.28 | 4569855 |
| MT-MD DimeNet++ | Zr | 0.157 | 0.0227 | 0.162 | 0.107 | 0.493 | 10610.50 | 4569855 |

Table S8. Results of traditional and graph algorithms on N element extrapolation tests with different number of N samples added into the training sets.

| Model | Added Samples | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | 0 | 0.626 | 0.00417 | 0.703 | 0.0507 | 0.293 | 10.88 | \ |
| Localized cos + GBR | 2 | 0.948 | 0.274 | 0.645 | 0.0192 | 0.101 | 10.94 | \ |
| Localized cos + GBR | 5 | 0.822 | 0.199 | 0.688 | 0.0286 | 0.137 | 10.92 | \ |
| Localized cos + GBR | 10 | 0.664 | 0.084 | 0.673 | 0.0246 | 0.184 | 10.70 | \ |
| Localized cos + GBR | 20 | 0.623 | 0.0831 | 0.648 | 0.0473 | 0.197 | 10.90 | \ |
| Localized cos + GBR | 30 | 0.562 | 0.0987 | 0.622 | 0.0533 | 0.244 | 10.92 | \ |
| Gaussian-cos + GBR | 0 | 0.641 | 0.00456 | 0.723 | 0.0640 | 0.267 | 10.84 | \ |
| Gaussian-cos + GBR | 2 | 1.04 | 0.319 | 0.725 | 0.0192 | 0.0795 | 10.80 | \ |
| Gaussian-cos + GBR | 5 | 0.921 | 0.272 | 0.744 | 0.0400 | 0.140 | 10.92 | \ |
| Gaussian-cos + GBR | 10 | 0.732 | 0.0909 | 0.684 | 0.0400 | 0.169 | 10.84 | \ |
| Gaussian-cos + GBR | 20 | 0.697 | 0.0854 | 0.680 | 0.0291 | 0.156 | 10.88 | \ |
| Gaussian-cos + GBR | 30 | 0.686 | 0.144 | 0.657 | 0.0355 | 0.120 | 10.94 | \ |
| Gaussian-tanh + GBR | 0 | 0.642 | 0.00434 | 0.714 | 0.0240 | 0.256 | 10.86 | \ |
| Gaussian-tanh + GBR | 2 | 1.06 | 0.339 | 0.749 | 0.0164 | 0.0794 | 11.14 | \ |
| Gaussian-tanh + GBR | 5 | 0.920 | 0.263 | 0.741 | 0.0114 | 0.126 | 11.00 | \ |
| Gaussian-tanh + GBR | 10 | 0.813 | 0.220 | 0.731 | 0.0246 | 0.169 | 10.74 | \ |
| Gaussian-tanh + GBR | 20 | 0.677 | 0.0621 | 0.613 | 0.0218 | 0.105 | 10.50 | \ |
| Gaussian-tanh + GBR | 30 | 0.667 | 0.129 | 0.662 | 0.0356 | 0.178 | 10.96 | \ |
| SchNet | 0 | 0.679 | 0.0482 | 0.685 | 0.0347 | 0.195 | 2758.90 | 541697 |
| SchNet | 2 | 0.691 | 0.0285 | 0.703 | 0.0301 | 0.200 | 2838.72 | 541697 |
| SchNet | 5 | 0.649 | 0.0380 | 0.717 | 0.0514 | 0.223 | 2826.41 | 541697 |
| SchNet | 10 | 0.658 | 0.0462 | 0.711 | 0.0523 | 0.231 | 2817.49 | 541697 |
| SchNet | 20 | 0.664 | 0.0542 | 0.622 | 0.0145 | 0.164 | 2777.01 | 541697 |
| SchNet | 30 | 0.672 | 0.111 | 0.652 | 0.0311 | 0.187 | 2732.14 | 541697 |
| CGCNN | 0 | 0.648 | 0.0133 | 0.743 | 0.0613 | 0.234 | 2915.61 | 703361 |
| CGCNN | 2 | 0.641 | 0.0146 | 0.666 | 0.0247 | 0.200 | 2926.10 | 703361 |
| CGCNN | 5 | 0.628 | 0.0348 | 0.694 | 0.0514 | 0.211 | 2884.18 | 703361 |
| CGCNN | 10 | 0.638 | 0.0419 | 0.713 | 0.0462 | 0.274 | 2893.19 | 703361 |
| CGCNN | 20 | 0.636 | 0.0770 | 0.704 | 0.0545 | 0.247 | 2886.16 | 703361 |
| CGCNN | 30 | 0.649 | 0.108 | 0.678 | 0.0444 | 0.227 | 2855.98 | 703361 |
| DimeNet | 0 | 0.627 | 0.0199 | 0.718 | 0.0613 | 0.245 | 17904.79 | 2100070 |
| DimeNet | 2 | 0.614 | 0.0292 | 0.686 | 0.0658 | 0.247 | 17836.77 | 2100070 |
| DimeNet | 5 | 0.590 | 0.0383 | 0.620 | 0.0600 | 0.209 | 17972.73 | 2100070 |
| DimeNet | 10 | 0.590 | 0.0531 | 0.632 | 0.0770 | 0.234 | 17813.67 | 2100070 |
| DimeNet | 20 | 0.558 | 0.0711 | 0.591 | 0.0727 | 0.225 | 17856.55 | 2100070 |
| DimeNet | 30 | 0.549 | 0.112 | 0.590 | 0.0532 | 0.222 | 17787.02 | 2100070 |
| DimeNet++ | 0 | 0.627 | 0.0269 | 0.675 | 0.0507 | 0.230 | 8770.32 | 3545542 |
| DimeNet++ | 2 | 0.624 | 0.00891 | 0.679 | 0.0411 | 0.205 | 8674.73 | 3545542 |
| DimeNet++ | 5 | 0.605 | 0.0294 | 0.585 | 0.0400 | 0.229 | 8687.96 | 3545542 |
| DimeNet++ | 10 | 0.619 | 0.0321 | 0.610 | 0.0462 | 0.166 | 8745.23 | 3545542 |
| DimeNet++ | 20 | 0.576 | 0.0977 | 0.586 | 0.0400 | 0.189 | 8640.62 | 3545542 |
| DimeNet++ | 30 | 0.571 | 0.0745 | 0.621 | 0.0622 | 0.240 | 8678.76 | 3545542 |
| MT-MD DimeNet++ | 0 | 0.623 | 0.0118 | 0.627 | 0.0293 | 0.189 | 10467.38 | 4569855 |
| MT-MD DimeNet++ | 2 | 0.628 | 0.0160 | 0.621 | 0.0411 | 0.186 | 10503.65 | 4569855 |
| MT-MD DimeNet++ | 5 | 0.620 | 0.0298 | 0.610 | 0.0400 | 0.226 | 10613.80 | 4569855 |
| MT-MD DimeNet++ | 10 | 0.619 | 0.0349 | 0.640 | 0.0462 | 0.185 | 10675.89 | 4569855 |
| MT-MD DimeNet++ | 20 | 0.565 | 0.104 | 0.587 | 0.0291 | 0.200 | 10906.97 | 4569855 |
| MT-MD DimeNet++ | 30 | 0.544 | 0.0909 | 0.610 | 0.0445 | 0.227 | 10604.65 | 4569855 |

Table S9. Results of traditional and graph algorithms on Re element extrapolation tests with different number of Re samples added into the training sets.

| Model | Added Samples | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | 0 | 0.266 | 0.0106 | 0.259 | 0.149 | 0.347 | 10.44 | \ |
| Localized cos + GBR | 2 | 0.188 | 0.0404 | 0.256 | 0.129 | 0.446 | 10.58 | \ |
| Localized cos + GBR | 5 | 0.159 | 0.0336 | 0.282 | 0.157 | 0.611 | 10.94 | \ |
| Localized cos + GBR | 10 | 0.125 | 0.0147 | 0.231 | 0.203 | 0.677 | 10.84 | \ |
| Localized cos + GBR | 20 | 0.106 | 0.0236 | 0.195 | 0.262 | 0.756 | 10.88 | \ |
| Localized cos + GBR | 30 | 0.0827 | 0.0112 | 0.142 | 0.266 | 0.822 | 10.78 | \ |
| Gaussian-cos + GBR | 0 | 0.275 | 0.00915 | 0.229 | 0.109 | 0.336 | 10.66 | \ |
| Gaussian-cos + GBR | 2 | 0.196 | 0.0384 | 0.233 | 0.132 | 0.463 | 10.74 | \ |
| Gaussian-cos + GBR | 5 | 0.168 | 0.0292 | 0.250 | 0.157 | 0.589 | 10.82 | \ |
| Gaussian-cos + GBR | 10 | 0.151 | 0.00649 | 0.230 | 0.160 | 0.622 | 10.78 | \ |
| Gaussian-cos + GBR | 20 | 0.129 | 0.0120 | 0.243 | 0.247 | 0.724 | 10.60 | \ |
| Gaussian-cos + GBR | 30 | 0.119 | 0.0188 | 0.218 | 0.275 | 0.760 | 10.52 | \ |
| Gaussian-tanh + GBR | 0 | 0.279 | 0.0101 | 0.230 | 0.112 | 0.325 | 10.72 | \ |
| Gaussian-tanh + GBR | 2 | 0.196 | 0.0426 | 0.236 | 0.137 | 0.463 | 10.78 | \ |
| Gaussian-tanh + GBR | 5 | 0.166 | 0.0384 | 0.250 | 0.154 | 0.566 | 10.78 | \ |
| Gaussian-tanh + GBR | 10 | 0.146 | 0.0121 | 0.230 | 0.169 | 0.662 | 10.76 | \ |
| Gaussian-tanh + GBR | 20 | 0.134 | 0.0135 | 0.249 | 0.218 | 0.713 | 10.84 | \ |
| Gaussian-tanh + GBR | 30 | 0.118 | 0.0192 | 0.190 | 0.209 | 0.724 | 10.92 | \ |
| SchNet | 0 | 0.829 | 0.117 | 0.513 | 0.0187 | 0.0801 | 2768.17 | 541697 |
| SchNet | 2 | 0.820 | 0.129 | 0.470 | 0.0219 | 0.0603 | 3191.80 | 541697 |
| SchNet | 5 | 0.485 | 0.243 | 0.336 | 0.0458 | 0.189 | 3002.82 | 541697 |
| SchNet | 10 | 0.452 | 0.239 | 0.297 | 0.0461 | 0.166 | 2842.11 | 541697 |
| SchNet | 20 | 0.596 | 0.378 | 0.392 | 0.0727 | 0.291 | 2773.65 | 541697 |
| SchNet | 30 | 0.266 | 0.131 | 0.268 | 0.102 | 0.409 | 2742.31 | 541697 |
| CGCNN | 0 | 0.235 | 0.0199 | 0.233 | 0.0667 | 0.299 | 2924.53 | 703361 |
| CGCNN | 2 | 0.291 | 0.0870 | 0.311 | 0.0686 | 0.266 | 3066.53 | 703361 |
| CGCNN | 5 | 0.341 | 0.229 | 0.314 | 0.0857 | 0.309 | 3012.20 | 703361 |
| CGCNN | 10 | 0.229 | 0.0429 | 0.196 | 0.0739 | 0.335 | 2971.26 | 703361 |
| CGCNN | 20 | 0.380 | 0.331 | 0.279 | 0.0799 | 0.273 | 2891.55 | 703361 |
| CGCNN | 30 | 0.323 | 0.190 | 0.241 | 0.0932 | 0.249 | 2864.91 | 703361 |
| DimeNet | 0 | 0.709 | 0.204 | 0.564 | 0.0694 | 0.253 | 17828.84 | 2100070 |
| DimeNet | 2 | 0.383 | 0.202 | 0.417 | 0.101 | 0.367 | 17773.99 | 2100070 |
| DimeNet | 5 | 0.241 | 0.0973 | 0.318 | 0.123 | 0.489 | 17976.12 | 2100070 |
| DimeNet | 10 | 0.15 | 0.0508 | 0.212 | 0.163 | 0.609 | 17618.26 | 2100070 |
| DimeNet | 20 | 0.108 | 0.0363 | 0.180 | 0.204 | 0.702 | 17690.00 | 2100070 |
| DimeNet | 30 | 0.106 | 0.0274 | 0.220 | 0.236 | 0.755 | 17783.58 | 2100070 |
| DimeNet++ | 0 | 0.829 | 0.154 | 0.653 | 0.056 | 0.237 | 8883.92 | 3545542 |
| DimeNet++ | 2 | 0.235 | 0.112 | 0.274 | 0.175 | 0.458 | 8821.24 | 3545542 |
| DimeNet++ | 5 | 0.145 | 0.0373 | 0.270 | 0.197 | 0.603 | 8802.98 | 3545542 |
| DimeNet++ | 10 | 0.101 | 0.0186 | 0.211 | 0.249 | 0.748 | 8760.63 | 3545542 |
| DimeNet++ | 20 | 0.0977 | 0.0283 | 0.222 | 0.291 | 0.778 | 8791.58 | 3545542 |
| DimeNet++ | 30 | 0.0895 | 0.0103 | 0.190 | 0.267 | 0.787 | 8735.51 | 3545542 |
| MT-MD DimeNet++ | 0 | 0.699 | 0.141 | 0.534 | 0.0694 | 0.267 | 10495.81 | 4569855 |
| MT-MD DimeNet++ | 2 | 0.289 | 0.151 | 0.289 | 0.181 | 0.438 | 10571.97 | 4569855 |
| MT-MD DimeNet++ | 5 | 0.150 | 0.0459 | 0.272 | 0.211 | 0.637 | 10609.75 | 4569855 |
| MT-MD DimeNet++ | 10 | 0.0881 | 0.0227 | 0.188 | 0.265 | 0.785 | 10466.42 | 4569855 |
| MT-MD DimeNet++ | 20 | 0.0841 | 0.0249 | 0.192 | 0.284 | 0.811 | 10594.05 | 4569855 |
| MT-MD DimeNet++ | 30 | 0.0739 | 0.0123 | 0.169 | 0.360 | 0.871 | 10423.43 | 4569855 |

Table S10. Results of traditional and graph algorithms on Ru element extrapolation tests with different number of Ru samples added into the training sets.

| Model | Added Samples | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | 0 | 0.287 | 0.00136 | 0.267 | 0.203 | 0.416 | 10.52 | \ |
| Localized cos + GBR | 2 | 0.188 | 0.0315 | 0.223 | 0.118 | 0.457 | 10.72 | \ |
| Localized cos + GBR | 5 | 0.137 | 0.0152 | 0.185 | 0.174 | 0.591 | 10.78 | \ |
| Localized cos + GBR | 10 | 0.121 | 0.0141 | 0.178 | 0.225 | 0.680 | 11.00 | \ |
| Localized cos + GBR | 20 | 0.0892 | 0.0127 | 0.127 | 0.255 | 0.767 | 10.82 | \ |
| Localized cos + GBR | 30 | 0.0796 | 0.0235 | 0.127 | 0.351 | 0.818 | 10.98 | \ |
| Gaussian-cos + GBR | 0 | 0.316 | 0.00185 | 0.304 | 0.181 | 0.384 | 10.46 | \ |
| Gaussian-cos + GBR | 2 | 0.214 | 0.0413 | 0.242 | 0.052 | 0.400 | 10.64 | \ |
| Gaussian-cos + GBR | 5 | 0.171 | 0.0222 | 0.232 | 0.143 | 0.509 | 10.78 | \ |
| Gaussian-cos + GBR | 10 | 0.153 | 0.0187 | 0.237 | 0.182 | 0.606 | 10.74 | \ |
| Gaussian-cos + GBR | 20 | 0.122 | 0.0152 | 0.204 | 0.269 | 0.716 | 10.96 | \ |
| Gaussian-cos + GBR | 30 | 0.109 | 0.0172 | 0.211 | 0.293 | 0.787 | 10.92 | \ |
| Gaussian-tanh + GBR | 0 | 0.303 | 0.00136 | 0.293 | 0.210 | 0.387 | 10.72 | \ |
| Gaussian-tanh + GBR | 2 | 0.216 | 0.0379 | 0.245 | 0.0985 | 0.403 | 10.64 | \ |
| Gaussian-tanh + GBR | 5 | 0.182 | 0.0215 | 0.238 | 0.134 | 0.466 | 10.76 | \ |
| Gaussian-tanh + GBR | 10 | 0.155 | 0.0104 | 0.237 | 0.160 | 0.588 | 10.94 | \ |
| Gaussian-tanh + GBR | 20 | 0.119 | 0.00575 | 0.201 | 0.258 | 0.702 | 10.96 | \ |
| Gaussian-tanh + GBR | 30 | 0.0999 | 0.0142 | 0.185 | 0.333 | 0.787 | 10.94 | \ |
| SchNet | 0 | 0.658 | 0.175 | 0.471 | 0.0267 | 0.117 | 2776.17 | 541697 |
| SchNet | 2 | 0.593 | 0.230 | 0.395 | 0.0247 | 0.132 | 2808.30 | 541697 |
| SchNet | 5 | 0.475 | 0.253 | 0.332 | 0.0343 | 0.214 | 2852.53 | 541697 |
| SchNet | 10 | 0.122 | 0.0155 | 0.164 | 0.166 | 0.652 | 2981.03 | 541697 |
| SchNet | 20 | 0.0867 | 0.0231 | 0.132 | 0.265 | 0.789 | 2837.19 | 541697 |
| SchNet | 30 | 0.177 | 0.189 | 0.167 | 0.235 | 0.658 | 2722.27 | 541697 |
| CGCNN | 0 | 0.339 | 0.0761 | 0.312 | 0.0666 | 0.275 | 2922.54 | 703361 |
| CGCNN | 2 | 0.323 | 0.0642 | 0.285 | 0.0604 | 0.282 | 2959.08 | 703361 |
| CGCNN | 5 | 0.209 | 0.0802 | 0.225 | 0.0944 | 0.417 | 2957.85 | 703361 |
| CGCNN | 10 | 0.132 | 0.0439 | 0.142 | 0.135 | 0.575 | 2974.80 | 703361 |
| CGCNN | 20 | 0.118 | 0.0232 | 0.149 | 0.193 | 0.625 | 2945.14 | 703361 |
| CGCNN | 30 | 0.203 | 0.119 | 0.179 | 0.0888 | 0.471 | 2917.93 | 703361 |
| DimeNet | 0 | 0.513 | 0.197 | 0.430 | 0.0667 | 0.315 | 17650.92 | 2100070 |
| DimeNet | 2 | 0.148 | 0.0299 | 0.189 | 0.183 | 0.553 | 17675.43 | 2100070 |
| DimeNet | 5 | 0.119 | 0.0263 | 0.199 | 0.229 | 0.657 | 17746.93 | 2100070 |
| DimeNet | 10 | 0.0786 | 0.0359 | 0.103 | 0.283 | 0.751 | 17654.60 | 2100070 |
| DimeNet | 20 | 0.0526 | 0.0178 | 0.0720 | 0.382 | 0.876 | 17708.90 | 2100070 |
| DimeNet | 30 | 0.0448 | 0.00988 | 0.059 | 0.356 | 0.920 | 17821.90 | 2100070 |
| DimeNet++ | 0 | 0.601 | 0.144 | 0.485 | 0.0906 | 0.299 | 8767.78 | 3545542 |
| DimeNet++ | 2 | 0.122 | 0.0587 | 0.156 | 0.216 | 0.652 | 8709.20 | 3545542 |
| DimeNet++ | 5 | 0.0837 | 0.0164 | 0.150 | 0.320 | 0.746 | 8706.15 | 3545542 |
| DimeNet++ | 10 | 0.0533 | 0.0241 | 0.0811 | 0.391 | 0.874 | 9789.56 | 3545542 |
| DimeNet++ | 20 | 0.0444 | 0.00772 | 0.0561 | 0.414 | 0.898 | 8755.73 | 3545542 |
| DimeNet++ | 30 | 0.0356 | 0.00321 | 0.0436 | 0.458 | 0.942 | 8697.02 | 3545542 |
| MT-MD DimeNet++ | 0 | 0.581 | 0.0343 | 0.439 | 0.0587 | 0.253 | 10907.55 | 4569855 |
| MT-MD DimeNet++ | 2 | 0.153 | 0.0561 | 0.172 | 0.236 | 0.559 | 10576.95 | 4569855 |
| MT-MD DimeNet++ | 5 | 0.0806 | 0.0251 | 0.113 | 0.269 | 0.763 | 10608.19 | 4569855 |
| MT-MD DimeNet++ | 10 | 0.0657 | 0.0213 | 0.134 | 0.403 | 0.868 | 10612.74 | 4569855 |
| MT-MD DimeNet++ | 20 | 0.0470 | 0.0189 | 0.0844 | 0.440 | 0.920 | 10824.70 | 4569855 |
| MT-MD DimeNet++ | 30 | 0.0310 | 0.00493 | 0.0413 | 0.511 | 0.960 | 10525.37 | 4569855 |

Table S11. Comparison of gradient boosting regression (GBR) models trained with dataset using different sites in the configurations as centers to build symmetry functions (SFs) as structure features

| Model | Features | Test MAE AEVR. | Test MAE STD. | Test STDAE AEVR. | Test within 0.02 AVER. | Test within 0.1 AVER. | Run Time AVER. | Number of Parameters |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Localized cos + GBR | All | 0.120 | 0.0178 | 0.457 | 0.299 | 0.758 | 6.83 | \ |
| Localized cos + GBR | Only centered at doping atoms | 0.117 | 0.0135 | 0.442 | 0.291 | 0.760 | 4.28 | \ |
| Localized cos + GBR | Only centered at C atoms | 0.348 | 0.0292 | 0.768 | 0.103 | 0.394 | 3.36 | \ |
| Gaussian-cos + GBR | All | 0.130 | 0.0192 | 0.482 | 0.271 | 0.738 | 6.82 | \ |
| Gaussian-cos + GBR | Only centered at doping atoms | 0.128 | 0.0156 | 0.461 | 0.278 | 0.739 | 4.39 | \ |
| Gaussian-cos + GBR | Only centered at C atoms | 0.346 | 0.0292 | 0.753 | 0.107 | 0.399 | 3.10 | \ |
| Gaussian-tanh + GBR | All | 0.132 | 0.0201 | 0.485 | 0.268 | 0.734 | 6.71 | \ |
| Gaussian-tanh + GBR | Only centered at doping atoms | 0.132 | 0.0184 | 0.474 | 0.281 | 0.737 | 4.44 | \ |
| Gaussian-tanh + GBR | Only centered at C atoms | 0.345 | 0.0292 | 0.751 | 0.103 | 0.397 | 3.17 | \ |

Details of constructing symmetry functions

Symmetry functions (SFs) 1, 2 are proposed as a method of extracting structure information from molecule or material systems. After assigning an atom as the center, the distance between the center atom and all the other atoms in the system within a cut-off radius is calculated, and a set of Gaussians with different means and standard deviations are applied as filters to represent the structure environment around the center atom at different locations. SFs have one-body, two-body and three-body terms, and the values of SFs of the first two terms are only related to the relative distance between atoms in the systems, while the three-body one incorporates relative distance and bond angle at the same time. Therefore, SFs are invariant when the system is translated, rotated, or when the positions of two atoms around the center are permutated.

The formulas of one-body, two-body and three-body SFs are

Gi1=j=1Natom fcRij,#1

Gi2=j=1Natom e-ηRij-Rs2⋅fcRij ,#2

Gi3=21-ζj≠ik≠i,j1+λ⋅cosθijkζ⋅e-ηRij-Rs2+Rik-Rs2+Rjk-Rs2⋅fcRij⋅fcRik⋅fcRjk,                                          (3)

respectively, in which i represents the center atom, Rc is the cut-off radius, j represents an atom within Rc, and Natom  denotes the number of surrounding atoms. Rij and θijk are the distance between atom i and j and the angle between bond ij and ik. η, Rs, λ, ζ are parameters to determine the shapes of the Gaussians, which are set by researchers. fcRij is the cut-off function with the form

fcRij=0.5⋅cosπRijRc+1    forRij≤Rc0.0                                       forRij>Rc  , #4

or

fcRij=tanh31-RijRc     forRij≤Rc0.0                            forRij>Rc  ,#5

which decreases monotonically and smoothly to zero as Rij increases, reflecting the physical pattern of interactions between atoms.

Another simplified version of SFs is proposed 3, 4 as

Gi2=j=1Natom fmRij,#6

and

Gi3=j≠ik≠i,jfmRij⋅fmRik⋅fmRjk .#7

fmRij is the localized piecewise cosine filter, instead of Gaussians, with the form

fmRij=0.5⋅cosRij-dmrπ+1        for|Rij-dm|≤r0.0                                                                      otherwise  ,#8

in which the system is divided into N layers with a thickness of r=RcN-1. The atoms in each layer within the range of (dm-r, dm+r) are counted independently with d1=0, dm=dm-1+r, and dN=Rc (dm+r should be smaller than dN).

In this work, the original SFs with cosine (formula (4)) and hyperbolic tangent (formula (5)) cut-off functions are denoted as ‘Gaussian-cos’ and ‘Gaussian-tanh’, respectively, and the simplified ones are denoted as ‘Localized cos’. SFs are constructed using the doping site and the carbon atom as centers with a cut-off radius of 12 Å for each configuration, and values of parameters for each type of SFs are summarized as

| Type of SFs | Values of parameters |
| --- | --- |
| Localized cos | N2=12 N3=4 |
| Gaussian-cos/Gaussian-tanh | η=0.001, 0.01, 0.05, 0.1, 0.5 ζ=0.1, 0.5 Rs=[1.0, 2.25, 3.5, 4.75, 6.0] λ=1.0 |

in which N2 and N3 represent the number of layers for the two-body terms and three-body terms, respectively. In this way, the number (length) of SF features for each center is 76 for all the three types of SFs, and the number of structure features is 152 when both of the doping site and the carbon atom are applied as centers and computed independently.

All configurations are expanded into a 3*3 superlattice before constructing SFs, so that the periodic boundary condition can be satisfied, while the adsorbed molecules are removed and doping atoms are substituted with Cu atoms in the expanded parts to simulate the real environment around the doping site for a single-atom alloy (SAA).

Training details of gradient boosting regression and graph neural networks

In the gradient boosting regression (GBR) process, each SAA catalyst is represented using the element features and structure features, in which structure features are SFs with the doping atom and carbon atom as centers, while element features and hyperparameters for GBR models (implemented by Scikit-learn 5) are illustrated as

| Element features (of the doping species) | period group atomic number relative atom mass atomic radius electronic affinity ionic potential electronegativity number of electrons in the p or d orbital number of valence electrons d-band center |
| --- | --- |
| Hyperparameters of GBR models | min_samples_leaf: 1 n_estimators: 200 max_leaf_nodes: 80 max_depth: 8 learning_rate: 0.1 |

The graph neural networks (GNNs) in this work are implemented by Open Catalyst Project 6, and the hyperparameters and training settings for each models are summarized as

| GNN Model | Hyperparameters |
| --- | --- |
| SchNet | hidden_channels: 256 num_filters: 128 num_interactions: 3 num_gaussians: 100 cutoff: 6.0 batch_size: 16 eval_batch_size: 16 num_workers: 16 lr_initial: 0.005 lr_gamma: 0.1 lr_milestones: - 1562 - 2343 - 3125 warmup_steps: 468 warmup_factor: 0.2 max_epochs: 400 |

| GNN Model | Hyperparameters |
| --- | --- |
| CGCNN | atom_embedding_size: 128 fc_feat_size: 256 num_fc_layers: 4 num_graph_conv_layers: 5 num_gaussians: 100 cutoff: 6.0 batch_size: 64 eval_batch_size: 64 num_workers: 16 lr_initial: 0.01 lr_gamma: 0.1 lr_milestones: - 781 - 1406 - 2031 warmup_steps: 468 warmup_factor: 0.2 max_epochs: 400 |

| GNN Model | Hyperparameters |
| --- | --- |
| DimeNet | hidden_channels: 128 num_blocks: 6 num_bilinear: 8 num_spherical: 7 num_radial: 6 cutoff: 6.0 envelope_exponent: 5 num_before_skip: 1 num_after_skip: 2 num_output_layers: 3 batch_size: 5 eval_batch_size: 5 num_workers: 2 lr_initial: 0.0001 lr_gamma: 0.1 lr_milestones: - 20000 - 40000 - 60000 warmup_steps: 10000 warmup_factor: 0.2 max_epochs: 160 |

| GNN Model | Hyperparameters |
| --- | --- |
| DimeNet++ | hidden_channels: 128 out_emb_channels: 256 num_blocks: 4 cutoff: 6.0 num_radial: 6 num_spherical: 7 num_before_skip: 1 num_after_skip: 2 num_output_layers: 3 batch_size: 5 eval_batch_size: 5 num_workers: 2 lr_initial: 0.0001 lr_gamma: 0.1 lr_milestones: - 20000 - 40000 - 60000 warmup_steps: 10000 warmup_factor: 0.2 max_epochs: 160 |

| GNN Model | Hyperparameters |
| --- | --- |
| DimeNet++ (emb256), MT DimeNet++ | hidden_channels: 256 out_emb_channels: 192 num_blocks: 4 cutoff: 6.0 num_radial: 6 num_spherical: 7 num_before_skip: 1 num_after_skip: 2 num_output_layers: 3 batch_size: 5 eval_batch_size: 5 num_workers: 2 lr_initial: 0.0001 lr_gamma: 0.1 lr_milestones: - 20000 - 40000 - 60000 warmup_steps: 10000 warmup_factor: 0.2 max_epochs: 160 |

References

1.	Behler, J. & Parrinello, M. Generalized neural-network representation of high-dimensional potential-energy surfaces. Phys. Rev. Lett. 98, 146401 (2007).

2.	Behler, J. Constructing high-dimensional neural network potentials: A tutorial review. Int. J. Quantum Chem. 115, 1032-1050 (2015).

3.	Chen, Y., Huang, Y., Cheng, T. & Goddard, W. A., III. Identifying Active Sites for CO2 Reduction on Dealloyed Gold Surfaces by Combining Machine Learning with Multiscale Simulations. J. Am. Chem. Soc. 141, 11651-11657 (2019).

4.	Huang, Y., Chen, Y., Cheng, T., Wang, L.-W. & Goddard, W. A., III. Identification of the Selective Sites for Electrochemical Reduction of CO to C2+ Products on Copper Nanoparticles by Combining Reactive Force Fields, Density Functional Theory, and Machine Learning. ACS Energy Lett. 3, 2983-2988 (2018).

5.	Pedregosa, F., et al. Scikit-learn: Machine Learning in Python. J. Mach. Learn. Res. 12, 2825-2830 (2011).

6.	Chanussot, L., et al. Open Catalyst 2020 (OC20) Dataset and Community Challenges. ACS Catal. 11, 6059-6072 (2021).