Scheme 1 (a) Extraction of cellulose from agriculture waste sugarcane bagasse and (b) synthetic scheme for the preparation of cellulose tethered N-heterocyclic carbene-palladium(II) complex as heterogeneous catalyst (Cellu@NHC-Pd).

Table 1 Optimization of reaction conditions for Suzuki–Miyaura cross-coupling reaction of 4-iodoanisole with phenylboronic acid in the presence of the Cellu@NHC-Pd heterogeneous catalysta

| Entry | Base | Solvent | Temp. (° C) | Pd (mol%) | Time (min) | Yield (%)b |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | NaOH | EtOH: H2O | RT | 2.22 | 30 | 90 |
| 2 | KOH | EtOH: H2O | RT | 2.22 | 60 | 95 |
| 3 | Cs2CO3 | EtOH: H2O | RT | 2.22 | 30 | 90 |
| 4 | Na2CO3 | EtOH: H2O | RT | 2.22 | 60 | 90 |
| 5 | KF | EtOH: H2O | RT | 2.22 | 45 | 30 |
| 6 | Na3PO4.12H2O | EtOH: H2O | RT | 2.22 | 30 | 70 |
| 7 | K2CO3 | H2O | RT | 2.22 | 90 | 60 |
| 8 | K2CO3 | EtOH | RT | 2.22 | 30 | Trace |
| 9 | K2CO3 | DMF | RT | 2.22 | 60 | Trace |
| 10 | K2CO3 | Acetonitrile | RT | 2.22 | 60 | Trace |
| 11 | K2CO3 | Toluene | RT | 2.22 | 60 | Trace |
| 12 | K2CO3 | 1,4-Dioxane | RT | 2.22 | 60 | Trace |
| 13 | K2CO3 | THF | RT | 2.22 | 60 | Trace |
| 14 | K2CO3 | EtOH: H2O | 50 | 2.22 | 30 | 95 |
| 15 | K2CO3 | EtOH: H2O | 40 | 2.22 | 30 | 95 |
| 16 | K2CO3 | EtOH: H2O | RT | 2.22 | 15 | 90 |
| 17 | K2CO3 | EtOH: H2O | RT | 2.22 | 30 | 95 |
| 18 | K2CO3 | EtOH: H2O | RT | 2.22 | 45 | 95 |
| 19 | K2CO3 | EtOH: H2O | RT | 1.67 | 30 | 90 |
| 20 | K2CO3 | EtOH: H2O | RT | 2.00 | 30 | 93 |
| 21 | K2CO3 | EtOH: H2O | RT | 2.78 | 30 | 90 |

aReaction conditions: 4-iodoanisole (1.0 equiv.), phenylboronic acid (1.1 equiv.), Cellu@NHC-Pd (1.67-2.78 mol% Pd with respect to aryl halide), base (2.5 equiv.) and solvent (6 mL) in air.

bIsolated yield after separation by column chromatography.

Table 2 Suzuki–Miyaura cross-coupling reactions of different aryl halides with aryl boronic acids in the presence of Cellu@NHC-Pd heterogeneous catalysta

| Entry | Aryl halide | Product | Time (min) | Yieldb (%) |
| --- | --- | --- | --- | --- |
| 1 |  |  | 45 | 80 |
| 2 |  |  | 30 | 95 |
| 3 |  |  | 60 | 80 |
| 4 |  |  | 60 | 90 |
| 5 |  |  | 2.5c | 40 |
| 6 |  |  | 30 | 95 |
| 7 |  |  | 30 | 95 |
| 8 |  |  | 60 | 85 |
| 9 |  |  | 3c | 85 |
| 10 |  |  | 45 | 95 |
| 11 |  |  | 45 | 90 |
| 12 |  |  | 45 | 90 |
| 13 |  |  | 45 | 90 |
| 14 |  |  | 45 | 90 |
| 15 |  |  | 60 | 95 |
| 16 |  |  | 2.5c | 80 |
| 17 |  |  | 75 | 80 |
| 18 |  |  | 4c | 60 |
| 19 |  |  | 2.5c | 80 |
| 20 |  |  | 4c | 60 |
| 21 |  |  | 90 | 95 |
| 22 |  |  | 45 | 99 |
| 23 |  |  | 60 | 95 |

aReaction condition: Aryl halide (1 equiv), arylboronic acid (1.1 equiv), Cellu@NHC-Pd heterogeneous catalyst (2.22 mol% Pd with respect to aryl halide), K2CO3 (2.5 equiv) and EtOH:H2O (1:1, 6 mL) in air at room temperature.

bIsolated yield after separation by column chromatography.

cTime in hours.

Table 3 Optimization of reaction conditions for Mizoroki-Heck cross-coupling reaction of 4-iodoanisole with tert-butylacrylate in the presence of Cellu@NHC-Pd heterogeneous catalysta

| Entry | Base | Solvent | Temp. (° C) | Pd (mol%) | Time (min) | Yield (%)b |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Na2CO3 | EtOH:H2O | 60 | 2.22 | 3 | 60 |
| 2 | KOH | EtOH:H2O | 60 | 2.22 | 4 | 40 |
| 3 | NaOH | EtOH:H2O | 60 | 2.22 | 3 | 35 |
| 4 | CS2CO3 | EtOH:H2O | 60 | 2.22 | 3 | 40 |
| 5 | KF | EtOH:H2O | 60 | 2.22 | 2 | Trace |
| 6 | K2CO3 | H2O | 60 | 2.22 | 2 | Trace |
| 7 | K2CO3 | EtOH | 60 | 2.22 | 2 | 10 |
| 8 | K2CO3 | Acetonitrile | 60 | 2.22 | 3 | Trace |
| 9 | K2CO3 | DMF | 60 | 2.22 | 3 | 10 |
| 10 | K2CO3 | THF | 60 | 2.22 | 3 | Trace |
| 11 | K2CO3 | Toluene | 60 | 2.22 | 3 | Trace |
| 12 | K2CO3 | 1,4-Dioxane | 60 | 2.22 | 4 | 40 |
| 13 | K2CO3 | EtOH:H2O | RT | 2.22 | 2 | Trace |
| 14 | K2CO3 | EtOH:H2O | 50 | 2.22 | 3 | 60 |
| 15 | K2CO3 | EtOH:H2O | 70 | 2.22 | 6 | 80 |
| 16 | K2CO3 | EtOH:H2O | 60 | 2.22 | 1 | 20 |
| 17 | K2CO3 | EtOH:H2O | 60 | 2.22 | 2 | 60 |
| 18 | K2CO3 | EtOH:H2O | 60 | 2.22 | 3 | 80 |
| 19 | K2CO3 | EtOH:H2O | 60 | 2.22 | 4 | 80 |
| 20 | K2CO3 | EtOH:H2O | 60 | 1.67 | 4 | 50 |
| 21 | K2CO3 | EtOH:H2O | 60 | 2.00 | 4 | 47 |
| 22 | K2CO3 | EtOH:H2O | 60 | 2.45 | 4 | 70 |
| 23 | K2CO3 | EtOH:H2O | 60 | 2.78 | 4 | 50 |

aReaction conditions: 4-iodoanisole (1.0 equiv.), tert-butylacrylate (1.1 equiv.), Cellu@NHC-Pd (1.67-2.78 mol% Pd with respect to aryl halide), base (2.5 equiv.) and solvent (6 mL) in air.

bIsolated yield after separation by column chromatography.

Table 4 Mizoroki-Heck cross-coupling reactions of different aryl halides with tert-butylacrylate in the presence of Cellu@NHC-Pd heterogeneous catalysta

| Entry | Aryl halide | Product | Time (h) | Yield (%) |
| --- | --- | --- | --- | --- |
| 1 |  |  | 3 | 80 |
| 2 |  |  | 4 | 70 |
| 3 |  |  | 3 | 95 |
| 4 |  |  | 2 | Trace |
| 5 |  |  | 4 | 65 |
| 6 |  |  | 8 | Trace |
| 7 |  |  | 4 | 65 |
| 8 |  |  | 3 | 85 |
| 9 |  |  | 2 | 95 |
| 10 |  |  | 8 | Trace |

aReaction condition: aryl iodide (1 equiv), tert-butylacrylate (1.2 equiv), Cellu@NHC-Pd heterogeneous catalyst (2.22 mol% Pd with respect to aryl iodide), K2CO3 (2.5 equiv) and EtOH:H2O (1:1, 5 mL) in air at 60 °C.

bIsolated yield after separation by column chromatography.