Appendix

As mentioned, combined parameter (CP) presented as CP = HInPDm. To investigate presented methodology with experiment a relation, which also define correlation is defined as Eq (A).

|  | (A) |
| --- | --- |

where P1 and P2 are constants, which interpret the slope and intercept of the fitted line. The introduced constants are provided in Table 8.

Table 8. The constants of presented CP for weld width, penetration-to-width ratio, distortion and fracture load

| CP parameters Weld properties | n | m | P1 | P2 |
| --- | --- | --- | --- | --- |
| D | 4.2 | -1 | 0.003 | -16.3 |
| W | 4.7 | 6 | -3.44×10-25 | 1972 |
| PW | 1 | 2 | 3.42×10-7 | 43.86 |
| F | 0.1 | 8 | 3.446×10-26 | 5.112 |

Acknowledgment

Firstly, this study was provided under fund support of Taha Ghaleb Toos (TGT) Co. through grant number of LEW: 2020-1-A. A special thanks to TGT Co. because of both spiritual and financial supports during all parts of preparation of presented paper. Secondly, the authors would like to express appreciation to Mr Ali Ehteshami who was good adviser to presented paper.