Supplementary Information

One-Pot Synthesis of Hyperbranched Polymers via Visible Light Regulated Switchable Catalysis

Shuaishuai Zhu†, Maoji Zhao†, Hongru Zhou, Yingfeng Wen, Yong Wang*, Yonggui Liao, Xingping Zhou, Xiaolin Xie

Key Laboratory for Material Chemistry of Energy Conversion and Storage, Ministry of Education, School of Chemistry and Chemical Engineering, Huazhong University of Science and Technology, Wuhan 430074, China

*Corresponding to: tcwy@mail.hust.edu.cn (Y. W.)

†These authors contributed equally to this work.

Table of Contents

Materials

Characterization methods

Experimental procedures

CO-insertion study

Characterization data

Supplementary References

Materials

All manipulations involving air- and/or water-sensitive compounds were carried out using standard Schlenk techniques under dry argon. propylene oxide (PO), tetrahydrofuran (THF), and glycidyl acrylate (GA) were distilled from calcium hydride (CaH2) under argon atmosphere. Methylene chloride (CH2Cl2) and toluene were distilled under argon atmosphere from sodium/benzophenone. Carbon monoxide (purity of 99.99%) were provided from Wuhan Huaerwen Gas Ltd. and used as received. Diglycidyl ether of bisphenol F (DGEBF, YD-F170) was supported by KUNDO Chemical Co., Ltd. 2-ethyl-4-meth-ylimidazole (EMI-2,4) used as cured agent was purchased from Aladdin Industrial Corporation. Other reagents and chemicals were used without further purification.

Characterization methods

NMR: 1H NMR and 13C NMR spectra were recorded on a Varian INOVA-400 MHz type (1H, 400 MHz and 13C, 100 MHz) spectrometer. Chemical shifts are reported in ppm from the internal standard, tetramethylsilane (0 ppm) for 1H. Data are presented as follows: chemical shift, multiplicity (s = singlet, d = doublet, m = multiplet and/or multiplet resonances, br = broad), coupling constant in hertz (Hz), and signal area integration in natural numbers.

SEC: Size exclusion chromatography (SEC) was performed at 35 oC using polystyrene standards for calibration on Waters 410 GPC instrument with THF as eluent, using differential detector, multi-angle laser light scattering (MALLS) detector (Wyatt Technology, DAWN EOS), and viscosity detector.

ESI-MS: ESI-MS analytical measurements were performed in dichloromethane solutions on a SolariX 7.0T spectrometer (Bruker Daltonics).

DSC: The thermogram were measured using DSC Q20 (DuPont TA Instruments). A sealed empty crucible was used as a reference, and the DSC was calibrated using indium. Samples were heated from room temperature to 190 °C, at a rate of 10 °C·min-1, under helium flow, and were kept at 190 °C for 2 mins to erase the thermal history. Subsequently, the samples were cooled to -10 °C, at a rate of 10 °C·min-1, and kept at -10 °C for further 2 mins, followed by a heating procedure from -10 °C to 190 °C, at a rate of 10 °C·min-1.

DMA: The dynamic mechanical properties were tested on a dynamic mechanical analyzer (DMA) 8000 (PerkinElmer Instruments, Inc., USA) at a frequency of 1 Hz. Rectangular samples with the dimension of 40 × 10 × 3 mm3 were measured using the three-point bending mode at a temperature range from 25 to 200 °C.

Pendulum impact testing: The test of impact strength was conducted through the plastic pendulum impact testing machine PTM7000 (Shenzhen SUNS Technology Stock Co., LTD., China).

Experimental procedures

Synthesis of (salen)CoIIICl

Salen ligand. To a solution of (R, R)-1,2-cyclohexanediamine (0.57 g, 5 mmol) in ethanol (40 mL) in a round-bottomed flask, 3,5-di-tert-butyl-2-hydroxybenzaldehyde (2.34 g, 10 mmol) in ethanol (50 mL) was slowly added. The mixture was heated to reflux for 6 hours at 80 oC and then cooled to room temperature. After filtration and dried in vacuum, a yellow solid was obtained with 95% yield. 1H NMR (CDCl3, 400 MHz): δ 1.26 (s, 18H), 1.45 (s, 20H), 1.64-2.0 (m, 6H), 3.37(s, 2H), 7.03 (s, 2H), 7.34 (s, 2H), 8.35 (s, 2H), 13.72 (s, 2H).

(Salen)CoII. To a solution of salen ligand (4.37 g, 8 mmol) in CH2Cl2 (50 mL), anhydrous cobalt acetate (1.77 g, 10 mmol) in ethanol (25 mL) was slowly added under Ar. The reaction mixture was allowed to stirred for 30 min at room temperature and another 15 min at 0 oC, then, it was filtrated and washed with cold methanol. A red solid was collected and dried in vacuum at 40 oC with 96% yield.

(Salen)CoIIICl. The (Salen)CoIIICl catalyst was prepared as previously described.1 Additional characterization: 1H NMR (DMSO-d6, 400 MHz): δ 1.28 (s, 18H), 1.52-1.62 (m, 2H), 1.72 (s, 18H), 1.85-1.97(m, 2H), 1.97-2.05 (m, 2H), 3.04-3.11 (m, 2H, CyH), 3.58-3.66 (m, 2H), 7.45 (d, 4H), 7.78 (s, 2H).

Synthesis of compound 2a via (salen)CoIIICl catalyzed ring-opening of GA under the CO atmosphere

In an argon filled glove box, (salen)CoIIICl complex (63.9 mg, 0.1 mmol), GA (23 μL, 0.2 mmol), and THF (1 mL) were charged into a 10 mL ampoule, which was wrapped in aluminum foil and equipped with a magnetic stir bar. The ampoule was then taken out of the glove box and allowed to be stirred under 1 atm CO at room temperature for 8 h. Dark green powder was obtained after GA and THF were evaporated under vacuum.

Chain extension of hb-PGA-CoIII(salen) with MA

In an argon filled glove box, hb-PGA-CoIII(salen) (0.96 g, Mn, SEC = 9.6 kDa, 0.1 mmol), MA (2.70 mL, 30 mmol), and THF (2 mL) were charged into a 25 mL ampoule, which was wrapped in aluminum foil and equipped with a magnetic stir bar. The ampoule was then taken out of the glove box and allowed to stirred at 25 oC under irradiation of a household white LED lamp with light intensity of 10 mW/cm-2. A small aliquot of the polymerization mixture was taken out for 1H NMR spectroscopy and the remained crude mixture was precipitated in cold methanol.

Preparation of hb-PGA-TEMPO/DGEBF

A certain amount of hb-PGA-TEMPO and DGEBF were dissolved in methylene chloride. Then most of solvent was rapidly removed using a rotary evaporator. The obtained mixture was further dried in a vacuum at 40 °C for 6 h. After which, 6 wt% EMI-2, 4 relative to epoxy resin was incorporated into the mixture and degassed for several minutes. Finally, the uncured mixture was decanted into a PTFE mold and underwent a programmed curing of 60 °C for 2 h, 150 °C for 8 h. For comparison, neat DGEBF were fabricated using the same process.

CO-insertion study

Supplementary Figure 1. ESI-MS spectrum of compound 2a.

Supplementary Figure 2. 1H NMR spectrum of compound 2a in DMSO-d6 at 25 oC.

Supplementary Figure 3. 13C NMR spectrum of compound 2a in DMSO-d6 at 25 oC.

Supplementary Figure 4. COSY NMR spectrum of compound 2a in DMSO-d6 at 25 oC.

Characterization of the hyperbranched polymers

Supplementary Figure 5. Evolution of  1H NMR spectra for the “ON/OFF” switching of OMR-SCVCP stage by light ([GA]/[1] = 30/1, [GA] = 2 M in THF).

Supplementary Figure 6. Evolution of 1H NMR spectra for the OMR-SCVCP stage ([GA]/[1] = 30/1, [GA] = 2 M in THF).

Supplementary Figure 7. 1H NMR spectrum of hb-PGA-CoIII(salen) in DMSO-d6 at 25 oC (Table 1, entry 3).

Supplementary Figure 8. SEC trace of hb-PGA-CoIII(salen) (Table 1, entry 5).

Supplementary Figure 9. SEC trace of hb-PGA-CoIII(salen) (Table 1, entry 6).

Supplementary Figure 10. SEC trace of hb-PGA-CoIII(salen) (Table 1, entry 7).

Supplementary Figure 11. SEC trace of hb-PGA-CoIII(salen) (Table 1, entry 8).

Supplementary Figure 12. 1H NMR spectrum of reaction mixture of the chain extension reaction with MA ([hb-PGA-CoIII(salen)]/[MA]=1/300, performed in THF) in DMSO-d6 at 25 oC.

Supplementary Figure 13. 1H NMR spectrum of hb-PGA-g-PMA-CoIII(salen) in DMSO-d6 at 25 oC.

Supplementary Figure 14. 1H NMR spectrum of hb-PGA-TEMPO in DMSO-d6 at 25 oC ((Table 1, entry 4).

Supplementary Figure 15. SEC trace of hb-PGA-TEMPO (Table 1, entry 4).

Supplementary Figure 16. The DSC results of the hb-PGA-TEMPO/DGEBF samples.

The cross-linking densities (ν) of the hb-PGA-TEMPO/DGEBF samples were calculated from the following equation referring to rubber-like elasticity theory

v=ER3RT

where ER is the storage modulus at rubbery state (Tg + 30 ℃), T is the absolute temperature (Tg + 30 K), and R is the gas constant (8.314 J mol−1 K−1). From the DMA results we could get the storage modulus and the absolute temperature.

Supplementary Table 1. Storage modulus and cross-linking density data for hb-PGA-TEMPO/DGEBF samples.

| Sample | Modulus at 25 ℃ （MPa） | Tg （℃） | Modulus at Tg + 30 ℃ （MPa） | v (×103 mol/m3) |
| --- | --- | --- | --- | --- |
| 0/100 | 6996 | 65.6 | 46 | 5.00 |
| 4/96 | 6468 | 87.3 | 78 | 8.01 |
| 8/92 | 6016 | 101.6 | 82 | 8.12 |

Supplementary References

(1)	Nielsen, L. P. C.; Stevenson, C. P.; Blackmond, D. G.; Jacobsen, E. N. J. Am. Chem. Soc. 2004, 126, 1360-1362.