Regulating photosalient behaviour in dynamic metal-organic crystals

Samim Khan,1 Basudeb Dutta,1 Sanobar Naaz,1 Aditya Choudhury,2 Pierre-Andre Cazade,3,4 Emma Kiely,3 Sarah Guerin3,4* Raghavender Medishetty,2*‡ and Mohammad Hedayetullah Mir1*†

1Department of Chemistry, Aliah University, New Town, Kolkata 700 156, India.

2Department of Chemistry, IIT Bhilai, Sejbahar, Raipur, Chhattisgarh 492015, India

3Department of Physics, Bernal Institute, University of Limerick, V94 T9PX, Ireland

4SSPC, The Science Foundation Ireland Research Centre for Pharmaceuticals, University of Limerick, V94 T9PX, Ireland

Supplementary information

Experimental Section

Materials and Methods

All chemicals purchased were reagent grade and were used without further purification. Elemental analysis (carbon, hydrogen and nitrogen) was performed on a Perkin–Elmer 240C elemental analyzer. Infrared spectrum in KBr (4500–500 cm-1) was recorded using a Perkin–Elmer FT-IR spectrum RX1 spectrometer. 1H NMR spectra were recorded on a 400 MHz Bruker Avance 400 FT NMR spectrometer with TMS as an internal reference in DMSO-d6 solution. The solid-state photoluminescence measurements were made using Horiba Fluorolog with a solid-state sample holder. The solid-state photoluminescence measurements were made using Horiba Jobin Yvon Fluoromax-4 Spectrophotometer (Excitation wavelength – 390 nm) with a solid-state sample holder. CARL ZEISS UHR Field Emission Scanning Electron Microscope (FESEM) was used for SEM images. Photodimerization reaction was carried out using Luzchem photoreactor (8 W UVA lamps) at ~350 nm at room temperature. Crystalline ground powder was packed between the glass slides and irradiated under UV light. Glass slides were flipped at regular intervals of time to maintain uniform exposure of UV radiation. Photosalient effects were studied by irradiating good quality single crystal with UV light using Xe-source using MAX-350 optical photoreactor under a microscope equipped with a high-quality camera for capturing videos.

Table S1 Crystal data and refinement parameters for compound 1, i1, p1 and 1.

| Formula | C48 H36N2O6Zn (1) | C96H68N4O12Zn2 ( i1) | C48H36N2O6Zn (p1) | 0.25(C96H72N4O12 Zn2) (1) |
| --- | --- | --- | --- | --- |
| fw | 802.18 | 1600.28 | 802.18 | 403.83 |
| cryst syst | Monoclinic | Monoclinic | Monoclinic | Monoclinic |
| space group | P21/c | P21/c | P21/c | P21/c |
| a (Å) | 22.9098(16) | 22.6733(13) | 14.1626(1) | 7.8757(2) |
| b (Å) | 15.4421(10) | 15.4419(4) | 20.5541(1) | 23.4713(8) |
| c (Å) | 22.7056(14) | 22.7005(8) | 13.0975(1) | 20.5487(8) |
| (deg) | 90 | 90 | 90 | 90 |
| (deg) | 103.112(7) | 103.606(4) | 90.615(1) | 90.977(3) |
| γ (deg) | 90 | 90 | 90 | 90 |
| V (Å3) | 7823.3(9) | 7724.8(6) | 3812.46(4) | 3797.9(2) |
| T (K) | 293 | 293 | 100 | 283 |
| Z | 8 | 4 | 4 | 8 |
| Dcalcd (g/cm3) | 1.362 | 1.376 | 1.398 | 1.413 |
| (mm-1) | 0.682 | 0.690 | 1.343 | 0.703 |
| (Å) | 0.71073 | 0.71073 | 0.71073 | 0.71073 |
| GOF on F2 | 1.024 | 0.940 | 1.031 | 1.47 |
| Final R indices [I >2σ(I)]a,b | R1= 0.0545 wR2= 0.1387 | R1= 0.0847 wR2= 0.2839 | R1= 0.0285 wR2= 0.0774 | R1= 0.0585 wR2= 0.1519 |

aR1 = Σ||Fo|  ̶  |Fc||/Σ|Fo|, b wR2 = [Σw(Fo2  ̶  Fc2)2/Σw(Fo2)2]1/2

Table S2 Crystal data and refinement parameters for compound 2 and 2.

| Formula | C48 H36CdN2O6 (2) | C96H72Cd2N4O12 (2') |
| --- | --- | --- |
| fw | 849.20 | 1698.40 |
| cryst syst | Monoclinic | Triclinic |
| space group | P21/c | P21/c |
| a (Å) | 22.9239(9) | 22.0832(11) |
| b (Å) | 15.4394(6) | 15.5975(7) |
| c (Å) | 22.7061(9) | 23.0664(10) |
| (deg) | 90 | 90 |
| (deg) | 103.143(1) | 105.172(3) |
| γ (deg) | 90 | 90 |
| V (Å3) | 7825.9(5) | 7668.1(6) |
| Z | 8 | 4 |
| T (K) | 293 | 293 |
| Dcalcd(g/cm3) | 1.441 | 1.471 |
| (mm-1) | 0.612 | 0.625 |
| (Å) | 0.71073 | 0.71073 |
| GOF on F2 | 1.430 | 1.126 |
| Final R indices [I >2σ(I)]a,b | R1= 0.0969 wR2= 0.3622 | R1= 0.2063 wR2= 0.53 |

aR1 = Σ||Fo|  ̶  |Fc||/ Σ|Fo|, b wR2 = [Σw(Fo2  ̶  Fc2)2/Σw(Fo2)2]1/2

Table S3 Selected bond lengths and bond angles 1 and i1.

| Bond length (Å) |  |  |  |
| --- | --- | --- | --- |
|  |  | 1 | i1 |
| Zn(1)-O(1) | 1.955(2) |  | 1.957(4) |
| Zn(1)-O(3) | 1.975(2) |  | 1.973(3) |
| Zn(1)-O(4) | 2.566(2) |  | 2.550(4) |
| Zn(1)-N(1) | 2.044(2) |  | 2.023(6) |
| Zn(1)-N(2) | 2.038(2) |  | 2.020(6) |
| Zn(2)-O(8) | 2.584(2) |  | 2.566(4) |
| Zn(2)-O(9) | 1.951(2) |  | 1.956(4) |
| Zn(2)-O(7) | 1.976(2) |  | 1.972(3) |
| Zn(2)-N(4) | 2.032(2) |  | 2.010(6) |
| Zn(2)-N(3) | 2.049(2) |  | 2.045(6) |
| Bond angle (°) |  |  |  |
|  |  | 1 | i1 |
| O(1)-Zn(1)-O(3) | 108.41(8) |  | 109.10(15) |
| O(1)-Zn(1)-O(4) | 163.90(8) |  | 165.06(12) |
| O(1)-Zn(1)-N(1) | 95.51(9) |  | 95.1(2) |
| O(1)-Zn(1)-N(2) | 102.23(9) |  | 100.92(19) |
| O(3)-Zn(1)-O(4) | 56.16(7) |  | 56.49(13) |
| O(3)-Zn(1)-N(1) | 113.03(9) |  | 111.51(18) |
| O(3)-Zn(1)-N(2) | 108.47(9) |  | 108.7(2) |
| O(4)-Zn(1)-N(1) | 87.74(8) |  | 87.70(19) |
| O(4)-Zn(1)-N(2) | 88.30(8) |  | 88.60(18) |
| N(1)-Zn(1)-N(2) | 126.35(9) |  | 128.4(2) |
| O(7)-Zn(2)-N(4) | 108.60(9) |  | 107.4(2) |
| O(8)-Zn(2)-O(9) | 164.83(7) |  | 165.81(12) |
| O(8)-Zn(2)-N(3) | 85.44(8) |  | 85.99(19) |
| O(8)-Zn(2)-N(4) | 88.37(8) |  | 88.33(18) |
| O(9)-Zn(2)-N(3) | 96.17(9) |  | 95.2(2) |
| O(9)-Zn(2)-N(4) | 102.60(9) |  | 101.77(19) |
| N(3)-Zn(2)-N(4) | 126.13(9) |  | 128.5(2) |
| O(7)-Zn(2)-O(9) | 110.07(8) |  | 110.72(15) |
| O(7)-Zn(2)-N(3) | 111.30(9) |  | 111.20(17) |
| O(7)-Zn(2)-O(8) | 55.79(7) |  | 56.12(13) |

Table S4 Selected bond lengths and bond angles 1.

| Bond length (Å) |  |
| --- | --- |
| Zn(1)-O(2) | 1.923(3) |
| Zn(1)-O(5) | 1.924(3) |
| Zn(1)-N(3) | 2.031(3) |
| Zn(1)-N(4) | 2.010(3) |
| Bond angle (°) |  |
| O(2)-Zn(1)-O(5) | 98.41(11) |
| O(2)-Zn(1)-N(3) | 111.16(12) |
| O(2)-Zn(1)-N(4) | 119.58(12) |
| O(5)-Zn(1)-N(3) | 112.58(12) |
| O(5)-Zn(1)-N(4) | 109.04(12) |
| N(3)-Zn(1)-N(4) | 106.10(11) |

Table S5 Selected bond lengths and bond angles p1.

| Bond length (Å) |  |
| --- | --- |
| Zn(1)-O(1) | 1.9746(11) |
| Zn(1)-O(2) | 2.6373(11) |
| Zn(1)-O(3) | 2.3956(11) |
| Zn(1)-O(4) | 2.0265(11) |
| Zn(1)-N(1) | 2.0539(12) |
| Zn(1)-N(2) | 2.0809(12) |
| Bond angle (°) |  |
| O(1)-Zn(1)-O(2) | 55.01(4) |
| O(1)-Zn(1)-O(3) | 91.23(4) |
| O(1)-Zn(1)-O(4) | 139.90(5) |
| O(1)-Zn(1)-N(1) | 106.77(5) |
| O(1)-Zn(1)-N(2) | 97.56(5) |
| O(2)-Zn(1)-O(3) | 81.64(4) |
| O(2)-Zn(1)-O(4) | 91.97(4) |
| O(2)-Zn(1)-N(1) | 93.14(4) |
| O(2)-Zn(1)-N(2) | 147.37(4) |
| O(3)-Zn(1)-O(4) | 58.82(4) |
| O(3)-Zn(1)-N(1) | 153.87(5) |
| O(3)-Zn(1)-N(2) | 81.75(4) |
| O(4)-Zn(1)-N(1) | 96.05(5) |
| O(4)-Zn(1)-N(2) | 103.04(4) |
| N(1)-Zn(1)-N(2) | 113.48(5) |

Table S6 Selected bond lengths and bond angles 2.

| Bond length (Å) |  |
| --- | --- |
| Cd(1)-O(1) | 1.966(3) |
| Cd(1)-O(2) | 2.581(4) |
| Cd(1)-O(4) | 1.940(4) |
| Cd(1)-N(1) | 2.030(4) |
| Cd(1)-N(2) | 2.047(4) |
| Cd(2)-O(10) | 1.987(3) |
| Cd(2)-O(11) | 2.557(4) |
| Cd(2)-O(7) | 1.947(4) |
| Cd(2)-N(4) | 2.037(4) |
| Cd(2)-N(3) | 2.039(4) |
| Bond angle (°) |  |
| O(1)-Cd(1)-O(2) | 56.01(12) |
| O(1)-Cd(1)-O(4) | 110.26(13) |
| O(1)-Cd(1)-N(1) | 108.56(14) |
| O(1)-Cd(1)-N(2) | 111.44(15) |
| O(1)-Cd(1)-C(35) | 27.93(14) |
| O(2)-Cd(1)-O(4) | 165.44(12) |
| O(2)-Cd(1)-N(1) | 88.07(14) |
| O(2)-Cd(1)-N2 | 85.72(14) |
| O(2)-Cd(1)-C(35) | 28.14(12) |
| O(4)-Cd(1)-N(1) | 102.09(16) |
| O(4)-Cd(1)-N(2) | 96.35(16) |
| O(4)-Cd(1)-C(35) | 137.79(14) |
| N(1)-Cd(1)-N(2) | 126.16(16) |
| N(1)-Cd(1)-C(35) | 100.53(15) |
| N(2)-Cd(1)-C(35) | 98.37(15) |
| O(7)-Cd(2)-O(10) | 108.09(13) |
| O(7)-Cd(2)-O(11) | 163.73(12) |
| O(7)-Cd(2)-N(3) | 95.89(16) |
| O(7)-Cd(2)-N(4) | 102.20(15) |
| O(7)-Cd(2)-C(90) | 135.95(14) |
| O(10)-Cd(2)-O(11) | 56.17(12) |
| O(10)-Cd(2)-N(3) | 112.74(16) |
| O(10)-Cd(2)-N(4) | 108.08(14) |
| O(10)-Cd(2)-C(90) | 28.13(14) |
| O(11)-Cd(2)-N(3) | 87.79(14) |
| O(11)-Cd(2)-N(4) | 87.97(14) |
| O(11)-Cd(2)-C(90) | 28.08(12) |
| N(3)-Cd(2)-N(4) | 126.97(16) |
| N(3)-Cd(2)-C(90) | 100.37(15) |
| N(4)-Cd(2)-C(90) | 100.00(15) |

Table S7 Selected bond lengths and bond angles 2.

| Bond length (Å) |  |
| --- | --- |
| Cd(1)-O(1) | 2.623(11) |
| Cd(1)-O(2) | 1.994(10) |
| Cd(1)-O(4) | 1.929(10) |
| Cd(1)-N(4) | 2.042(12) |
| Cd(1)-N(1)a | 2.060(13) |
| Cd(2)-O(8) | 1.930(11) |
| Cd(2)-O(10) | 1.961(11) |
| Cd(2)-O(11) | 2.698(11) |
| Cd(2)-N(2) | 2.039(13) |
| Cd(2)-N(3) | 2.058(12) |
| Bond angle (°) |  |
| O(1)-Cd(1)-O(2) | 53.2(4) |
| O(1)-Cd(1)-O(4) | 166.3(4) |
| O(1)-Cd(1)-N(4) | 86.8(4) |
| O(1)-Cd(1)-C(91) | 28.0(4) |
| O(1)-Cd(1)-N(1)a | 86.3(5) |
| O(2)-Cd(1)-O(4) | 113.8(4) |
| O(2)-Cd(1)-N(4) | 105.1(5) |
| O(2)-Cd(1)-C(91) | 25.2(4) |
| O(2)-Cd(1)-N(1)a | 107.5(5) |
| O(4)-Cd(1)-N(4) | 102.0(4) |
| O(4)-Cd(1)-C(91) | 138.7(4) |
| O(4)-Cd(1)-N(1)a | 95.0(5) |
| N(4)-Cd(1)-C(91) | 98.2(5) |
| N(1)a-Cd(1)-N(4) | 132.9(5) |
| N(1)a-Cd(1)-C(91) | 97.0(5) |
| O(8)-Cd(2)-O(10) | 115.2(5) |
| O(8)-Cd(2)-O(11) | 166.5(4) |
| O(8)-Cd(2)-N(2) | 102.3(5) |
| O(8)-Cd(2)-N(3) | 93.5(5) |
| O(8)-Cd(2)-C(42) | 141.0(5) |
| O(10)-Cd(2)-O(11) | 52.3(4) |
| O(10)-Cd(2)-N(2) | 104.6(5) |
| O(10)-Cd(2)-N(3) | 110.5(5) |
| O(10)-Cd(2)-C(42) | 26.1(5) |
| O(11)-Cd(2)-N(2) | 87.1(4) |
| O(11)-Cd(2)-N(3) | 87.5(4) |
| O(11)-Cd(2)-C(42) | 26.2(4) |
| N(2)-Cd(2)-N(3) | 130.2(5) |

Symmetric transformation: a = 1+x, y, 1+z

Fig. S1 A perspective view of the compound (a) 1; (b) i1 and (c) 1.

Fig. S2 1H NMR spectrum (400 MHz, DMSO-d6) of compound 1.

Fig. S3 1H NMR spectrum (400 MHz, DMSO-d6) of compound 1.

Fig. S4 1H NMR spectrum (400 MHz, DMSO-d6) of compound 2.

Fig. S5 1H NMR spectrum (DMSO-d6) of compound 2.

Fig. S6 PXRD patterns of simulated (blue) and as-synthesized (olive) compound 1.

Fig. S7 PXRD patterns of simulated (blue) and as-synthesized (magenta) compound 1.

References

- G. Sheldrick, M.SHELXT–Integrated space group and crystal structure determination. Acta Crystallogr. A, 2015, 71, 3–8.

- SMART and SAINT; Bruker AXS Imc.: Madison, WI, 1998.

- SADABS. Bruker AXS area detector scaling and absorption correction, Bruker AXS Inc., Madison, Wisconsin, USA, 2014.