Table 5: Measured displacements, strains and Poisson’s ratio of auxetic composite in the case of tensile test

| ∆L | ∆T | εl | εt | ν |
| --- | --- | --- | --- | --- |
| 20 | 13.52 | 0.028 | 0.080 | - 2.86 |

Table 6: Measured displacements, strains and Poisson’s ratio of honeycomb composite in the case of tensile test

| ∆L | ∆T | εl | εt | ν |
| --- | --- | --- | --- | --- |
| 15 | - 24.61 | 0.019 | - 0.154 | 8.10 |

Table 7: Measured displacements, strains and Poisson’s ratio of auxetic composite in the case of compression test

| ∆h | ∆d | εl | εt | ν |
| --- | --- | --- | --- | --- |
| - 20.04 | - 10.1 | 0.014 | 0.118 | - 0.12 |

Table 8: Measured displacements, strains and Poisson’s ratio of honeycomb composite in the case of compression test

| ∆h | ∆d | εl | εt | ν |
| --- | --- | --- | --- | --- |
| - 20.06 | 10 | - 0.125 | 0.118 | 0.11 |