Supplementary information

Luminescent Cd coordination polymer: synthesis, crystal structure and its application as a dual-responsive chemosensor for 4-nitroaniline and CrO42− in water

Akram Karbalaee Hosseini, Azadeh Tadjarodi*

Research Laboratory of Inorganic Materials Synthesis, Department of Chemistry, Iran University of Science and Technology (IUST), 16846-13114 Tehran, Iran

Corresponding author: Tel: +98(21) 77240517; Fax: +98(21) 77491204.

Email: tajarodi@iust.ac.ir  (A. Tadjarodi)

Fig. S1. XRD patterns of IUST-3: Simulated, as-synthesized, immersed in water.

Fig. S2. TGA curve of IUST-3.

Fig. S3. FT-IR spectrum of IUST-3.

Fig. S4. XRD patterns of IUST-3: Simulated, as-synthesized, immersed in water solution of 4-NA, immersed in water solution of CrO42⁻ anion.

Table. S1. Data Collection and Refinement Parameters for Single Crystal Analysis for IUST-3.

| Crystal data |  |
| --- | --- |
| Chemical formula | C28H16CdN4O5S2 |
| Mr | 664.97 |
| Crystal system, space group | Triclinic, Pī |
| Temperature (K) | 290 |
| a, b, c (Å) | 9.766 (2), 13.729 (3), 15.495 (3) |
| α, β, γ (◦) | 102.93 (3), 96.74 (3), 96.05 (3) |
| V (Å3) | 1992.2 (7) |
| Z | 2 |
| Radiation type | Mo Kα |
| μ (mm−1) | 0.68 |
| Crystal size (mm) | 0.3 × 0.25 × 0.2 |
| Data collection |  |
| Diffractometer | MAR-345dtb |
| Absorption correction | Multi-scan R.H. Blessing, Acta Crystallogr., Sect A 1995, 51, 33-38 |
| Tmin, Tmax | 0.903, 1.160 |
| No. of measured, independent and observed [I > 2σ(I)] reflections | 13945, 7232, 5824 |
| Rint | 0.052 |
| (sin θ/λ)max (Å−1) | 0.625 |
| Refinement |  |
| R[F2 > 2σ(F2)], wR(F2), S | 0.068, 0.218, 1.04 |
| No. of reflections | 7232 |
| No. of parameters | 361 |
| H-atom treatment | H-atom parameters constrained |
| Δρmax, Δρmin (e Å−3) | 0.75, −1.13 |

Table S2. Comparison of Ksv values and LOD between IUST-3 and the selected MOFs for 4-NA.

| LMOFs | LOD (µM) | Ksv (M-1) | Ref. |
| --- | --- | --- | --- |
| {[Zn2(tda)2(azopy)2]·DMF}n | 0.47 | 2.75×104 | [S1] |
| {Zn4(TPOM)(1,4-NDC)4}n | 0.64 | 7.87×104 | [S2] |
| [Zn(bpba)(NO3)] | 0.72 | 2.28×104 | [S3] |
| [H3O][Mn3(CPCP)(CH3COO)(DMF)]·11H2O | 2.04 | 5.19×104 | [S4] |
| {[Cd2(tpbn)(mbhna)2].2DMF}n | 12.9 | 2.87×104 | [S5] |
| {[Cd(CIP)2(H2O)2]n·2.5H2O} | - | 4.59×104 | [S6] |
| Tb2(TDC)3(CH3OH)2 | - | 9.52×103 | [S7] |
| [Cd(H2BDDA)]n | 4.9 | 8.79×104 | [S8] |
| IUST-3 | 0.52 | 1.03×105 | This work |

Table S3. Comparison of Ksv values and LOD between IUST-3 and the selected MOFs for CrO42⁻ anion.

| LMOFs | LOD (µM) | Ksv (M-1) | Ref. |
| --- | --- | --- | --- |
| [Zn(btz)]n | 10 | 3.19×103 | [S9] |
| [Zn(ttz)H2O]n | 20 | 2.35×103 | [S9] |
| {[Cd3(μ4‐cpboda)2(μ1,1‐ OH2)2(phen)2]∙2DMF∙1. 5H2O}n | 4.4 | 1.43×104 | [S10] |
| [Zn2(TPOM)(NDC)2]·3·5H2O | 2.50 | 0.781×104 | [S11] |
| {[Eu(L)(HCOO)(H2O)]}n | - | 1.54×103 | [S12] |
| [Zn(IPA)(L)]n | 13.6 | 4.34×103 | [S13] |
| [Cd3(cpota)2(phen)3]n·5nH2O | 0.418 | 6.9×103 | [S14] |
| Zn2(bpdc)2(tpeb) | 1.07 | 1.08×104 | [S15] |
| IUST-3 | 1.37 | 2.93×104 | This work |

References

[S1]	Li, L., Zou, J. Y & You, S. Y. A luminescent pillar-layer Zn (II) metal–organic framework for the ultrasensitive detection of nitroaniline. Inorganica Chim. Acta. 509, 119703 (2020).

[S2]	Chakraborty, G., Das P. & Mandal, S. K. Strategic construction of highly stable metal–organic frameworks combining both semi-rigid tetrapodal and rigid ditopic linkers: selective and ultrafast sensing of 4-Nitroaniline in water. ACS Appl. Mater. Interfaces.10, 42406-42416 (2018).‏

[S3]	Ji, N. N., Shi, Z. Q., Hu, H. L. & Zheng, H. G. A triphenylamine-functionalized luminescent sensor for efficient p-nitroaniline detection. Dalton Trans Dalton Trans. 47, 7222-7228 (2018).‏

[S4]	Lv, M. X. et al. Manganese cyclotriphosphazene multicarboxylate frameworks and composite encapsulated 1, 3, 6, 8-tetrakis (p-benzoic acid) pyrene as visualization of highly selective fluorescence sensors for aromatic compounds with NH2/NO2 Group. Cryst. Growth Des. 21, 6824-6839 (2021).‏

[S5]	Chakraborty, G., Das, P. & Mandal, S. K. Structural diversity in luminescent MOFs containing a bent electron‐rich dicarboxylate linker and a flexible capping ligand: selective detection of 4‐nitroaniline in water. Chem. Asian J. 14, 3712-3720 (2019).‏

[S6]	Wang, X. Q. et al. A multifunctional 1D Cd-based metal-organic complex for the highly luminescent sensitive detection of Fe3+, CrO42-/Cr2O72-, and nitroaromatic explosives. J. Solid State Chem. 274, 40-46 (2019).

[S7]	Xu, K. et al. Selective fluorescence detection of anilines and Fe3+ ions by two lanthanide metal–organic frameworks. RSC Adv. 6, 91741-91747 (2016).‏

[S8]	Shu, T. et al. A new three‐dimensional Cd (II) metal‐organic framework for highly selective sensing of Fe3+ as well as nitroaromatic compounds. ChemistrySelect. 2, 12046-12050 (2017).‏

[S9]	Cao, C. S., Hu, H. C., Xu, H., Qiao, W. Z. & Zhao, B. Two solvent-stable MOFs as a recyclable luminescent probe for detecting dichromate or chromate anions. CrystEngComm. 18, 4445-4451 (2016).

[S10]	Yang, D. D., Lu, L. P. & Zhu, M. L. Structural diversity, magnetic property, or luminescence sensing of Co (II) and Cd (II) coordination polymers derived from designed 3, 3′-((5-carboxy-1, 3-phenylene) bis (oxy)) dibenzoic acid. Dalton Trans. 48, 10220-10234 (2019).‏

[S11]	Lv, R. et al.Zinc metal–organic framework for selective detection and differentiation of Fe(III) and Cr(VI) ions in aqueous solution. Inorg. Chem. 56, 12348-12356 (2017).‏

[S12]	Huang, X. H. et al. Two lanthanide metal–organic frameworks as sensitive luminescent sensors for the detection of Cr2+ and Cr2O72− in aqueous solutions. CrystEngComm. 20, 189-197 (2017).‏

[S13]	Parmar, B., Rachuri, Y., Bisht, K. K., Laiya, R. & Suresh, E. Mechanochemical and conventional synthesis of Zn(II)/Cd(II) luminescent coordination polymers: dual sensing probe for selective detection of chromate anions and TNP in aqueous phase. Inorg. Chem. 56, 2627-2638 (2017).‏

[S14]	Li, S., Lu, L., Zhu, M., Yuan, C. & Feng, S. A bifunctional chemosensor for detection of volatile ketone or hexavalent chromate anions in aqueous solution based on a Cd(II) metal–organic framework. Sens. Actuators B Chem. 258, 970-980 (2018).‏

[S15]	Rath, B. B. & Vittal, J. J. Water stable Zn (II) metal–organic framework as a selective and sensitive luminescent probe for Fe(III) and chromate ions. Inorg. Chem. 59, 8818-8826 (2020).