Significantly Enhanced Dielectric and Energy Storage Performance of Epoxy Nanocomposites via Constructing Continuous 3D BaTiO3 Network Collaborated with Graphene Oxide

Xueqing Bi1, Wenqing Xue1, Zhen Wang1, Zi Wang2, Yuchao Li1*, Yanhu Zhan1, Shuangshuang Wang1, Jigong Hao1, Wei Li1, Weifang Han1, Bo Ge1, Junwen Ren2*, Junwei Zha3*

- School of Materials Science and Engineering, Liaocheng University, Liaocheng, 252059, P.R. China;

- College of Electrical Engineering, Sichuan University, Chengdu, 610065, P.R. China;

3. School of Chemistry and Biological Engineering, University of Science and Technology Beijing, Beijing, 100083, P.R. China;

* Corresponding author: liyuchao@lcu.edu.cn; myboyryl@scu.edu.cn; zhajw@ustb.edu.cn

Figure S1. SEM images of (a) cleanroom wiper and (b) 3DBT network structure.

Figure S2. The variation of (a) ε′-ε″ and (b) M′-M″, and frequency denpendence of the (c) real and (d) imaginary parts of dielectric modulus for epoxy composites.

Table S1. The composition, dielectric and thermal properties of GEBT and EBT composites

| Composites | BT Content | GO content | Tdi (oC) | Tdf (oC) | ε′ (100 Hz) | tanδ (100 Hz) | E0 (kV·mm-1) | Ue (J·cm-3) at 40 kV·mm-1 | Ul (J·cm-3) (Linear) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| EP GEBT-1 GEBT-2 GEBT-3 GEBT-4 EBT-1 EBT-2 | 0 wt% 15.0 wt% 14.3 wt% 14.5 wt% 15.4 wt% 15.0 wt% 25.0 wt% | 0 wt% 0 wt% 0.25 wt% 0.5 wt% 0.75 wt% 0 wt% 0 wt% | 363.5 357.0 356.0 317.1 305.1 314.0 369.6 | 538.7 529.0 536.9 543.4 519.4 513.8 533.0 | 4.4 9.2 9.4 12.0 15.6 5.2 6.3 | 0.023 0.020 0.021 0.012 0.020 0.015 0.017 | 140.2 128.8 133.8 224.9 239.8 137.6 121.0 | 0.25 0.30 0.37 0.47 0.36 0.23 0.23 | 0.38 0.68 0.75 2.68 3.97 0.44 0.41 |  |

Note: GO is a relative concentration just to epoxy.