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Fig. S1 TEM image of MIL-101(Fe).
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Fig. S2 Surface and interfacial tension of the MC aqueous dispersion with different content of MCs. Inset is the appearance of the MC aqueous dispersion.

























Table. S1 Specific surface area and average pore size of MIL-101(Fe) and MIL-101(Fe)/CNC
	Samples
	BET surface area (m2/g)
	Pore volume (cm3/g)
	Pore size (nm)

	MIL-101(Fe)
	550
	0.14
	2.8

	MC-0.1
	554
	0.15
	4.9

	MC-0.25
	436
	0.17
	6.3

	MC-0.5
	399
	0.09
	4.5

	MC-1.0
	390
	0.08
	4.1
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Fig. S3 Microscope image of the Pickering emulsion stabilized by MIL-101(Fe) nanoparticles without CNCs.
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Fig. S4 Average droplet size versus different (a) CMCs, (b) CCNCs and (c) φo.
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Fig. S5 CLSM of the emulsion stabilized by MCs with 1.0 wt% CNCs.
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Fig. S6 Degradation rate of the MC-0.5 in the Pickering emulsion system with different pH.
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Fig. S7 Optical images of the emulsion droplets after 1st and 5th catalytic cycles.
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