Table 2. Description of the general data of the selected articles and surface treatments and intermediate agents tested

| Author/ Year | Sample size (per group) | Resin Composite (Substrat) | Aging | Surface treatment | Intermediate agent | Resin Composite (repair) | Storage time and media after repair | Bond Strength Test |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Benzi, 2021 | 66 (22) | FTKa-Z250 (3M ESPE, St. Paul, USA) AND OBFa-Filtek One (3M ESPE, St. Paul, USA) | Thermocycled 10000 cycles at 5°C-55°C | no | Universal adhesive Scotchbond ( 3M ESPE, St. Paul, USA) | FTKa-Z250 (3M ESPE, St. Paul, USA) | Stored in relative humidity, at 37°C, for 24 hours | Microtensile strength test (mTBS) Universal testing machine (EMIC Ltda, Model DL 2000, São José dos Pinhais, PR, Brazil) |
|  |  |  |  | Roughened diamond bur #2223 (KG Sorensen; Cotia, SP, Brazil) + 35% phosphoric-acid (Vivadent, Schann, Liechtenstein) 60s |  |  |  |  |
|  |  |  |  | Sandblasted Al2O3 (BioArt, São Carlos, SP, Brazil) + 35% phosphoric-acid (Vivadent, Schann, Liechtenstein) 60s |  |  |  |  |
| Chuenweravanicha, 2022 | 35 (6) | Filtek Z350XT (3M ESPE, St. Paul, USA) | Stored in distilled water at 37°C for 30 days in an incubator | no | Universal adhesive Single Bond (3M Oral Care,St Paul, MN, USA) | Filtek Z350XT (3M ESPE, St. Paul, USA) | Stored in distilled water for 24h at 37°C in the incubator OR Thermocycled 10000 cycles at 5°C-55°C | Microtensile Bond Strength (μTBS) Universal testing machine (LF plus, Lloyd Instruments; Bognor Regis, UK) |
|  |  |  |  | Roughened extra-fine diamond bur #837 (Komet; Lemgo, Germany) |  |  |  |  |
|  |  |  |  | Roughened extra-fine diamond bur #837 (Komet; Lemgo, Germany) + 35% phosphoric-acid (Ultradent, South Jordan, UT, USA) 30s |  |  |  |  |
|  |  |  |  | Roughened extra-fine diamond bur #837 (Komet; Lemgo, Germany) | Silane (Porcelain primer, Bisco, Schaumburg, IL, USA) + Universal adhesive Single Bond (3M Oral Care, St Paul, MN, USA) |  |  |  |
|  |  |  |  | Roughened extra-fine diamond bur #837 (Komet; Lemgo, Germany) + 35% phosphoric-acid (Ultradent, South Jordan, UT, USA) 30s |  |  |  |  |
|  |  |  |  | Grit-blasted with 50-μm Al2O3 (American Dental Airsonic Technologies; Corpus Christi, TX, USA) + 35% phosphoric-acid (Ultradent, South Jordan, UT, USA) |  |  |  |  |
| Hoseinifar, 2021 | 66 (11) | Z350 composite (3M Oral Care, St Paul, MN, USA) | Stored in distilled water for 6 months + Thermocycled 2000 cycles at 5°C-55°C | 35% phosphoric-acid (Fine Etch 37, Spident, Korea) | Silane (Ultradent, South Jordan, UT, USA) + Clearfil Universal Bond (Kuraray Noritake Dental, Tokyo, Japan) | Z350 composite (3M Oral Care, St Paul, MN, USA) | Stored in distilled water for 24h AND Thermocycled 2000 cycles at 5°C-55°C | Shear bond strength (SBS) Universal testing machine (Testometric M350-10CT, England) |
|  |  |  |  |  | Clearfil Universal Bond (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
|  |  |  |  |  | Silane (Ultradent, South Jordan, UT, USA) + Single Bond Universal (3M Oral Care, St Paul, MN, USA) |  |  |  |
|  |  |  |  |  | Single Bond Universal (3M Oral Care, St Paul, MN, USA) |  |  |  |
|  |  |  |  |  | Silane (Ultradent, South Jordan, UT, USA) + Single Bond 2 (3M Oral Care, St Paul, MN, USA) |  |  |  |
|  |  |  |  |  | Single Bond 2 (3M Oral Care, St Paul, MN, USA) |  |  |  |
| Jusué-Esparza, 2022 | 80(10) | Empress Direct (Ivoclar Vivadent AG, Liechtenstein) | Boiled in water for 8h and Stored in distilled water at 37ºC for 2 Weeks | no | Tetric N-Bond Universal (Ivoclar Vivadent AG, Liechtenstein) | Empress Direct (Ivoclar Vivadent AG, Liechtenstein) | Stored in distilled water at 37ºC for 24h or stored in distilled water for 6months at 37°C | Shear bond strength (SBS) Universal testing machine (Instron 4465, MA) |
|  |  |  |  |  | Silane (Ultradent, South Jordan, UT, USA) + Tetric N-Bond Universal (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Single Bond Universal (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane (Ultradent, South Jordan, UT, USA) + Single Bond Universal (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Clearfil SE Bond 2 (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
|  |  |  |  |  | Silane (Ultradent, South Jordan, UT, USA) + Clearfil SE Bond 2 (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
| Karadağlioğlu, 2022 | 120 (12) | Filtek Z250 (3M ESPE, St. Paul, MN, USA) AND Clearfil Majesty Esthetic (Kuraray Noritake Dental, Tokyo, Japan) | Incubated (FN 400, Nuve, Ankara, Turkey) at 37°C for 1 year in distilled water | no | Scotchbond Universal Adhesive (3M ESPE, St. Paul, MN, USA) | Clearfil Majesty Esthetic (Kuraray Noritake Dental, Tokyo, Japan) | Stored in distilled water at 37°C for 24h | Micro‑shear bond strength (μSBS) Universal test machine (EZ‑test‑500N Shimadzu, Kyoto, Japan) |
|  |  |  |  | Roughened with a diamond coarse brown disc of BISCO (Schaumburg, IL, USA) |  |  |  |  |
|  |  |  |  | Roughened with Al2O3 extra coarse disc of OPTIDISC (Kerr, Bioffio, Switzerland) |  |  |  |  |
|  |  |  |  | Roughened with a silicon carbide and Al2O3 coarse disc of Super‑Snap Rainbow Kit (Shofu, Kyoto, Japan) |  |  |  |  |
|  |  |  |  | Roughened with diamond bur with coarse grain size (Meisinger Dental, Germany) |  |  |  |  |
| Willers, 2021 | 35 (9) | Charisma (Heraeus Kulzer GmbH, Hanau, Germany) | Stored in distilled water in a laboratory oven (Fanem Ltda., São Paulo, SP, Brazil) at 37ºC for 4 years | Sandblasted with 50 mm with Al2O3 (Microetcher, Danville Material, San Ramon, CA, USA) | Silane-coupling agent, Ceramic Primer (3M Oral Care, Saint Paul, MN, USA) Adper Scotchbond Multi-Purpose Adhesive (3M Oral Care, Saint Paul, MN, USA) | Charisma (Heraeus Kulzer GmbH, Hanau, Germany) | Storage in distilled water at 37ºC for 24h | Shear bond strength (SBS) Universal testing machine (EZ Test, Shimadzu Corp., Kyoto, Japan) |
|  |  |  |  |  | Gluma Bond Universal (Heraeus Kulzer GmbH, Hanau, Germany) |  |  |  |
|  |  |  |  |  | Adhese Universal (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Scotchbond Bond Universal (3M Oral Care, Saint Paul, MN, USA) |  |  |  |
| Negreiros, 2021 | 42(6) | Filtek Supreme Ultra (3M Oral Care, St Paul, MN, USA) | Stored in distilled water at 37ºC for 4 months | Sandblasted with Al2O3 (Microetcher, CA, USA) | Silane (Ceramic Primer, 3M Oral Care, USA) + Adhesive Adper Scotchbond Multi-Purpose (3M Oral Care, USA) | Charisma (Heraeus Kulzer GmbH, Hanau, Germany) Filtek Supreme Ultra (3M Espe, USA) | Storad in water at 37°C for 1 year, | Micro-shear bond strength (MSBS) Universal testing machine (EZ Test, Shimadzu Corp., Kyoto, Japan). |
|  |  |  |  | no | Plasma Argon + Adhesive Adper Scotchbond Multi-Purpose (3M Oral Care, USA) |  |  |  |
|  |  |  |  | Sandblasted with Al2O3 (Microetcher, CA, USA) | Adhesive Adper Scotchbond Multi-Purpose (3M Oral Care, USA) |  |  |  |
|  |  |  |  | Sandblasted with Al2O3 (Microetcher, CA, USA) | Plasma Argon + Adhesive Adper Scotchbond Multi-Purpose (3M Oral Care, USA) |  |  |  |
| Akgül, 2021 | 140 (10) | Filtek Bulk Fill (3M Espe, USA) | Stored in distilled water at 37˚C for 24 h, AND Thermocycled, 5000 cycles at 5-55˚C | 32% phosphoric-acid Scotchbond Universal (3M Espe, USA) | Adhesive Single bond Universal (3M Espe, USA) | Filtek Z250 (3M Espe, USA) | Stored at 37˚C for 24h in distilled | Shear bond strength (SBS) Universal testing machine (Shimadzu AG-IS; Shimadzu) |
|  |  |  |  | 32% phosphoric-acid Scotchbond Universal (3M Espe, USA) + Sandblasted silica-coated Al2O3 (CoJet, 3M) |  |  |  |  |
|  |  |  |  | 32% phosphoric-acid Scotchbond Universal (3M Espe, USA) + Al2O3 size 50 μm (RONDOflex ™, Kavo, BR) |  |  |  |  |
|  |  |  |  | Sandblasted silica-coated Al2O3 (CoJet, 3M) |  |  |  |  |
|  |  |  |  | Al2O3 size 50 μm (RONDOflex ™, Kavo, BR) |  |  |  |  |
| Zanatta, 2021 | 120 (10) | Filtek P90 (3M Espe, USA) | Thermocycled, 10000 cycles at 5-55° C | Roughened diamond bur #1014 (KG Sorensen; Cotia, SP, Brazil) | Adhesive Adper Scotchbond Multipurpose (3M Espe, USA) | Filtek P90 (3M Espe, USA) | no | Tensile bond strength Universal testing machine (EMIC Ltda, Model DL 1000, São José dos Pinhais, PR, Brazil) |
|  |  |  |  |  | Adhesive Filtek P90 (3M Espe, USA) | Filtek P90 (3M Espe, USA) |  |  |
|  |  |  |  | Sandblasted with 50μm Al2O3 particles (Micro-etcher ERC, Danville Engineering, USA) |  |  |  |  |
| Ayar, 2018 | 60 (10) | Filtek P60 (3M Espe, USA) Filtek Bulk Fill Posterior (3M Espe, USA) | Boiled for 8 hours and stored in water for 2 weeks | Etched with 37% phosphoric-acid | no | Filtek Bulk Fill Posterior (3M Espe, USA) Filtek P60 (3M Espe, USA) | Stored in water at 37°C for 24 h. | Shear bond strengths (SBS) Universal testing machine (SD Mechatronic MTD 500, Germany) |
|  |  |  |  | Etched with 10% hydrofluoric-acid |  |  |  |  |
|  |  |  |  | Etched with 37% phosphoric-acid | Adhesive Adper Single Bond 2 (3M Espe, USA) |  |  |  |
|  |  |  |  | Etchedwith 10% hydrofluoric-acid |  |  |  |  |
|  |  |  |  | no |  |  |  |  |
| Imbery, 2014 | 120 (12) | Filtek Supreme Ultra (3M Espe, U | Stored in deionized water at 37ºC for 7 days | Etched phosphoric-acid | Bonding agent Optibond Solo Plus (Kerr, Orange, CA, USA) | Filtek Supreme Ultra (3M Espe, USA) | Stored in water at 37°C for 24 h. | Shear bond strengths (SBS) Flexural bond strength Diametral Tensile Strengths Instron Universal Testing Machine (Model #TTC, Instron Corporation, Canton, MA, USA) |
|  |  |  |  | no | Add & Bond (Parkell, Edgewood, NY, USA) |  |  |  |
|  |  |  |  | Etched phosphoric-acid | Silane Bond Enhancer (Pulpdent, Watertown, MA, USA) + Bonding agent Optibond Solo Plus (Kerr, Orange, CA, USA) |  |  |  |
|  |  |  |  | Quarter round bur, phosphoric-acid etched | Bonding agent Optibond Solo Plus (KERR) |  |  |  |
| Lemos, 2016 | 90 (10) | Z350 XT (3M Espe, USA) | Stored in distilled water at 37ºC for 7days or 180 days | Etched phosphoric-acid 37% (FGM, Joinville, Brazil) | Adper Single Bond Plus (3M Espe, USA) | Filtek Z350 XT (3M Espe, USA) Esthet-X (Dentsply Caulk, Milford, DE, USA) | no | Shear bond strengths (SBS) Universal testing machine (EMIC Ltda, Model DL 1000, São José dos Pinhais, PR, Brazil) |
| Wiegand, 2012 | 272 (16) | FiltekTM (3M Espe, USA) | Thermocycled 5000 cycles, 5–55 ◦C dwell time: 20s, transfer time: 10s | Etched hydrofluoric acid gel 5% (Vita Ceramics Etch) | Filtek Silorane Adhesive (3M Espe, USA) | Filtek Silorane (3M Espe, USA) Filtek supreme XTE (3M Espe, USA) | Additional thermal cycling procedure (5000 cycles, between 5–55 ◦C, dwell time: 20s, transfer time: 10s) | Shear bond strengths (SBS) Universal testing machine (Z010, Zwick, Ulm, Germany) |
|  |  |  |  |  | Adhesive Heliobond (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein)+ Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein)+ Adhesive Heliobond (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  | Roughened with a cylindrical diamond bur (40 m grit) | Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein)+ Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein)+ Adhesive Heliobond (Ivoclar) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus Ivoclar Vivadent AG, Liechtenstein)+ Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein)+ Adhesive Heliobond (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  | Sandblasted with Al2O3 (Renfert) | Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Adhesive Heliobond (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein)+ Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus, (Ivoclar Vivadent AG, Liechtenstein)Adhesive Heliobond (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  | Sandblasted silica-coated Al2O3 (CoJet, 3M) | Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Adhesive Heliobond (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein) + Filtek Silorane Adhesive Bond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent (Monobond Plus, (Ivoclar Vivadent AG, Liechtenstein)+ Adhesive Heliobond (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
| Nagano, 2018 | 108 (12) | Cleafil AP-X (APX) (Kuraray Noritake Dental, Tokyo, Japan) Beautifil II (Shofu; Kyoto, Japan) Filtek Supreme Ultra (Supreme) (3M Oral Care; St Paul, MN, USA) Estelite Quick (Estelite) (Tokuyama Dental Japan; Tokyo, Japan) | Stored in water at 37°C for 1 week, 2 weeks or 1 month | no | no | Cleafil AP-X (APX) (Kuraray Noritake Dental, Tokyo, Japan) | Stored in water at 37°C for 24 h. | Shear bond strengths (SBS) Testing device (EZ test 500N, Shimadzu; Kyoto, Japan) |
|  |  |  |  |  | Clearfil SE One (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
|  |  |  |  |  | Silane coupling adhesive agent (mixture of Clearfil SE One with Clearfil Porcelain Bond Activator (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
| Alqarni, 2018 | 96 (8) | Filtek Supreme Ultra (3M, St. Paul, MN, USA) Estelite Sigma Quick (Tokuyama Dental, Tokyo, Japan) Beautifil II (Shofu, Kyoto, Japan), Clearfil AP-X (Kuraray Noritake Dental, Tokyo, Japan | Stored in distilled water at 37°C for 60s, 1 week, 1 month | no | no | Filtek Supreme Ultra (3M, St. Paul, MN, USA) Estelite Sigma Quick (Tokuyama Dental, Tokyo, Japan) Beautifil II (Shofu, Kyoto, Japan), Clearfil AP-X (Kuraray Noritake Dental, Tokyo, Japan | Stored in distilled water at 37°C for 24 h. | Microshear bond strengths (μSBSs) EZ test 500 N (Shimadzu, Kyoto, Japan) |
|  |  |  |  |  | Clearfil SE One (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
|  |  |  |  |  | Clearfil SE One + Silane coupling agent (Clearfil Porcelain Bond Activator (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
| Melo, 2011 | 192 (8) | Charisma (Heraeus Kulzer GmbH, Hanau, Germany) | Artificial accelerated aging 4h exposure ultraviolet rays (UV-B) at 60 °C and 4h condensation at 60°C, for 192 h. | Etched phosphoric-acid 37% (FGM, Joinville, Brazil) | Silane coupling agent (Dentsply, Milford, USA)+ Adhesive Excite (Ivoclar Vivadent AG, Liechtenstein) | Charisma (Heraeus Kulzer GmbH, Hanau, Germany) | Stored in distilled water in a incubator at 37°C for 24 h, OR C-UV accelerated aging ASTM-G-53 machine (Adexim Comexim Ltda., São Paulo, Brazil) | Shear bond strengths (SBS) Universal testing machine (EMIC Ltda, Model DL 2000, São José dos Pinhais, PR, Brazil) |
|  |  |  |  |  | Adhesive Excite (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  | Roughened diamond bur #4138 (KG Sorensen; Cotia, SP, Brazil) + 37% phosphoric-acid (FGM, Joinville, Brazil) | Silane coupling agent (Dentsply, Milford, USA)+ Adhesive Excite (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Adhesive Excite (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  | Sandblasted (air abrasion) Al2O3 particles (Bio-Art, São Carlos, Brazil).+ 37% phosphoric-acid etched (FGM, Joinville, Brazil) | Silane coupling agent (Dentsply, Milford, USA)+ Adhesive Excite (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Adhesive Excite Empress Direct (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
| Dias, 2003 | 60 (10) | Filtek P60 (3M Espe, USA) Pertac (3M Espe, USA) | Stored in distilled and deionized water for 7 days | Polished 600-grit silicon carbide abrasive paper + Sandblasted 30um Al2O3 (Cojet) | Silane coupling agent (ESPE-sil) + Adhesive EBS- Multi (3M Espe, USA) | Filtek P60 (3M Espe, USA) Pertac (3M Espe, USA) | Stored in distilled and deionized water for 24h | Shear bond strengths (SBS) Instron universal (Instron Corporation, Canton, MA, USA) |
|  |  |  |  |  | Silane coupling agent (ESPE-sil) + One-Step UNI (BISCO, Inc. Schaumburg) |  |  |  |
|  |  |  |  |  | Silane coupling agent (ESPE-sil) Prompt L-Pop SE(3M Espe, USA) |  |  |  |
| Yap, 1999 | 48 (6) | Dyract (Dentsply, Weybridge, UK) | Stored in water at 37°C for 3 months or 6 months | 320- grit sandpaper | no | Dyract (Dentsply, Weybridge, UK) | no | Shear bond strengths (SBS) Instron universal (Instron Corporation, Canton, MA, USA) |
|  |  |  |  | Etched maleic acid 10% (Scotchbond Multi-Purpose Dental Adhesive; 3M Espe, USA) | Low-viscosity resin (Scotchbond Multi-Purpose) |  |  |  |
|  |  |  |  | Etched polyacrylic acid 10% (GC Corporation, Tokyo, Japan) |  |  |  |  |
|  |  |  |  | Sandblasted with 50 μm Al2O3 (Keramo 3; Renfert-GmbH) |  |  |  |  |
| Brum, 2017 | 120 (10) | Filtek Z350 XT (3M ESPE) Empress Direct Empress Direct (Ivoclar Vivadent AG, Liechtenstein) | Stored in water at 37°C for 7 days or 6 moths | Polished with SiC paper | no | Filtek Z350 XT (3M Espe, USA) Empress Direct (Ivoclar Vivadent AG, Liechtenstein) | Stored at 100% relative humidity for 7 days | Microshear bond strengths (μSBSs) Universal testing machine (EMIC Ltda, São José dos Pinhais, PR, Brazil) |
|  |  |  |  | Polished with SiC paper + Sandblasted Al2O3 (Bioart, SP, Brazil) | Silane coupling agent Monobond Plus (Ivoclar Vivadent AG, Liechtenstein) + Scotchbond Multi‑Purpose (3M ESPE, St. Paul, MN, USA) |  |  |  |
|  |  |  |  | Polished with SiC paper + Acetone liquid 99.5% (Biotec, Labmaster, PR, Brazil) |  |  |  |  |
|  |  |  |  | Polished with SiC paper +Acetone gel 75% (Farmadoctor, Paraná, Brazil) |  |  |  |  |
|  |  |  |  | Polished with SiC paper + Alcohol liquid 95% (Biotec, Labmaster, Paraná, Brazil) |  |  |  |  |
|  |  |  |  | Polished with SiC paper + Alcohol gel 80% (Farmadoctor, Paraná, Brazil) |  |  |  |  |
| Ayres, 2019 | 45 (5) | Charisma (Heraeus Kulzer GmbH, Hanau, Germany) | Stored in distilled water at 37ºC for 6 months | Polished with 600-grit silicon carbide paper + Air abrasion Al2O3 | Silane-coupling- (Ceramic Primer 3M espe USA) + Adhesive Adper Scotchbond Multi-Purpos (3M Espe, USA) | Charisma (Heraeus Kulzer GmbH, Hanau, Germany) | Stored in water for 24 hours or 1 year | Microshear bond strengths (μSBSs) Universal testing machine (EZ Test, Shimadzu Corp, Kyoto, Japan) |
|  |  |  |  | Polished with 600-grit silicon carbide paper + Air abrasion Al2O3+ PLASMA argon |  |  |  |  |
|  |  |  |  | Polished with 600-grit silicon carbide paper + PLASMA argon |  |  |  |  |
|  |  |  |  |  | Silane coupling agent (Ceramic Primer 3M Espe, USA) |  |  |  |
|  |  |  |  |  | Adhesive Adper Scotchbond Multi-Purpos (3M Espe, USA) |  |  |  |
|  |  |  |  | PLASMA argon | no |  |  |  |
| Bektas, 2012 | 96 (24) | Esthet·X (Dentsply, Weybridge, UK) | Stored in distilled water at 37°C for 24h or Thermocycled 1,000 / 5,000, or 10,000 cycles 5-55°C, dwell time 30s. | Irradiated by Er:YAG laser (Smart 2940D Plus, Deka Laser, Florence, Italy) + 37% phosphoric-acid | Adhesive Prime & Bond (Dentsply, DeTrey, Konstanz Germany) | Filtek Z250 (3M Espe, USA) | Stored in 37°C water for 24 h | Microshear bond strengths (μSBSs) Universal testing machine (LF Plus, Lloyd Instruments, Ametek Inc., England) |
|  |  |  |  | Roughened five strokes with coarse diamond bur (837314111534012C, M&A, Heerbrugg, Switzerland) + Etched phosphoric-acid 37% |  |  |  |  |
| Kiomarsi, 2017 | 120 (10) | Filtek Z250 (3M Espe, USA) | Thermocycled 5000 and 10000 cycles 5-55°C time of 20s | Roughened with diamond bur (835/008; Tees Kavan, Iran) + Etched phosphoric-acid 37% (Etch Royal, Pulpdent, Watertown, USA) | Silane (Angelus, Emergo Erupe, Metherland) + Adper Single Bond 2 (3M Espe, USA) | Filtek Z250 (3M Espe, USA) | Thermocycled 5000 OR Stored in distilled water at 37°C for 24h | Shear bond strengths (SBS) Universal testing machine (Zwick Roell, Ulm, Germany) |
|  |  |  |  | Irradiated by Er,Cr:YSGG laser (water lase, Biolase, CA, USA) + Etched phosphoric-acid (Etch Royal, Pulpdent, Watertown, USA) |  |  |  |  |
| Rinastiti; Siswomihardjo, 2011 | 72 (9) | Tetric Evo Ceram (Ivoclar Vivadent AG, Liechtenstein) Filtek- Supreme XT 3M Espe, USA | Thermocycled 5000 cycles in water from 5 -55ºC time of 30s | Polished and planed and using 1200-grit silicone carbide papers + sandblasted aluminum trioxide CoJet®- (3M Espe, Germany) | Silane ESPE®-Sil (3M Espe, Germany) + VisioTMBond (3M Espe, Germany) + Multilink (Ivoclar Vivadent AG, Schaan, Liechtenstein) | Tetric Evo Ceram (Ivoclar Vivadent AG, Liechtenstein) Filtek- Supreme XT 3M Espe, USA | no | Shear bond strengths (SBS) Microtensile bond strength (mTBS) Universal Testing Machine (Zwick ROELL X2.5MA 18-1-3/7, Zwick, Ulm, Germany) |
|  |  |  |  | Polished and Planed 1200-grit silicone carbide papers | Adper Scotchbond 1XT (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Adhesive Multilink (Ivoclar Vivadent AG, Schaan, Liechtenstein) |  |  |  |
| Silva, 2015 | 80 (10) | Universal Filtek™ Z350 (3M Espe, USA) | Thermocycled 106 cycles 5º- 55ºC | Roughened diamond bur abrasion + Etched phosphoric-acid 37% | Adper Scotchbond Multi- Purpose (3M Espe, USA) | Universal Filtek™ Z350 (3M Espe, USA) | Thermocycled 106 cycles 5º- 55ºC (Half of the samples) | Surface roughness analysis Microtensile bond strength (mTBS) Universal Test Machine (EMIC Ltda - Model 1L-2000, São José dos Pinhais, PR, Brazil) |
|  |  |  |  | Roughened diamond bur abrasion | Clearfil Liner bond 2V Primers A and B, and bond (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
| Sousa, 2013 | 80 (10) | 4 Seasons (Ivoclar Vivadent AG, Liechtenstein) | Stored in artificial saliva for 24 h or 7 days or 30 days or accelerated aging for 384h | Sandblasted Al2O3 particles (Microjato Bioart: SP, Brazil) + Etched phosphoric-acid 35% (Dentsply; RJ, Brazil) | Adper Single Bond 2 (3M Espe, USA) | 4 Seasons (Ivoclar Vivadent AG, Liechtenstein) | no | Microtensile bond strength (mTBS) Universal testing machine (EMIC Ltda, Model 1L-2000, São José dos Pinhais, PR, Brazil) |
|  |  |  |  |  | Adper Scotchbond Multi-Purpose (3M Espe, USA) |  |  |  |
| Papacchini, 2007 | 70 (10) | Gradia Direct Anterior (GC Corp., Tokyo, Japan) | Stored 0.9% saline solution at 37°C for 1 month | Sandblasted Al2O3 (Microetcher II; Danville Engineering, USA) + Etched phosphoric-acid 35% Scotchbond (3M Espe, USA ) | Adhesive Scotchbond Multi- Purpose Adhesive (3M Espe, USA) | Gradia Direct Anterior (GC Corp., Tokyo, Japan) | Divided 2 subgroups: Storad 24 h of storad in 0.9% saline solution at 37°C or Thermocycled for 5,000 cycles (5–55ºC in a 0.9% saline solution | Microtensile bond strength (mTBS) Universal testing machine (cross-head speed: 0.5 mm min)1; Controls, Milano, Italy). |
|  |  |  |  |  | Flowable resin composites, Filtek Supreme XT Flow (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Flowable resin composites Gradia LoFlo (GC Corp.), |  |  |  |
|  |  |  |  |  | Prehydrolized Silane Monobond-S (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Mixed non-prehydrolized Clearfil Porcelain Bond Activator (Kuraray Medical, CA, USA) AND Adhesive system Clearfil New Bond Activator (Kuraray Medical, CA, USA) |  |  |  |
|  |  |  |  |  | Mixed non-prehydrolized Clearfil Porcelain Bond Activator (Kuraray Medical, CA, USA) AND Adhesive Clearfil SE Bond Activator (Kuraray Medical, CA, USA) |  |  |  |
|  |  |  |  |  | Mixed non-prehydrolized Clearfil Porcelain Bond Activator (Kuraray Medical, CA, USA) AND adhesive Clearfil Tri-S Bond (Kuraray Medical, CA, USA) |  |  |  |
| Ozcan, 2007 | 36 (6) | Esthet·X® (Dentsply, Weybridge, UK) | Immersion in citric acid, pH 3.0 at 37°C for 1 week or Boiling in water for 8h 2OR Thermocycled 5000 cycles 5-55°C time for 30s | Polished silicone carbide papers with 1200-grit (3M, St. Paul, USA) + Sandblasted silica coating air abrasion (Dento-PrepTM, Denmark) with CoJet®-Sand (30-m SiOx particles) (3M Espe, Germany) | Silane coupling agent, (ESPE-Sil, 3M Espe, USA) | Esthet·X® (Dentsply, Weybridge, UK) | Stored in water at 37°C for 24h | Microtensile bond strength (mTBS) Universal testing machine (EMIC Ltda, Model DL-1000, São José dos Pinhais, PR, Brazil) |
|  |  |  |  | Polished silicone carbide papers with 1200-grit (3M, St. Paul, USA)+ Etched phosphoric-acid 35% (3M Espe, USA) | Single Bond (3M Espe, USA) |  |  |  |
| Perriard, 2009 | 270 (30) | Tetric EvoCeram (Ivoclar Vivadent AG, Liechtenstein) | Stored in distilled water at 37°C for 30 days | Roughened carbide bur (E136-1558, Dentsply-Maillefer; Ballaigues, Switzerland) | no | Tetric EvoCeram (Ivoclar Vivadent AG, Liechtenstein) | Stored in distilled water at 37°C for 1h OR 7 days | Tensile bond strength (TBS) Universal testing machine (1114, Instron; Norwood, MA, USA) |
|  |  |  |  | Grit blasted using 50 μm alumina particles |  |  |  |  |
|  |  |  |  | Etched phosphoric-acid 37% (3M Espe, USA) |  |  |  |  |
|  |  |  |  | Sandblasted 50 μm alumina particles + Etched phosphoric-acid 37% (3M Espe, USA) | Layer of unfilled resin |  |  |  |
|  |  |  |  | Sandblasted tribochemical particles (Cojet System, 3M ESPE) | Silane Monobond-S (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
| Ozcan, 2013 | 64 (16) | Tetric EvoCeram (Ivoclar Vivadent AG, Liechtenstein) Filtek Supreme (3M Espe, USA) | Thermocycled 5000 cycles 5–55 °C | Polished 1,200-grit silicone carbide papers + Sandblasted air abrasion with 30-μm SiO2 particles (CoJet Sand) | Silane coupling agent (ESPE-Sil) (3M Espe, USA) + Adhesive VisioBond (3M Espe, USA) | Tetric EvoCeram (Ivoclar Vivadent AG, Liechtenstein) Filtek Supreme (3M Espe, USA) | no | Microtensile bond strength (mTBS) Universal Testing Machine (EMIC Ltda, Model DL 1000, São José dos Pinhais, PR, Brazil) |
|  |  |  |  |  | Adhesive Multilink (A+B) (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
|  |  |  |  |  | Adhesive Adper ScotchBond 1XT (3M Espe, USA) |  |  |  |
| Altinci, 2018 | 300 (24) | Venus Pearl (Heraeus Kulzer GmbH, Germany) Z100 (3M Espe, USA) Filtek Supreme XTE (3M Espe, USA) | Stored water at 37ºC 48h, Boiled in water 8h, Water-stored at 37ºC, 3 weeks | no | no | Venus Pearl (Heraeus Kulzer GmbH, Germany) Z100 (3M Espe, USA) Filtek Supreme XTE (3M Espe, USA) | Storad at 37°C for 24h. or Thermocycled 6000 cycles 5-55°C | Microtensile bond strength (mTBS) Bisco Microtensile Tester; Bisco, Schaumburg, IL) |
|  |  |  |  | Surface roughened with 320-grit | no |  |  |  |
|  |  |  |  |  | Adhesive iBOND |  |  |  |
|  |  |  |  |  | Silane (Signum, Ceramic Bond I) Adhesive iBOND |  |  |  |
|  |  |  |  | Surface roughened with 320-grit + Sandblasted (CoJet Sand, 3M espe USA) |  |  |  |  |
| El-Askary, 2012 | 80 (10) | Grandio Caps (Voco; Cuxhaven, Germany) | Stored in tap water at room temperature 1 month | Ground 320-grit SiC paper +34.5% phosphoric-acid leaving the surface apparently Wet (Voco; Cuxhaven, Germany) | Monobond S Silane coupling agent (Ivoclar Vivadent AG, Liechtenstein) + Solobond Plus primer + Solobond adhesive (wet bonding) (Voco; Cuxhaven, Germany) | Grandio Caps (Voco; Cuxhaven, Germany) | Stored in water at room temperature for 24h or 1 month | Tensile bond strength (TBS) Universal testing machine (Lloyd Instruments, LR5 series; Hampshire, UK) |
|  |  |  |  |  | Solobond Plus primer + Solobond adhesive (wet bonding) (Voco; Cuxhaven, Germany) |  |  |  |
|  |  |  |  | Polished ground 320-grit SiC paper + Etched phosphoric-acid 34.5% leaving the surface apparently Dry (Voco;Cuxhaven, Germany) | Monobond S Silane coupling agent (Ivoclar Vivadent AG, Liechtenstein) + Solobond Plus primer + Solobond adhesive (Dry bonding) (Voco; Cuxhaven, Germany) |  |  |  |
|  |  |  |  |  | Solobond Plus primer + Solobond adhesive (Dry bonding) (Voco; Cuxhaven, Germany) |  |  |  |
| Dias, 2011 | 120 (15) | TPH Spectrum (Dentsply, Weybridge, UK) | Stored in distilled and deionized water for 7 days or 6 months | Roughened diamond bur #4138 medium grit (KG Sorensen; Cotia, SP, Brazil) | no | TPH Spectrum (Dentsply, Weybridge, UK) | no | Flexural Failure Strength Universal testing machine (EMIC Ltda, Model DL 500, São José dos Pinhais, PR, Brazil) |
|  |  |  |  | Roughened diamond bur #4138 medium grit (KG Sorensen; Cotia, SP, Brazil) + Etched phosphoric-acid 37% (Denstsply International) | no |  |  |  |
|  |  |  |  |  | Two layers of Prime & Bond 2.1 adhesive (Dentsply Caulk, Milford, USA) |  |  |  |
|  |  |  |  |  | Silane Primer mixed Silane Activator (Dentsply International) + Two layers of Prime & Bond 2.1 adhesive (Dentsply Caulk, Milford, USA) |  |  |  |
| Soderholm, 1991 | 60 (3) | P-30 Batch (3M, St Paul, MI) | Stored dry for either 24 h or 60 days al 37°C. | no | no | P-30 Batch (3M, St Paul, MI) | Stored at 37°C for either 3 or 12 months. | Flexural Failure Strength Instron Flexure Fixtures A 336-9b and A 336-6b (Instron Corporation, Canton, MA, USA) |
|  |  |  |  | Etched phosphoric-acid Scotchbond Etched Gel (3M, St Paul, MI) | Scotchprime + Scotchbond (3M, St Paul, MI) |  |  |  |
|  |  |  |  |  | Scotchbond (3M, St Paul, MI) |  |  |  |
|  |  |  |  |  | Toluene (Gertified A.C.S. toluene. Fischer Scientific Company, PA, USA) + Scotchprime + Scotchbond (3M, St Paul, MI) |  |  |  |
|  |  |  |  |  | no |  |  |  |
| Tantbirojn, 2015 | 94 (14) (12) (11) (10) | Filtek Supreme Ultra (3M Espe, USA) | Stored dry at room temperature for 7 days | Polished wet grinding with 600-grit silicon carbide paper + Etched Scotchbond Universal (3M Espe, USA) | Adper Single Bond Plus adhesive (3M Espe, USA) | Filtek Supreme Ultra (3M Espe, USA) | Stored dry at room temperature for 24 hours | Flexural Failure Strength Universal testing machine (Instron Electromechanical Testing System, series 5567, Instron, Norwood, MA, USA) |
|  |  |  |  |  | Scotchbond Universal Adhesive (3M Espe, USA) |  |  |  |
|  |  |  |  | Polished wet grinding with 600-grit silicon carbide paper + Sandblasted tribochemical treatment CoJet (3M Espe, Germany) | Adper SingleBond Plus (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Sil Silane Coupling Agent (3M Espe, Germany) Visio Bond (3M Espe, Germany) |  |  |  |
|  |  |  |  |  | Scotchbond Universal Adhesive(3M Espe, USA) |  |  |  |
| Staxrud, 2011 | 59 (10) | Filtek Silorane/ Filtek Supreme XT/ Filtek Z 250 (3M Espe, USA) CeramX Mono Charisma (Heraeus Kulzer GmbH, Hanau, Germany) Tetric Evo Ceram (Ivoclar Vivadent AG, Liechtenstein) | Stored in distilled water at 37°C for 60 days | no | Adper Scotchbond (3M Espe, USA) | Filtek Silorane /Filtek Supreme XT/ Filtek Z 250 (3M Espe, USA) CeramX Mono Charisma (Heraeus Kulzer GmbH, Hanau, Germany) Tetric Evo Ceram (Ivoclar Vivadent AG, Liechtenstein) | Stored in water for 24 horas ORThermocycled 5000 cycles 5–55°C | Shear bond strengths (SBS) Universal testing machine (Instron 1121, Instron, High Wycombe, Bucks, UK) |
|  |  |  |  |  | Silorane bonding (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Adper Scotchbond 1XT (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Xeno III (Dentsply, Weybridge, UK) |  |  |  |
|  |  |  |  |  | AdheSE (Ivoclar Vivadent AG, Liechtenstein) |  |  |  |
| Dursun, 2021 | 21 (6) | Harmonize Nanohybrid Universal Composite (Kerr Corporation, Orange, USA) | Thermocycled 10,000 or 30,000 or 50,000 cycles 5 - 55°C | Laser with an Erbium, Chromium: Yttrium-Scandium-Gallium-Garnet (Er, Cr: YSGG) + 37.5% phosphoric-acid (Kerr Corporation, Orange, USA) | Etch&rinse adhesive agent (Optibond FL, Kerr Corporation, Orange, USA) | Harmonize Nanohybrid Universal Composite (Kerr Corporation, Orange, USA) | no | Microtensile test device μTBS (Bisco, USA) |
|  |  |  |  | Intraoral air abrasion unit (PrepStart, Danville Materials, San Ramon, Calif., USA) using 50‑μm Al2O3 + 37.5% phosphoric-acid (Kerr Corporation, Orange, USA) |  |  |  |  |
|  |  |  |  | Silicone Carbide - grounded with 600‑grit SiC papers + 37.5% phosphoric-acid (Kerr Corporation, Orange, USA) |  |  |  |  |
| Kuşdemir, 2021 | 720 (15) | Clearfil Majesty Esthetic (Kuraray Noritake Dental, Tokyo, Japan) | Stored in water for 6 months or Thermocycled 5000 cycles, 5–55 ºC | Air-abrasion Al2O3 (AirSonic Mini Sandblaster, Hager Worldwide, Inc., Hickory, USA) | All Bond Universal (Bisco, Schaumburg, IL, USA) | Clearfil Majesty Esthetic (Kuraray Noritake Dental, Tokyo, Japan) | no | Shear bond strengths (SBS) Universal Testing Machine (Shimadzu Autograph AGS-X, Japan) |
|  |  |  |  | no |  |  |  |  |
|  |  |  |  | Air-abrasion Al2O3 (AirSonic Mini Sandblaster, Hager Worldwide, Inc., Hickory, USA) | Clearfil Universal Bond Quick (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
|  |  |  |  | no |  |  |  |  |
|  |  |  |  | Air-abrasion Al2O3 (AirSonic Mini Sandblaster, Hager Worldwide, Inc., Hickory, USA) | Clearfil Universal Bond (Kuraray Noritake Dental, Tokyo, Japan) |  |  |  |
|  |  |  |  | no |  |  |  |  |
|  |  |  |  | Air-abrasion Al2O3 (AirSonic Mini Sandblaster, Hager Worldwide, Inc., Hickory, USA) | G-Premio Bond GP (Corp., Tokyo, Japan) |  |  |  |
|  |  |  |  | no |  |  |  |  |
|  |  |  |  | Air-abrasion Al2O3 (AirSonic Mini Sandblaster, Hager Worldwide, Inc., Hickory, USA) | Gluma Bond Universal (Heraeus Kulzer GmbH, Hanau, Germany) |  |  |  |
|  |  |  |  | no |  |  |  |  |
|  |  |  |  | Air-abrasion Al2O3 (AirSonic Mini Sandblaster, Hager Worldwide, Inc., Hickory, USA) | Monobond Plus (Ivoclar Vivadent, Schaan, Liechtenstein) |  |  |  |
|  |  |  |  | no |  |  |  |  |
| Michelotti, 2020 | 78(6) | Filtek Supreme XTE (3M, St. Paul, MN, USA) | Thermocycled for 5000 cycles, 5°- 55 °C | Roughened 40 μm diamond bur (4325 L, Intensiv, Grancia, Switzerland) | Adhesive Scotchbond (3M Espe, USA) | Filtek Supreme XTE (3M, St. Paul, MN, USA) | Thermocycled for 5000 cycles, 5°- 55 °C | Microtensile Bond Strength Test universal testing machine (Z010, Zwick, Ulm, Germany) |
|  |  |  |  |  | Silane coupling agent (Monobond Plus, Ivoclar Vivadent, Schaan, Liechtenstein) + Adhesive Scotchbond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent (Monobond Plus, Ivoclar Vivadent, Schaan, Liechtenstein) + Optibond FL Adhesive,(Kerr, Orange, CA, USA) |  |  |  |
|  |  |  |  | Sandblasted with 50 μm Al2O3 particles (Airflow Handy, EMS, Nyon, Switzerland) | Adhesive Scotchbond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent (Monobond Plus, Ivoclar Vivadent, Schaan, Liechtenstein) + Adhesive Scotchbond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent (Monobond Plus, Ivoclar Vivadent, Schaan, Liechtenstein) + Optibond FL Adhesive,(Kerr, Orange, CA, USA) |  |  |  |
|  |  |  |  | Sandblasted with silica-coated Al2O3 (CoJet, 3M ESPE, Seefeld, Germany) | Adhesive Scotchbond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent (Monobond Plus, Ivoclar Vivadent, Schaan, Liechtenstein) + Adhesive Scotchbond (3M Espe, USA) |  |  |  |
|  |  |  |  |  | Silane coupling agent (Monobond Plus, Ivoclar Vivadent, Schaan, Liechtenstein) + Optibond FL Adhesive,(Kerr, Orange, CA, USA) |  |  |  |
| Ritter, 2020 | 60 (10) | Filtek Supreme Ultra (3M, St. Paul, MN, USA) Clearfil Majesty ES-2 (Kuraray Noritake, New York, NY, USA) | Thermocycled for 50.000 cycles, 5°- 55 °C | Roughened diamond bur #471271 (Midwest Dental, USA) | Adhesive, Clearfil Universal Bond Quick (Kuraray Noritake, New York, NY, USA) | Filtek Supreme Ultra (3M, St. Paul, MN, USA) Clearfil Majesty ES-2 (Kuraray Noritake, New York, NY, USA) | storad in 100% humidity and at 37°C for 24 hours | Interfacial fracture toughness test (iFT) using a four-point bending fixture Universal testing machine (Instron 4411, Instron, Norwood, MA, USA) |
|  |  |  |  | Roughened diamond bur #471271 (Midwest Dental, USA) + Sandblaster (MB11 MicronBlaster) 30-lm Al2O3 particles |  |  |  |  |
|  |  |  |  | Roughened diamond bur #471271 (Midwest Dental, USA) + CoJet sand: 30-lm silicatized Al2O3 and Sílica (3M, St. Paul, MN, USA) | Espe-Sil: silane CoJet (3M, St. Paul, MN, USA) + Adhesive Visio-Bond CoJet (3M, St. Paul, MN, USA) |  |  |  |
| Saleh, 2020 | 8 (2) | Opallis (FGM products, Joinville, SC, Brazil.) | Stored in artificial saliva for 6 months | Roughened Fine grit diamond bur (Microdont, Brazil) + Phosphoric-acid 35% (Coltène/Whaledent AG, Altstätten, Swizerland) | Adhesive One coat bond SL (Coltène/Whaledent AG, Altstätten, Swizerland.) + Brilliant Flow flowable compsite (Coltène/Whaledent AG, Altstätten, Swizerland.) | Brilliant Ever Glow (Coltène /Whaledent AG, Altstätten, Swizerland.) | no | Microtensile bond strength (μTBS) Universal testing machine (Controls, Milano, Italy) |
|  |  |  |  | Roughened Super Fine grit diamond bur (Microdont, Brazil) + Phosphoric-acid 35% (Coltène/Whaledent AG, Altstätten, Swizerland) |  |  |  |  |
|  |  |  |  | Irradiated by Erbium-Yag Laser (Fotona LightWalker AT) + Phosphoric-acid 35% (Coltène/Whaledent AG, Altstätten, Swizerland) |  |  |  |  |
| Valizadeh, 2020 | 120 (30) | Filtek Z250 (3M ESPE, St. Paul, MN, USA) | Thermocycled for 5000 cycles, 5 - 55 ºC | Roughened diamond bur (835/008; Tees Kavan, Tehran, Iran) + 37% phosphoric-acid (Etch Royal, Pulpdent, Watertown, NY, USA) | Scotchbond Universal (3M ESPE, St. Paul, MN, USA) | Filtek Z250 repair composite (3M ESPE, St. Paul, MN, USA) | Stored in distilled water and incubated at 37º C for 24 h OR Thermocycled for 5000 cycles, 5 - 55 ºC | Microshear bond strength (μSBSs) Universal testing machine (Zwick Roell, Ulm, Germany) |
|  |  |  |  | Irradiation Er,Cr:YSGG laser (Waterlase, Biolase, Technology, San Clement, CA, USA) + 37% phosphoric-acid (Etch Royal, Pulpdent, Watertown, NY, USA) |  |  |  |  |
|  |  |  |  | Sandblasted 50 mm Al2O3 particles by AeroEtcher (D670; PARKELL Farmingdale, NY, USA) ) + 37% phosphoric-acid (Etch Royal, Pulpdent, Watertown, NY, USA) |  |  |  |  |
|  |  |  |  | Atmospheric plasma jet (Model: Medaion-S; Nik Fanavaran Plasma, Tehran. Iran) ) + 37% phosphoric-acid (Etch Royal, Pulpdent, Watertown, NY, USA) |  |  |  |  |
| Aquino, 2020 | 80(8) | Filtek Bulk Fill, (3M Oral Care; St Paul, MN, USA) | Thermocycled (5±1°C, 37±1°C and 55±1°C) | 37% phosphoric-acid (Condac 37, FGM; Joinvile, SC, Brazil) | Adper Single Bond 2 adhesive (3M Oral Care; St Paul, MN, USA) | Filtek Bulk Fill, (3M Oral Care; St Paul, MN, USA) | Stored in distilled water at 37°C for 24 h | Microtensile Bond Strength Test (μTBS) Universal Testing Machine (EZ Test L, Shimadzu; São Paulo, SP, Brazil) |
|  |  |  |  | Roughened diamond bur #4138 (KG Sorensen; Cotia, SP, Brazil) + 37% phosphoric-acid (Condac 37, FGM; Joinvile, SC, Brazil) |  |  |  |  |
|  |  |  |  | Sandblasted with 50-μm Al2O3 particles (Bio-Art, São Carlos, SP, Brazil) + 37% phosphoric-acid (Condac 37, FGM; Joinvile, SC, Brazil) |  |  |  |  |
|  |  |  |  | Roughened diamond bur #4138 (KG Sorensen; Cotia, SP, Brazil) + 37% phosphoric-acid (Condac 37, FGM; Joinvile, SC, Brazil) | Silane (Prosil, FGM products, Joinville, SC, Brazil.) + Adper Single Bond 2 adhesive (3M Oral Care; St Paul, MN, USA) |  |  |  |
|  |  |  |  | Sandblasted with 50-μm Al2O3 particles (Bio-Art, São Carlos, SP, Brazil) + 37% phosphoric-acid (Condac 37, FGM; Joinvile, SC, Brazil) |  |  |  |  |
| Dieckmann, 2020 | 60 (6) | Filtek Supreme XTE (3M Oral Care; St Paul, MN, USA) | Thermocycled 5000 cycles, 5–55°C and stored in water for 6 months | Roughened diamond bur 46-μm (fine) cylindrical 8837 314 014 (Komet Dental Gebr Brasseler; Lemgo, Germany) | Silane coupling agent Monobond Plus (Ivoclar Vivadent; Schaan, Liechtenstein) + OptiBond FL, primer and adhesive (Kerr; Orange, CA, USA) | Filtek Supreme XTE (3M Oral Care; St Paul, MN, USA) | Thermocycled 5000 cycles, 5–55°C | Microtensile Bond Strength Test (μTBS) Universal testing machine (ZwickRoell Z010, ZwickRoell; Ulm, Germany) |
|  |  |  |  | Diamond bur 100-μm (coarse) 837 314014 (Komet Dental Gebr Brasseler) |  |  |  |  |
|  |  |  |  | Diamond bur 46-μm (fine) cylindrical 8837 314 014 (Komet Dental Gebr Brasseler; Lemgo, Germany) + Sandblasted 50-μm Al2O3 particles (FG 3-82 sandmaster, Sandmaster; Zofingen, Switzerland) |  |  |  |  |
|  |  |  |  | Diamond bur 100-μm (coarse) 837 314014 (Komet Dental Gebr Brasseler) + Sandblasted 50-μm Al2O3 particles (FG 3-82 sandmaster, Sandmaster; Zofingen, Switzerland) |  |  |  |  |
| Yarmohammadi, 2020 | 60 (12) | Filtek Z250 (3M ESPE, ST Paul, MN, USA) | Thermocycled 1000 cycles between 5°C and 55°C | no | G-Premio Universal Adhesive (GC; japan, Tokyo) | Filtek Z250 (3M ESPE, ST Paul, MN, USA) | Stored in distilled water 37°C for 24 h | Shear bond strength (SBS) Universal testing machine (Dartec, HC.10, England) |
|  |  |  |  | Abrasion 50-micron Al2O3 (Dento-prep TM/ Denmark/dental micro Blaster) |  |  |  |  |
|  |  |  |  | Roughened diamond milling (Switzerland) with 125-micrometer particles |  |  |  |  |
|  |  |  |  | hydrofluoric acid 9% for 60s (Ultradent, South Jordan, UT, USA) |  |  |  |  |
|  |  |  |  | hydrofluoric acid 9% for 120s (Ultradent, South Jordan, UT, USA) | Silane (product Inc, Utah, USA) + G-Premio Universal Adhesive (GC; japan, Tokyo) |  |  |  |