Supporting Information

Fig. S1. Synthetic steps of the WS2/CuAl LDH nanocomposite.

Table S1. The TFC, CuAl LDH TFN and WS2/CuAl LDH TFN membranes prepared at different fillers concentrations.

| Membranes | MPD in water phase (wt%) | TMC in n-hexane phase (wt%) | CuAl LDH in water phase (wt%) | WS2/CuAl LDH in water phase (wt%) |  |
| --- | --- | --- | --- | --- | --- |
| TFC | 2 | 0.15 | 0.000 |  | 0.000 |
| TFN-L1 | 2 | 0.15 | 0.010 |  | 0.000 |
| TFN-L2 | 2 | 0.15 | 0.025 |  | 0.000 |
| TFN-L3 | 2 | 0.15 | 0.050 |  | 0.000 |
| TFN-WL1 | 2 | 0.15 | 0.000 |  | 0.010 |
| TFN-WL2 | 2 | 0.15 | 0.000 |  | 0.025 |
| TFN-WL3 | 2 | 0.15 | 0.000 |  | 0.050 |

Fig S2. Schematic diagram of the laboratory-scale FO set-up, 1) digital weight balance, 2) feed solution, 3) conductometer, 4) pump, 5) controlling valve, 6) flow meter, 7) heat controller, 8) membrane cell and 9) draw solution.

Fig. S3. Top surface EDX elemental mapping of the TFC and TFN-WL membranes.

Table S2. Calculated amplitude parameters for synthesized membranes by AFM.

| Membrane | Amplitude parameters |  |  |
| --- | --- | --- | --- |
|  | Ra (nm) | Rq (nm) | R10z (nm) |
| TFC | 72.01 | 92.05 | 867.0 |
| TFN-WL1 | 55.81 | 69.33 | 552.8 |
| TFN-WL2 | 48.3 | 60.95 | 480.9 |
| TFN-WL3 | 43.56 | 55.83 | 423.0 |

Fig. S4. The schematic diagram of membrane function mechanisms (a) overlapping of nanosheets and creating nanochannels, (b) formation of water layer and absorbing water molecules, (c) formation of hourglass-shaped nanopores.

Fig. S5. (a) Water flux and (b) reverse salt flux of the TFC and TFN-WL2 membranes against different DS concentrations (0.5 M–1.5 M) under FO and PRO mode.

Table S3. Comparison of the FO performances of the TFN-WL2 membrane with previously reported ones in the literature.

| Membranes with filler wt.% | Feed and draw solution | Jw (LMH) | Js (gMH) | Js/Jw (g/L) | Membrane orientation | References |
| --- | --- | --- | --- | --- | --- | --- |
| TFN-WL2 | NaCl 1 M and DI water | 47.7 29.3 | 20.35 11.42 | 0.42 0.38 | PRO FO | Present work |
| TFC |  | 25.55 14.45 | 15.14 7.63 | 0.59 0.52 | PRO FO |  |
| TFN-2 | NaCl 1 M and DI water | 23.6 13.4 | 6.9 6.2 | 0.29 0.46 | PRO FO | [1] |
| TFC |  | 15.3 8.6 | 7.2 6.8 | 0.47 0.79 | PRO FO |  |
| TFN-U2 | NaCl 1 M and DI water | 36.7 20.7 | 7.1 4.3 | 0.20 0.21 | PRO FO | [2] |
| TFC |  | 26.2 16.5 | 4.21 2.6 | 0.16 0.16 | PRO FO |  |
| TFN-QMo-2 | NaCl 1 M and DI water | 55.0 40.1 | 17.0 14.4 | 0.31 0.36 | PRO FO | [3] |
| TFC |  | 24.7 15.3 | 11.1 7 | 0.45 0.46 | PRO FO |  |
| TFN-0.1 | NaCl 1 M and DI water | 38.7 17.5 | 15 7.5 | 0.39 0.43 | PRO FO | [4] |
| TFC |  | 25.7 11.5 | 9.7 5.1 | 0.37 0.44 | PRO FO |  |
| LDH@TFC-LDH | NaCl 1 M and DI water | 21.4 12.5 | 9.9 4.3 | 0.46 0.34 | PRO FO | [5] |
| TFC |  | 21.5 12.6 | 9.2 5.6 | 0.43 0.45 | PRO FO |  |
| TFN-0.25 | NaCl 1 M and DI water | 85.3 59.3 | 36.8 19.1 | 0.42 0.32 | PRO FO | [6] |
| TFC |  | 50.7 29.3 | 27.2 14.0 | 0.53 0.47 | PRO FO |  |

References

1. P. Lu, S. Liang, T. Zhou, X. Mei, Y. Zhang, C. Zhang, A. Umar, and Q. Wang, RSC Adv. 6, 56599 (2016).

2. D. Ma, S. B. Peh, G. Han, and S. B. Chen, ACS Appl. Mater. Interfaces 9, 7523 (2017).

3. M. Amini, H. Naslhajian, A. Akbari, S. M. F. Farnia, E. Jabbari, S. Gautam, and K. H. Chae, Polyhedron 168, 138 (2019).

4. N. Ma, J. Wei, R. Liao, and C. Y. Tang, J. Memb. Sci. 405, 149 (2012).

5. P. Lu, W. Li, S. Yang, Y. Liu, Q. Wang, and Y. Li, Sep. Purif. Technol. 220, 231 (2019).

6. M. Bagherzadeh, A. Bayrami, and M. Amini, J. Water Process Eng. 33, 101107 (2020).