Supplementary Information

A Local Water Molecular-heating Strategy for NIR Long-lifetime Imaging-guided Photothermal Therapy of Deep-tissue-bearing Tumor

Dongkyu Kang1*, Hyung Shik Kim2*, Soohyun Han3, Yeonju Lee4, Young-Pil Kim,3,4,5,6, Dong Yun Lee2,5,7,8**, Joonseok Lee1,6**

1Department of chemistry, Hanyang University, Seoul 04763, Republic of Korea

2Department of Bioengineering, College of Engineering, and BK FOUR Biopharmaceutical Innovation Leader for Education and Research Group, Hanyang University, Seoul 04763, Republic of Korea

3Department of HY-KIST Bio-Convergence, Hanyang University, Seoul 04763, Republic of Korea

4Department of Life Science, Hanyang University, Seoul 04763, Republic of Korea

5Institute of Nano Science and Technology (INST), Hanyang University, Seoul 04763, Republic of Korea

6Research Institute for Convergence of Basic Sciences, Hanyang University, Seoul 04763, Republic of Korea

7Institute for Bioengineering and Biopharmaceutical Research (IBBR), Hanyang University, Seoul 04763, Republic of Korea

8Elixir Pharmatech Inc., Seoul 07463, Republic of Korea

*Equally contributed in this study

**Corresponding author

E-mail address: joonseoklee@hanyang.ac.kr, dongyunlee@hanyang.ac.kr

Supplementary Figure S1. Characterizations of water-heating core. a) TEM images and size distributions of CR-core and water-heating core, Scale bar : 20 nm. b) XRD patterns of core nanoparticles.

Supplementary Figure S2. a) Zetapotential profiles of dopamine-ligand exchanged water-heating core (+29.1 mV) and CR-core (+27.8 mV). Observed charge for each ligand were demonstrated the homogeneously exchanged ligand of nanoparticle. b) Fourier transform infrared spectroscopic (FT-IR) spectrum of oleic acid-ligand (black) and dopamine-ligand (red). The surface modification was confirmed by the appearance of two new bands at 1608 nm and 3390 nm, attributed to N-H bending and stretching of amine groups.

Fig. S3. Optimizations of core nanoparticle a) TEM images of core nanoparticles. 27.2 ± 4.7, 31.2 ± 2.0, 36.4 ± 1.4, and 43.5 nm ± 4.0 nm, respectively. b) TEM images of core@shell nanoparticle. 28.7 nm ± 5.5, 43.2 ± 2.0, 45.2 ± 2.3, and 48.9 ± 3.1 nm, respectively. Scale bar: 20 nm.

Fig. S4. Optimizations of Yb concentrations of core. a) 1.0 µm emission spectrum of core@shell nanoparticle (NaYF4:x%Yb@NaYF4:20%Yb,50%Nd) with various doping concentration of Yb in core and b) corresponding emission intensities

Supplementary Figure S5. a) TEM images of CR NP. Their size distributions were calculated to be 33.2 ± 1.8 nm and 44.9 ± 2.2 nm, respectively. Scale bar: 20 nm b) XRD patterns of core@shell nanoparticles

Supplementary Figure S6. Zetapotential profiles of water-heating NIR NP dopamine-ligand (+ 36.5 mV and 36.4 mV, water-heating NP and CR NP, respectively), SMCC-ligand (-32.9 mV) and antibody-ligand (-9.8 mV) of conjugated each nanoparticle.

Supplementary Figure S7. a) Temperature profiles of water-heating NP (NaYF4:50%Yb@NaYF4:40%Nd,20%Yb) (5 mg/mL) in aqueous solution with an irradiation of continuous NIR laser (808 nm, 2 W/cm2). b) Linear time data versus -ln(θ) obtained from the cooling period. c) temperature profiles of CR NP (NaYF4@NaYF440%Nd) (5 mg/mL) in aqueous solution with an irradiation of continuous NIR laser (808 nm, 2 W/cm2). d) Linear time data versus -ln(θ) obtained from the cooling period. Detailed calculation is described in method.

Supplementary Figure S8. Characterizations of optical properties of water-heating NIR NP. a) EDS mapping images of water-heating NIR NP. b) TEM images of NaYF4:50%Yb,2%Tm and NaYF4:50%Yb,2%Tm@NaYF4:40%Nd,20%Yb (water-heating NIR NP), Scale bar: 20 nm. c) NIR emission spectrum for 800 nm emission under 980 nm laser excitation. 800 nm emission shape is slightly absorbed by the outer shell doped the Nd3+ ion d) NIR absorption spectrum of Nd3+ ion e) 1.0 μm emission spectrum of water-heating NIR NP and water-heating NP in cyclohexane under 808 nm laser excitation.

Supplementary Figure S9. Biodistribution of bare-NP and Ab-NP that administered by tail vein. a) In vivo luminescence image of dissected organs of GBM-bearing mice sacrificed at 1, 5, and 60 min after tail vein injection of bare-NP and Ab-NP (20 mg/kg dose of total drug, respectively). b) Mean intensity of luminescence detected in organs 1, 5, and 60 min after tail vein injection of bare-NP and Ab-NP, respectively.

Supplementary Figure S10. Histopathological analysis of heart, lung, liver, kidney, spleen, and intestine after repeated doses. The tissues were histologically analyzed after intravenous administration of 3-repeated doses at a concentration of 5 mg/kg to GBM-modeled mice. Scale bar: 100 μm.

Supplementary Figure S11. Relative body weight of each groups, that monitored for 25 days. Data were expressed as mean ± S.E.M (n=4).

Fig. S12. Investigation of spleen enlargement occurred due to unwanted immune stimulation after repeated drug administration. a) Images of spleen of PBS-vehicle- (Control), bare-NP-, and Ab-NP- treated group after repeated treatments. b) Spleen weight (mg) / body weight (g) of each group. Data are expressed as mean ± S.E.M (n=3).